96M03/29/06

S306-96M.doc

Include Subsection 725.02 and the following with projects requiring dust palliatives:

Section 306. - DUST PALLIATIVE

Delete the text of this section and substitute the following:

Description

306.01  This work consists of furnishing and applying one or more applications of a dust palliative on a prepared surface.

Material

306.02  Conform to the following Subsections:

Blotter	703.13

Calcium chloride	725.02

Calcium chloride flake	725.02

Emulsified asphalt	702.03

Lignosulfonate	725.20

Magnesium chloride	725.02

Water	725.01

Construction Requirements

306.03  General.  Use distributor equipment conforming to Subsection 409.04, except heating capability is not required.  Equip the distributor with a hose and nozzle for areas inaccessible to the distributor and for touch-up work.  Do not apply a dust palliative when the weather is foggy or rainy or when rain is anticipated within 24 hours of application.  Do not apply chloride brines, emulsified asphalt, or lignosulfonate when the ground is frozen.

Protect the surfaces of structures and trees from splatter or marring during application.  Use multiple applications at a reduced rate if necessary to prevent runoff.  Do not discharge dust palliative into streams.

306.04  Preparation and Application.  Prepare the roadbed by blading and shaping to leave 25 to 50 millimeters of relatively loose material on the surface.

(a) Emulsified asphalt.  When a slow setting emulsified asphalt is used, dilute it with water until the emulsion contains 20 to 30 percent residual asphalt.  The CO will approve the exact proportion.  Thoroughly blend the emulsified asphalt with the added water.  When the ambient air temperature is 4°C or above, apply according to Subsection 409.08.

(b) Lignosulfonate, calcium chloride, or magnesium chloride.  Water the loose material so it is visibly moist.

When lignosulfonate is used, dilute it with water until the mixture contains a minimum 48 percent concentration.  When calcium chloride brine is used, provide a minimum 36 percent concentration.  When magnesium chloride brine is used, provide a minimum 28 percent concentration.  When calcium chloride flake is used, provide flakes with a minimum 77 percent purity.

The CO will approve the exact proportion.  Thoroughly mix the components.  Apply when the ambient air temperature is 4°C or above.  Apply liquid concentrations at a rate of 1.4 to 2.7 liters per square meter as approved.  Apply the chloride flakes at the rate of 0.5 to 1.1 kilograms per square meter as approved.

Distribute the dust palliative uniformly throughout the layer, moisten as necessary, and compact the surface.

306.05  Maintenance and Opening to Traffic.  Do not permit traffic treated surface until the dust palliative has penetrated and cured enough to prevent excessive pickup under traffic.  If it becomes necessary to permit traffic before that time, apply blotter as necessary.

306.06  Acceptance.  Dust palliative material (emulsified asphalt, lignosulfonate, calcium chloride, calcium chloride flake, and magnesium chloride) will be evaluated under Subsection 106.03.

When lignosulfonate is furnished, provide a commercial certification that includes the following information for each shipment:  date, identification number (truck, trailer, etc.), net mass, net volume at 15°C, specific gravity at 15°C, percent solids by weight, pH, base cation, and brand name.

Application of dust palliative will be evaluated under Subsections 106.02 and 106.04.

Measurement

306.07  Measure dust palliative application by the kilometer or  by the square meter.

Measure dust palliative material (emulsified asphalt, lignosulfonate, calcium chloride, calcium chloride flake, and magnesium chloride) by the metric ton.  Mass measurements apply to the diluted quantity.

Payment

306.08  The accepted quantities, measured as provided above, will be paid at the contract price per unit of measurement for the pay items listed below that are shown in the bid schedule.  Payment will be full compensation for the work prescribed in this section.  See Subsection 109.05.

Payment will be made under:

Pay Item	Pay Unit

30601	Dust palliative application	Kilometer

30602	Dust palliative application	Square meter

30603	Emulsified asphalt 	Metric ton

30604	Lignosulfonate	Metric ton

30605	Calcium chloride	Metric ton

30606	Magnesium chloride	Metric ton

30707	Calcium chloride flake	Metric ton