$$308.00A

Section 308.—MINOR CRUSHED AGGREGATE

Revised 6 May 2005

INCLUDE THE FOLLOWING WHEN CRUSHED RECYCLED CONCRETE IS PERMITTED IN TEMPORARY PAVEMENTS

$$308.02A

308.02.  Add the following:

Crushed recycled concrete				703.20

$$308.02B

Crushed recycled concrete may be used for aggregate courses in temporary pavements.

$$308.04A

308.04(a).  Add the following:

Remove and replace any layer of crushed recycled concrete material that exhibits heaving, pumping, rutting, or shearing under construction equipment even if the layer meets the density requirements in Subsection 308.05(a).

$$308.06A

308.06.  Add the following:

Crushed recycled concrete will be evaluated under Subsections 106.02 and 106.04.

INCLUDE THE FOLLOWING FOR A SMALL QUANTITY OF AGGREGATE FOR MINOR ROADS, PARKING LOTS AND FOR TEMPORARY PAVEMENTS (Quantity to be determined during the design and review process)

$$308.06B

  - Delete Table 308-1 and substitute the following:

Table 308-1

Sampling and Testing Requirements

| Material or Product | Type of Acceptance (Subsection) | Property or Characteristic | Test Methods Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Crushed aggregate for roadway | Measured and tested for conformance (106.04) | Moisture-Density | AASHTO T 180 method D(2) | 1 for each aggregate supplied | Production output or stockpile | --- | Before using in work |
|  |  | Gradation(1) | AASHTO T 11 and T 27 | 1 for each 1000 tons | From windrow or roadbed after processing | --- | Before placing next layer |
|  |  | In-place density and moisture content | AASHTO T 310 or other approved procedures | 1 for each 500 tons | In-place | --- | Before placing next layer |
| Crushed aggregate for bedding and backfill | Measured and tested for conformance (106.04) | Moisture-Density | AASHTO T 99 method C(2) | 1 for each aggregate supplied | Production output or stockpile | --- | Before using in work |
|  |  | In-place density and moisture content | AASHTO T 310 or other approved procedures | 2 per lift | In-place | --- | Before placing next layer |

(1)Use only sieves indicated for the specified gradation.

(2)Minimum of 5 points per proctor.

$$308.06C

  - Delete the third and fourth paragraphs and substitute the following:

Construction of roadway aggregate courses, and bedding and backfill aggregate will be evaluated under Subsections 106.02 and 106.04.  Method 2 compaction will be evaluated under Section 106.04. Sample crushed aggregate for roadway according to Table 308-1.  Submit crushed aggregate for roadway samples to the CO for verification. Materials that do not meet the approved certification will be considered unacceptable.

INCLUDE THE FOLLOWING WHEN CRUSHED RECYCLED CONCRETE IS PERMITTED IN TEMPORARY PAVEMENTS

$$308.07A

308.07.  Add the following:

Measure crushed recycled concrete by the cubic yard (meter) in the hauling vehicle.