03M03/29/06

S308-03M.doc

Use on projects with less than 5000 tons (certification acceptance).

Section 308. - Minor Crushed Aggregate

308.06  Acceptance  Delete the second paragraph and substitute the following:

Construction of roadway aggregate courses will be evaluated under Subsections 106.02 and 106.04.  Method 2 compaction will be evaluated under Section 106.04.  Sample material from the windrow or roadbed after processing but prior to compaction at the frequency shown in Table 308-1.  Submit samples to the CO for verification.  Materials that do not meet the approved certification will be considered unacceptable.

Delete Table 308-1 and substitute the following:

Table 308-1

Sampling and Testing Requirements

| Material or Product | Type of Acceptance (Subsection) | Property or Characteristic | Test Methods or Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Crushed aggregate (1) | Measured and tested for conformance (106.04) | Moisture-Density | AASHTO T180 Method D (3) | 1 for each aggregate supplied. | Production output or stockpile. | --- | Before using in work |
|  |  | Gradation (2) | AASHTO T11 and T27 | 1 for each 1000 t. | From the windrow or roadbed after processing. | --- | Before placing next layer |
|  |  | In-place density and moisture content | AASHTO T310 or other approved procedures | 1 for each 1000 t. | In-place completed compaction layer. | --- | Before placing next layer |

(1) Sampling and testing required for roadway aggregate.

(2) Use only sieves indicated for the specified gradation.

(3) Minimum of 5 points per proctor.