03M06/13/07

S552-03M.doc

Use on projects when structural concrete is required. Generally structural concrete is required for bridges, culverts, walls, and foundations (items that require load analysis or “that you can drive on”). A low water crossing may be paid under Section 552 or 501 as determined by the Design Team (including roadway designer, bridge engineer, and pavements engineer).

Section 552. - STRUCTURAL CONCRETE

# Material

# 552.02  Add the following:

Concrete coloring agent	711.05

Precast reinforced concrete box sections	706.07

Precast concrete units	725.11

Reinforcing fibers	725.29

# Construction Requirements

# 552.03  Composition (Concrete Mix Design).  Delete Tables 552-1, 2, and 3 and substitute the following:

# Table 552-1

Composition of Concrete

| Class of Concrete | Minimum Cement Content (kg/m3) | Maximum W/C Ratio | Slump (1) (mm) | Maximum Nominal Coarse Aggregate Size (5) (mm) |
| --- | --- | --- | --- | --- |
| A | 360 | 0.49 | 50 to 100 | 37.5 |
| A(AE) | 360 | 0.44 | 25 to 100 | 37.5 |
| B | 310 | 0.58 | 50 to 100 | 63 |
| B(AE) | 310 | 0.58 | 50 to 100 | 63 |
| C | 390 | 0.49 | 50 to 100 | 19 |
| C(AE) | 390 | 0.44 | 25 to 75 | 19 |
| D(AE)(2) | 360 | 0.40 | 25 to 75 | 37.5 |
| E(AE)(3) | 360 | 0.40 | 100 to 150 (4) | 19 |
| P (Prestressed) | 390 | 0.44 | 0 to 100 | 25 |
| P(AE) | 390 | 0.44 | 0 to 100 | 25 |
| Seal | 390 | 0.54 | 100 to 200 | 37.5 |

(1) Maximum slump is 200 millimeters if approved mix design includes a high-range water reducer.

(2) Concrete with a water reducing and retarding admixture conforming to AASHTO M 194, type D.

(3) A latex modified concrete with 0.31 liters of modifier per kilogram of cement.

(4) Measure the slump 4 to 5 minutes after the concrete is discharged from the mixer.

(5) Meeting the processing requirements of AASHTO M43, Table 1 – Standard Sizes of Processed Aggregate.

# Table 552-2

Minimum Air Content for Air Entrained Concrete

| Nominal Maximum Aggregate Size (1) | As Delivered Minimum Air Content (2) (3) (%) |
| --- | --- |
| 63 mm | 3.5 |
| 50mm | 3.5 |
| 37.5 mm | 4.0 |
| 25 mm | 4.5 |
| 19 mm | 4.5 |
| 12.5 mm | 5.5 |

(1) Meeting the processing requirements of AASHTO M 43, Table 1 – Standard Sizes of Processed Aggregate.

(2) These air contents apply to the total mix.  When testing these concretes, aggregates larger than 37.5 millimeters is removed by handpicking or sieving, and air content is determined on the minus 37.5-millimeter fraction of the mix.  Air content of the total mix is computed from the value determined on the minus 37.5-millimeter fraction.

(3) For P(AE) concrete, the as delivered minimum air contents may be reduced 1.0 % and the maximum air content is 6.0 %

# Table 552-3

Required Average Compressive Strength (1)

| Specified Compressive Strength (f’c) (MPa) | Required Average Compressive Strength (f’cr) (MPa) |
| --- | --- |
| Less than 21 | f’c + 7.0 |
| 21 to 35 | f’c + 8.5 |
| Over 35 | 1.10f’c + 5.0 |

(1) Use this table when there is not enough data available to establish a standard deviation

552.09  Quality Control of Mix.  Add the following after the first paragraph:

At least 2 weeks prior to the start of concrete placement operations, arrange a pre-concrete placing conference.  Coordinate attendance with the CO and any applicable subcontractors.  Be prepared to discuss and/or submit the following:

(1) Proposed concrete placement schedule.

(2) Review approved concrete mix design and determination of batch weights.

(3) Discuss Section 153, Contractor Quality Control, minimum frequency schedule for process control sampling and testing (to be performed by the Contractor).

(4) Discuss batching, mixing, placing, and curing requirements.

(5) Discuss Subsections 106.03, Certification, and 106.05, Statistical Evaluation of Material for Acceptance.

552.12  Construction Joints.  Delete the third paragraph and substitute the following:

When the joint is between two fresh concrete placements, rough float the first placement to thoroughly consolidate the surface and leave the surface in a roughened condition.  Clean the joint surface of laitance, curing compound, and other foreign material.  Use an abrasive blast or another approved method to expose the aggregate on the joint surface.  Re-tighten forms where the joint overlaps the first placement.  Immediately before placing new concrete, flush the joint surface with water and allow to dry to a surface dry condition.

Include Subsection 552.16 when integral concrete coloring is specified. Insert the description of the concrete to be colored and the color number in the spaces provided below.

552.16  Finishing Formed Concrete Surfaces.  Add the following after the first paragraph:

Use an approved form release agent to produce a minimum of staining, air holes, and hydration discoloration.

# Add the following:

(h) Class 8 - Integral color finish.  All concrete in the                                       will be integrally colored by adding a concrete coloring agent.  After curing the colored concrete will match as closely as possible to Standard Color Chart Number                of Federal Specification 595B.

Prepare five square textured test panels with each panel 300 mm square.  Use coarse and fine aggregates and cement as delivered on the project at the job mix rates with variable quantities of coloring agent as directed by the CO.  Complete a Class 1 finish according to (a) above.  The CO will select a test panel to serve as a guide for the colored concrete. Use the same rate of coloring agent used in the selected panel on all relative subsequent work.

Prepare and transport the test panels to the project staging area.  Cure the test panels similar to the structure.  Allow test panels a minimum of four weeks to cure prior to placing concrete requiring coloring agent.

# Measurement

Include the following when concrete for footing is to be poured against disturbed rock.

552.20

# Add the following:

Do not measure for payment the volume of concrete required outside the neat lines of the footing to pour against undisturbed rock as shown on the plans.  When the CO directs the removal of material below the established elevation of the bottom of the footing, the volume of concrete required to fill the void will be measured for payment.

Include the following when integral concrete coloring is used in the concrete.

Add the following:

Measure concrete coloring agent by the pound.

Always include the following.

Delete footnote (3) in Table 552-9 and substitute the following:

(3)  A single compressive strength test result is the average result form 2 cylinders cast from the same load and tested at 28 days.