03E05/01/08

S401-03E.doc

Use on all projects with more than 4000 tons (statistical acceptance) of Superpave hot asphalt concrete pavement.

Section 401. - SUPERPAVE HOT ASPHALT CONCRETE PAVEMENT

Description

401.01  Delete the third paragraph and substitute the following:

A minimum of one percent lime is required in the Superpave hot asphalt concrete mixture.

Enter the pavement roughness type and asphalt binder grade here. Materials or Pavements will provide to the designer the following: 1) Roughness type: Type III for new construction (4R work) or Type IV for reconstruction (3R work). If project is a combination of types then identify different roughness type by station. 2) Asphalt binder grade: Binder grade is project specific. 3) If this is a desert project, the Pressure Aging Vessel testing temperature should be 230°F, else delete the highlighted second sentence.

Pavement roughness is type III or IV

Asphalt binder grade is PG xx-xx.  The Pressure Aging Vessel test temperature shall be 230°F.

Material

401.02  Delete the first line and substitute the following:

Aggregate								703.07

Construction Requirements

401.03  Composition of Mix (Job-Mix Formula).  Delete the second paragraph and substitute the following:

Compact specimens with the gyratory effort corresponding to the design ESAL level of 0.3 to <3 million.  Volumetric mix properties will be determined at Ndesign.  Use a gyratory compactor which meets the internal angle requirement according to AASHTO T 312.

Table 401-1 Superpave Hot Asphalt Concrete Pavement Design Requirements Table.  Delete Table 401-1 and substitute the following:

Table 401-1

Superpave Hot Asphalt Concrete Pavement Design Requirements,  AASHTO R 35

| Design ESAL (Million) | Gyratory Compaction Level (% Theoretical Maximum Specific Gravity, Gmm) AASHTO T 312 | Minimum Voids-in-the Mineral Aggregate (VMA), % (1) | Voids Filled with Asphalt (VFA), % (3) | Minimum Hveem Stabilometer value | Dust-to-Binder Ratio (4) | Minimum Tensile Strength Ratio, AASHTO T 283 (5) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Nominal Maximum Size Aggregate (2) |  |  |  |  |
|  | Ninitial | Ndesign | Nmax | 1 inch | ¾ inch | ½ inch | ⅜ inch |  |  |  |  |
| < 0.3 | 6 (≤91.5%) | 50 (96.0%) | 75 (≤98.0%) | 12.0 | 13.0 | 14.0 | 15.0 | 70.0 - 80.0 | 30 | 0.8 -1.6 | 0.80 |
| 0.3 to 3 | 7 (≤90.5%) | 75 (96.0%) | 115 (≤98.0%) |  |  |  |  | 65.0 - 78.0 |  |  |  |
| 3 to 30 | 8 (≤89.0%) | 100 (96.0%) | 160 (≤98.0%) |  |  |  |  | 65.0 - 78.0 |  |  |  |

(1) When mineral filler or hydrated lime is used, include in the calculation for compliance with the VMA.

(2) The nominal maximum size aggregate is one size greater than the first sieve to retain more than 10 percent of the combined aggregate.

(3) For 1-inch nominal maximum size aggregate mixtures with <0.3 million ESALs, provide a VFA ≥67.0 percent.

(4) Dust to binder ratio is defined as the percent of material including lime, baghouse fines, and other mineral matter added to the mixture.  Calculate the ratio using the effective asphalt content calculated by mass of mix.

(5) Specimens shall be 4 inches in diameter.  Note that AASHTO T 283 requires a freeze-thaw cycle.

(c) Verification.  Delete the Subsection and substitute the following:

(1) Aggregate Gradations.  Representative aggregate samples from each stockpile, when combined according to the Contractor’s recommendation for stockpile percentages, shall be within the gradation defined by the Contractor’s target values plus or minus the following tolerance for each sieve.

Sieve Size				Tolerance, % (±)

1 inch					3.0

¾ inch					3.0

½ inch					3.0

⅜ inch					3.0

No. 4						3.0

No. 8						3.0

No. 30					2.0

No. 50					2.0

No. 200					1.0

(2) Bulk specific gravity of aggregate (Gsb).  The Contractor’s coarse and fine Gsb is verified if the CO’s results are within the acceptable range for the AASHTO Multilaboratory precision D2S shown in AASHTO T 84 and T 85.  Once verified, the mean of the Contractor’s and CO’s combined coarse and fine Gsb values will be used to calculate volumetrics on field produced mix samples.

(3) Voids in the mineral aggregate (VMA).  The Contractor’s VMA result is verified if the CO’s result is above the minimum specification limit in Table 401-1.

(4) Voids filled with asphalt (VFA).  The Contractor’s VFA result is verified if the CO’s result is within the specification limit in Table 401-1.

(5) Air Voids (Va).  The Contractor’s Va result is verified if the CO’s result at the same design asphalt binder content is between 3.0 and 5.0 percent.

(6) Hveem stabilometer value.  The Contractor’s Hveem stabilometer value is verified if the CO’s result is above the minimum specification of 30.

(7) Tensile strength ratio (TSR).  The Contractor’s TSR result is verified if the CO’s result is above the minimum specification of 0.80.

401.04  Mixing Plant.  Delete the text and substitute the following:

(2) Dust collector.  AASHTO M 156, Requirements for All Plants, Emission Controls is amended as follows:

Equip the plant with a dust collector.  Dispose of the collected material.  In the case of baghouse dust collectors, dispose of the collected material or return the collected material uniformly.

Use of baghouse fines in asphalt concrete mixes requires approval unless included as part of the approved job-mix formula.  If baghouse fines are approved for use, batch or continuous mix plants will meter it by volume or mass into the mixing chamber.

401.08  Asphalt Preparation.  Delete the Subsection and substitute the following:

Uniformly heat the asphalt binder to provide a continuous supply of the heated asphalt binder from storage to the mixer.  Do not heat asphalt binder above 365 ºF.

401.09  Aggregate Preparation.  Delete the Subsection and substitute the following:

Adjust the aggregate moisture to at least 4 percent by mass of aggregate.  Mix the lime uniformly with the aggregate before introducing the aggregate into the dryer or dryer drum.  Use calibrated weighing or metering devices to measure the amount of lime and moisture added to the aggregate.

For batch plants, heat, dry, and deliver aggregate for pugmill mixing at a temperature sufficient to produce a mix temperature within the approved range.  Adjust flames used for drying and heating to prevent damage to and contamination of the aggregate.

Control plant operations so the moisture content of the mix behind the paver is 0.5 percent or less according to AASHTO T 255.

Add lime to the aggregate by Method A, B, or C below.

Method A - Add lime to the combined cold feed aggregate using an enclosed in-line cold feed mechanical pugmill mixer.  Use a twin-shaft, continuous mixing pugmill with adjustable mixing paddles.  Adjust the retention time of the mixture in the pugmill so no unmixed lime is visible after the lime and aggregate exit the pugmill.

Method B - Add lime to the produced aggregates during stockpiling using a pugmill.  Add twenty-five (25) percent of the lime to be added to the coarse aggregate stockpile, and add seventy-five (75) percent of the lime to be added to the fine aggregate stockpile.  When more than two stockpiles are used, include the distribution of lime per stockpile in the mix design.

A minimum moisture content of two (2) percent by dry weight for coarse aggregate and four (4) percent by dry weight for fine aggregate is required at the time the aggregates and lime are mixed.

Method C - Use a lime slurry consisting of one part lime and three parts water.  Equipped the plant with a mixing unit to allow mixing of the slurry and aggregate prior to entering the dryer or dryer drum.

Adjust the moisture of the coarse and fine aggregates, or combination of aggregates, to obtain uniform coating of the aggregate with the lime.

Prior to the production of Superpave hot asphalt concrete pavement, obtain approval of synchronized metering and weighing devices used to introduce a constant rate of lime and water.

For all 4R projects add the following to Subsection 401.13 (also include detail C634-50):

401.13  Placing and Finishing.  Add the following to the fifth paragraph:

For simple curve widening locations (widening only on one side) shift the centerline joint location such that the final layer is midway between the normal edge of shoulders.  The shift from the staked centerline will be towards the widened lane one-half the total curve widening specified for the given station as shown in the plans.

OR For all 3R projects add the following to Subsection 401.13:

401.13  Placing and Finishing.  Delete the fifth paragraph and substitute the following:

Make the longitudinal joint in the top layer along the existing striped centerline, as recorded under Subsection 152.03(n), or at the lane lines of roadways with more than two lanes.

Add the following to Subsection 401.13 when the hot mix haul is anticipated to be long. Also be sure to include the pay item 62202-1000 for “Material Transfer Vehicle”.

401.13  Placing and Finishing.  Add the following:

Use a Materials Transfer Vehicle (MTV) with storage and remixing capabilities on all mainline construction when placing asphalt concrete mixtures.  The MTV will independently remix and deliver mixture from the hauling equipment to the paving equipment.

Furnish an MTV with the following capabilities:

•  An unloading system to receive mixtures from the hauling equipment.

•  A minimum storage capacity of 13 tons with a remixing system in the MTV storage bin.

•  A discharge conveyor to deliver the mixture to the paver hopper.

•  The MTV system cannot exceed maximum legal loadings on structures.

Acceptable Material Transfer Vehicles are:

•  Barber Greene MTV-3500

•  Roadtec SB-1500

•  Roadtec SB-2500

In the event the MTV malfunctions during paving operations, the Contractor must suspend paving, however hot mix in transit and stored in the silo at the time of breakdown may be placed without the use of an MTV.  Do not resume hot mix placement until the MTV is operational.

401.14  Compacting.  Delete the first sentence of the first paragraph and substitute the following:

Furnish at least 3 rollers.  Furnish one roller each for breakdown, intermediate, and finish rolling.  At least one roller will be pneumatic-tired.  Size the rollers to achieve the required results.  Operate rollers according to the recommendation of the manufacturer.  Diesel fuel will not be used as a release agent with any roller used to compact the asphalt mix.

401.16  Pavement Smoothness/Roughness.  Delete the Subsection and substitute the following:

401.16  Pavement Roughness.  Measure the roughness of the final paved surface course within 21 days after final rolling of the completed roadway paving, and before placement of any surface treatment.  In addition to meeting the pavement roughness type requirements, construct all pavement surfaces to meet the requirements of Type V pavement roughness.

(a) International roughness index (IRI).

Equipment.  Provide an ASTM E 950, class 1, high speed inertial profiling system meeting all the requirements and specifications found in AASHTO MP 11, with emphasis on the filter and sampling intervals specified in sections 4.2.3 and 4.2.4.  Certify profiler in accordance with AASHTO PP 49.  Operate profiler in accordance with AASHTO PP 50.  At the pre-construction meeting and before profiling provide copies of profiling system to be used and certification(s).  Display a current decal on the equipment indicating the expiration date of certification(s).

Personnel.  Certify operator in accordance with AASHTO PP 49. At the pre-construction meeting and before profiling provide copies of operator certification(s).

Measuring.  Measure the pavement profile in both wheel paths, two longitudinal traces with a sensor path spacing of 65-71 inches, centered in the traveled way of the lane.  For each lane, submit on disk one continuous raw IRI data file (*.ERD) for the “left” and “right” wheel paths to the CO immediately after profiling.  Use profiler’s automatic start/stop activation when collecting data.  The CO must coordinate and observe profiling operations.  Non-continuous data files will not be accepted.  Submit inertial profiler setup parameters (e.g. filters, sampling interval, and segment length, etc.).  Measure excluded areas according to Type V pavement roughness.

Evaluation.  The CO will review, analyze and may perform verification testing on all IRI measurements.  The CO will analyze profile data using Profile Viewer and Analysis (ProVAL) software.  The CO’s analysis will be used to determine the Mean Roughness Index (MRI), and the associated roughness pay factor.

Defective areas include the following:

- Bumps or Localized Roughness Areas (LRA) in excess of 0.2 inches in 25 feet, using ProVAL’s Localized Roughness Analysis.

- 0.1-lane mile MRI greater than a Ride Quality Threshold of 105 inches/mile, using ProVAL’s Smoothness Assurance Analysis.

Correct defective areas according to paragraph (c) below.

If the final MRI for the entire traveled way is greater than 125 inches/mile using ProVAL’s Ride Statistics Analysis, the traveled way is in reject.  Correct rejected traveled way according to paragraph (c) below.

An MRI value will be determined for each 0.1-lane mile of traveled way.  The total traveled way will be analyzed including partial segments less than 0.1-lane mile.  Exclusion areas are 25 feet on either side of Beginning and End of Project, cattle guards, and bridges.  These areas will be excluded from the calculation of MRI and determination of localized roughness.

(1) Type III pavement roughness (IRI measurements for reconstructed and new roads).  Measure the roughness of the final paved surface course.  Pay factors from Table 401-3 will be used in conjunction with the histogram printout from ProVAL’s Smoothness Assurance Analysis.  The final pay factor (PFrough) is equal to the sum of the products of the individual pay factors indicated in Table 401-3 multiplied by ProVAL’s corresponding histogram percentages, divided by 100.  Calculate the final pay factor to two decimal places.

Table 401-3

Type III Pavement Roughness

| MRI (in/mi) | Pay Factor (PFrough) |
| --- | --- |
| Greater than 95 | 0.70 |
| 95.0 to 90.0 | 0.80 |
| 90.0 to 80.0 | 0.90 |
| 80.0 to 70.0 | 0.96 |
| 70.0 to 60.0 | 1.00 |
| 60.0 to 50.0 | 1.02 |
| 50.0 to 40.0 | 1.03 |
| 40.0 to 30.0 | 1.04 |
| Less than 30.0 | 1.05 |

(2) Type IV pavement roughness (IRI measurements for overlay, recycle with overlay, or milling with overlay projects).  Measure the roughness of the existing surface before construction traffic.  The existing surface is defined as the original surface before overlaying, recycling, or milling.  Submit original surface raw data files (*.ERD).  The CO will review, analyze and may perform verification testing on all IRI measurements.  No work that will disturb the original surface will proceed until CO’s analysis is complete.  The original surface MRI will be used to determine the percent improvement for the entire traveled way.

The percent improvement in MRI will be determined to one decimal place for the entire traveled way according to the following formula:

% Improvement = [(Original MRI – Final MRI) / Original MRI] x 100

Table 401-4 will be used to determine the final pay factor (PFrough) for the entire traveled way.  No deductions will be made when the final MRI value is less than or equal to 70.0 inches per mile (PFrough = 1.00).  Compute the final pay factor to two decimal places.

Table 401-4

Type IV Pavement Roughness

| Single Lift Percent Improvement (%) | Pay Factor (PFrough) | Multi-Lift Percent Improvement (%) | Pay Factor (PFrough) |
| --- | --- | --- | --- |
| Greater than 50.0 | PF = 1.05 | Greater than 60.0 | PF = 1.05 |
| 47.6 to 50.0 | PF = 1.04 | 58.6 to 60.0 | PF = 1.04 |
| 45.1 to 47.5 | PF = 1.03 | 57.6 to 58.5 | PF = 1.03 |
| 43.6 to 45.0 | PF = 1.02 | 56.6 to 57.5 | PF = 1.02 |
| 42.1 to 43.5 | PF = 1.01 | 55.1 to 56.5 | PF = 1.01 |
| 25.0 to 42.0 | PF = 1.00 | 49.0 to 55.0 | PF = 1.00 |
| 24.0 to 24.9 | PF = 0.99 | 48.0 to 48.9 | PF = 0.99 |
| 23.0 to 23.9 | PF = 0.98 | 47.0 to 47.9 | PF = 0.98 |
| 22.0 to 22.9 | PF = 0.97 | 46.0 to 46.9 | PF = 0.97 |
| 21.0 to 21.9 | PF = 0.96 | 45.0 to 45.9 | PF = 0.96 |
| 20.0 to 20.9 | PF = 0.95 | 44.0 to 44.9 | PF = 0.95 |
| 19.0 to 19.9 | PF = 0.94 | 43.0 to 43.9 | PF = 0.94 |
| 18.0 to 18.9 | PF = 0.93 | 42.0 to 42.9 | PF = 0.93 |
| 17.0 to 17.9 | PF = 0.92 | 41.0 to 41.9 | PF = 0.92 |
| 16.0 to 16.9 | PF = 0.91 | 40.0 to 40.9 | PF = 0.91 |
| 15.0 to 15.9 | PF = 0.90 | 38.0 to 39.9 | PF = 0.90 |
| 14.0 to 14.9 | PF = 0.89 | 36.0 to 37.9 | PF = 0.89 |
| 13.0 to 13.9 | PF = 0.88 | 35.0 to 35.9 | PF = 0.88 |
| 12.0 to 12.9 | PF = 0.87 | 34.0 to 34.9 | PF = 0.87 |
| 11.0 to 11.9 | PF = 0.86 | 33.0 to 33.9 | PF = 0.86 |
| 10.0to 10.9 | PF = 0.85 | 31.0 to 32.9 | PF = 0.85 |
| 5.0 to 9.9 | PF = 0.80 | 25.0 to 30.9 | PF = 0.80 |
| Less than 4.9 | PF = 0.70 | Less than 24.9 | PF = 0.70 |

NOTE: A single lift is defined as asphalt concrete pavement placed in one operation.

(b) Type V pavement roughness (straightedge measurement).  Use a 10 foot metal straight edge to measure at right angles and parallel to the centerline.  Type V localized roughness areas (LRA) are surface deviations in excess of 0.25 inches in 10 feet between any two contacts of the straightedge with the surface.

(c) Defective area correction.  Correct defective areas from paragraphs (a) or (b) above.  Obtain approval from the CO for correction of defected areas as well as the method of correction.  When grinding is allowed, the area ground shall not exceed 720 square feet per location, and is limited to 10 locations per lane mile.  Grinding depth is limited to 12.5% of the design pavement thickness.  Grinding in excess of these limits is not an acceptable method of correction unless it is accompanied by an overlay or a single-course surface treatment over the entire length of the project.

If grinding is allowed, grind the pavement surface with a diamond blade machine and apply a surface treatment according to Sections 409 or 410 as approved by the CO.  The endpoints of the areas where a grinder is to be applied must be optimized using ProVAL.

If corrections are allowed, re-measure the pavement profile.  Data from the re-measurement and re-analysis will be used to determine PFrough in accordance with Table 401-3 or Table 401-4.

If corrections are not allowed, no adjustment will be made to the final pay factor (PFrough) determined from Table 401-3 or Table 401-4.  A dollar adjustment per remaining bump when grinding is not allowed will be determined according to subsection 401.19.

Defective area corrections and surface treatments shall be provided at no cost to the Government.

401.17  Acceptance.  Delete the second paragraph and substitute the following:

Asphalt binder will be evaluated under Subsections 106.04, and 702.09, and Table 401-5.

Payment

401.19  Delete the Subsection and substitute the following:

The accepted quantities will be paid at the contract price per unit of measurement for the Section 401 pay items listed in the bid schedule except the Superpave hot asphalt concrete pavement contract unit bid price will be adjusted according to Subsections 106.05, 401.16, and Table 401-5.  Payment will be full compensation for the work prescribed in this Section.  See Subsection 109.05.

Payment for Superpave hot asphalt concrete pavement will be made at a price determined by multiplying the contract unit bid price by the material pay factor.  The material pay factor is calculated as follows:

A1 = [(PFSuperpave – 1) + (PFPG – 1)]

where:

A1 =		Material pay factor.

PFSuperpave =	Pay factor for Superpave hot asphalt concrete pavement.  PFSuperpave is the lowest single pay factor determined for asphalt binder content, VMA, and core density.

PFPG =		Pay factor for asphalt binder.  The PFPG formula is as follows:

PFPG = (PF1 + PF2 + PF3 + ….PFn) / n

where:

PF# =	For each sample, the lowest pay factor determined from any test in Table 401-5.  If the lowest pay factor for a sample is in reject, the sample’s pay factor is zero.

n =	Number of samples tested.

If either the pay factor for the asphalt binder (PFPG) or the pay factor for Superpave hot asphalt concrete pavement (PFSuperpave) is below 0.75, the lot for Superpave hot asphalt concrete pavement is in reject.

When the bid schedule contains a pay item for Superpave hot asphalt concrete pavement, type III and type IV pavement roughness, a separate pay adjustment will be made for pavement roughness calculated as follows:

Type III and Type IV Pay Adjustment = 40,000 (PFrough - 1.00)(L) – (NLRA x 300)

where:

PFrough  = 	Pay factor from Table 401-3 or Table 401-4.

L = 	Total project length in lane miles of traveled way.  Measure the project length to 3 decimals.

NLRA = 	Number of localized roughness areas (bumps) remaining in final traveled way as determined by ProVAL and Type V measurements.

Table 401-5 Asphalt Binder Pay Factor Table.  Delete Table 401-5 and substitute the following:

Table 401-5

Asphalt Binder Pay Factor Table

| Tests on Original | Specifications (See 702.01) | Pay Factor = |
| --- | --- | --- |
|  |  | 1.01 | 1.00 | 0.95 | 0.90 | 0.75 | Reject |
| Dynamic Shear Rheometer, kPa | ≥ 1.00 | ≥ 1.17 | 1.16 to 1.00 | 0.99 to 0.89 | 0.88 to 0.77 | 0.76 to 0.50 | < 0.50 |
| Tests after Rolling Thin Film Oven (RTFO) |
| Dynamic Shear Rheometer, kPa | ≥ 2.20 | ≥ 2.69 | 2.68 to 2.20 | 2.19 to 1.96 | 1.95 to 1.43 | 1.42 to 1.10 | < 1.10 |
| Tests on Pressure Aging Vessel (PAV) |
| Bending Beam Rheometer, s, MPa | ≤ 300 | ≤ 247 | 248 to 300 | Use Direct Tension | > 600 |
| Bending Beam Rheometer, m | ≥ 0.300 | ≥ 0.320 | 0.319 to 0.300 | 0.299 to 0.294 | 0.293 to 0.278 | 0.277 to 0.261 | < 0.261 |
| Direct Tension (1), % | ≥ 1.00 | --- | ≥ 1.00 | 0.99 to 0.56 | --- | --- | < 0.56 |

(1) Use Direct Tension for payment if the creep stiffness values from the Bending Beam Rheometer are between 301 and 600 Mpa.

Table 401-6 Sampling and Testing Requirements Table.  Delete Table 401-6 and substitute the following:

Table 401-6

Sampling and Testing Requirements

| Material or Product | Type of Acceptance (Subsection) | Characteristic | Category | Test Method Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Aggregate source quality (703.07) | Measured and tested for conformance (106.04 and 105) | LA abrasion | --- | AASHTO T 96 | 1 per type & source of material | Source of materials | Yes | Before producing |
|  |  | Sodium sulfate soundness loss (coarse & fine) | --- | AASHTO T 104 | “ | “ | “ | “ |
|  |  | Fractured faces | --- | ASTM D 5821 | “ | “ | “ | “ |
|  |  | Fine aggregate angularity | --- | AASHTO T 304 | “ | “ | “ | “ |
|  |  | Flat and elongated particles | --- | ASTM D 4791 | “ | “ | “ | “ |
|  |  | Sand equivalent | --- | AASTHO T 176 | “ | “ | “ | “ |
| Superpave hot asphalt concrete (mix design) | Measured and tested for conformance (106.04) | Gradation | --- | AASHTO T 11 AASHTO T 27 | 1 per each submitted mix design | Stockpiles | Yes | 28 days before paving |
|  |  | Bulk specific gravity of aggregate (coarse & fine) | --- | AASHTO T 84 AASHTO T 85 | “ | “ | “ | “ |
|  |  | VMA | --- | AASHTO R 35 | “ | --- | “ | “ |
|  |  | VFA | --- | AASHTO R 35 | “ | --- | “ | “ |
|  |  | Hveem S-value | --- | AASHTO T 246 | “ | --- | “ | “ |
|  |  | Retained strength (TSR) | --- | AASHTO T 283 | “ | --- | “ | “ |
| Asphalt binder (mix design) |  | (quality) | --- | AASHTO M 320 | “ | Mixing plant (702.09(c)) | “ | “ |

Table 401-6 (continued)

Sampling and Testing Requirements

| Material or Product | Type of Acceptance (Subsection) | Characteristic | Category | Test Method Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Superpave hot asphalt concrete (control strip) | Statistical (106.05) | Gradation: | AASHTO T 30 | 3 minimum | Behind the paver before compaction | Yes | 4 hours |
|  |  | No. 4 | I |  |  |  |  |  |
|  |  | No. 30 | I |  |  |  |  |  |
|  |  | No. 50 | I |  |  |  |  |  |
|  |  | No. 200 | I |  |  |  |  |  |
|  |  | Other specified sieves | II |  |  |  |  |  |
|  |  | Asphalt content (1) | I | AASHTO T 308 | “ | “ | “ | “ |
|  |  | VMA | I | AASHTO R 35 | “ | “ | “ | “ |
|  |  | VFA | I | AASHTO R 35 | “ | “ | “ | “ |
|  |  | Core density (2) | I | AASHTO T 166 | 5 minimum | In-place after compacting | To CO after determining specific gravity & compaction | 24 hours |
|  | Measured and tested for conformance (106.04) | Maximum specific gravity | --- | AASHTO T 209 | 3 minimum | Behind the paver before compaction | Yes | 24 hours |
|  |  | Mix temperature | --- | --- | First load & as determined by the CO | Hauling vehicle before dumping or windrow before pickup | --- | “ |

Table 401-6 (continued)

Sampling and Testing Requirements

| Material or Product | Type of Acceptance (Subsection) | Characteristic | Category | Test Method Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Superpave hot asphalt concrete (production) | Statistical (106.05) | Asphalt content (1) | I | AASHTO T 308 | 1 per 700 tons | Behind the paver before compaction | Yes | 4 hours |
|  |  | VMA | I | AASHTO R 35 | “ | “ | “ | “ |
|  |  | Core density (2) | I | AASHTO T 166 | “ | In-place after compacting | To CO after determining specific gravity & compaction | 24 hours |
|  | Measured and tested for conformance (106.04) | Gradation | --- | AASHTO T 308 AASHTO T 30 | “ | Behind the paver before compaction | Yes | 4 hours |
|  |  | VFA | --- | AASHTO R 35 | “ | “ | “ | “ |
|  |  | Maximum specific gravity (3) | --- | AASHTO T 209 | Minimum 1 per day | “ | “ | “ |
| Asphalt binder (production) | Measured and tested for conformance (106.04 & Table 401-5) | Quality | Table 401-5 | AASHTO M 320 | 1 per 2100 ton of mix, but not less than 5 samples | In line between tank & mixing plant (702.09(c)) | Two 1-quart samples | --- |

Table 401-6 (continued)

Sampling and Testing Requirements

| Material or Product | Type of Acceptance (Subsection) | Characteristic | Category | Test Method Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Superpave hot asphalt concrete pavement (final surface) | Measured and tested for conformance (106.04) | Type III Pavement Roughness | --- | AASHTO PP 49 & PP 50 | See Subsection 401.16 | Left and Right Wheel Paths | --- | 21 days after final paving |
|  |  | Type IV Pavement Roughness, before construction | --- | AASHTO PP 49 & PP 50 | See Subsection 401.16 | Left and Right Wheel Paths | --- | Original surface before overlaying, recycling, or milling. |
|  |  | Type IV Pavement Roughness, after construction | --- |  |  |  | --- | 21 days after final paving |

(1) Use AASHTO T 308, Method A.  Calculate the asphalt binder content by weighing the sample before and after the burn using a calibrated external balance.  Modify AASHTO T 308, parts 8.2 and 10.2 to allow the use of AASHTO T 255, Total Evaporable Moisture Content of Aggregate by Drying.

(2) Cut core samples from the compacted pavement and carefully remove using a core retriever.  Fill and compact the sample holes with asphalt concrete mixture.  Cores shall be 6 inches in diameter.  Perform specific gravity, and thickness tests on the cores and deliver to the CO after testing is completed.  Label cores and protect from damage due to handling or alteration due to temperature during storage or transfer.  If more than 2.0 percent of water volume is absorbed as determined by AASHTO T 166, use AASHTO T 331 in lieu of AASHTO T 275.

(3) After production paving has begun, use the Maximum specific gravity value (AASHTO T 209) for each day to adjust the percent compaction for the cores that represent that day’s paving.