96E06/13/07

S402-96E.doc

Use on projects with less that 1000 tons or for paved ditches.

Section 402. - MINOR HOT ASPHALT CONCRETE

Construction Requirements

402.09  Acceptance.  Add the following:

During construction, submit samples of the loose mix to the CO.

Use on projects with 1000 to 5000 tons of asphalt hot mix.

Section 402. - MINOR HOT ASPHALT CONCRETE

Construction Requirements

402.02 Composition of Mix (Job-Mix Formula).  Delete the text and substitute the following:

Furnish hot asphalt concrete mix composed of crushed stone or gravel and asphalt binder mixed in an approved plant.  Use an aggregate quality, gradation and an asphalt binder grade conforming to those used locally in the construction of highways by the State Department of Transportation.  A job-mix formula developed solely for this project will not be allowed.

Submit a currently approved State Department of Transportation job-mix formula for approval at least 28 days before production.  Include the location of all commercial mixing plants to be used and a separate job-mix formula for each plant.

For each proposed job-mix formula, submit a production certification meeting state agency specifications and conforms to design parameters (a), (b), or (c) from Table 402-1 for the type of mix submitted.  The job-mix formula must meet design parameter (d) in Table 402-1.  Submit a sample of loose mix to the CO 21 days prior to placement.  Include a signed statement prepared by the testing laboratory that certifies the proposed job-mix formula meets the requirements of the contract and can be compacted in the field during production to meet the contract requirements.  For each job-mix formula include copies of laboratory test results with the following information:

•  Stockpile blend ratios

•  Individual stockpile and combined aggregate gradations

•  Target value for percent passing each sieve size for the aggregate blend

•  Aggregate properties

•  Target asphalt binder content

•  Maximum density value according to AASHTO T 209

•  Test values for (a), (b), or (c) and (d) from the Table 402-1

•  Submit loose mix sample three weeks prior to paving

•  History demonstrating the job-mix formula has been used in the area

Table 402-1

Minor Hot Asphalt Concrete Mix Requirements

| Design Parameters | Specification |
| --- | --- |
| (a) Superpave (AASHTO M 323, R 35, and T 312) (1) Gyratory compaction effort (2) Volumetric properties 0.3 to 3 million ESALS’s traffic level (AASHTO M 323) | 7, 75, 115 Table 6 |
| (b) Hveem (AASHTO T 246 and AASHTO T 247) (1) Stabilometer, minimum (2) Percent Air Voids (1) | 35 3 – 5 |
| (c) Marshall (AASHTO T 245) (1) Stability, pounds minimum (2) Flow, 0.01 inch (3) Percent Air Voids (1) (4) Compaction, number of blows per side | 2800 8 - 16 3 - 5 75 |
| (d) Moisture Susceptibility (AASHTO T 165 and T 167 or AASHTO T 283) (1) Retained strength, % minimum | 70 |

(1) The percent of air voids are based on AASHTO T 166, AASHTO T 209 and AASHTO  T 269.

Up to 25 percent recycled asphalt pavement material by mass may be used in the mix.

402.07 Compacting.  Add the following:

Do not use diesel fuel or other petroleum derivatives as a release agent with any roller or other compaction device used to compact the asphalt mix

(a) Roadway paving.  Delete the text and substitute the following:

Compact the mix to a minimum of 92 percent of maximum specific gravity (density).  Determine density by nuclear gauge.

402.09 Acceptance.  Delete the text and substitute the following:

Minor hot asphalt concrete mixture will be evaluated under Subsections 106.02, 106.03 and 106.04.

Minor hot asphalt concrete construction work will be evaluated under Subsections 106.02 and 106.04.  See Table 402-2 for minimum sampling and testing requirements.

During placement the contractor will sample the loose mix according to Table 402-2. A split sample will be submitted to the CO for verification.  Materials that do not meet the approved job mix formula will be considered unacceptable.

Delete Table 402-2 and substitute the following:

Table 402-2

Sampling, Testing and Acceptance Requirements

| Material or Property | Type of Acceptance (Subsection) | Characteristic | Test Methods or Specifications | Sampling Frequency | Point of Sampling | Split Sample | Reporting Time |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Minor Hot Asphalt Concrete Pavement (design) | Measured and Tested for Conformance (106.03 & 106.04) | Job-mix formula verification | Subsection 402.02 (1) | 1 per job-mix formula | Flowing mix stream (bin or belt discharge) or behind the laydown machine before rolling. | --- | 21 days before approval of job-mix formula |
| Minor Hot Asphalt Concrete Pavement (production) | Measured and Tested for Conformance (106.04) | Job-mix formula verification | Subsection 402.02 (1) | 1 per 700 ton | Behind the laydown machine before rolling | Yes | 24 hours |
|  |  | Compaction (2) | AASHTO T 166 and AASHTO T 209 | 1 per 700 ton | In-place after compaction. | “ | “ |
|  |  | Smoothness | Subsection 402.08 | --- | --- | --- | --- |

(1) Use only sieves indicated on the job-mix formula for the specified gradation.

(2) Cut core samples from the compacted pavement and carefully remove using a core retriever.  Fill and compact the sample holes with asphalt concrete mixture.