USE FOR PAVEMENTS THAT DO NOT REQUIRE STATISTICAL EVALUATION (LESS THAN 4000 TONS) SUCH AS DRIVEWAYS, PULL-OFFS, AND PARKING AREAS BUT AREN’T MINOR ASPHALT (SECTION 404).

USE WHERE THE CONSTRUCTION CONTRACT WILL BE ADMINISTERED BY THE FOREST SERVICE (FS DOES NOT USE STATISTICAL ACCEPTANCE THEREFORE DO NOT USE SECTION 401 OR 402 EXCEPT FOR WHERE NOTED IN SECTION 401 INSTRUCTIONS).

IF SECTION 403 IS USED, ALSO INCLUDE SECTION 401 WITH SUBSECTION $$401.15A.

$$403.00A

Section 403. — HOT ASPHALT CONCRETE PAVEMENT

Revised 1 October 2008

INCLUDE THE FOLLOWING

$$403.01A

403.01.  Add the following:

Asphalt binder is designated as performance grade PG (ASK MATERIALS ENGINEER FOR SPECIFIC GRADE).

INCLUDE THE FOLLOWING FOR 401 SUPERPAVE HACP (DO NOT INCLUDE $$403.03B)

$$403.03A

403.03.  Delete the second and third bullet paragraphs and substitute the following:

(	State Department of Transportation Superpave hot asphalt concrete pavement mixture with the same nominal maximum size aggregate, traffic level (design ESAL), and asphalt binder grade as specified.  Meet the requirements for the location and type of facility being constructed as designated by the current State Department of Transportation specification.  Submit the aggregate quality, gradation requirements, and mixture criteria for the asphalt concrete mix.

INCLUDE THE FOLLOWING FOR 402 HACP BY HVEEM OR MARSHALL METHOD (DO NOT INCLUDE $$403.03A)

$$403.03B

403.03.  Delete the first and third bullet paragraphs and substitute the following:

(	State Department of Transportation Hveem or Marshall designed asphalt mixture with the same maximum size aggregate as the specified grading.  Meet the requirements for the location and type of facility being constructed as designated by the current State Department of Transportation specification.  Submit the aggregate quality, gradation requirements, and mixture criteria for the asphalt concrete mix.

INCLUDE THE FOLLOWING

$$403.03F

403.03(a).  Add the following:

Do not use mixes with over 15 percent recycled asphalt pavement in the top lift.

$$403.03D

403.03(b).  Add the following after the first sentence:

Submit all job-mix formula materials and information to the EFLHD Central Laboratory in Sevierville, Tennessee, with a copy to the CO as directed.

$$403.03C

403.03(b).  Add the following:

For State Department of Transportation mixes, submit a job-mix formula that is currently approved and has been tested by the State within a year of the date of intended use.  Include documentation from a State Department of Transportation official certifying that it is an approved State mix.

$$403.03E

403.03(c).  Add the following:

Allow a minimum of 21 calendar days for verification of each job-mix formula after receipt of all materials and information at the EFLHD Central Laboratory.

$$403.13A

403.13.  Add the following:

Begin paving operations at the furthest location from the asphalt plant and proceed towards the plant.