USE FOR PAVEMENTS THAT ARE NOT STATISTICAL (< 4000 TONS), SUCH AS DRIVEWAYS, PULL-OFFS, AND PARKING AREAS BUT AREN’T MINOR AS IN SECTION 404.  ALSO USE WHERE THE CONSTRUCTION WILL BE ADMINISTERED BY THE FOREST SERVICE.  FS DOES NOT DO STATISTICAL ACCEPTANCE DO NOT USE 401 OR 402.

$$403.00A

Section 403.—HOT ASPHALT CONCRETE PAVEMENT

Revised 25 January 2005

INCLUDE THE FOLLOWING

$$403.01A

403.01.  Add the following:

Asphalt binder is designated as performance grade PG (ASK MATERIALS ENGINEER FOR SPECIFIC GRADE).

INCLUDE THE FOLLOWING FOR SUPERPAVE

$$403.03A

403.03.  Delete the second and third bullet item and substitute the following:

(  State Department of Transportation Superpave Hot Asphalt Concrete mixture with the same nominal maximum size aggregate, traffic level (design ESAL), and asphalt binder grade as specified.  Meet the requirements for the location and type of facility being constructed as designated by the current State Department of Transportation specification.  Submit the aggregate quality, gradation requirements, and mixture criteria for the asphalt concrete mix.

INCLUDE THE FOLLOWING FOR HACP BY HVEEM OR MARSHALL

$$403.03B

403.03.  Delete the first and third bullet item and substitute the following:

(  State Department of Transportation Hveem or Marshall designed mixture with the same maximum size aggregate as the specified grading.  Meet the requirements for the location and type of facility being constructed as designated by the current State Department of Transportation specification.  Submit the aggregate quality, gradation requirements, and mixture criteria for the asphalt concrete mix.

###### INCLUDE THE FOLLOWING

$$403.03C

403.03(b).  Add the following:

For State Department of Transportation mixes, submit a job-mix formula that is currently approved and has been tested by the State within a year of the date of intended use.  Include documentation from a State highway official certifying that it is an approved State mix.

$$403.03D

403.03(b).  Add the following:

Submit all materials and information to the EFLHD Central Laboratory in Sevierville, Tennessee.

$$403.03E

403.03(c).  Add the following:

Allow a minimum of 21 calendar days for verification of each job-mix formula after receipt of all materials and information at the EFLHD Central Laboratory.