96M03/29/06

S412-96M.doc

Use on projects when a Tack coat is specified.

Section 412. - ASPHALT TACK COAT

Description

412.01  Delete the text and substitute the following:

This work consists of applying an emulsified asphalt or hot asphalt cement tack coat.

Tack coat emulsified asphalt grade will meet AASHTO T 140 or AASHTO T 208.

Tack coat asphalt cement grade will meet AASHTO M 20, M 226, or M 320

Construction Requirements

412.06  Asphalt Application.  Delete the first sentence of the second paragraph and substitute the following:

Apply the diluted emulsified asphalt according to Subsection 409.08 at a rate of 0.15 to 0.70 liters per square meter.

Measurement

412.08  Delete the text and substitute the following:

The quantity of emulsion indicated in the bid schedule is an undiluted quantity.

Water for diluting tack coat in accordance with Subsection 412.06 will not be measured for payment.

The load invoices supplied to the CO for payment will indicate a breakdown of total emulsion and water added.