03M03/29/06

S416-03M.doc

Use on projects when specifying Continuous Cold Recycled Asphalt Base Course.

Section 416. – CONTINOUOUS COLD RECYCLED

ASPHALT BASE COURSE

Construction Requirements

416.08  Spreading, Finishing, and Compacting.

(a) Initial Compaction.

(1) Type A.  Delete the last sentence of the second paragraph and substitute the following:

Measure the density of the inplace recycled mix according to ASTM D 2950.

(d) Curing.

(2) Recycled mix without quicklime.  Delete the last sentence and substitute the following:

Do not overlay until the moisture content of the recycled base is less than or equal to 1.5 percent according to ASTM D 2950 or until 21 days after recycling.

Table 416-1 Sampling and Testing Requirements.  Delete reference to AASHTO T 310 in the Test Methods Specifications column, and substitute ASTM D 2950.