UNITED STATES DEPARTMENT OF AGRICULTURE

NATURAL RESOURCES CONSERVATION SERVICE

OREGON

MATERIAL SPECIFICATION

MS-206  PLASTIC PIPE

1.	SCOPE

This specification governs the quality of plastic pipe and fittings.

2.	QUALITY

The pipe shall conform to American Society of Testing Material Specification, ASTM or Natural Resources Conservation Service (NRCS) standard applicable for the manufacture of this pipe.

Material			SDR1		SCH 40 & 80		PIP2

NRCS or ASTM	     ASTM		NRCS

Acrylonitrile-Butadiene-		D-2282	     D-1527		430-DD

Styrene, ABS				430-DD				430-EE

430-EE

Polyethylene, PE			D-2239	     D-2104

D-3035	     D-2247

430-DD

430-EE

Polyvinyl Chloride, PVC		D-2241	     D-1785		430-DD

430-DD				430-EE

430-EE

*For pipelines conveying potable water, the material also requires approval of the National        Sanitary  Foundation, NSF.

1  SDR, Standard Dimension Ratio

2 PIP, Plastic Irrigation Pipe

3.	FITTINGS

The fittings shall be of a material, size and pressure rating compatible with the pipe materials and withstand a working pressure equal to or greater than the pipe.

4.	JOINTS

a.	Solvent welding of joints shall be in accordance with the recommendation of the pipe 	manufacturer.

b.	Rubber gasket joints and the gasket material shall conform to ASTM D-3139.

c.	All joints and connections shall withstand a working pressure equal to or greater 	than the 	pipe.