| CABLE No. | . L3T-B0908-R1,R2,R3 |
| --- | --- |
| MFG. | 3/22/05 |
| OPERATOR: | H. Higley & N.Liggins |

CABLE LOG SHEET

LBNL-SUPERCON-AFRD

SUPERCONDUCTING MAGNET CABLES

BLD 52

Objective :  Anneal and resize LHC-IRQ-Inner cable to improve the cable’s winding characteristics.

This cable was originally Mfg. as L3T-B0908 10/26/04 at 1308m in length.  Cable 908 failed insulation\winding test at FNAL and was returned to LBNL 2/28/05 for further evaluation.  Fred Nobrega of FNAL was present during initial annealing, rerolling and test winding.  Cable measurements showed that we had ~ 0.007mm in thickness and ~0.025mm in width available to resize and remain in tolerance. The Roll angles were reground 4 times optimizing for minimum keystone angle.  Re-rolling tests with cable made to the minimum dimensions in width, thickness and angle showed that rolling alone was not sufficient.  Annealed cable typically grew in thickness ~ 0.01mm and width ~ 0.08mm giving better results after rerolling.  Anneal time and temperature were tried from 180c to 200c and time was increased from ~1hr. to 4hrs. with best results at the higher temperatures and longest times.  Due to annealing spool size we are limited to lengths of 395m @ 6.75m/kg. = 59kg.   Rerolled cable had some surface finish problems at the cables minor edge.  A roller cassette device was improvised.  Edge treatment consisted of lightly spring loaded flat rollers at 22 and 45deg. angles at the cables minor edges. .  The roller cassette worked best upstream of the turkshead.  Meny 5m lengths were cut for wind-ability testing.

In the end we settled on an anneal of 200c/4hrs with near minimum cable dimensions as our target. Wind ability test done at the start of 908-R2 went well, at 70lb winding tension, uninsulated and on FNAL tooling.  There were no out of lay strands for 3 of 3 turns. Spool # 908-R1 had to be re annealed before rerolling, so cables were finish rolled in the order 908-R2, R1, R3.  Spool R2 Shipped to FNAL first on 3/21, with spools R1 and R3 shipped 3/23/05.  Spool 908-R1 had some difficulty during reroll but was repaired.

* IMPORTANT NOTE:  During rerolling of cable 908-R1 the cable collapsed at 92m from the hub end.  Fortunately it was at the roller cassette, upstream of the turkshead and was repaired with apparently minor surface scratches.  The repaired location was marked with blue Sharpie and a paper tag was spooled in.  As there may be a greater chance for this one location to have out of lay strands when handled, I suggest giving this location extra attention during insulation and winding.

- STRAND INFORMATION -

| MANUFACTURER : | TWC Teledyne From SSCL inventory at LBNL |
| --- | --- |
| BILLET #: | 3T-00067-A01, -A01, -A02, -A02 2 spools “A01” & 2 spools “A02” |
| SPOOL #: | See original strand map |
| COMPOSITION : | NbTi |
| STRAND Dia.. NOMINAL : | 0.808mm | INSP. DIA..: | 0.8074mm |
| Cu/SC RATIO NOMINAL : | 1.3 | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : | 13 | DIRECTION : | Right |

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | 5520-MA-369677 LHC IR QUAD magnet inner cable drawing |
| --- | --- |
| No. of STRANDS: | 37 |
| PITCH DIRECTION: | Left | PITCH LENGTH: | 118 |
| ROLLER ID #: | P25 & 26 | WIDTH: | 15.210 | ANGLE:: | 1.090 deg. |
| LUBRICATION : | 4BR Saturated roll wipers only. |
| Nom. THICKNESS: | 1.465mm +/- 0.006 ( min = 1.459mm) |
| Nom. WIDTH: | 15.40mm +/- 0.025 ( min = 15.375mm |
| Nom. ANGLE: | 1.079 deg. +/- 0.05 ( min = 1.029 deg.) |

Note Rolls P25 & 26 are at the end of there useful range further angle grinding may not be possible.

- FINISHED CABLE -

|  | L3T-B0908-R1 | L3T-B0908-R2 | L3T-B0908-R3 |
| --- | --- | --- | --- |
| FINISHED LENGTH: | *334m | 351m | 322.8m |
| Avg. THICKNESS: | 1.4615mm | 1.4610mm | 1.4610mm |
| Avg. WIDTH: | 15.3837mm | 15.3838mm | 15.3918mm |
| Avg. ANGLE: | 1.0296deg. | 1.0466deg. | 1.0365deg. |
| ETCH for FILAMENT DAMAGE: | At start of 908-R1 Etched sample had no significant damage visible. |

Average dimensions of the cable are reported from CME measurements taken during rerolling with a cable respool tension of ~ 35lbs.

CME Data:

| 03-21-2005 Cable RunLHC-3-T-B908R1 Unit 0 10:25:37 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| LHC-HGQ-INNER CME #2 |  |  |  |  |  |  |
| Notes. | POINT | METERS | kPa | ANGLE deg. | WIDTH mm | THICK mm |  |  |  |  |
| Gage Start | 1 | 0 | 34,463 | 0.004 | 16.0685 | 1.5118 |  |  |  |  |
| Gage Start | 2 | 0 | 34,473 | 0.004 | 16.0684 | 1.5116 |  |  |  |  |
| Gage Start | 3 | 0 | 34,502 | 0.004 | 16.0685 | 1.5116 |  |  |  |  |
| Gage Start | 4 | 0 | 34,511 | 0.004 | 16.0685 | 1.5118 |  |  |  |  |
| Gage Start | 5 | 0 | 34,511 | 0.004 | 16.0685 | 1.5117 |  |  |  |  |
| Gage Start | 6 | 0 | 34,511 | 0.004 | 16.0685 | 1.5116 |  |  |  |  |
| Gage Start | 7 | 0 | 34,511 | 0.004 | 16.0686 | 1.5116 |  |  |  |  |
| Gage Start | 8 | 0 | 34,511 | 0.004 | 16.0686 | 1.5116 |  |  |  |  |
| Gage Start | 9 | 0 | 34,511 | 0.004 | 16.0686 | 1.5116 |  |  |  |  |
| Gage Start | 10 | 0 | 34,492 | 0.004 | 16.0692 | 1.5119 |  |  |  |  |
| L3T-B0908-R1 Hub End. | 11 | 0.67 | 34,420 | 1.028 | 15.412 | 1.4787 |  |  |  |  |
| L3T-B0908-R1 | 12 | 0.67 | 34,420 | 1.021 | 15.4196 | 1.4771 |  |  |  |  |
| gage check | 13 | 0.67 | 34,028 | 0.004 | 16.0685 | 1.5125 |  |  |  |  |
| gage check | 14 | 0.67 | 34,028 | 0.004 | 16.0683 | 1.5117 |  |  |  |  |
| gage check | 15 | 0.67 | 34,028 | 0.004 | 16.0683 | 1.5119 |  |  |  |  |
| L3T-B0908-R1 | 16 | 1 | 34,463 | 1.032 | 15.406 | 1.4632 |  |  |  |  |
| L3T-B0908-R1 | 17 | 1.33 | 34,463 | 1.039 | 15.4031 | 1.4635 |  |  |  |  |
| L3T-B0908-R1 | 18 | 1.67 | 34,463 | 1.033 | 15.3884 | 1.461 |  |  |  |  |
| L3T-B0908-R1 | 19 | 2 | 34,463 | 1.034 | 15.3756 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 20 | 3 | 34,424 | 1.036 | 15.3711 | 1.462 |  |  |  |  |
| L3T-B0908-R1 | 21 | 3.67 | 34,415 | 1.039 | 15.3667 | 1.4617 |  |  |  |  |
| L3T-B0908-R1 | 22 | 4 | 34,415 | 1.04 | 15.3747 | 1.4626 |  |  |  |  |
| L3T-B0908-R1 | 23 | 5 | 34,415 | 1.042 | 15.3812 | 1.4604 |  |  |  |  |
| L3T-B0908-R1 | 24 | 5.67 | 34,415 | 1.039 | 15.3754 | 1.4611 |  |  |  |  |
| L3T-B0908-R1 | 25 | 6.67 | 34,415 | 1.042 | 15.3571 | 1.4613 |  |  |  |  |
| L3T-B0908-R1 | 26 | 7.33 | 34,415 | 1.047 | 15.3669 | 1.4616 |  |  |  |  |
| L3T-B0908-R1 | 27 | 8.33 | 34,415 | 1.039 | 15.3695 | 1.4618 |  |  |  |  |
| L3T-B0908-R1 | 28 | 9.33 | 34,415 | 1.046 | 15.369 | 1.4616 |  |  |  |  |
| L3T-B0908-R1 | 29 | 10.33 | 34,415 | 1.039 | 15.3806 | 1.4611 |  |  |  |  |
| L3T-B0908-R1 | 30 | 11.33 | 34,415 | 1.044 | 15.3633 | 1.4602 |  |  |  |  |
| L3T-B0908-R1 | 31 | 12 | 34,415 | 1.044 | 15.3651 | 1.4602 |  |  |  |  |
| L3T-B0908-R1 | 32 | 13 | 34,415 | 1.038 | 15.3615 | 1.4606 |  |  |  |  |
| L3T-B0908-R1 | 33 | 14.67 | 34,415 | 1.043 | 15.3671 | 1.4609 |  |  |  |  |
| L3T-B0908-R1 | 34 | 15.67 | 34,415 | 1.047 | 15.3526 | 1.4607 |  |  |  |  |
| L3T-B0908-R1 | 35 | 16.67 | 34,415 | 1.044 | 15.3655 | 1.4605 |  |  |  |  |
| L3T-B0908-R1 | 36 | 17.67 | 34,415 | 1.041 | 15.3734 | 1.4609 |  |  |  |  |
| L3T-B0908-R1 | 37 | 18.67 | 34,415 | 1.04 | 15.3743 | 1.4606 |  |  |  |  |
| L3T-B0908-R1 | 38 | 21 | 34,415 | 1.045 | 15.3806 | 1.4608 |  |  |  |  |
| L3T-B0908-R1 | 39 | 21.67 | 34,415 | 1.043 | 15.3874 | 1.461 |  |  |  |  |
| L3T-B0908-R1 | 40 | 22.67 | 34,415 | 1.041 | 15.3682 | 1.4604 |  |  |  |  |
| L3T-B0908-R1 | 41 | 23.67 | 34,415 | 1.044 | 15.367 | 1.4591 |  |  |  |  |
| L3T-B0908-R1 | 42 | 24.33 | 34,415 | 1.039 | 15.3636 | 1.4603 |  |  |  |  |
| L3T-B0908-R1 | 43 | 25.33 | 34,415 | 1.041 | 15.3726 | 1.4618 |  |  |  |  |
| L3T-B0908-R1 | 44 | 26 | 34,415 | 1.047 | 15.3702 | 1.4625 |  |  |  |  |
| L3T-B0908-R1 | 45 | 26.67 | 34,415 | 1.034 | 15.3819 | 1.4599 |  |  |  |  |
| L3T-B0908-R1 | 46 | 27.67 | 34,415 | 1.045 | 15.3585 | 1.4592 |  |  |  |  |
| gage check | 47 | 27.67 | 34,415 | 0 | 16.0696 | 1.5186 |  |  |  |  |
| gage check | 48 | 27.67 | 34,415 | 0.001 | 16.0692 | 1.5162 |  |  |  |  |
| gage check | 49 | 27.67 | 34,420 | 0.001 | 16.069 | 1.5159 |  |  |  |  |
| gage check | 50 | 27.67 | 34,415 | 0.003 | 16.0691 | 1.5127 |  |  |  |  |
| gage check | 51 | 27.67 | 34,415 | 0.003 | 16.069 | 1.5129 |  |  |  |  |
| gage check | 52 | 27.67 | 34,415 | 0.003 | 16.0687 | 1.5124 |  |  |  |  |
| gage check | 53 | 27.67 | 34,420 | 0.003 | 16.0685 | 1.5122 |  |  |  |  |
| gage check | 54 | 27.67 | 34,424 | 0.003 | 16.0686 | 1.5127 |  |  |  |  |
| gage check | 55 | 27.67 | 34,415 | 0.003 | 16.0672 | 1.5121 |  |  |  |  |
| gage check | 56 | 27.67 | 34,560 | 0.003 | 16.0686 | 1.512 |  |  |  |  |
| gage check | 57 | 27.67 | 34,560 | 0.004 | 16.0687 | 1.5124 |  |  |  |  |
| gage check | 58 | 27.67 | 34,584 | 0.003 | 16.0685 | 1.5128 |  |  |  |  |
| gage check | 59 | 27.67 | 34,574 | 0.003 | 16.0685 | 1.5129 |  |  |  |  |
| gage check | 60 | 27.67 | 34,589 | 0.003 | 16.0685 | 1.5122 |  |  |  |  |
| gage check | 61 | 27.67 | 34,560 | 0.003 | 16.0685 | 1.5123 |  |  |  |  |
| L3T-B0908-R1 | 62 | 27.67 | 34,511 | 1.031 | 15.3645 | 1.4599 |  |  |  |  |
| L3T-B0908-R1 | 63 | 28.67 | 34,502 | 1.021 | 15.3645 | 1.4608 |  |  |  |  |
| L3T-B0908-R1 | 64 | 29 | 34,511 | 1.029 | 15.3756 | 1.4607 |  |  |  |  |
| L3T-B0908-R1 | 65 | 29.33 | 34,507 | 1.02 | 15.3725 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 66 | 29.67 | 34,463 | 1.021 | 15.3737 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 67 | 30 | 34,478 | 1.027 | 15.3809 | 1.4614 |  |  |  |  |
| L3T-B0908-R1 | 68 | 30.33 | 34,468 | 1.036 | 15.3691 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 69 | 30.67 | 34,502 | 1.033 | 15.3641 | 1.4618 |  |  |  |  |
| L3T-B0908-R1 | 70 | 31 | 34,511 | 1.041 | 15.3706 | 1.4629 |  |  |  |  |
| L3T-B0908-R1 | 71 | 31.67 | 34,482 | 1.04 | 15.3706 | 1.4627 |  |  |  |  |
| L3T-B0908-R1 | 72 | 33 | 34,463 | 1.015 | 15.3967 | 1.4605 |  |  |  |  |
| L3T-B0908-R1 | 73 | 33.33 | 34,463 | 1.033 | 15.3849 | 1.4626 |  |  |  |  |
| L3T-B0908-R1 | 74 | 34 | 34,458 | 1.02 | 15.4164 | 1.4617 |  |  |  |  |
| L3T-B0908-R1 | 75 | 34.33 | 34,463 | 1.032 | 15.4169 | 1.4633 |  |  |  |  |
| L3T-B0908-R1 | 76 | 35.67 | 34,463 | 1.029 | 15.4068 | 1.461 |  |  |  |  |
| L3T-B0908-R1 | 77 | 36.33 | 34,463 | 1.028 | 15.4259 | 1.4624 |  |  |  |  |
| L3T-B0908-R1 | 78 | 37.33 | 34,463 | 1.029 | 15.3993 | 1.4634 |  |  |  |  |
| L3T-B0908-R1 | 79 | 38 | 34,463 | 1.029 | 15.4032 | 1.4605 |  |  |  |  |
| L3T-B0908-R1 | 80 | 39 | 34,463 | 1.032 | 15.3981 | 1.4616 |  |  |  |  |
| L3T-B0908-R1 | 81 | 39.67 | 34,463 | 1.033 | 15.3987 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 82 | 40.33 | 34,463 | 1.035 | 15.3944 | 1.4623 |  |  |  |  |
| L3T-B0908-R1 | 83 | 40.67 | 34,463 | 1.037 | 15.4278 | 1.4622 |  |  |  |  |
| L3T-B0908-R1 | 84 | 41.67 | 34,463 | 1.035 | 15.4216 | 1.4627 |  |  |  |  |
| L3T-B0908-R1 | 85 | 43 | 34,463 | 1.027 | 15.3747 | 1.4609 |  |  |  |  |
| L3T-B0908-R1 | 86 | 43.67 | 34,463 | 1.03 | 15.3837 | 1.462 |  |  |  |  |
| L3T-B0908-R1 | 87 | 46.33 | 34,463 | 1.019 | 15.3847 | 1.4606 |  |  |  |  |
| L3T-B0908-R1 | 88 | 48 | 34,444 | 1.025 | 15.3802 | 1.4604 |  |  |  |  |
| L3T-B0908-R1 | 89 | 49.33 | 34,463 | 1.03 | 15.4301 | 1.4606 |  |  |  |  |
| L3T-B0908-R1 | 90 | 51.33 | 34,463 | 1.035 | 15.3955 | 1.4607 |  |  |  |  |
| L3T-B0908-R1 | 91 | 53 | 34,463 | 1.026 | 15.3989 | 1.4606 |  |  |  |  |
| L3T-B0908-R1 | 92 | 55.67 | 34,458 | 1.023 | 15.3745 | 1.4612 |  |  |  |  |
| L3T-B0908-R1 | 93 | 58.67 | 34,463 | 1.024 | 15.3855 | 1.46 |  |  |  |  |
| L3T-B0908-R1 | 94 | 61 | 34,449 | 1.02 | 15.3752 | 1.4617 |  |  |  |  |
| L3T-B0908-R1 | 95 | 62.67 | 34,453 | 1.029 | 15.3865 | 1.462 |  |  |  |  |
| L3T-B0908-R1 | 96 | 66.67 | 34,463 | 1.023 | 15.3881 | 1.4614 |  |  |  |  |
| L3T-B0908-R1 | 97 | 69.33 | 34,453 | 1.019 | 15.3947 | 1.4614 |  |  |  |  |
| L3T-B0908-R1 | 98 | 70.67 | 34,463 | 1.027 | 15.3976 | 1.4618 |  |  |  |  |
| L3T-B0908-R1 | 99 | 72.33 | 34,444 | 1.02 | 15.3757 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 100 | 74.33 | 34,463 | 1.029 | 15.3683 | 1.462 |  |  |  |  |
| L3T-B0908-R1 | 101 | 75.67 | 34,458 | 1.027 | 15.3672 | 1.4614 |  |  |  |  |
| L3T-B0908-R1 | 102 | 77 | 34,458 | 1.025 | 15.704 | 1.461 |  |  |  |  |
| L3T-B0908-R1 | 103 | 78 | 34,463 | 1.029 | 15.3415 | 1.4622 |  |  |  |  |
| L3T-B0908-R1 | 104 | 80 | 34,444 | 1.028 | 15.3546 | 1.4627 |  |  |  |  |
| L3T-B0908-R1 | 105 | 81.33 | 34,458 | 1.024 | 15.361 | 1.4614 |  |  |  |  |
| L3T-B0908-R1 | 106 | 83.33 | 34,463 | 1.031 | 15.3591 | 1.4609 |  |  |  |  |
| L3T-B0908-R1 | 107 | 84.33 | 34,463 | 1.027 | 15.3577 | 1.4606 |  |  |  |  |
| L3T-B0908-R1 | 108 | 86.33 | 34,453 | 1.034 | 15.375 | 1.4626 |  |  |  |  |
| L3T-B0908-R1 | 109 | 89.33 | 34,458 | 1.025 | 15.3693 | 1.4608 |  |  |  |  |
| L3T-B0908-R1 Marked 92m | 110 | 93.33 | 34,415 | 1.012 | 15.3658 | 1.4607 |  |  |  |  |
| L3T-B0908-R1 | 111 | 93.67 | 34,415 | 1.021 | 15.3638 | 1.4611 |  |  |  |  |
| L3T-B0908-R1 | 112 | 93.67 | 34,415 | 1.023 | 15.3713 | 1.4609 |  |  |  |  |
| L3T-B0908-R1 | 113 | 96.33 | 34,415 | 1.017 | 15.3731 | 1.4607 |  |  |  |  |
| L3T-B0908-R1 | 114 | 97.33 | 34,415 | 1.027 | 15.3757 | 1.4617 |  |  |  |  |
| L3T-B0908-R1 | 115 | 98.33 | 34,415 | 1.026 | 15.381 | 1.4598 |  |  |  |  |
| L3T-B0908-R1 | 116 | 101.33 | 34,415 | 1.024 | 15.3769 | 1.4605 |  |  |  |  |
| L3T-B0908-R1 | 117 | 104.33 | 34,415 | 1.026 | 15.374 | 1.4606 |  |  |  |  |
| L3T-B0908-R1 | 118 | 109 | 34,415 | 1.022 | 15.3845 | 1.461 |  |  |  |  |
| L3T-B0908-R1 | 119 | 118.67 | 34,415 | 1.022 | 15.3824 | 1.4598 |  |  |  |  |
| L3T-B0908-R1 | 120 | 123 | 34,415 | 1.02 | 15.3789 | 1.4599 |  |  |  |  |
| L3T-B0908-R1 | 121 | 128.33 | 34,415 | 1.03 | 15.3815 | 1.46 |  |  |  |  |
| L3T-B0908-R1 | 122 | 131 | 34,415 | 1.027 | 15.3756 | 1.4604 |  |  |  |  |
| L3T-B0908-R1 | 123 | 133.67 | 34,415 | 1.024 | 15.3789 | 1.4604 |  |  |  |  |
| L3T-B0908-R1 | 124 | 139 | 34,415 | 1.022 | 15.3779 | 1.4607 |  |  |  |  |
| L3T-B0908-R1 | 125 | 146 | 34,415 | 1.024 | 15.3836 | 1.4603 |  |  |  |  |
| L3T-B0908-R1 | 126 | 153.33 | 34,415 | 1.02 | 15.3838 | 1.4602 |  |  |  |  |
| L3T-B0908-R1 | 127 | 156.67 | 34,415 | 1.021 | 15.3821 | 1.4607 |  |  |  |  |
| L3T-B0908-R1 | 128 | 162.67 | 34,415 | 1.026 | 15.3801 | 1.4619 |  |  |  |  |
| L3T-B0908-R1 | 129 | 169.67 | 34,415 | 1.025 | 15.3857 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 130 | 175.33 | 34,415 | 1.018 | 15.3931 | 1.4611 |  |  |  |  |
| L3T-B0908-R1 | 131 | 182.33 | 34,415 | 1.017 | 15.3809 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 132 | 186 | 34,415 | 1.024 | 15.387 | 1.462 |  |  |  |  |
| L3T-B0908-R1 | 133 | 190.33 | 34,415 | 1.028 | 15.3863 | 1.4617 |  |  |  |  |
| L3T-B0908-R1 | 134 | 195 | 34,415 | 1.024 | 15.3919 | 1.4623 |  |  |  |  |
| L3T-B0908-R1 | 135 | 199.33 | 34,415 | 1.026 | 15.3803 | 1.4611 |  |  |  |  |
| L3T-B0908-R1 | 136 | 200 | 34,415 | 1.024 | 15.3902 | 1.4607 |  |  |  |  |
| L3T-B0908-R1 | 137 | 200.33 | 34,434 | 1.031 | 15.3789 | 1.4621 |  |  |  |  |
| L3T-B0908-R1 | 138 | 207 | 34,415 | 1.023 | 15.381 | 1.4605 |  |  |  |  |
| L3T-B0908-R1 | 139 | 211.33 | 34,415 | 1.021 | 15.3798 | 1.461 |  |  |  |  |
| L3T-B0908-R1 | 140 | 216.67 | 34,415 | 1.024 | 15.3942 | 1.4619 |  |  |  |  |
| L3T-B0908-R1 | 141 | 221.67 | 34,415 | 1.028 | 15.3881 | 1.4627 |  |  |  |  |
| L3T-B0908-R1 | 142 | 228.33 | 34,415 | 1.03 | 15.3852 | 1.4629 |  |  |  |  |
| L3T-B0908-R1 | 143 | 232.33 | 34,415 | 1.02 | 15.3811 | 1.4613 |  |  |  |  |
| L3T-B0908-R1 | 144 | 243.33 | 34,415 | 1.027 | 15.3884 | 1.4619 |  |  |  |  |
| L3T-B0908-R1 | 145 | 261.67 | 34,415 | 1.021 | 15.3792 | 1.4618 |  |  |  |  |
| L3T-B0908-R1 | 146 | 264 | 34,415 | 1.027 | 15.3855 | 1.4622 |  |  |  |  |
| L3T-B0908-R1 | 147 | 273.33 | 34,415 | 1.028 | 15.3779 | 1.4612 |  |  |  |  |
| L3T-B0908-R1 | 148 | 279 | 34,415 | 1.026 | 15.3879 | 1.4613 |  |  |  |  |
| L3T-B0908-R1 | 149 | 284.67 | 34,410 | 1.024 | 15.3837 | 1.4618 |  |  |  |  |
| L3T-B0908-R1 | 150 | 291.33 | 34,415 | 1.025 | 15.4006 | 1.4601 |  |  |  |  |
| L3T-B0908-R1 | 151 | 295 | 34,415 | 1.024 | 15.3856 | 1.4612 |  |  |  |  |
| L3T-B0908-R1 | 152 | 299.33 | 34,415 | 1.024 | 15.393 | 1.4618 |  |  |  |  |
| L3T-B0908-R1 | 153 | 306.33 | 34,415 | 1.023 | 15.3782 | 1.4605 |  |  |  |  |
| L3T-B0908-R1 | 154 | 309.67 | 34,415 | 1.026 | 15.3866 | 1.4612 |  |  |  |  |
| L3T-B0908-R1 | 155 | 312.33 | 34,415 | 1.03 | 15.3766 | 1.4602 |  |  |  |  |
| L3T-B0908-R1 | 156 | 317.33 | 34,415 | 1.029 | 15.3812 | 1.4606 |  |  |  |  |
| L3T-B0908-R1 | 157 | 322 | 34,415 | 1.03 | 15.3802 | 1.4616 |  |  |  |  |
| L3T-B0908-R1 | 158 | 330 | 34,415 | 1.03 | 15.3786 | 1.4615 |  |  |  |  |
| L3T-B0908-R1 | 159 | 332 | 34,415 | 1.023 | 15.3794 | 1.4617 |  |  |  |  |
| L3T-B0908-R1 | 160 | 333.33 | 34,415 | 1.031 | 15.3828 | 1.4622 |  |  |  |  |
|  |  |  | 34,435 | 1.0296 | 15.3837 | 1.4615 |  |  |  |  |
| Gage End | 161 | 333.33 | 34,415 | 0.006 | 16.0696 | 1.5129 |  |  |  |  |
| Gage End | 162 | 333.33 | 34,449 | 0.005 | 16.0694 | 1.5129 |  |  |  |  |
| Gage End | 163 | 333.33 | 34,463 | 0.006 | 16.0693 | 1.5127 |  |  |  |  |
| Gage End | 164 | 333.33 | 34,463 | 0.006 | 16.0691 | 1.5127 |  |  |  |  |
| Gage End | 165 | 333.33 | 34,463 | 0.005 | 16.0691 | 1.5128 |  |  |  |  |
| Gage End | 166 | 333.33 | 34,463 | 0.005 | 16.0691 | 1.5129 |  |  |  |  |
| Gage End | 167 | 333.33 | 34,463 | 0.006 | 16.0691 | 1.5128 |  |  |  |  |
| Gage End | 168 | 333.33 | 34,468 | 0.006 | 16.0691 | 1.5123 |  |  |  |  |
| Gage End | 169 | 333.33 | 34,463 | 0.005 | 16.0692 | 1.5126 |  |  |  |  |
| Gage End | 170 | 333.33 | 34,463 | 0.005 | 16.0688 | 1.5131 |  |  |  |  |
| Gage flip | 171 | 333.33 | 34,463 | -0.001 | 16.0745 | 1.5129 |  |  |  |  |
| Gage flip | 172 | 333.33 | 34,463 | -0.001 | 16.0743 | 1.5129 |  |  |  |  |
| Gage flip | 173 | 333.33 | 34,463 | -0.001 | 16.0742 | 1.5129 |  |  |  |  |
| Gage flip | 174 | 333.33 | 34,463 | -0.001 | 16.0742 | 1.5128 |  |  |  |  |
| Gage End | 175 | 333.33 | 34,453 | 0.004 | 16.0687 | 1.5131 |  |  |  |  |
| Gage End | 176 | 333.33 | 34,463 | 0.004 | 16.0687 | 1.5132 |  |  |  |  |
| Gage End | 177 | 333.33 | 34,463 | 0.004 | 16.0687 | 1.5131 |  |  |  |  |

| 03-18-2005 Cable RunLHC-3-T-B908R2 Unit 0 07:39:36 |  |  |  |
| --- | --- | --- | --- |
| LHC-HGQ-INNER CME #2 |  |  |  |  |
| Notes. | POINT | METERS | kPa | ANGLE | WIDTH | THICK |  |
| Gage Start | 1 | 0 | 34,492 | 0.002 | 16.0688 | 1.5122 |  |
| Gage Start | 2 | 0 | 34,511 | 0.003 | 16.069 | 1.5123 |  |
| Gage Start | 3 | 0 | 34,511 | 0.003 | 16.0689 | 1.5128 |  |
| Gage Start | 4 | 0 | 34,511 | 0.003 | 16.069 | 1.5128 |  |
| Gage Start | 5 | 0 | 34,516 | 0.004 | 16.069 | 1.5128 |  |
| Gage Start | 6 | 0 | 34,511 | 0.003 | 16.0687 | 1.5128 |  |
| Gage Start | 7 | 0 | 34,511 | 0.003 | 16.0687 | 1.5128 |  |
| Gage Start | 8 | 0 | 34,516 | 0.003 | 16.0688 | 1.5128 |  |
| Gage Start | 9 | 0 | 34,555 | 0.003 | 16.0687 | 1.5126 |  |
| Gage Start | 10 | 0 | 34,511 | 0.003 | 16.069 | 1.5125 |  |
| Gage Start | 11 | 0 | 34,487 | 1.044 | 15.4048 | 1.4625 |  |
| L3T-B0908-R2 Start Hub End | 12 | 0.33 | 34,463 | 1.042 | 15.4097 | 1.4602 |  |
| L3T-B0908-R2 | 13 | 0.67 | 34,463 | 1.045 | 15.3921 | 1.4609 |  |
| L3T-B0908-R2 | 14 | 1 | 34,468 | 1.048 | 15.3969 | 1.461 |  |
| L3T-B0908-R2 | 15 | 1.33 | 34,487 | 1.044 | 15.3808 | 1.4606 |  |
| L3T-B0908-R2 | 16 | 1.67 | 34,511 | 1.049 | 15.3823 | 1.4617 |  |
| L3T-B0908-R2 | 17 | 2 | 34,511 | 1.053 | 15.3851 | 1.4614 |  |
| L3T-B0908-R2 | 18 | 2 | 34,511 | 1.057 | 15.3636 | 1.4627 |  |
| L3T-B0908-R2 | 19 | 3.67 | 34,473 | 1.051 | 15.4095 | 1.4627 |  |
| L3T-B0908-R2 | 20 | 5.67 | 34,463 | 1.05 | 15.3931 | 1.4616 |  |
| L3T-B0908-R2 | 21 | 6.33 | 34,463 | 1.054 | 15.3809 | 1.4609 |  |
| L3T-B0908-R2 | 22 | 7.33 | 34,463 | 1.051 | 15.367 | 1.461 |  |
| L3T-B0908-R2 | 23 | 8 | 34,463 | 1.053 | 15.3694 | 1.4613 |  |
| L3T-B0908-R2 | 24 | 9.33 | 34,463 | 1.05 | 15.371 | 1.462 |  |
| L3T-B0908-R2 | 25 | 10.33 | 34,463 | 1.059 | 15.3581 | 1.462 |  |
| L3T-B0908-R2 | 26 | 11.33 | 34,463 | 1.049 | 15.37 | 1.4614 |  |
| L3T-B0908-R2 | 27 | 13.33 | 34,463 | 1.054 | 15.3696 | 1.4603 |  |
| L3T-B0908-R2 | 28 | 15 | 34,468 | 1.051 | 15.3862 | 1.4599 |  |
| L3T-B0908-R2 | 29 | 16.33 | 34,468 | 1.048 | 15.3836 | 1.4604 |  |
| L3T-B0908-R2 | 30 | 19 | 34,463 | 1.045 | 15.3874 | 1.4603 |  |
| L3T-B0908-R2 | 31 | 24 | 34,463 | 1.051 | 15.3798 | 1.4609 |  |
| L3T-B0908-R2 | 32 | 27 | 34,463 | 1.054 | 15.3811 | 1.4607 |  |
| L3T-B0908-R2 | 33 | 29.67 | 34,463 | 1.048 | 15.3841 | 1.4609 |  |
| L3T-B0908-R2 | 34 | 32.67 | 34,463 | 1.046 | 15.3741 | 1.4606 |  |
| L3T-B0908-R2 | 35 | 33.67 | 34,463 | 1.048 | 15.3921 | 1.4601 |  |
| L3T-B0908-R2 | 36 | 36.67 | 34,463 | 1.05 | 15.3826 | 1.4612 |  |
| L3T-B0908-R2 | 37 | 39 | 34,463 | 1.047 | 15.3791 | 1.4605 |  |
| L3T-B0908-R2 | 38 | 42.67 | 34,463 | 1.047 | 15.395 | 1.4595 |  |
| L3T-B0908-R2 | 39 | 47 | 34,463 | 1.044 | 15.3868 | 1.4587 |  |
| L3T-B0908-R2 | 40 | 47.67 | 34,463 | 1.046 | 15.4032 | 1.4588 |  |
| L3T-B0908-R2 | 41 | 48.67 | 34,463 | 1.044 | 15.3932 | 1.4592 |  |
| L3T-B0908-R2 | 42 | 50.67 | 34,463 | 1.046 | 15.3933 | 1.4597 |  |
| L3T-B0908-R2 | 43 | 53.33 | 34,463 | 1.046 | 15.393 | 1.4587 |  |
| L3T-B0908-R2 | 44 | 56 | 34,463 | 1.047 | 15.3892 | 1.4604 |  |
| L3T-B0908-R2 | 45 | 58.33 | 34,463 | 1.045 | 15.4007 | 1.4609 |  |
| L3T-B0908-R2 | 46 | 61.67 | 34,463 | 1.047 | 15.392 | 1.4607 |  |
| L3T-B0908-R2 | 47 | 65.67 | 34,463 | 1.048 | 15.3868 | 1.4611 |  |
| L3T-B0908-R2 | 48 | 68.33 | 34,463 | 1.049 | 15.3798 | 1.4606 |  |
| L3T-B0908-R2 | 49 | 72.67 | 34,463 | 1.048 | 15.3883 | 1.4608 |  |
| L3T-B0908-R2 | 50 | 74.67 | 34,463 | 1.045 | 15.3861 | 1.4614 |  |
| L3T-B0908-R2 | 51 | 77.33 | 34,463 | 1.042 | 15.3866 | 1.4609 |  |
| L3T-B0908-R2 | 52 | 80.67 | 34,463 | 1.047 | 15.3823 | 1.4614 |  |
| L3T-B0908-R2 | 53 | 83 | 34,463 | 1.049 | 15.3829 | 1.4603 |  |
| L3T-B0908-R2 | 54 | 84.67 | 34,463 | 1.05 | 15.3841 | 1.4606 |  |
| L3T-B0908-R2 | 55 | 87 | 34,463 | 1.046 | 15.3835 | 1.4607 |  |
| L3T-B0908-R2 | 56 | 89.33 | 34,463 | 1.045 | 15.3772 | 1.4608 |  |
| L3T-B0908-R2 | 57 | 92 | 34,463 | 1.042 | 15.3794 | 1.4611 |  |
| L3T-B0908-R2 | 58 | 94 | 34,463 | 1.041 | 15.378 | 1.4607 |  |
| L3T-B0908-R2 | 59 | 95.33 | 34,463 | 1.045 | 15.3892 | 1.4602 |  |
| L3T-B0908-R2 | 60 | 97 | 34,463 | 1.047 | 15.385 | 1.4603 |  |
| L3T-B0908-R2 | 61 | 99 | 34,463 | 1.048 | 15.3868 | 1.461 |  |
| L3T-B0908-R2 | 62 | 100.33 | 34,458 | 1.05 | 15.3794 | 1.4612 |  |
| L3T-B0908-R2 | 63 | 102.67 | 34,463 | 1.045 | 15.3881 | 1.461 |  |
| L3T-B0908-R2 | 64 | 106.67 | 34,458 | 1.043 | 15.3877 | 1.46 |  |
| L3T-B0908-R2 | 65 | 109.33 | 34,444 | 1.044 | 15.4014 | 1.461 |  |
| L3T-B0908-R2 | 66 | 112 | 34,463 | 1.047 | 15.3877 | 1.4615 |  |
| L3T-B0908-R2 | 67 | 118.33 | 34,439 | 1.048 | 15.3866 | 1.4607 |  |
| L3T-B0908-R2 | 68 | 126 | 34,453 | 1.043 | 15.3848 | 1.4603 |  |
| L3T-B0908-R2 | 69 | 133.33 | 34,444 | 1.045 | 15.3952 | 1.4599 |  |
| L3T-B0908-R2 | 70 | 137.33 | 34,420 | 1.044 | 15.385 | 1.4605 |  |
| L3T-B0908-R2 | 71 | 142 | 34,453 | 1.048 | 15.3787 | 1.461 |  |
| L3T-B0908-R2 | 72 | 146 | 34,429 | 1.048 | 15.3792 | 1.4605 |  |
| L3T-B0908-R2 | 73 | 151.33 | 34,429 | 1.049 | 15.3826 | 1.4616 |  |
| L3T-B0908-R2 | 74 | 155 | 34,415 | 1.049 | 15.3764 | 1.4613 |  |
| L3T-B0908-R2 | 75 | 159.67 | 34,424 | 1.051 | 15.3846 | 1.4604 |  |
| L3T-B0908-R2 | 76 | 164.67 | 34,434 | 1.048 | 15.3829 | 1.4601 |  |
| L3T-B0908-R2 | 77 | 168.33 | 34,434 | 1.043 | 15.3868 | 1.4608 |  |
| L3T-B0908-R2 | 78 | 171.67 | 34,439 | 1.042 | 15.3747 | 1.4608 |  |
| L3T-B0908-R2 | 79 | 187.33 | 34,434 | 1.046 | 15.3818 | 1.4616 |  |
| L3T-B0908-R2 | 80 | 202.67 | 34,429 | 1.049 | 15.3902 | 1.4617 |  |
| L3T-B0908-R2 | 81 | 209 | 34,424 | 1.046 | 15.3864 | 1.4614 |  |
| L3T-B0908-R2 | 82 | 211.33 | 34,444 | 1.045 | 15.3918 | 1.4611 |  |
| L3T-B0908-R2 | 83 | 214.33 | 34,424 | 1.047 | 15.3844 | 1.4613 |  |
| L3T-B0908-R2 | 84 | 217.33 | 34,420 | 1.046 | 15.3811 | 1.4626 |  |
| L3T-B0908-R2 | 85 | 225 | 34,424 | 1.045 | 15.3878 | 1.461 |  |
| L3T-B0908-R2 | 86 | 228.67 | 34,415 | 1.045 | 15.3818 | 1.4623 |  |
| L3T-B0908-R2 | 87 | 232 | 34,424 | 1.047 | 15.3876 | 1.4618 |  |
| L3T-B0908-R2 | 88 | 234.67 | 34,429 | 1.047 | 15.3863 | 1.4614 |  |
| L3T-B0908-R2 | 89 | 236 | 34,453 | 1.045 | 15.3857 | 1.4614 |  |
| L3T-B0908-R2 | 90 | 241 | 34,424 | 1.044 | 15.381 | 1.4617 |  |
| L3T-B0908-R2 | 91 | 244 | 34,424 | 1.048 | 15.3762 | 1.4609 |  |
| L3T-B0908-R2 | 92 | 246.33 | 34,420 | 1.044 | 15.3839 | 1.4611 |  |
| L3T-B0908-R2 | 93 | 247.33 | 34,453 | 1.039 | 15.3855 | 1.4611 |  |
| L3T-B0908-R2 | 94 | 252 | 34,449 | 1.045 | 15.381 | 1.4618 |  |
| L3T-B0908-R2 | 95 | 259.67 | 34,434 | 1.04 | 15.3844 | 1.4614 |  |
| L3T-B0908-R2 | 96 | 261 | 34,463 | 1.045 | 15.3824 | 1.4605 |  |
| L3T-B0908-R2 | 97 | 264.33 | 34,439 | 1.047 | 15.3741 | 1.4617 |  |
| L3T-B0908-R2 | 98 | 265.33 | 34,439 | 1.044 | 15.3808 | 1.4613 |  |
| L3T-B0908-R2 | 99 | 268.67 | 34,439 | 1.055 | 15.3853 | 1.4625 |  |
| L3T-B0908-R2 | 100 | 276.67 | 34,424 | 1.05 | 15.3789 | 1.4602 |  |
| L3T-B0908-R2 | 101 | 278 | 34,434 | 1.041 | 15.3743 | 1.4615 |  |
| L3T-B0908-R2 | 102 | 278.67 | 34,453 | 1.041 | 15.3803 | 1.4614 |  |
| L3T-B0908-R2 | 103 | 281.33 | 34,434 | 1.039 | 15.3934 | 1.4611 |  |
| L3T-B0908-R2 | 104 | 287 | 34,434 | 1.051 | 15.3817 | 1.4612 |  |
| L3T-B0908-R2 | 105 | 292.67 | 34,429 | 1.047 | 15.3814 | 1.4619 |  |
| L3T-B0908-R2 | 106 | 293.33 | 34,453 | 1.042 | 15.3833 | 1.4611 |  |
| L3T-B0908-R2 | 107 | 294 | 34,458 | 1.045 | 15.386 | 1.4615 |  |
| L3T-B0908-R2 | 108 | 299.33 | 34,429 | 1.043 | 15.3844 | 1.4608 |  |
| L3T-B0908-R2 | 109 | 302.67 | 34,415 | 1.045 | 15.3801 | 1.4613 |  |
| L3T-B0908-R2 | 110 | 306 | 34,453 | 1.048 | 15.3798 | 1.4614 |  |
| L3T-B0908-R2 | 111 | 313.33 | 34,420 | 1.049 | 15.3755 | 1.461 |  |
| L3T-B0908-R2 | 112 | 316.67 | 34,424 | 1.045 | 15.385 | 1.4624 |  |
| L3T-B0908-R2 | 113 | 317.33 | 34,449 | 1.047 | 15.3787 | 1.462 |  |
| L3T-B0908-R2 | 114 | 318 | 34,463 | 1.04 | 15.4017 | 1.4602 |  |
| L3T-B0908-R2 | 115 | 320.33 | 34,429 | 1.047 | 15.3901 | 1.4621 |  |
| L3T-B0908-R2 | 116 | 324 | 34,434 | 1.042 | 15.3811 | 1.462 |  |
| L3T-B0908-R2 | 117 | 326 | 34,415 | 1.048 | 15.3794 | 1.4614 |  |
| L3T-B0908-R2 | 118 | 328 | 34,434 | 1.041 | 15.3762 | 1.4613 |  |
| L3T-B0908-R2 | 119 | 330.67 | 34,415 | 1.039 | 15.3754 | 1.4606 |  |
| L3T-B0908-R2 | 120 | 335 | 34,420 | 1.045 | 15.3808 | 1.4605 |  |
| L3T-B0908-R2 | 121 | 337.67 | 34,424 | 1.047 | 15.3871 | 1.4608 |  |
| L3T-B0908-R2 | 122 | 341.33 | 34,434 | 1.047 | 15.3733 | 1.4626 |  |
| L3T-B0908-R2 | 123 | 342.33 | 34,449 | 1.043 | 15.3824 | 1.4612 |  |
| L3T-B0908-R2 | 124 | 344.33 | 34,449 | 1.05 | 15.3848 | 1.4602 |  |
| L3T-B0908-R2 | 125 | 347 | 34,415 | 1.046 | 15.3822 | 1.4609 |  |
| L3T-B0908-R2 | 126 | 348.67 | 34,415 | 1.049 | 15.3801 | 1.4606 |  |
| L3T-B0908-R2 | 127 | 349.67 | 34,415 | 1.049 | 15.3788 | 1.4615 |  |
| L3T-B0908-R2 | 128 | 351.67 | 34,420 | 1.043 | 15.3797 | 1.4604 |  |
| L3T-B0908-R2 End Spoot Top | 129 | 352 | 34,429 | 1.048 | 15.3819 | 1.4601 |  |
|  |  | Avg. = | 34,448 | 1.0466 | 15.3838 | 1.4610 |  |
| Gage End | 130 | 352.67 | 34,463 | 0.006 | 16.0692 | 1.5128 |  |
| Gage End | 131 | 352.67 | 34,463 | 0.006 | 16.0693 | 1.5129 |  |
| Gage End | 132 | 352.67 | 34,502 | 0.006 | 16.0688 | 1.5126 |  |
| Gage End | 133 | 352.67 | 34,511 | 0.005 | 16.0685 | 1.5128 |  |
| Gage End | 134 | 352.67 | 34,511 | 0.005 | 16.0686 | 1.5127 |  |

| 03-22-2005 Cable RunLHC-3-T-B908R3 Unit 0 09:09:12 |  |
| --- | --- |
| LHC-HGQ-INNER CME #2 |  |  |  |
| Notes: | POINT | METERS | kPa | ANGLE | WIDTH | THICK |
| Gage Start | 1 | 0 | 34,463 | 0.003 | 16.0693 | 1.5124 |
| Gage Start | 2 | 0 | 34,463 | 0.004 | 16.0686 | 1.5121 |
| Gage Start | 3 | 0 | 34,492 | 0.004 | 16.0686 | 1.5124 |
| Gage Start | 4 | 0 | 34,511 | 0.004 | 16.0684 | 1.5124 |
| Gage Start | 5 | 0 | 34,511 | 0.004 | 16.0686 | 1.5121 |
| Gage Start | 6 | 0 | 34,511 | 0.004 | 16.0686 | 1.5124 |
| Gage Start | 7 | 0 | 34,511 | 0.004 | 16.0687 | 1.5122 |
| Gage Start | 8 | 0 | 34,511 | 0.004 | 16.0687 | 1.5123 |
| Gage Start | 9 | 0 | 34,511 | 0.004 | 16.0687 | 1.5123 |
| Gage Start | 10 | 0 | 34,511 | 0.004 | 16.0687 | 1.5123 |
| L3T-B0908-R3 Start Hub End | 11 | 0 | 34,463 | 1.013 | 15.4559 | 1.4728 |
| L3T-B0908-R3 | 12 | 0 | 34,463 | 1.028 | 15.4402 | 1.4716 |
| L3T-B0908-R3 | 13 | 0 | 34,463 | 1.026 | 15.4235 | 1.4696 |
| L3T-B0908-R3 | 14 | 1 | 34,434 | 1.026 | 15.4135 | 1.4656 |
| L3T-B0908-R3 | 15 | 1.33 | 34,458 | 1.026 | 15.4106 | 1.4662 |
| L3T-B0908-R3 | 16 | 1.67 | 34,463 | 1.029 | 15.3979 | 1.4715 |
| L3T-B0908-R3 | 17 | 2.33 | 34,458 | 1.022 | 15.396 | 1.4681 |
| L3T-B0908-R3 | 18 | 3 | 34,444 | 1.033 | 15.3853 | 1.4636 |
| L3T-B0908-R3 | 19 | 3.33 | 34,463 | 1.023 | 15.3795 | 1.4634 |
| L3T-B0908-R3 | 20 | 3.67 | 34,463 | 1.03 | 15.3738 | 1.4616 |
| L3T-B0908-R3 | 21 | 4.33 | 34,424 | 1.02 | 15.3742 | 1.4604 |
| L3T-B0908-R3 | 22 | 5.33 | 34,453 | 1.034 | 15.3818 | 1.4624 |
| L3T-B0908-R3 | 23 | 5.67 | 34,424 | 1.038 | 15.3738 | 1.4615 |
| L3T-B0908-R3 | 24 | 6.33 | 34,424 | 1.038 | 15.3608 | 1.4613 |
| L3T-B0908-R3 | 25 | 7 | 34,463 | 1.044 | 15.3577 | 1.4622 |
| L3T-B0908-R3 | 26 | 7.33 | 34,458 | 1.036 | 15.3533 | 1.4618 |
| L3T-B0908-R3 | 27 | 8.33 | 34,463 | 1.025 | 15.3619 | 1.4619 |
| L3T-B0908-R3 | 28 | 9 | 34,463 | 1.039 | 15.3716 | 1.4638 |
| L3T-B0908-R3 | 29 | 10 | 34,444 | 1.039 | 15.361 | 1.4621 |
| L3T-B0908-R3 | 30 | 10.67 | 34,453 | 1.034 | 15.3674 | 1.4611 |
| L3T-B0908-R3 | 31 | 12 | 34,463 | 1.036 | 15.3626 | 1.4626 |
| L3T-B0908-R3 | 32 | 13 | 34,463 | 1.037 | 15.3432 | 1.4616 |
| L3T-B0908-R3 | 33 | 15 | 34,463 | 1.037 | 15.3636 | 1.4619 |
| L3T-B0908-R3 | 34 | 15.67 | 34,458 | 1.032 | 15.3566 | 1.4619 |
| L3T-B0908-R3 | 35 | 17.67 | 34,453 | 1.035 | 15.3534 | 1.4611 |
| L3T-B0908-R3 | 36 | 18 | 34,463 | 1.031 | 15.3506 | 1.4615 |
| L3T-B0908-R3 | 37 | 18.67 | 34,463 | 1.044 | 15.3642 | 1.4615 |
| L3T-B0908-R3 | 38 | 19.33 | 34,463 | 1.045 | 15.368 | 1.4616 |
| L3T-B0908-R3 | 39 | 20.67 | 34,463 | 1.042 | 15.3567 | 1.4626 |
| L3T-B0908-R3 | 40 | 21.67 | 34,458 | 1.038 | 15.3654 | 1.462 |
| L3T-B0908-R3 | 41 | 22.67 | 34,463 | 1.041 | 15.3664 | 1.4618 |
| L3T-B0908-R3 | 42 | 23 | 34,463 | 1.026 | 15.3989 | 1.4615 |
| L3T-B0908-R3 | 43 | 23.67 | 34,463 | 1.044 | 15.3916 | 1.4606 |
| L3T-B0908-R3 | 44 | 25 | 34,463 | 1.031 | 15.3663 | 1.4606 |
| L3T-B0908-R3 | 45 | 25.67 | 34,463 | 1.04 | 15.3689 | 1.4624 |
| L3T-B0908-R3 | 46 | 27 | 34,458 | 1.035 | 15.3853 | 1.4614 |
| L3T-B0908-R3 | 47 | 28 | 34,463 | 1.029 | 15.3966 | 1.4617 |
| L3T-B0908-R3 | 48 | 29.67 | 34,463 | 1.046 | 15.3586 | 1.4609 |
| L3T-B0908-R3 | 49 | 30.67 | 34,463 | 1.031 | 15.3959 | 1.4618 |
| L3T-B0908-R3 | 50 | 31.67 | 34,463 | 1.044 | 15.3727 | 1.4613 |
| L3T-B0908-R3 | 51 | 33 | 34,444 | 1.037 | 15.3552 | 1.4606 |
| L3T-B0908-R3 | 52 | 36.67 | 34,453 | 1.029 | 15.3769 | 1.46 |
| L3T-B0908-R3 | 53 | 37.33 | 34,463 | 1.029 | 15.3626 | 1.4604 |
| L3T-B0908-R3 | 54 | 38.33 | 34,463 | 1.035 | 15.3834 | 1.4611 |
| L3T-B0908-R3 | 55 | 40 | 34,458 | 1.033 | 15.3889 | 1.4606 |
| L3T-B0908-R3 | 56 | 42 | 34,463 | 1.031 | 15.3919 | 1.4605 |
| L3T-B0908-R3 | 57 | 44 | 34,449 | 1.038 | 15.4203 | 1.4598 |
| L3T-B0908-R3 | 58 | 44.67 | 34,463 | 1.034 | 15.3761 | 1.4592 |
| L3T-B0908-R3 | 59 | 46.67 | 34,449 | 1.04 | 15.3897 | 1.46 |
| L3T-B0908-R3 | 60 | 50.33 | 34,434 | 1.037 | 15.381 | 1.4612 |
| L3T-B0908-R3 | 61 | 53.67 | 34,429 | 1.038 | 15.3758 | 1.4603 |
| L3T-B0908-R3 | 62 | 56 | 34,420 | 1.037 | 15.3743 | 1.46 |
| L3T-B0908-R3 | 63 | 57 | 34,463 | 1.039 | 15.3895 | 1.46 |
| L3T-B0908-R3 | 64 | 59 | 34,444 | 1.04 | 15.3979 | 1.4597 |
| L3T-B0908-R3 | 65 | 60.67 | 34,458 | 1.041 | 15.3908 | 1.4607 |
| L3T-B0908-R3 | 66 | 62.33 | 34,458 | 1.034 | 15.4031 | 1.4596 |
| L3T-B0908-R3 | 67 | 65 | 34,444 | 1.039 | 15.3876 | 1.4598 |
| L3T-B0908-R3 | 68 | 67.33 | 34,415 | 1.039 | 15.3917 | 1.4608 |
| L3T-B0908-R3 | 69 | 71 | 34,449 | 1.034 | 15.3985 | 1.4595 |
| L3T-B0908-R3 | 70 | 81 | 34,424 | 1.031 | 15.3875 | 1.4595 |
| L3T-B0908-R3 | 71 | 83 | 34,415 | 1.04 | 15.4277 | 1.46 |
| L3T-B0908-R3 | 72 | 84.33 | 34,458 | 1.031 | 15.4064 | 1.4592 |
| L3T-B0908-R3 | 73 | 86 | 34,420 | 1.034 | 15.4149 | 1.4592 |
| L3T-B0908-R3 | 74 | 88.33 | 34,415 | 1.034 | 15.4078 | 1.4596 |
| L3T-B0908-R3 | 75 | 90 | 34,424 | 1.035 | 15.4227 | 1.4599 |
| L3T-B0908-R3 | 76 | 93.67 | 34,458 | 1.033 | 15.3992 | 1.4591 |
| L3T-B0908-R3 | 77 | 96.33 | 34,420 | 1.036 | 15.39 | 1.4599 |
| L3T-B0908-R3 | 78 | 98.67 | 34,424 | 1.039 | 15.409 | 1.4596 |
| L3T-B0908-R3 | 79 | 100.67 | 34,429 | 1.041 | 15.3955 | 1.4595 |
| L3T-B0908-R3 | 80 | 102.33 | 34,449 | 1.032 | 15.3862 | 1.4597 |
| L3T-B0908-R3 | 81 | 104 | 34,424 | 1.038 | 15.4044 | 1.4589 |
| L3T-B0908-R3 | 82 | 110.33 | 34,415 | 1.034 | 15.412 | 1.4585 |
| L3T-B0908-R3 | 83 | 113.67 | 34,415 | 1.03 | 15.3992 | 1.4587 |
| L3T-B0908-R3 | 84 | 117.33 | 34,415 | 1.032 | 15.401 | 1.4587 |
| L3T-B0908-R3 | 85 | 118.67 | 34,420 | 1.031 | 15.3924 | 1.4588 |
| L3T-B0908-R3 | 86 | 123 | 34,424 | 1.037 | 15.4001 | 1.461 |
| L3T-B0908-R3 | 87 | 126 | 34,415 | 1.04 | 15.4518 | 1.4594 |
| L3T-B0908-R3 | 88 | 127.33 | 34,424 | 1.036 | 15.4047 | 1.4602 |
| L3T-B0908-R3 | 89 | 131.67 | 34,424 | 1.031 | 15.4044 | 1.4606 |
| L3T-B0908-R3 | 90 | 133.33 | 34,420 | 1.042 | 15.4113 | 1.4606 |
| L3T-B0908-R3 | 91 | 135.33 | 34,415 | 1.031 | 15.4037 | 1.4599 |
| L3T-B0908-R3 | 92 | 140.33 | 34,415 | 1.045 | 15.3999 | 1.4605 |
| L3T-B0908-R3 | 93 | 143.33 | 34,449 | 1.042 | 15.3967 | 1.4616 |
| L3T-B0908-R3 | 94 | 146.67 | 34,424 | 1.035 | 15.4041 | 1.4595 |
| L3T-B0908-R3 | 95 | 164.67 | 34,415 | 1.034 | 15.4028 | 1.4604 |
| L3T-B0908-R3 | 96 | 169.67 | 34,415 | 1.033 | 15.4097 | 1.4605 |
| L3T-B0908-R3 | 97 | 173.33 | 34,415 | 1.036 | 15.397 | 1.4604 |
| L3T-B0908-R3 | 98 | 178.67 | 34,415 | 1.037 | 15.3973 | 1.4605 |
| L3T-B0908-R3 | 99 | 181.33 | 34,415 | 1.038 | 15.4022 | 1.46 |
| L3T-B0908-R3 | 100 | 183 | 34,415 | 1.037 | 15.3958 | 1.4607 |
| L3T-B0908-R3 | 101 | 186.67 | 34,415 | 1.039 | 15.3985 | 1.4603 |
| L3T-B0908-R3 | 102 | 197.67 | 34,415 | 1.037 | 15.4317 | 1.4614 |
| L3T-B0908-R3 | 103 | 198.33 | 34,420 | 1.037 | 15.4026 | 1.4603 |
| L3T-B0908-R3 | 104 | 199.33 | 34,415 | 1.037 | 15.3859 | 1.4611 |
| L3T-B0908-R3 | 105 | 201.67 | 34,424 | 1.036 | 15.3955 | 1.461 |
| L3T-B0908-R3 | 106 | 206.33 | 34,415 | 1.034 | 15.4203 | 1.4616 |
| L3T-B0908-R3 | 107 | 212 | 34,415 | 1.042 | 15.3916 | 1.46 |
| L3T-B0908-R3 | 108 | 229 | 34,415 | 1.037 | 15.3854 | 1.4575 |
| L3T-B0908-R3 | 109 | 230 | 34,415 | 1.033 | 15.4034 | 1.4579 |
| L3T-B0908-R3 | 110 | 231 | 34,415 | 1.036 | 15.3987 | 1.4582 |
| L3T-B0908-R3 | 111 | 234 | 34,415 | 1.044 | 15.3824 | 1.4588 |
| L3T-B0908-R3 | 112 | 236 | 34,415 | 1.043 | 15.402 | 1.4589 |
| L3T-B0908-R3 | 113 | 238.67 | 34,415 | 1.041 | 15.3851 | 1.4585 |
| L3T-B0908-R3 | 114 | 241 | 34,420 | 1.038 | 15.3873 | 1.4591 |
| L3T-B0908-R3 | 115 | 243.33 | 34,429 | 1.043 | 15.4052 | 1.4595 |
| L3T-B0908-R3 | 116 | 244.67 | 34,415 | 1.038 | 15.4138 | 1.4585 |
| L3T-B0908-R3 | 117 | 249.67 | 34,415 | 1.037 | 15.4166 | 1.4588 |
| L3T-B0908-R3 | 118 | 252 | 34,415 | 1.041 | 15.3937 | 1.4599 |
| L3T-B0908-R3 | 119 | 255 | 34,415 | 1.037 | 15.4074 | 1.4597 |
| L3T-B0908-R3 | 120 | 258 | 34,415 | 1.039 | 15.4113 | 1.4586 |
| L3T-B0908-R3 | 121 | 260 | 34,415 | 1.041 | 15.3985 | 1.4598 |
| L3T-B0908-R3 | 122 | 263 | 34,415 | 1.042 | 15.4116 | 1.459 |
| L3T-B0908-R3 | 123 | 266 | 34,415 | 1.039 | 15.4018 | 1.4605 |
| L3T-B0908-R3 | 124 | 269.67 | 34,415 | 1.041 | 15.3958 | 1.4607 |
| L3T-B0908-R3 | 125 | 273.33 | 34,415 | 1.043 | 15.3936 | 1.4602 |
| L3T-B0908-R3 | 126 | 278 | 34,415 | 1.034 | 15.4079 | 1.4603 |
| L3T-B0908-R3 | 127 | 281 | 34,420 | 1.038 | 15.3894 | 1.461 |
| L3T-B0908-R3 | 128 | 283.33 | 34,415 | 1.046 | 15.3874 | 1.4603 |
| L3T-B0908-R3 | 129 | 286 | 34,415 | 1.038 | 15.3826 | 1.461 |
| L3T-B0908-R3 | 130 | 288 | 34,415 | 1.044 | 15.4054 | 1.461 |
| L3T-B0908-R3 | 131 | 290.33 | 34,415 | 1.046 | 15.3856 | 1.4598 |
| L3T-B0908-R3 | 132 | 293 | 34,415 | 1.04 | 15.3932 | 1.4616 |
| L3T-B0908-R3 | 133 | 295.67 | 34,415 | 1.043 | 15.3744 | 1.4611 |
| L3T-B0908-R3 | 134 | 299.67 | 34,415 | 1.046 | 15.3831 | 1.4607 |
| L3T-B0908-R3 | 135 | 304 | 34,415 | 1.038 | 15.3708 | 1.4614 |
| L3T-B0908-R3 | 136 | 306.67 | 34,415 | 1.044 | 15.3832 | 1.4614 |
| L3T-B0908-R3 | 137 | 310.33 | 34,415 | 1.041 | 15.3819 | 1.4604 |
| L3T-B0908-R3 | 138 | 313.67 | 34,415 | 1.043 | 15.3972 | 1.4612 |
| L3T-B0908-R3 | 139 | 315.67 | 34,415 | 1.042 | 15.4257 | 1.4605 |
| L3T-B0908-R3 | 140 | 318 | 34,415 | 1.044 | 15.4289 | 1.4606 |
| L3T-B0908-R3 | 141 | 320.33 | 34,415 | 1.041 | 15.4092 | 1.4617 |
| L3T-B0908-R3 | 142 | 321.67 | 34,415 | 1.044 | 15.3948 | 1.4616 |
| L3T-B0908-R3 |  | avg. = | 34,435 | 1.0365 | 15.3918 | 1.4610 |
| Gage End | 143 | 321.67 | 34,429 | 0.005 | 16.0694 | 1.5121 |
| Gage End | 144 | 321.67 | 34,415 | 0.005 | 16.0694 | 1.5123 |
| Gage End | 145 | 321.67 | 34,458 | 0.005 | 16.0694 | 1.512 |
| Gage End | 146 | 321.67 | 34,463 | 0.005 | 16.0696 | 1.5123 |