96E09/22/06

S551-96E.doc

Include the following when driven piles are specified.

Section 551. - DRIVEN PILES

551.03  Pile Driving Equipment

(a) Pile Hammers

(5) Nonimpact hammers.  Delete the first sentence and substitute the following:

Use nonimpact hammers, such as vibratory hammers, only when permitted in writing or when specified in the contract.

Add the following:

(6) Hydraulic hammers.  Provide a power plant for hydraulic hammers with sufficient capacity to maintain the volume and pressure, specified by the manufacturer, at the hammer under working conditions.  Equip the power plant and equipment with accurate pressure gauges that are easily accessible to the CO.

(b) Approval of pile driving equipment.  Delete the second and third paragraphs and substitute the following:

Approval of pile driving equipment will be based on a wave equation analysis unless the contract specifies the dynamic formula to determine the ultimate driven pile capacity.  If the contract specifies the dynamic formula, approval of pile driving equipment will be based on minimum hammer energy in Table 551-1.  The CO will evaluate the proposed equipment and accept or reject the driving system within 14 calendar days of receipt of the pile and driving equipment information.

Use only the approved equipment during pile driving operations. Approval of the pile driving system is specific to the equipment submitted.  If the proposed equipment is modified or replaced, re-evaluate and resubmit the analysis and revised data for approval before using.  The CO will accept or reject the revised driving system within 14 days of receipt of the revised submittal.  Approval of a pile hammer does not relieve the Contractor of responsibility for piles damaged due to driving stress.

(1) Equipment submittal.  Delete the first paragraph and substitute the following:

Submit the following pile driving equipment information to the CO at least 30 days before driving piles.  Include a wave equation analysis for the proposed pile driving system, unless the contract specifies the use of the dynamic formula to determine the ultimate driven pile capacity.  Use a professional engineer with at least 3 years experience in wave equation analyses to perform the wave equation analysis.  Submit a resume of the engineer for approval.

Include subsection 551.03(b)(2) if wave equation analysis is required.

(2) Wave equation.  Delete the first paragraph and substitute the following:

The required number of hammer blows indicated by the wave equation at the ultimate pile capacity shall be between 3 and 10 per inch.

Use the following hammer efficiencies in the wave equation analysis unless more specific hammer efficiency information is available:

| Hammer Type | Efficiency in Percent |
| --- | --- |
| Single acting air/steam | 67 |
| Double acting air/steam | 50 |
| Diesel | 72 |

In addition, the pile stresses resulting from the wave equation analysis shall not exceed the values at which pile damage is impending.  The point of impending damage is defined for steel, concrete, and timber piles as follows.

(b) Concrete piles.  Delete the subparagraph and substitute the following:

Limit the tensile (TS) and compressive (CS) driving stresses to:

TS ≤ 0.25fc' 1/2 + EPV

CS ≤ 0.85fc' - EPV

Where:

fc' = The 28-day design compressive strength of the concrete in pounds.

EPV = The effective prestress value in pounds.

(c) Driving appurtenances.  Add the following:

(6) Pile cushion.

For concrete piles, use a new pile cushion to protect the head of each pile.  Cut the pile cushion at least 4 inches thick and to match the cross-section of the pile top.  Replace the pile cushion if it is compressed more than one-half its original thickness or it begins to burn.  For steel and timber piles, protect each pile with an approved driving cap.  Enclose timber piles with approved collars or bands to prevent splitting or brooming.  Replace caps when damaged.  Do not reuse cushions or caps.

(7) Pile shoes.  When specified, provide shoes to protect the pile-tip from damage during driving.  Fabricate all shoes to snugly fit the pile tip.  For concrete piles, attach the shoe to the pile using dowels or other approved methods.  For steel piles, design and fit the shoe to the steel shape and weld the shoe to the pile so as not to stress the web or the flange.  For timber piles, carefully shape the tip to secure an even uniform bearing for the pile shoe.  Treat all holes, cuts, or caps in treated timber piles with 2-brush applications of creosote-coal tar solution.

551.06  Driven Pile Capacity.  Delete the second paragraph and substitute the following:

Use the wave equation to determine ultimate pile capacity of the in-place pile.

Include subsection 551.07 when pre-boring is approved for the project

551.07 Preboring.  Delete the first and second paragraphs and substitute the following:

Use auguring, wet rotary drilling, or other approved methods of preboring.

In compacted embankments more than 5 feet deep, prebore the pile hole to natural ground.  Prebore holes 6 inches greater than the diameter of the pile.  For square, rectangular or H piles, make the diameter of the hole equal to the diagonal of the pile cross-section plus 6 inches.

For piles end-bearing on rock or hardpan, preboring may extend to the surface of the rock or hardpan.  Seat the pile into the end-bearing strata.

For piles not end-bearing on rock or hardpan, stop preboring at least 5 feet above the estimated pile tip elevation and drive the pile with an impact hammer to a penetration which achieves the required ultimate pile capacity.  Prebore holes smaller than the diameter or diagonal of the pile cross-section while allowing penetration of the pile to the specified depth.

If subsurface obstructions such as boulders or rock layers are encountered, the hole diameter may be increased to the least dimension adequate for pile installation.  Fill any void space remaining around the pile after completion of driving with sand or other approved material.  Do not use a punch or a spud in lieu of preboring.

Include subsection 551.08 when driven piles are specified.

551.08  Preparation and Driving.  Delete the first and second paragraphs and substitute the following:

Perform the work under Section 208. Make the heads of all piles plane and perpendicular to the longitudinal axis of the pile. Coordinate pile driving to prevent damage to other parts of the completed work.

Drive piles to within 3 inches of plan location at cutoff elevation.  Drive piles no closer than 6 inches from any cap face.  Drive piles so that the axial alignment is within ¼ inch per foot, along the longitudinal axis, of the required alignment.  The CO may stop driving to check the pile alignment.  Check alignment of piles that cannot be internally inspected after installation before the last 5 feet are driven.  Do not pull laterally on piles or splice to correct misalignment.  Do not splice a properly aligned section on a misaligned pile.

Include subsection 551.08(a) when timber piles are specified.

551.08  Preparation and Driving.

(a) Timber piles.  Delete the second paragraph.

Include subsection 551.08(c) when precasted or prestressed concrete piles are specified.

551.08  Preparation and Driving.

(c) Precast and prestressed concrete piles.  Delete the second and third paragraphs and substitute the following:

Reject concrete piles with reduced strength caused by external defects such as spalls or cracks or internal defects such as cavities revealed with non-destructive testing.

Include subsection 551.09(b) when pile splices are approved for concrete piles.

551.09  Splices.

(b) Concrete pile splices.  Delete the text and substitute the following:

Use dowels or other acceptable mechanical means to splice precast concrete or precast prestressed concrete piles.  Submit drawings of proposed splices for acceptance.

If dowels are used, cast the dowels into the tip end of the following pile with corresponding holes at the butt end of the driven pile.  Serrate the holes to provide a mechanical bond.  Separate the ends of the piles by at least ½ inch.  Clean all surfaces and dowel holes.  Grout the dowels in place and allow the grout to cure.  Enclose the gap with forms and inject a bonding agent capable of withstanding the impact and driving forces and having the same compressive strength as the pile.  Follow the manufacturer's recommendations regarding the use and curing of grouting and bonding products.

Attach manufactured splices to the concrete piles as recommended by the manufacturer.  The splice shall develop strengths in compression, tension, and bending equal to or exceeding the strength of the pile being spliced.

Include subsection 551.11(a) when driven piles are specified.

551.11  Pile Load Tests.

(a) Dynamic load test.  Delete the second and fifth paragraphs.

Include subsection 551.12(a) when driven piles are specified.

551.12  Pile Cutoffs.

(a) Steel piles.  Delete the fourth and fifth sentences and substitute the following:

Paint piles before driving.  Use one prime coat and 2 finish coats on trestles or other exposed piling to at least 3 feet below the finished groundline or waterline.