$$563.00A

Section 563. – PAINTING

Revised 18 January 2006

$$563.03A

563.03.  Add the following:

SSPC Painting Contractor Certification Program (PCCP) Requirements.   All contractors and subcontractors that perform surface preparation, paint application, and any related work involving containment and collection of surface preparation debris, disposal of surface preparation debris, and a worker health protection program (including decontamination facilities) shall be certified by the Society for Protective Coatings (formerly Steel Structures Painting Council (SSPC)) to the requirements of SSPC-QP 1.  In addition, all contractors and subcontractors engaged in lead paint removal and any other related work shall be certified by the SSPC to the requirements of SSPC-QP 2.  Contractors and subcontractors shall be certified at time of bid, must remain certified for the respective work for the duration of the project and submit documentation of certification at time of bid.  If a contractor’s certification expires, the company will not be allowed to perform any work until the certification is reissued.  Requests for extension of time for any delay to the completion of the project due to inactive certification will not be considered and liquidated damages will apply.  Notify the CO of any change in contractor certification status.