UNITED STATES DEPARTMENT OF AGRICULTURE

NATURAL RESOURCES CONSERVATION SERVICE

OREGON

MATERIAL SPECIFICATION

MS-217 WOOD PRESERVATIVES AND TREATMENT

1.	SCOPE

This specification governs the quality of wood preservatives and methods of treatment of wood products.

2.	TREATING PRACTICES

Treating practices, penetration, retention, sampling, inspection and test procedures shall conform to the requirements of Federal Specification TT-W-571, “Wood Preservation:  Treating Practices.”

3.	PRESERVATIVES

The wood shall be treated with the specified type of preservative.  Wood preservatives shall conform to the requirements of the applicable specifications listed in Federal Specification TT-W-571.  Creosote and pentachlorophenol are classified as hazardous materials and shall not be used.

4.	QUALITY OF TREATED MATERIALS

Treated lumber, timber, piles, poles, or posts shall be free from heat checks, water bursts, excessive checking, results of chafing or from any other damage or defects that would impair their usefulness or durability.  Holes bored for tests shall be filled with tight fitting treated plugs.

5.	MARKING

Each treated wood item delivered to the job site shall be marked as specified in Federal Specification TT-W-571.