$$607.00A

Section 607.—CLEANING, RECONDITIONING, AND REPAIRING EXISTING DRAINAGE STRUCTURES

Revised 8 May 2005

# INCLUDE THE FOLLOWING FOR PIPE LINERS

$$607.01A

607.01.  Add the following:

This work includes of lining existing culverts.

# INCLUDE THE FOLLOWING FOR PIPE LINER MATERIALS

$$607.01B

607.01.  Add the following after Subsection 607.01:

607.01A.  Materials.  Conform to the following Sections and Subsections:

INCLUDE THE FOLLOWING FOR CEMENT MORTAR PIPE LINERS

$$607.01C

Portland cement	701.01

Water	725.01

# INCLUDE THE FOLLOWING FOR POLYURETHANE PIPE LINERS

$$607.01D

Furnish a polyurethane pipe liner conforming to:

###### INSERT THE SPECIFICATIONS FOR THE PIPE LINER

INCLUDE THE FOLLOWING FOR CEMENT MORTAR PIPE LINERS

$$607.01E

Furnish a cement mortar pipe lining conforming to AWWA C 602.

Furnish sand meeting the following gradation:

| Sieve Sizes | Percentage Passing |
| --- | --- |
|  | 14 (1.18 mm) | 100 |
|  | 20 (850 m) | 95-100 |
|  | 30 (600 m) | 85-95 |
|  | 40 (300 m) | 15-35 |
|  | 100 (150 m) | 1.5-5 |
|  | 200 (75 m) | 1-3 |
|  | 37.5µm | 0 |

$$607.02A

607.02.  Add the following:

The dry components of the cement mortar shall be 50 percent sand and 50 percent portland cement by weight.

After addition of the water, provide a mortar that is well mixed and will provide a dense, homogeneous lining that will hold firmly against the pipe surface.  Carefully control and keep the water-cement ratio to a minimum.  Allow for any existing moisture on the walls of the pipe.  Premix the mortar by machine for a sufficient length of time to obtain maximum plasticity, or 3 minutes minimum.

# INCLUDE THE FOLLOWING WHEN WATER IS BEING USED

$$607.02B

607.02.  Add the following:

Provide for the control and disposal of any accumulation of water that interferes with construction.

# INCLUDE THE FOLLOWING FOR PIPE LINERS

$$607.06A

607.06.  Add the following after Subsection 607.06:

607.06A.  Pipe Lining.  Remove and dispose all silt, sand, debris, detritus, or other sedimentation or foreign material from within pipe to be lined, and from inlet and outlet areas.  Remove all dirt, rust, tubercles, scale, loose or deteriorated remnants of old lining materials, accumulated water, and all other foreign materials from the interior surface of the pipe before lining.  After cleaning, the interior of the pipe shall present a surface free of all foreign material except nondeteriorated original coating.

Install pipe lining according to the manufacturer's recommendations.  Hand-place cement mortar lining only at sharp bends and special locations where machine placing is impracticable.

Patch holes in the existing pipe with cement mortar before the application of the lining.

Pave existing culvert inverts with cement mortar if they are deteriorated to the extent that an acceptable lining would not be achieved before centrifugal application of linings.  Fill cavities beneath badly deteriorated inverts with concrete, grout, or other method acceptable to the CO.

Close the pipe at both ends to prevent the circulation of air.  After the final pass with the machine, introduce water into the closed section to create a moist atmosphere and keep the lining damp.  Maintain curing for a minimum of 3 calendar days.

$$607.07A

607.07.  Add the following:

Lining materials will be evaluated under Subsection 106.03.  Lining construction will be evaluated under Subsection 106.04.  After curing, drill holes (1 per 50 feet (15 meters)) to verify lining thickness at random locations selected by the CO.  Patch the hole after thickness verification.