$$609.00A

Section 609.—CURB AND GUTTER

Revised 8 May 2005

# INCLUDE THE FOLLOWING FOR GRANITE BRIDGE CURB

$$609.02A

609.02.  Add the following:

Granite bridge curb					620.01(a)

Masonry anchors for bridge curb			717.18

INCLUDE THE FOLLOWING FOR STONE CURB ON DC PROJECTS

$$609.03A

609.03.  Add the following:

Furnish an air-entrained, portland cement concrete dry mix of 1 part cement, 2 parts sand, and 4 parts crushed stone, with just enough water added to the mix to make the mix adhesive.

$$609.04A

609.04.  Delete the second sentence of the first paragraph and substitute the following:

Set stone curb in dry-pack concrete so the curb face and top, are to line and grade.

INCLUDE THE FOLLOWING FOR GRANITE BRIDGE CURB

$$609.04B

609.04.  Add the following after Subsection 609.04:

609.04A.  Granite bridge curb.  On bridges, after the concrete base has set and before the concrete in back of the curb is placed, set the granite bridge curb to line and grade in full mortar beds and full mortar end joints with the anchors in the stone grouted in place.

Grout 2 0.5-inch (1.25-centimeter) diameter, stainless steel anchors into the back of each stone curb.  Pitch the anchor holes downward at approximately 45 degrees, and locate approximately 3 inches (7.5 centimeters) below the top and 12 inches (30 centimeters) from each end.  Furnish anchors with a 3-inch  (7.5-centimeter) square hook on one end and a 3–inch (7.5-centimeter) 45 degree bend on the other end, both pointing downward and separated by a minimum 6-inch (15-centimeter) straight shank.

Brush each stone curb clean and free from loose particles, and thoroughly wetted with clean water before setting.  Carefully lay the stone in a full bed of mortar.  Do not slide the stone on the mortar bed.  Set the curb with full mortar joints and leave all joints smooth and flush.  Hold each stone securely in position by 2 steel anchors.  Carefully place the concrete in back of the curb to avoid disturbing the line or grade of the curb.  Keep exposed faces of the curb free of mortar and cement stains.  Joints in granite bridge curb shall be raked out to a depth of 0.5 inches (1.25 centimeters) and sealed flush with the sealing material.

If a construction joint is required in the curb or sidewalk over a pier or bent, lay out the curb so that a joint in the curb will be opposite the joint in the sidewalk.