96M09/22/06

S609-96M.doc

Use on projects as appropriate.

Section 609. – CURB AND GUTTER

Description

609.01  Add the following:

This work also consists of constructing paved ditches contiguous to the traveled way.

Construction Requirements

609.03  General.  Add the following:

For asphalt paved ditches, form the bed parallel to the finished surface of the ditch.

When gluing concrete curb to asphalt pavement, insert 609.03.

609.03  General.  Add the following:

When bonding concrete curb to existing asphalt pavement thoroughly clean the pavement surface in advance of placing the curb.  Abrade and/or high pressure water wash the existing asphalt pavement to assure removal of all dust and loose material.

Bond the extruded curb or precast curb to the existing asphalt pavement using an approved concrete to asphalt adhesive or a two-component epoxy, designed to bond fresh concrete to the existing pavement.  Submit proposed adhesive for approval by the CO prior to use.  Apply according to the manufacturer’s recommendations.

Add the following Subsection:

609.08A  Asphalt Paved Ditch.  Perform the work according to Section 402.  Before overlaying existing asphalt paved ditches, clean and seal the cracks according to Section 414.  Compact according to Subsection 402.07(a).  Compact according to Subsection 402.07(b), only if paved ditch cannot be rolled safely.

Measurement

Use on all projects with curbing and/or ditches.

609.10  Add the following:

No separate measurement will be made for the asphalt mixture included in asphalt curb or paved ditch.

Measure paved ditches by the square meter width horizontally to include total width.

Measure curb by the linear meter.

Payment

Use on projects with asphalt paved ditches.

609.11  Add the following:

Pay Item	Pay Unit

60915B	Asphalt paved ditch	Square meter