96E03/29/06

S620-96E.doc

Include the following when stone masonry is specified.

Section 620. - STONE MASONRY

620.02.  Delete the reference to Mortar and substitute the following:

Mortar	712.05(a)

620.04  Placing Stone.  Delete the first paragraph and substitute the following:

Place stone to provide a uniform pattern and color.  Do not place stone masonry when the ambient temperature is below 32(F.  Maintain completed masonry at a temperature above 40(F for 24 hours after construction.  Clean all stones thoroughly and moisten immediately before placing.  Clean and moisten the bed.

Add the following after the first paragraph:

When removing and resetting stone masonry, use hand tools to clean the exposed faces of the stones of all mortar before resetting.