SPEC-SHEET RATINGS

From Manufacturers’ Websites

Compiled by Bolko von Roedern

June 2007

| Ranked Module Efficiency (%) | Description of best module | Same module with lowest power rating |
| --- | --- | --- |
| 17.7 (non-stan) | SunPower SPR220 (SunPower rear-point contacted cells, single crystal FZ) Tcoeff = -0.38 %/C, VOC/cell = 671 mV | Also SPR 200, efficiency 16.3% |
| 17.0 (non-stan) | Sanyo HIP-200BE3 (single crystal CZ Si, HIT (Tcoeff = -0.30 %/C), VOC/cell = 716 mV | Also HIP-180B3, efficiency 15.3% |
| 15.1 (non-stan) | BP7190 (single crystal laser grooved buried grid cells, CZ-Si, Spain) Tcoeff= -(0.5±0.05) %/C, VOC/cell = 622 mV | Also BP 7170, efficiency 13.5% |
| 14.2 (multi) | Kyocera KC200GT (cast multi-Si diffused cells) Tcoeff.(only given for Voc, -0.123 V/C), VOC/cell = 609 mV | Only one rating listed |
| 14.2 (mono) | Solar World AG SW 185 (mono-Si “Shell”) Tcoeff.: VOC= -0.35%/C, VOC/cell = 622 mV | Also SW 160, efficiency 12.3% |
| 13.9 (multi) | BP 175B ("Solarex" multi-Si diffused Cells) Tcoeff= -(0.5±0.05) %/C, VOC/cell = 614 mV | Also BP 160B, efficiency 12.7% |
| 13.8 (mono) | Sharp NT-180-U1 (mono-Si, diffused) no Tcoeff given, VOC/cell = 622 mV | Only one rating listed |
| 13.7 (non-stan) | Advent Solar Advent 180 (emitter wrap thru multi-Si) Tcoeff= -0.48%/C, VOC/cell = 599 mV | Also Advent 160, efficiency 12.2% |
| 13.7 (multi) | GE GEPVp-200-M (multi-Si) Tcoeff= -0.5%/C (max.), VOC/cell = 609 mV | Also GEPVp 185-M, efficiency 12.7% |
| 13.4 (multi) | SunTech STP 260S-24V/b (cast multi-Si diffused cells) VOC/cell = 608 mV | Same module with mono-Si cells is also 260 W |
| 13.4 (multi) | Solar World AG SW 225 (multi-Si) Tcoeff.: VOC= -0.33V/C, VOC/cell = 613 mV | Also SW 200, efficiency 11.9% |
| 12.8 (multi) | Sharp ND-208-U1 (multi-Si, diffused) no Tcoeff given , VOC/cell = 605 mV | Also ND-200-U1, efficiency 12.3% |
| 12.7 (ribbon) | Evergreen Solar ES 190-RL (string ribbon Si) Tcoeff= -0.49%/C, VOC/cell = 607 mV | Also ES-170-RL, efficiency 11.4% |
| 11.0 (CIS) | WürthSolar WS11007/80 (CIS) Tcoeff.= -0.36 %/C | Also WS 11007/75, efficiency 10.3% (20-year warranty) |
| 9.4 (CdTe) | First Solar FS-267 (CdTe) Tcoeff= -0.25 %/C | Also FS-260, efficiency 8.3 % (25-year warranty) |
| 8.5 (a-Si/nc-Si) | Sharp NA-901-WP (90-W) (amorphous/nanocrystalline Si tandem) | Only one rating listed but +/- 10% power spec |
| 8.1 (CIGS) | GSE Soar GSE 120-W Tcoeff=-0.5%/C | Only one rating, but +/-!5% power spec |
| 6.3 (a-Si 1-j) | Mitsubishi Heavy MA100 T2 (single j. a-Si, VHF deposition), Tcoeff.= -0.2 %/C | Only one rating (20-year warranty) |
| 6.3 (a-Si 3-j) | Uni-Solar PVL 136 (triple-j. amorphous silicon roofing laminate), Tcoeff = -0.26% | Also as 124 W, eff. 5.7% (20-year warranty) |
| 6.3 (a-Si 1-j) | Kaneka T-SC(EC)-120 (single-j. a-Si) No Tcoeff. given | Only one rating (25-year warranty) |
| 5.3 (a-Si/a-Si) | Schott Solar ASI-F 32/12 (same-bandgap double junction a-Si) Tcoeff = - 0.20%/C | Only one rating (20-year warranty) |
| 5.3 (a-Si/a-Si) | EPV EPV-42 (same-bandgap double junction a-Si) Tcoeff = - 0.19%/C | Also as EPV-40, eff. = 5.1% (20-year warranty) |
| 4.9 (a-Si 1-j) | Soltech PVS 60-24 (single-j amorphous Si |  |