| f | Fermi National Accelerator Laboratory Batavia, IL 60510 |
| --- | --- |
| LQF 5 TURN QUADRANT 1/3 COIL WINDING TRAVELER |
| Reference Drawing(s) 5 Turn ME-351095 |
| Budget Code: FGA | Project Code: CCW |
| Released by: | Date: |
| Prepared by: R. Safarik |
| Title | Signature | Date |
| TD / E&F Process Engineering |  |  |
| TD / E&F Assembly |  |  |
| TD / E&F Tooling |  |  |
| TD / E&F Fabrication Manager |  |  |
| TD / E&F Device Design |  |  |
| TD / QA/QC Manager |  |  |
| TD / E&F Department Head |  |  |

Revision Page

| Revision | Revision Description | Date |
| --- | --- | --- |
| A | Major re-write due to first edition changes. TRR No. 0640 | 4/4/97 |
| B | Changed Budget Code to ‘FGA’ on cover page. Corrected text in Step(s) 6.4 to read ‘five turn’. Inserted Step(s) 5.10 to indicate location of possible conductor joint. TRR No. 0696 | 8/15/97 |

Ensure appropriate memos and specific instructions are placed with the traveler before issuing the sub traveler binder to production.

1.0	General Notes

1.1	White (Lint Free) Gloves (Fermi stock 2250-1800) or Surgical Latex Gloves

(Fermi stock 2250-2494) shall be worn by all personnel when handling all product parts after the 			parts have been prepared/cleaned.

1.2	All steps that require a sign-off shall include the Technician/Inspectors first initial and full last name.

1.3	No erasures or white out will be permitted to any documentation.  All incorrectly entered data shall be corrected by placing a single line through the error, initial and date the error before adding the correct data.

1.4	All Discrepancy Reports issued shall be recorded in the left margin next to the applicable step.

1.5 	All personnel performing steps in this traveler must have documented training for this traveler and associated operating procedures.

1.6	Personnel shall perform all tasks in accordance with current applicable ES&H guidelines and those specified within the step.

1.7	Cover the LQF Coils with green Herculite (Fermi stock 1740-0100) when not being serviced or assembled.  Completed coils are to be stored in the LQF Coil Storage Area.

2.0	Parts Kit List

2.1	Attach the completed Parts Kit List for the LQF 5 Turn Coil Winding to this traveler.  Ensure that the serial number on the Parts Kit List matches the serial number of this traveler.  Verify that the Parts Kit received is complete.

Process Engineering/Designee				Date

[This Page Intentionally Left Blank]

3.0	Coil Winding Table Setup Procedure

3.1	Set up the winding fixture as indicated in below for the coil which is about to be wound.  Attach the Outside End Plate (Return End MD-185811) to the winding fixture.  All coil contacting surfaces of the fixture must be cleaned with KPC 820N (Fermi stock 1920-0700) and Heavy Disposable Wipers (Fermi stock 1660-2600) or equivalent

| LQF Coil Winding Fixture |
| --- |
| Turns | Quadrant | Print Number | Fixture Number | Init. |
| 5 | 1 / 3 | ME-351095 | ME-135575 |  |

Technician(s)						Date

X	3.2	Using a Steel Measuring Tape (Starrett Cat. No. W530F-50 or equivalent) verify the length of the winding mandrel from the two outer most sides of the fixture.  The nominal length is indicated in the table below.  Complete the table.

| LQF Coil Winding Fixture |
| --- |
| Turns | Quadrant | Print Number | Fixture Number | Fixture Length | Length |
| 5 | 1 / 3 | ME-351095 | ME-135575 | 38.182" |  |

Lead Person						Date

3.3	Set the adjustable tensioning arm on the spindle to the half way point.  Position the winding fixture so that the transition is facing the tensioning arm.  Turn the fixture so that the transition Step is vertical to the winding table.  (See diagram below).

Pictures for Reference only.

Technician(s)						Date

[This Page Intentionally Left Blank]

4.0	Conductor Prep

X	4.1	Perform a BB Inspection of the conductor cooling passage with a .344" diameter ball bearing.  Cover the exit hole on the reel of conductor with a rag or slide a glove over the end of the conductor to catch the ball bearings.  Use minimum required air pressure (1 to 10 psi.) to test the reel of conductor.

Reel # 1	Pass		Fail	

Note(s):

If the BB Inspection fails notify supervisor.

Lead Person						Date

4.2	After clamping the conductor to the winding fixture, anneal sufficient conductor to complete the first 90° Bend BEFORE winding.  Flame anneal at a temperature of 800° F to 1200° F.  Monitor the conductor temperature using Temperature Crayons (McMaster-Carr Part Numbers 3261K91 (800° F), (1000° F), (1200° F) or equivalent).

Note(s):

The conductor should be clamped to the fixture in a manner such that the joint will NOT be closer than 6” from any bend.

Technician(s)						Date

4.3	Engage the adjustable tensioning arm, backing it away from the fixture, increase the pressure on the Phenolic block until the gage reads 1000 lbs. force ± 100 lbs. not to exceed 1100 lbs. force. and stop the tensioning arm.

Technician(s)						Date

5.0	5 Turn Winding

Note(s):

For all subsequent operations of the winding table refer to the Large Turn Table (Winding Table) Operation Procedure (5525-OP-318944).

At no time is a hammer to be used directly against the conductor.

At no time is a hammer to be used directly against the conductor.  The 			following materials are acceptable wood or nylon.

Ensure that no twist has occurred in the conductor between the reel and 			the Phenolic guide block.

5.1	Engage the winding table in the clockwise direction for 90°, use minimum hammer force necessary to form the turn to the fixture and avoid conductor damage.  Monitor the clamping cylinder pressure so that the load cell gauge reads 1000 lbs. force ± 100 lbs.  Maximum pressure should not exceed 1100 lbs force.  Adjust the pressure to the clamping cylinder as necessary.

Technician(s)						Date

5.2	Energize the Tilt-Top and rotate the winding fixture 90° forming the conductor to the fixture.  Winding through the transition down on to the two (2) turn layer section of the winding fixture.  Maintain tension with the adjustable tensioning arm on the tensioning device.  Clamp the conductor to the winding fixture using Clamps (MC-185804/MC-185805) as required.  Attach the Outside End Plate (MD-185808) to the lead end over the conductor.

Technician(s)						Date

5.3	Adjust the pressure valve to maintain the tensioner clamping cylinder at 1500 lbs. force ± 100 lbs. as winding continues for the next 180°, then stop.  Ensure that the maximum readings do not exceed 1600 lbs. force.  Use minimum hammer force necessary to form the turn and avoid conductor damage.  Restrain the conductor to the end plate as necessary by using Clamps (MC-185804 / MC-185805).

Technician(s)						Date

X	5.4	Verify that the tension of the conductor load cell gauge reads 1500 lbs. force ± 100 lbs measured during the continued winding table rotation.  Ensure that the maximum readings do not exceed 1600 lbs force.

Record Actual Tension					Pass		Fail	

Lead Person						Date

X	5.5	Perform a Height and Width Dimension Check of the conductor half-way between the tensioner and the winding fixture before winding the coil.

| Dimension | Limit | Actual Measurement | Pass | Fail | Out of Tolerance |
| --- | --- | --- | --- | --- | --- |
| Height | 1.485” to 1.505” |  |  |  |  |
| Width | .615” to .630” |  |  |  |  |

Lead Person						Date

5.6	Energize the Tilt-Top and form the conductor to the fixture as it rotates 90°.  Use minimum hammer force necessary to form the turn and avoid conductor damage.

Technician(s)						Date

5.7	Rotate the winding table clockwise 180°, forming the conductor to the winding fixture as it rotates.  Use minimum hammer force necessary to form the turn and avoid conductor damage, clamping the conductor to the winding fixture using the Clamps (MC-185804/MC-185805) as required.

Technician(s)						Date

5.8	Cut a .0299" shim (MA-xxxxxx) to a length fitting the saddle section of the coil.  Position the shim between the turns as the Tilt-Top rotates 90°, form the conductor to the fixture as it rotates.  Use minimum hammer force necessary to form the turn and avoid conductor damage.

Technician(s)						Date

5.9	Cut a .0299" shim (MA-xxxxxx) to a length of 25".  Position the shim along the straight section of the coil between the turns as the winding table rotates clockwise 180°, forming the conductor to the winding fixture as it rotates.  Use minimum hammer force necessary to form the turn and avoid conductor damage, clamping the conductor as required to the winding fixture using Clamps (MC-185804/MC-185805).

Note(s):

At no time are there to be shims placed at the one inch radius from the saddles to the straight sections or straight sections to the saddles.  The shims from the straight sections and the saddles shall not protrude out (into the one inch radius area) from the conductor in such a way as to effect the winding of the two turn layer.

At NO TIME during the winding process is the conductor to be pulled

free of the tensioning device.

Technician(s)						Date

5.10	Using the following picture, mark the location of any conductor splices.

Distance from lead end: 			 	Turn count:

Technician(s)						Date

5.11	Repeat steps 5.8 through 5.9 until five (5) turns may be counted on both sides (straight sections) of the winding fixture.

Technician(s)						Date

6.0	Lead Bending Procedure

X	6.1	Verify that all 5 turns are wound, that no twist is in the conductor and that the shims are installed between the turns and the saddles.  Ensure that none of the shims extend into the transition between the straight sections to the saddles interfering with the six turn layer.

Lead Person						Date

6.2	Rotate the winding table clockwise 90°, forming the conductor to the winding fixture as it rotates.  Use minimum hammer force necessary to form the turn and avoid conductor damage, clamping the conductor to the winding fixture using a c-clamps as required.  Attach The Bend Attachment (MC-185784) to the winding fixture.

Technician(s)						Date

6.3	Clamp the conductor presently going to the tensioner to the winding fixture.  Mark the lead to be cut beyond the winding fixture.  Release the tensioning device.

Technician(s)						Date

XX	6.4	Verify that the fixture is of the correct configuration to bend the five turn layer lead.  Verify that the lead is marked long enough to allow the lead to be bent by hand, ensuring that once the lead is bent, there is a sufficient amount of material remaining to scribe the lead as indicated by the bending fixture.

Lead Person						Date

Crew Chief						Date

6.5	Cut the leads beyond the end of the fixture, using a portable band saw or equivalent.

Technician(s)						Date

6.6	Anneal the conductor BEFORE completing the Lead Bending.  Flame anneal at a temperature of 800° F to 1200° F.  Monitor the conductor temperature using Temperature Crayons (McMaster-Carr Part Numbers 3261K91 (800° F), (1000° F), (1200° F) or equivalent).

Technician(s)						Date

6.7	Bend the conductor to conform to the bending fixture attachments.  Use minimum hammer force necessary to form the turn and avoid conductor damage.  Scribe the lead as indicated by the bending 	fixture attachment.

Technician(s)						Date

X	6.8	Verify that the conductor lead conforms to the bending fixture attachments and the leads have been

scribed as indicated by the bending fixture attachments.

Lead Person						Date

6.9	Using a hand drill and vise or equivalent with a 1/2" drill bit, clamp the leads into the vise and counter bore the leads to a depth of 3/8".

Note(s):

When drilling, DO NOT drill through the side of the conductor.

Technician(s)						Date

6.10	Position two (2) pieces into the counter bored holes, one (1) per lead of 1/2" x .032" x 3" Soft Copper Tubing (Fermi stock 1065-0075) or equivalent.  Heat the copper conductor with a torch until the area surrounding the joint is cherry red.  Apply Sil-Fos # 15 (MA-116256) at the joint.  Feed the Sil-Fos #15 into the joint and move the torch around the joint to produce 100% Sil-Fos #15 flow and a uniform braze.  Refer to the General Brazing Specification (ES-318973).

Note(s):

CAUTION, material and areas being heated represent a burn hazard.

Do not over heat the material causing the copper to flow.

Do not use water to cool the joint.  Allow all brazed joint to air cool.

Allow the joints to cool to below 100° F before proceeding to the next step.

Technician(s)						Date

6.11	Remove all c-clamps/clamping fixtures.  Remove the bolts from both the inside and outside end plates located at the return and lead end of the winding fixture.

Note(s):

When disassembling the winding fixture use extreme caution so as not to damage the wound coil.

Technician(s)						Date

X	6.12	Ensure that there are no further obstructions that may interfere with the removal of the wound coil from the winding fixture.

Lead Person						Date

6.13	Remove the coil from the winding fixture.  Install Tie-Wraps (MX-XXXXXX) to retain coil shape.  Transport the wound coil to the coil staging area using a coil transport cart and cover the coil with green Herculite (Fermi stock 1740-0100) .

Technician(s)						Date

[This Page Intentionally Left Blank]

7.0	Production Complete

XXX	7.1	Process Engineering verify that the LQF 5 Turn Coil Winding Traveler (5520-TR-333197) is accurate and complete.  This shall include a review of all steps to ensure that all operations have been completed and signed off.  Ensure that all Discrepancy Reports, Reports, Repair/Rework Forms, Deviation Index and dispositions have been reviewed by the Responsible Authority for conformance before being approved.

Comments:

Process Engineering/Designee				Date

XXX	7.2	Assembly verify that the LQF 5 Turn Coil Winding Traveler (5520-TR-333197) is accurate and complete.  This shall include a review of all steps to ensure that all operations have been completed and signed off.  Ensure that all Discrepancy Reports, Nonconformance Reports,Repair/Rework Forms, Deviation Index and dispositions have been reviewed by the Responsible	 Authority for conformance before being approved.

Comments:

Assembly/Designee					Date

8.0	Attach the Process Engineering "Okay to Proceed" Tag to the coil.

Process Engineering/Designee				Date

9.0	Proceed to the next major assembly operation -  LQF 5 Turn Coil Prep Traveler (5520-TR-333209).