96E03/29/06

S701-96E.doc

Use when shotcrete is required, include Section 566, 703.18 and the following. If colored shotcrete is required, include 711.05.

Section 701. - HYDRAULIC CEMENT

701.01 Portland Cement and Masonry Cement.  Add the following:

For shotcrete, use one of the following:

(a) Low alkali Portland cement.  Conform to AASHTO M 85, limiting alkalies according to Table 1A in AASHTO M 85.

(b) Blended hydraulic cement.  Use AASHTO M 240, type 1S, 1S-A, 1P, or 1P-A cement.

When the quality improvements for hydraulic cement are adopted for the FP-03, the following change will be made to section 701.

Section 701. - HYDRAULIC CEMENT

701.01  Portland Cement and Masonry Cement.  Delete the title and text of this subsection and substitute the following:

701.01  Portland Cement.  Conform to AASHTO M 85 and Subsection 701.04.

For shotcrete, limit alkalies according to Table 1A.

701.02  Blended Hydraulic Cement.  Conform to AASHTO M 240 and Subsection 701.04.

For shotcrete, use type 1S, 1S-A, 1P, or 1P-A cement.

701.03  Masonry Cement.  Conform to ASTM C 91 and Subsection 701.04.

701.04  Do not use different brands or types of cement, or the same brand or type of cement from different mills without approval.