03M03/29/06

S701-03M.doc

Use as appropriate when shotcrete or concrete is specified on the project.

Section 701. - CEMENT

When Prestressed concrete is specified (Section 553) include Subsection 701.01(a).

701.01  Hydraulic Cement

(a) Portland Cement.  Add the following:

When Prestressed Concrete is specified, Type III cement is allowed.

When shotcrete is specified, include Subsection 701.01(c), and Section 566, 703.18. If colored shotcrete is required, also include 711.05.

701.01  Hydraulic Cement  Add the following:

(c) Shotcrete.  Use one of the following:

(1) Portland cement.  Conform to AASHTO M 85, limiting alkalies according to Table 2 in AASHTO M 85.

(2) Blended hydraulic cement.  Use AASHTO M 240, type IS, IS-A, IP, or IP-A cement.