$$705.00A

Section 705.—ROCK

Revised 13 July 2005

INCLUDE THE FOLLOWING FOR STONE GUARDWALLS OR MASONRY

$$705.03A

705.03(a).  Delete the text and substitute the following:

Do not use rock with depressions or projections that might weaken it or prevent it from being properly embedded.

In the wall face, no stone shall be less than 2 inches in vertical dimension, 6 inches (15 centimeters) in horizontal dimension, or 4 inches (10 centimeters) in depth dimension.

On the top of the wall, no stone shall be less than 4 inches (10 centimeters) in least dimension.

Submit stone samples representing every color to be used on the project to the CO for approval.

INCLUDE THE FOLLOWING FOR GRANITE BRIDGE CURB

$$705.06A

705.06 Add the following after 705.06(b):

(c)  Granite bridge curb.  Granite bridge curb shall consist of granite stone curbs conforming to the following:

Top width	5 inches (125 millimeters)

Bottom width (min., for 2/3 length)	5 inches (125 millimeters)

Depth	9 ± 0.25 inches (225 ± 6 millimeters)

Length	6 feet (1.8 meters) (except as noted below)

Ten percent of the length of curb installed on the project may consist of stones no more than 6 inches (15 centimeters) shorter than the length specified, except as follows:

(1)  Stones used in making closures may be one-third shorter than specified.

(2)  On curves with radii greater than 160 feet (49 meters), but less than 492 feet (150 meters), stones may be from 4 to 6 feet (1.2 to 1.8 meters) in length.

(3)  Cut stones set on a radius of 160 feet (49 meters) or less to the required curvature and, except for making closures, the following minimum lengths:

Radius (feet) (meters)	Minimum Length (feet) (meters)

49 to 160 (15 to 49)	6 (1.8)

25 to less than 49 (7.6 to less than 15)	5 (1.4)

Less than 25 (7.6)	3 (0.9)

Cut the ends of all curved stones on radial lines.

Furnish granite curb that is light gray in color, free from seams and other structural imperfections or flaws which would impair its structural integrity, and of a smooth splitting appearance.  Natural color variation characteristics of the deposit from which the stone curb is obtained will be permitted.

Whenever stone curb is sawed, clean all surfaces that will be exposed and remove any iron rust or iron particles by sandblasting or other approved method.

Remove saw marks in excess of 0.12 inches (3 millimeters).

Supply either type A or type B stone curb, but use only 1 type on the project.

(d) Stone curb, Types A and B.

(1) Type A.  This type of curbstone shall be peen hammered or sawed to an approximately true plane, having no projections or depressions greater than 0.12 inches (3 millimeters) and have a top surface free from kerf.  The front and back arris lines shall be pitched straight and true and the back surface shall have no projection or depression greater than 1.5 inches (38 millimeters).

The front face shall have a batter of approximately 2:12 and shall be hammered or sawed, free from drill holes and with no projection through the arris or pitch lines for the full depth of the face.  The front arris shall be ¼-inch (6-millimeter) bullnose.

(2) Type B.  This type of curbstone shall be peen hammered or sawed to an approximately true plane, having no projections or depressions greater than 0.12 inches (3 millimeters) and have a top surface free from kerf.  The front and back arris lines shall be pitched straight and true and the back surface shall have no projection or depression greater than 1.5 inches (38 millimeters).

The front face shall have a batter of approximately 3/4:10 and shall be smooth quarry split, free from drill holes and with no projection of more than ¾-inch  (19 millimeters)and no depression of more than ½ inch (13 millimeters) measured from the plane of the face through the arris or pitch line for a distance down to within 1 inch (25 millimeters) of the bottom.  For the remaining distance there shall be no projection or depression greater than 1 inch (25 millimeters) measured in the same manner.

For both types of curb, the ends of all stones shall be square with the planes of the top and face so that when the stones are placed end to end as closely as possible, no space shall show in the joint at the top and face of more than ¼ inch (6 millimeters) for the full width of the top and for the full depth, after which the end may break back not over 2 inches (50 millimeters) from the plane of the joint.  The arris formed by the intersection of the plane of the joint with the planes of the top and exposed faces shall have no variation from the plane of the top and exposed faces greater than 0.12 inches (3 millimeters).