Questions/Answers to 03-C3D-002

The following questions and their answers were submitted in response to 03-C3D-002.

Q.  What material is to be used( by one of;Mil#, UNS, AISI,SAE,ASTM,ASM)

A.  Alloy is commercially know as :"IMI 834", a high temperature titanium alloy.   Isothermal forging is required.  Post-heat treatments of the forgings in the alpha-beta phase field to produce a fine alpha-beta structure is required and will be agreed between vendor and NASA.

Q.  Finished dimensions to be protected:

A.  1.  Thin isothermally forged pancake 2" thick x 15" dia.

2.  Thick isothermally forged pancake 6" thick x 15" dia

Q.  Are the billets provided by another source or should we include the cost of the billets.

A.  Vendor will procure/purchase good quality billets with low oxygen content and impurities (Fe, Ni, Cr).  Vendor will follow established steps to  prepare and heat treat Ti-alloy stock material.  Billets should be free of defects prior to forging; the use of die lubrication and stock coatings is required.  If multiple forging steps are used, vendor shall remove any oxide layer between successive forging operations.  Vendor will provide forging steps and final chemistry of forgings.