96M03/29/06

S708-96M.doc

When paint is specified, include the following:

Section 708. - PAINT

708.01  General.

(b) Volatile organic compound (VOC) content.

(1) Delete the text and substitute the following:

Clear (unpigmented) coatings	450 g/L max.

When paint for steel structures is specified, include the following:

708.04 Paint for Steel Structures.  Delete the text and substitute the following:

Conform to the following:

(a) Inorganic zinc primer	AASHTO M 300 type II

(b) Vinyl wash primer	SSPC no. 27

(c) Aluminum vinyl paint	SSPC no. 8

(d) White or colored vinyl paint	SSPC no. 9

(e) Aliphatic urethane coating	SSPC no. 36

(f) Latex primer for steel surfaces	SSPC no. 23

(g) Acrylic latex coating	SSPC no. 24

(h) Epoxy coating	SSPC no. 22

(i) Alkyd primer	SSPC no. 31

(j) Silicone alkyd coating	SSPC no. 21