96E09/22/06

S709-96E.doc

Use when reinforced steel or wire rope is specified.

Section 709. – REINFORCED STEEL AND WIRE ROPE

709.01  Reinforcing Steel.

Include the following when reinforcing bars are required:

(b) Reinforcing bars.  Delete the text and substitute the following:

Furnish deformed, grade 60 bars conforming to AASHTO M31 or M322.

Include the following when epoxy-coated reinforcing bars are required:

(c) Epoxy coated reinforcing bars.  Delete the first paragraph and substitute the following:

Furnish bars conforming to Subsection 709.01(b).  Conform to AASHTO M 284.

Include the following when tie bars are required:

(d) Tie bars.  Delete the text and substitute the following:

Furnish deformed, grade 60 bars conforming to AASHTO M31.

Include the following when hook bolts are required:

(e) Hook bolts.  Delete the text and substitute the following:

Furnish deformed, grade 60 bars conforming to AASHTO M31 with M14 rolled threads or M16 cut threads.  Furnish a threaded sleeve nut capable of sustaining a minimum axial load of 15,000 pounds.

Include the following when prestressed steel is required:

709.03  Prestressing Steel.  Delete the first and second bullets and substitute the following:

- Stress-relieved steel wire, AASHTO M 204, type BA or WA

- Uncoated seven-wire steel strand, AASHTO M 203, grade 270; or