03M03/29/06

S710-03M.doc

Use when Steel-Backed Timber or Log Rail guardrail is specified.

Section 710. - FENCE AND GUARDRAIL

When steel backed timber rail is specified, include the following:

710.08  Steel-Backed Timber Rail.  Add the following:

Refractory species such as larch and Rocky Mountain Douglas fir are not acceptable.

Use the following for projects with log rails. Verify copper naphthenate preservative is acceptable. See design memorandum.

710.12  Log Rails.  Add the following:

Use logs that are seasoned, straight, and sound No. 1 Grade Western Hemlock, Western Red Cedar, or Pine of the dimensions shown on the drawings.  Logs that taper in excess of 30 millimeters will not be permitted.  Remove all bark and at least 80% of the inner bark.  Peeler marks or incision marks on visible portions of logs will not be allowed.  Utilize logs that do not have season checks, singular or any 2 opposite each other that exceed 2 the thickness of the member.  Incorporate logs that are free of knot clusters, but may contain sound, tight, well-spaced knots.

Incise that portion of the log which will be below ground.  Make all dimensional cuts and holes in the timber members prior to pressure treatment.  Treat all timber members with Copper Naphthenate preservative treatment conforming to AWPA C14.  Preservative retention in the assay zone shall not be less than 1.2 kilograms per cubic meter.  Assay only in the incised, below ground portion of the posts.