96E03/29/06

S714-96E.doc

Use on all projects with Section 255, MSE walls.

Section 714. – GEOTEXTILE AND GEOCOMPOSITE DRAIN MATERIAL

714.02  Geocomposite Drains.

(b) Geocomposite sheet drains. Add the following:

For MSE wall construction, furnish prefabricated sheet drain with a core or net encapsulated in a Type I-D (Subsection 714.01) non-woven geotextile.  Provide a sheet drain capable of draining from both sides of the sheet and a minimum flow rate of 5 gallons per minute per foot of width when tested according to ASTM D 4716.  Perform the test under the following test conditions:

(1) 12 inch long specimen

(2) Pressure of 14.5 psi

(3) Gradient of 1.0

(4) 100-hour seating period

(5) Closed-cell foam rubber between platens and geocomposite