HIGH-EFFICIENCY AMORPHOUS SILICON ALLOY BASED SOLAR CELLS AND MODULES

Quarterly Technical Progress Report

December 1, 2003 through February 29, 2004

S. Guha and J. Yang

United Solar Ovonic Corporation

Troy, Michigan

NREL Technical Monitor:  Bolko von Roedern

Prepared under Subcontract No. ZDJ-2-30630-19

# Overview

In the last quarterly report, we showed a significant improvement of (c-Si:H solar cell performance by using an optimized hydrogen dilution profiling.  An initial active-area efficiency of 8.4% has been achieved using a (c-Si:H single-junction structure and 13.4% using an a-Si:H/(c-Si:H double-junction structure.  The main improvement is in the short circuit current density (Jsc) and fill factor (FF).  In this quarter, we continued to optimize the hydrogen dilution profiling for improving cell efficiency, especially for high Jsc.  We have obtained  Jsc over 27 mA/cm2 from a (c-Si:H single-junction solar cell.  We used the optimized (c-Si:H as the bottom cell in an a-Si:H/a-SiGe:H/(c-Si:H triple-junction structure and achieved an initial active-area efficiency of 13.6%.

For high rate modified very high frequency (MVHF) deposition, we continued to optimize a-Si:H/(c-Si:H double-junction and a-Si:H/a-SiGe:H/(c-Si:H triple-junction solar cells.  We have achieved an initial active-area efficiency of 12.5% using an a-Si:H/(c-Si:H double-junction structure.  This cell stabilized to 11.0% after prolonged light soaking.  Using an a-Si:H/a-SiGe:H/(c-Si:H triple-junction structure, we have achieved an initial active-area efficiency of 12.4% and a stable active-area efficiency of 11.2%.

Two different projects have been carried out using the large area deposition reactor.  In the first project, we have optimized a-Si:H/a-SiGe:H/a-SiGe:H triple-junction solar cell on Al/ZnO back reflector under production constraints.  We have achieved a stable active-area efficiency of 9.8% using a new cathode design with SiH4 and GeH4 mixture instead of Si2H6 and GeH4 mixture. This efficiency is equivalent to a total area efficiency of 9.1% and ties the previous record made with Si2H6 and GeH4 mixture. The second project is to optimize the a-Si:H/(c-Si:H double-junction solar cells on large area substrate. We achieved a stable aperture-area efficiency of 9.4% with an aperture area of 460 cm2.  An outdoor measurement of the same module at NREL showed an efficiency of 9.2%.

The stability of (c-Si:H solar cells against light soaking is an interesting topic in real device application.  Although many groups reported that no light-induced degradation was observed in their (c-Si:H solar cells, we found that there are still light-induced degradations in the range of 7% to 15%, depending on the material quality and device structure (presented at the last team meeting).  In this quarter, we systematically studied the metastability of (c-Si:H single-junction solar cells under various light soaking conditions and found that absorption in the amorphous phase is responsible for the light-induced degradation.  Since (c-Si:H covers a very wide range of materials with various microstructures such as different grain size and microcrystalline volume fraction, it is understandable to observe different metastability behavior in (c-Si:H materials and solar cells.

# (c-Si:H solar cells made using RF glow discharge at a low rate and their application as the bottom cell in multi-junction solar cells

##### 2.1. (c-Si:H single-junction cells with hydrogen dilution profiling

As presented in the last quarterly report, we have developed a hydrogen dilution profiling technique for (c-Si:H deposition where the hydrogen dilution ratio is decreased during the intrinsic layer deposition.  The purpose of the hydrogen dilution profiling is to keep the material structure close to the transition from the microcrystalline to amorphous phases.  Materials made under this condition normally have relatively large fraction of amorphous component, small grains, and improved grain boundary passivation by hydrogen.  Of course, if one could find a way to effectively passivate grain boundary defects for materials with large grains and high crystalline volume fractions, one would not need to make the materials close to the transition edge.  As a consequence, one could obtain high Jsc without significant loss in FF and open circuit voltage (Voc).  However, at the current stage, we believe that the materials with small grains and compact structures are still the choice for high efficiency (c-Si:H solar cells.

The (c-Si:H single-junction solar cell with an 8.4% efficiency was made using a hydrogen dilution profiling with linearly decreasing hydrogen dilution ratio.  It was found that the cell efficiency could be improved with the increase of the profiling rate in a certain range.  A hydrogen profiling that  is too steep in its grading leads to a significant amount of amorphous phase in the i/p interface region, which causes problems in carrier transport, and hence, poor solar cell performance.  In this quarter, we continued to optimize the design of gas flow profiling.  We have obtained  Jsc over 27 mA/cm2 in a (c-Si:H single-junction structure.  Figure 1 shows the (a) J-V characteristics and (b) quantum efficiency of this cell.  Although the Jsc is higher, the Voc and FF are lower than the previous champion cell.  Continued optimization is ongoing.

##### (c-Si:H single-junction solar cells made at various substrate temperatures

Substrate temperature is one of the important deposition parameters to be optimized.  A high substrate temperature provides a high mobility for radicals on the growing surface and allows the radicals to find low energy locations to form compact structure and grains.  Generally, (c-Si:H films deposited at high substrate temperatures have higher crystalline volume fractions than those deposited at low temperatures.  Too high a substrate temperature causes low hydrogen coverage on the growing surface and low hydrogen content in the material, resulting in a high dangling bond density and a poor grain boundary passivation in the material.  The optimized substrate temperature for low defect material has been found at around 250 (C, similar to the optimized temperature for a-Si:H deposition.  Another crucial factor for high efficiency (c-Si:H solar cells is a low impurity density, especially oxygen.  Oxygen is not electronically active in a-Si:H, but forms donors in (c-Si:H.  It has been reported that deposition at low substrate temperatures can suppress the oxygen related donor formation in (c-Si:H and allows for a relatively high impurity level without significant deterioration of cell performance.  In this quarter, we systematically   studied (c-Si:H deposition at different substrate temperatures to obtain optimum deposition condition.

Table I lists a series of (c-Si:H single-junction solar cells made under the same conditions except at different substrate temperatures.  It shows that decreasing the substrate temperature results in an increase in Voc, which could be related to the increase of the amorphous component in the material.  However, there is no clear trend in the changes of Jsc and FF.  The differences in the FF and Jsc may be due to run-to-run variation.  These results show that the range of substrate temperature for the (c-Si:H solar cell deposition is reasonably wide, which provides a wide window for optimization of cell efficiency, especially for multi-junction structures.

##### Multi-junction solar cells

We have reported an initial active efficiency of 13.4% using an a-Si:H/(c-Si:H double-junction structure, where the (c-Si:H bottom cell was deposited with a profiled hydrogen dilution.  In this quarter, we used the same recipe for (c-Si:H deposition in an a-Si:H/a-SiGe/(c-Si:H triple-junction structure and obtained an initial active area efficiency of 13.6%.  Figure 2 shows the (a) J-V characteristics and (b) quantum efficiency of this solar cell.

Two solar cells with the highest initial efficiencies were light soaked under 100 mW/cm2 of white light at 50 (C for over 1000 hours.  Table II summarizes their initial and stable performance.  The cells both stabilized  at 11.8%.  The triple-junction cell did not show advantage over the double-junction cell.  In fact, it degraded more than the double-junction cell.  The high degradation in the a-Si:H/a-SiGe/(c-Si:H triple-junction cell is attributed to the middle cell's limited current mismatching as shown in Table II.  We know that the a-SiGe:H middle cell degrades more than the a-Si:H top cell and the (c-Si:H bottom cell.  In order to obtain a high stable efficiency, a bottom cell limited current mismatching is desirable.

# 3. MVHF glow discharge at high deposition rate

We continue to optimize a-Si:H/(c-Si:H double-junction and a-Si:H/a-SiGe:H/(c-Si:H triple-junction structures using a high rate MVHF glow discharge.  The intrinsic a-Si:H layer in the top cell and the intrinsic (c-Si:H layer in the bottom cell were deposited using a MVHF glow discharge, but the intrinsic a-SiGe:H layer in the middle cell was deposited using a RF glow discharge at a low rate of ~ 1 Å/s.  New high initial active area efficiencies of 12.5% and 12.4% were achieved using the double-junction and the triple-junction structures, respectively.  Figure 3 shows the (a) J-V characteristics (b) quantum efficiency of the triple-junction cell where a matched current density is found among the component cells.  As reported previously, the c-Si:H bottom cell in the double junction structure showed a very good FF and less degradation under prolonged illumination. Thus, a triple-junction cell with a c-Si:H bottom cell limited current mismatch is desirable for a stabilized efficiency.  Based on this analysis, we optimized the cell structure by adjusting the current mismatching.  We have made an a-Si:H/a-SiGe:H/(c-Si:H  triple-junction  solar cell  (#12468)  with  a  strong bottom cell limited current mismatching

and obtained a very high FF of 0.79 as listed in Table III.  Although this cell did not have the highest initial efficiency, it showed the highest stable efficiency.

We light-soaked the a-Si:H/(c-Si:H double-junction cell with the highest initial efficiency (#12065) and three a-Si:H/a-SiGe:H/(c-Si:H triple-junction cells with different current mismatches.  The stability results are listed in Table III.  The a-Si:H/(c-Si:H double-junction cell with an initial efficiency of 12.5% stabilized at 11.0%, a new record for stable efficiency with the high rate a-Si:H/(c-Si:H double-junction solar cells.

For the a-Si:H/a-SiGe:H/(c-Si:H triple-junction solar cells, the light-induced degradation is in the range from 8% to 15%, which is similar to the degradation in a-Si:H/(c-Si:H double-junction solar cells.  Although the top cell is thinner in the triple-junction structure, the degradation in the a-SiGe:H middle cell has contributed significantly to the overall degradation.  Similar to a-Si:H/(c-Si:H double-junction cells, the cell with a strong bottom cell limited current mismatch (#12468) shows the lowest light induced degradation and the highest stable efficiency of 11.2%, which is slightly higher than the best stable efficiency of 11.0% from the a-Si:H/(c-Si:H double-junction structure.  Figure 4 plots the (a) J-V characteristics and (b) quantum efficiency of the best a-Si:H/a-SiGe:H/(c-Si:H triple-junction cell.

# Large-area deposition

In the large-area deposition, we continued to work on two projects.  One is the optimization of a-Si:H/a-SiGe:H/a-SiGe:H triple-junction solar cells and modules on Al/ZnO back reflectors using the deposition conditions under the constraints of a production machine.  The other is the deposition of an a-Si:H/(c-Si:H double-junction solar cell on a large area substrate.

In the last quarter, we achieved initial aperture-area efficiencies of 11.8% and 11.3% for the modules with aperture areas of 45 cm2 and 460 cm2, respectively for the double-junction solar cells.  After encapsulation, the 11.3% module's aperture-area efficiency became 10.6%.  In this quarter, we light-soaked these large-area modules under 100 mW/cm2 of white light at 50 (C for over 1000 hours.  The results are summarized in Table IV.  A stable aperture-area efficiency of 9.4% (# 9456) has been obtained.  These modules were sent to NREL for efficiency measurements.  NREL’s outdoor measurement shows an efficiency of 9.2%, and the indoor measurement under a Spire simulator shows an efficiency of 8.8%.

For a-Si:H/a-SiGe:H/a-SiGe:H triple-junction solar cells with production constraints, we reported a stable active-area efficiency of 9.4% in the last quarter.  This result was achieved with a new cathode design and with a SiH4 and GeH4 mixture instead of a Si2H6 and GeH4 mixture.  In this quarter, we optimized the material quality and device structure further and achieved a stable active-area efficiency of 9.8%.  This corresponds to a stable total area efficiency of 9.1% and ties with the previous record made with a Si2H6 and GeH4 mixture.  Figure 5 shows the (a) J-V characteristics and (b) quantum efficiency of this solar cell.

# 5. Stability of (c-Si:H single-junction solar cells

The Staebler-Wronski effect has limited the development of a-Si:H solar cells.  Although  significant work has been carried out in the last twenty-five years,  nor  an effective way has been developed to eliminate the light-induced degradation in a-Si:H based solar cells.  As an alternative material, (c-Si:H has attracted remarkable attention.  One advantage of using (c-Si:H in thin film solar cell is the better stability against prolonged light soaking than a-Si:H and a-SiGe:H alloys.  It has generally been reported that no light-induced degradation was observed in (c-Si:H solar cells.  However, the term (c-Si:H represents a wide range of materials comprised of various grain sizes and different microcrystalline volume fractions.  The highest efficiency (c-Si:H solar cells are normally deposited near the transition from microcrystalline to the amorphous phase, which means a large amount of amorphous phase still exists in the (c-Si:H materials.  Therefore, it would be logical to assume  light induced degradation in (c-Si:H solar cells deposited in this regime.  Indeed, Finger and his colleagues found that (c-Si:H solar cells made with a hydrogen dilution close to the transition show light induced degradation.  The amount of degradation depends on the dilution ratio, hence, on the microcrystalline volume fraction and grain size [1].

In general, (c-Si:H can be considered as a two-phase material with microcrystallites surrounded  by amorphous tissue.  The photons with energy higher than the band gap of a-Si:H are largely absorbed in the amorphous phase  while the lower energy photons are absorbed in the grains., Since the material properties inside of the grains would be similar to crystalline silicon with no light induced defects, one may expect no light induced defect generation in (c-Si:H when it is exposed to a red light with photon energy lower than the optical band gap of a-Si:H.  If this hypothesis is correct, there would be much less light induced degradation in the (c-Si:H bottom cell in an a-Si:H/(c-Si:H double-junction structure, because the high-energy photons are absorbed in the a-Si:H top cell.

In this quarter, we did a systematic study of light induced degradation of (c-Si:H single-junction solar cells with various light sources.  Two sets of (c-Si:H single-junction solar cells  were studied.  The cells in each set were from one run of deposition on the same substrate; and therefore, the cell performance is very similar.  One set was deposited using MVHF at a high rate with relatively low Voc.  The other set was deposited with RF at a low rate with relatively high Voc.  We believe that the RF cells have a lower microcrystalline volume fraction than the MVHF cells.  As a comparison, we also studied a set of a-SiGe:H bottom cells.  Light soaking was done at 25 (C under  open circuit condition.  An AM1.5 solar simulator was used as the light source.  Focus lenses and color filters were used to vary the light intensity and the spectrum.  The current density versus voltage (J-V) characteristics were measured as a function of light soaking time under the same light as used for the light soaking.  The light soaking time was 15 hours.  The J-V characteristics in the initial state and degraded state after light soaking were measured under an AM1.5 illumination and by quantum efficiency measurement.  Due to the difference in responses for different wavelengths, we used the same photo-generated carrier density for different light spectra.  We have found that for solar cells with a good FF,  Jsc is a reasonable measure of the photo-carrier density.  Thus, we adjusted the light intensities for different spectra to produce the same initial Jsc value.  Here, two Jsc values were chosen: one is the same as the Jsc under AM1.5 illumination, and the other is double the value under AM1.5.

Figure 6 shows a comparison of the normalized maximum power, Pmax, as a function of light soaking time for the MVHF (c-Si:H single-junction solar cell and the a-SiGe:H single-junction bottom cell, where the red and blue lights were obtained using a 665 nm long-pass filter and a 650 nm short-pass filter.  The long-pass filter only allows the photons with energy lower than 1.86 eV, smaller than the optical band gap of a-Si:H, to pass through and illuminates the sample.  For the (c-Si:H cell, the light intensities were adjusted to produce a Jsc(44 mA/cm2, approximately twice the Jsc under AM1.5 illumination, for the white, red, and blue lights.  For the a-SiGe:H cell, the light intensities were adjusted to produce a Jsc(46 mA/cm2 with the same consideration.  The figure clearly shows that there is no detectable light-induced degradation for the (c-Si:H cell under the red light, some degradation under the white light, and more degradation under the blue light.

Table V shows a comparison of the initial and degraded performance for five MVHF deposited (c-Si:H cells.  The first two cells were light-soaked under light intensities that produced the same Jsc as under AM1.5. Cell 1 and cell 2 were under the white light and the red light, respectively.  Notice that no light induced degradation was found in cell 2 under the red

light, but it was 3.7% under the white light.  To enhance the light soaking effect, we increased the light intensities to produce 44 mA/cm2, which is twice the Jsc under AM1.5 illumination.  There is still no detectable degradation under the red light within the experimental errors.

As discussed above, the undetectable light induced degradation under the red light is due to very little absorption in the amorphous phase, while the absorption in the microcrystalline phase does not produce defects.  Two mechanisms could explain the difference between the white and blue light soaking.  First, the blue light has a large portion absorbed in the amorphous phase, which produces more defects.  For the white light, the portion of red light is mainly absorbed in the microcrystalline phase and does not produce degradation.  Second, more blue light is absorbed nearer the i/p interface than in the bulk.  Guha, et al. showed that the i/p junction is the dominant junction and any changes in the dominant junction can cause noticeable changes on the cell performance [2].

Table VI lists the J-V characteristics at the initial and degraded states for three RF deposited solar cells.  The general trend is the same as the MVHF deposited cells, i.e., the red light produces low degradation, the white light some degradation, and the blue light more degradation.  However, unlike the MVHF cell, this cell still has 2.2% degradation under the red light.  We believe that the difference could be caused by the different material structure.  For the RF deposited cells, the Voc is larger than the MVHF deposited ones.  It could indicate that there is more amorphous component in the RF cells than in the MVHF cells, which may partially play a role in the light-induced degradation.  Although the cut-on filter with a wavelength longer than 665 nm blocks most of the high energy photons, there are still some photons absorbed by the amorphous tissue, which degrades  the cell performance.

Table VII summarizes the results of the a-SiGe:H bottom cells.  For the a-SiGe:H cell, the material is homogeneous, and only one optical band gap is defined with a value around 1.4 eV.  The differences among the light soaked samples under the lights with the three spectra are mainly due to the second mechanism (dominant junction effect)discussed above.

Overall, the light-induced degradation in (c-Si:H is much less than that in the a-SiGe:H cell even under white and blue light sources.  We need to point out that the light-soaked state is not a stabilized state since only a 15-hour light soaking was performed.

The above experiment confirms no or very little light-induced degradation for (c-Si:H solar cells under red light with photon energy lower than the band gap of a-Si:H.  In an a-Si:H/(c-Si:H double-junction solar cell, most blue light is absorbed by the a-Si:H top cell, and the (c-Si:H bottom cell only absorbs red light with low photon energy.  Therefore, there is very little light-induced degradation in the (c-Si:H bottom cell in multi-junction structures, and a bottom cell limited current mismatching is desirable for stable efficiency as shown above and in the previous reports.

In summary, we have systematically studied the light-induced degradation in (c-Si:H single-junction solar cells under various light soaking conditions.  We found no detectable degradation under red light with photon energies less than the band gap of a-Si:H.  We believe that the low energy photons are only absorbed in the microcrystalline phase, where no light induced defect generation occurs.  Under white and blue lights, the defect generation in the amorphous phase causes certain degradation.  The fact that a larger degradation is observed under blue light than white light is due to more absorption in the amorphous phase and more absorption near the i/p interface under blue light than under white light.  These results provide an explanation that a bottom cell limited-current mismatch in multi-junction structures with (c-Si:H as the bottom cell leads to a high stable efficiency.

# References:

- S. Klein, F. Finger, R. Carius, T. Dylla, B. Rech, M. Grimm, L. Houben, and M. Stutzmann, Proceeding of 2nd International Conference on Cat-CVD (Hot-Wire CVD) Process, (Denver, Colorado, Sep. 2002), p. 202.

- A. Pawlikiewicz and S. Guha, Mat. Res. Soc. Symp. Proc. 118, 599 (1988).

# Text boxes

Figure 5. Initial and stable (a) J-V characteristics and (b) quantum efficiency of an a-Si:H/a-SiGe:H/a-SiGe:H triple-junction solar cell made on a large area substrate with production constraints.

Table II: Summary of stability results of an a-Si:H/(c-Si:H double-junction solar cell (L14643) and an a-Si:H/a-SiGe:H/(c-Si:H triple-junction solar cell (L14682).  The data in bold are the limiting Jsc.

| Run # | state | Eff (%) | Jsc (mA/cm2) | Voc (V) | FF |
| --- | --- | --- | --- | --- | --- |
|  |  |  | top | middle | bottom |  |  |
| L14643 | initial | 13.45 | 12.75 | ( | 12.61 | 1.439 | 0.741 |
|  | stable | 11.81 | 12.22 | ( | 12.38 | 1.399 | 0.691 |
|  | degradation | 12.2% | 4.2% |  | 1.8% | 2.8% | 6.7% |
| L14682 | initial | 13.62 | 8.65 | 8.14 | 8.34 | 2.190 | 0.764 |
|  | stable | 11.77 | 8.33 | 7.82 | 8.15 | 2.154 | 0.699 |
|  | degradation | 13.6% | 3.7% | 3.9% | 2.3% | 1.7% | 8.5% |

Table I: J-V characteristics of (c-Si:H solar cells made at different substrate temperatures.

| Run # | Ts ((C) | Eff (%) | Jsc (mA/cm2) | Voc (V) | FF | Rs ((.cm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 14787 | 300 | 7.81 | 24.21 | 0.489 | 0.661 | 2.9 |
| 14748 | 275 | 7.92 | 24.81 | 0.504 | 0.633 | 3.4 |
| 14784 | 250 | 8.00 | 25.13 | 0.512 | 0.622 | 3.4 |
| 14788 | 225 | 7.92 | 24.39 | 0.527 | 0.616 | 2.9 |
| 14800 | 200 | 8.18 | 24.40 | 0.531 | 0.632 | 3.0 |

Figure 3. (a) J-V characteristic and (b) quantum efficiency of an a-Si:H/a-SiGe:H/c-Si:H triple junction solar cell with an initial efficiency of 12.4%.

Table III. Initial and stable J-V characteristics of an a-Si:H/(c-Si:H double-junction (#12065) and three a-Si:H/a-SiGe:H/(c-Si:H triple-junction solar cells. The numbers in bold are the limiting current densities; in red are the highest stable efficiencies.

| Sample No. | State | Voc (V) | FF | Jsc (mA/cm2) | Q (mA/cm2) | Eff (%) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Top | Mid. | Bott. |  |
| 12065 | Initial | 1.425 | 0.767 | 11.45 | 11.51 | ( | 11.45 | 12.51 |
|  | Stable | 1.381 | 0.712 | 11.18 | 11.18 | ( | 11.36 | 10.99 |
|  | Degr. | 3.09% | 7.17% | 2.36% | 2.87% | ( | 0.79% | 12.2% |
| 12427 | Initial | 2.203 | 0.730 | 7.42 | 8.19 | 7.42 | 7.68 | 11.93 |
|  | Stable | 2.122 | 0.669 | 7.18 | 7.93 | 7.18 | 7.69 | 10.19 |
|  | Degr. | 3.68% | 8.36% | 3.23% | 3.17% | 3.23% | 0% | 14.6% |
| 12454 | Initial | 2.201 | 0.731 | 7.20 | 8.24 | 7.20 | 7.57 | 11.58 |
|  | Stable | 2.134 | 0.701 | 6.92 | 7.98 | 6.92 | 7.47 | 10.35 |
|  | Degr. | 3.04% | 4.10% | 3.89% | 3.16% | 3.89% | 1.32% | 10.6% |
| 12468 | Initial | 2.165 | 0.790 | 7.16 | 7.56 | 7.95 | 7.16 | 12.25 |
|  | Stable | 2.117 | 0.746 | 7.10 | 7.34 | 7.64 | 7.10 | 11.21 |
|  | Degr. | 2.27% | 5.57% | 0.84% | 2.91% | 3.90% | 0.84% | 8.49% |

Figure 2. (a) J-V characteristics and (b) quantum efficiency of an a-Si:H/a-SiGe:H/(c-Si:H triple-junction solar cell made using RF glow discharge at a low rate (1 Å/s.

Figure 1. (a) J-V characteristics and (b) quantum efficiency of a (c-Si:H single-junction solar cell with a high Jsc.

Table V: Summary of the light soaking results for the c-Si:H single junction solar cells made with MVHF at a high rate.  The red light was obtained by a focused white light with a 665 nm long-pass filter, and the blue light with a 650 nm short-pass filter.

| Cell No. | State | Jsc (mA/cm2) | Voc (V) | FF | Pmax (mW/cm2) | Light source |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Initial | 22.02 | 0.475 | 0.624 | 6.53 | White (AM1.5) Jsc(22 mA/cm2 |
|  | Light soaked | 21.82 | 0.474 | 0.608 | 6.29 |  |
|  | Degradation | 0.91 % | 0 % | 2.56 % | 3.68 % |  |
| 2 | Initial | 21.86 | 0.481 | 0.623 | 6.55 | Red light with Jsc(22 mA/cm2 |
|  | Light soaked | 21.86 | 0.480 | 0.623 | 6.55 |  |
|  | Degradation | 0 % | 0 % | 0 % | 0 % |  |
| 3 | Initial | 22.20 | 0.474 | 0.621 | 6.53 | White light with Jsc(44 mA/cm2 |
|  | Light soaked | 22.00 | 0.467 | 0.598 | 6.14 |  |
|  | Degradation | 0.9 % | 1.48 % | 3.70 % | 5.97 % |  |
| 4 | Initial | 22.19 | 0.472 | 0.620 | 6.49 | Red light with Jsc(44 mA/cm2 |
|  | Light soaked | 22.11 | 0.473 | 0.619 | 6.47 |  |
|  | Degradation | 0.36 % | 0 % | 0 % | 0.31 % |  |
| 5 | Initial | 21.98 | 0.476 | 0.621 | 6.50 | Blue light with Jsc(44 mA/cm2 |
|  | Light soaked | 21.78 | 0.469 | 0.591 | 6.04 |  |
|  | Degradation | 0.91 % | 1.47 % | 4.83 % | 7.08 % |  |

Figure 6. Light soaking kinetics of normalized efficiency of a (c-Si:H single-junction solar cell and an a-SiGe:H single-junction solar cell.

Table VII: Summary of the light soaking results for the a-SiGe:H bottom single-junction

solar cells.  The red light was a focused white light with a 665 nm long-pass filter, and the

blue light with a 650 nm short-pass filter.

| Cell No. | State | Jsc (mA/cm2) | Voc (V) | FF | Pmax (mW/cm2) | Light source |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Initial | 23.40 | 0.624 | 0.575 | 8.30 | White light with Jsc(23 mA/cm2 (AM 1.5) |
|  | Light soaked | 22.94 | 0.608 | 0.653 | 7.85 |  |
|  | Degradation | 1.97% | 2.56% | 2.09% | 6.55% |  |
| 2 | Initial | 23.10 | 0.628 | 0.601 | 8.72 | White light with Jsc(46 mA/cm2 |
|  | Light soaked | 22.88 | 0.601 | 0.567 | 7.80 |  |
|  | Degradation | 0.95 % | 4.30 % | 5.66 % | 10.55 % |  |
| 3 | Initial | 23.91 | 0.614 | 0.587 | 8.62 | Red light with Jsc(46 mA/cm2 |
|  | Light soaked | 23.48 | 0.601 | 0.563 | 7.94 |  |
|  | Degradation | 1.80 % | 2.12 % | 4.09 % | 7.89 % |  |
| 4 | Initial | 23.50 | 0.621 | 0.572 | 8.35 | Blue light with Jsc(46 mA/cm2 |
|  | Light soaked | 22.91 | 0.591 | 0.539 | 7.30 |  |
|  | Degradation | 2.51 % | 4.83 % | 5.77 % | 12.57 % |  |

Table VI: Summary of the light soaking results for the c-Si:H single junction solar cells

made with RF at a low rate.  These cells have a high Voc and probably a high amorphous component in the intrinsic layer. The red light was a focused white light with a 665 nm

long-pass filter and the blue light with a 650 nm short-pass filter.

| Cell No. | State | Q (mA/cm2) | Voc (V) | FF | Pmax (mW/cm2) | Light source |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Initial | 24.43 | 0.525 | 0.596 | 7.64 | White light with Jsc(48 mA/cm2 |
|  | Light soaked | 23.86 | 0.521 | 0.578 | 7.51 |  |
|  | Degradation | 1.80 % | 0.76 % | 3.02 % | 5.89 % |  |
| 2 | Initial | 24.42 | 0.526 | 0.598 | 7.68 | Red light with Jsc(48 mA/cm2 |
|  | Light soaked | 24.22 | 0.523 | 0.593 | 7.51 |  |
|  | Degradation | 0.82 % | 0.57 % | 0.84 % | 2.20 % |  |
| 3 | Initial | 24.28 | 0.525 | 0.605 | 7.71 | Blue light with Jsc(48 mA/cm2 |
|  | Light soaked | 23.80 | 0.521 | 0.580 | 7.19 |  |
|  | Degradation | 1.98 % | 4.83 % | 5.77 % | 7.23 % |  |

Figure 4. Initial and stable (a) J-V characteristics and (b) quantum efficiency of an a-Si:H/a-SiGe:H/(c-Si:H triple-junction solar cell.

Table IV.  Stability results of a-Si:H/c-Si:H double-junction modules.  The stabilized state was reached by 1050 hours of light soaking under 100 mW/cm2 of white light at 50 oC.

| Sample No. | Area (cm2) | State | Voc (V) | Isc (A) | FF | Pmax (W) | Eff. (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 9446 | 459.67 | Initial | 1.400 | 4.860 | 0.703 | 4.782 | 10.40 |
|  |  | Stabilized | 1.378 | 4.774 | 0.662 | 4.356 | 9.48 |
|  |  | Degradation | 1.57 % | 1.77 % | 5.83 % | 8.91 % | 8.9 % |
| 9456 | 455.82 | Initial | 1.395 | 4.914 | 0.693 | 4.750 | 10.42 |
|  |  | Stabilized | 1.373 | 4.817 | 0.648 | 4.283 | 9.40 |
|  |  | Degradation | 1.58 % | 1.97 % | 6.49 % | 9.83 % | 9.8 % |
| 9461 | 457.96 | Initial | 1.408 | 5.008 | 0.688 | 4.849 | 10.59 |
|  |  | Stabilized | 1.378 | 4.827 | 0.638 | 4.246 | 9.27 |
|  |  | Degradation | 2.13 % | 3.61 % | 7.27 % | 12.44 % | 12.4 % |
| 9464 | 457.96 | Initial | 1.420 | 4.756 | 0.658 | 4.445 | 9.71 |
|  |  | Stabilized | 1.399 | 4.631 | 0.633 | 4.104 | 8.96 |
|  |  | Degradation | 1.48 % | 2.63 % | 3.82 % | 7.67 % | 7.7 % |