MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A17568 | In-Flight Anomaly Number -- | Contractor Report Number S-083 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title MULTIPLE RADIOGRAPHIC INSPECTION CONCERNS |
| EICN# -- | ELEMENT ET | Contractor LMMSS | FSCM# -- | FCRIT 3 |
| HCRIT 1 | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE RADIOGRAPHIC INSPECT | PART# STP 2503 | SER/LOT# -- | MANUFACTURER LMMSS-MAF |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U UC | Fail Mode UC - UNSAT | Cause MP - MFG-PRC |
| System PRESSURE VES | Defect XN - NA | Material W - RMEDIA | Work Contact W.MATTHEESSE | Fail Date 03/06/2000 |
| Received at MSFC 03/24/2000 | Date Isolated 03/06/2000 | FMEA Reference N/A | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom -- | Time Cycle -- |
| Effectivity Text ET 92, 93, 102-112 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 11/29/2001 | CN RSLV SBMT -- | Defer Date -- | Add Date 03/24/2000 | R/C Codes -- -- -- |
| Assignee |
| Design M. BUTLER | Chief Engineer N. OTTE | S & MA K. LAYNE | Project -- | Project MGR J. SMELSER |
| Approval |
| Design J. KRESS | Chief Engineer N. OTTE | S & MA K. LAYNE | Project -- | Project MGR J. SMELSER |
| PAC Assignee T. WHITE | PAC Review Complete TW | MSFC Closure Date 10/23/2001 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID N037989; N037990; N037982 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID N037983; N037986; N037987 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID N037988; N037985;N037976 |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description PROBLEM ------- MULTIPLE CONCERNS WERE NOTED IN THE PRESSURE VESSEL POST PROOF X-RAY PROCESS. THESE CONCERNS INCLUDED AREAS OF MISSED REQUIREMENTS (AREAS OF COVERAGE), FILM DOCUMENTATION, FILM ACCEPTANCE, AND FILM STORAGE. CRITICALITY: THIS CONDITION IS A NON-CONFORMANCE AND DID NOT RESULT IN A FAILURE. THIS IS A DISCRETIONARY CAPS. REVISION F: SEE ASTERISKS (*) FOR CHANGES: UPDATED FLEET CLEARANCE FOR 350 ANGLE, TRANSFERRED ALL OPEN ENHANCEMENTS TO SI-2001-S005, AND CLOSED ALL OPEN TASKS. |
| Contractor Investigation/Resolution GENERAL ------- DURING PREPARATIONS FOR INCORPORATING THE PRODUCTION OPERATIONS NDT WELD LOCATION GUIDE INTO THE 80900000069 ENGINEERING DRAWINGS, IT WAS DETERMINED THAT THE START LOCATION FOR PREVIOUS O-1 X-RAY MEASUREMENT POSITIONING TAPE HAD BEEN MISLOCATED 3.4 INCHES (LOCATION TOLERANCE IS 1 1.0 INCH). THIS POTENTIALLY IMPACTED ADEQUATE POST PROOF FILM COVERAGE OF THE INADEQUATELY PROOFED ZONES AND ROOT/COVER OVERLAP ZONES. REVIEW OF THE PRODUCTION OPERATIONS NDT WELD LOCATION GUIDE SHOWED THAT ALL KNOWN COPIES OF THIS GUIDE INCLUDING THOSE THAT ARE 15 PLUS YEARS OLD SHOWED THE SAME MISLOCATED O-1 START POINT. RESEARCH OF THE MISLOCATED O-1 START POINT ANOMALY IDENTIFIED AREAS OF INADEQUATE FILM COVERAGE ON MULTIPLE TANKS AND THAT THE POST PROOF O-1 WELD ROOT BEAD OVERLAP, +/- 7.5 DEGREE ANGLE X-RAY FILM WAS MISSING FOR ET-111. ADDITIONALLY, REVIEW OF THE OTHER ET-102 POST PROOF FILM REVEALED THE FOLLOWING MISSED REQUIREMENTS: 1. HFF-4 WELD: THE PENETRAMETERS WERE MISLOCATED AND THE PROPER ACCEPTANCE HAD NOT BEEN PERFORMED ON THE FILM. 2. ODG-9 AT 19 INCHES THRU 32-1/4 INCHES: THE AT RISK PERPENDICULAR X-RAY FILMS ARE MISSING. 3. ODG-5 AT 100 INCHES THRU 116 INCHES: THE AT RISK PERPENDICULAR X-RAY FILMS ARE MISSING. 4. OADC AT 315 INCHES THRU 334-1/2 INCHES: THE REQUIRED FILMS ARE MISSING. NCDS HAVE BEEN GENERATED FOR ET'S 92, 93, AND 102 THRU 111 ON EVERY X-RAY ISSUE FOUND TO DATE (3-17-2000). AS OTHER ITEMS HAVE BEEN FOUND APPROPRIATE NONCONFORMANCE DOCUMENTATION WAS GENERATED. AS THE RESULT OF A MEETING CHAIRED BY PRODUCT ASSURANCE AND ATTENDED BY TECHNICAL, MANUFACTURING ENGINEERING, PRODUCTION OPERATIONS AND MISSION SUCCESS THE LISTED ACTION ITEMS WERE ESTABLISHED. ATTENDEES: PRODUCT ASSURANCE P. POWELL, D. WESTPHAL, D. OWENS, T. MCKEOUGH, & W. MATTHEESSEN TECHNICAL OPERATIONS P. HINKELDEY & D. BOLSTAD MANUFACTURING ENGINEERING R. WHITE & R. WEAVER PRODUCTION OPERATIONS D. LINCOLN & P. THERRIEN MISSION SUCCESS E. HORAK GENERAL CONTINUED DURING A POST PROOF LOX TANK X-RAY INSPECTION (ET-113) AN X- RAY TECHNICIAN DETERMINED THAT ON THE O-5 WELD, THE WELD REPAIR 35 DEGREE ANGLE SHOTS COULD NOT BE PERFORMED. ON THE FORWARD (+35) SHOT THERE EXISTS INTERFERENCE WITH SUPPORT TOOLING. A REVIEW SHOWED THAT OTHER WELDS HAVE INTERFERENCE PROBLEMS OF VARIOUS TYPES. THESE CAN BE BROKEN DOWN INTO SEVERAL BROAD CLASSES: 1. PHYSICAL INTERFERENCE DUE TO OTHER FLIGHT HARDWARE. 2. PHYSICAL INTERFERENCE DUE TO REQUIRED SUPPORT TOOLING. 3. METAL THICKNESS THAT DOES NOT ALLOW ALL REQUIRED FILM ELEMENTS (PENETRAMETERS, X-RAY TAPE, AND BOTH FACES OF THE WELD) TO BE RECORDED ON THE SAME PIECE OF 70MM FILM. 4. GEOMETRY & THICKNESSES THAT MAKE THE RADIOGRAPH DIFFICULT TO INTERPRET. * DURING THE INSPECTION OF ET-113 LOX TANK AN AREA OF FILM DENSITY BEING INCORRECT WAS FOUND. THIS WAS DOCUMENTED & DISPOSITIONED UAI ON NCD N051237. TASK I. FAILURE INVESTIGATION A. PERFORM AND DOCUMENT A DETAILED STEP BY STEP PROCESS FLOW OF THE X-RAY PROCESSES FROM ENGINEERING REQUIREMENTS TO ARCHIVAL STORAGE OF THE FILM. RESPONSIBILITY: W. MATTHEESSEN/3741 - D. WESTPHAL/3740 - RELIABILITY D. LOWE/4420 - P. HINKELDEY/4640 - ENGINEERING R. WHITE/3614 - R. WEAVER/36 - MANUFACTURING ENGINEERING C. CLAUSS/3623 - J. STANLEY/3620 - X-RAY OPERATIONS S. MCEVOY/3742 - D. WESTPHAL/3740 - QUALITY NDE C. CULVER/3743 - D. WESTPHAL/3740 - QUALITY ENGINEERING G. CROMER/3743 - D. WESTPHAL/3740 - HAC ECD: 3/31/00 COMPLETE: 3/29/00 CLOSURE STATEMENT: PROCESS HAS BEEN REVIEWED AND FLOW CHARTS GENERATED. REF.: CAPS S-083_ATT2_ X-RAY PROCESS FLOW.PDF , ATTACHED. B. PERFORM AN ASSESSMENT OF THE X-RAY PROCESS DOCUMENTED IN TASK I.A. TO DETERMINE THE MATCH WITH COMMAND MEDIA. RESPONSIBILITY: J. RUSSELL/4210 /D. CALLAN/4210 - W. SIGUR/4010 TECHNICAL OPERATIONS ECD: 4/14/00 COMPLETE: 4/5/00 CLOSURE STATEMENT: FOUR FINDINGS WERE FOUND: #1: THE CURRENT PRACTICES RELATED TO SECURITY AND CONTROLLED ACCESS TO X-RAY FILMS DO NOT MEET THE REQUIREMENTS OF THE COMMAND MEDIA. #2: THE LEVEL OF INSTRUCTIONS AND DETAIL CONTAINED IN THE PRODUCTION PROCESS DATABASE (PPD) FOR IMPLEMENTATION OF STP- 2503 IS INADEQUATE TO CONTROL THE WORK AND ASSURE STAMP WARRANTY IS MAINTAINED." #3: THE PROCESS OF GENERATING THE HARDWARE ACCEPTANCE COMMITTEE (HAC) SUMMARY FOR EACH ET IS SUBJECT TO A SINGLE POINT FAILURE THAT CAN RESULT IN A WELD HEAT REPAIR NCD NOT BEING INCLUDED IN THE FINAL REPORT. MISSING SUCH AN NCD WILL RESULT IN NEEDED POST-PROOF X-RAYS NOT BEING ACCOMPLISHED. #4: THE LOCATION AND IDENTIFICATION OF X-RAY FILM STRIPS IS SUBJECT TO A SINGLE POINT FAILURE. THE FILM POSITION ON A WELD CAN BE IN ERROR. REF.: CAPS_S-083_IB_ATTACHMENT.DOC C. EVALUATE THE COMPLETE PROCESS FROM TASK I.A, AND BY INCORPORATING ANY RESULTING AUDIT FINDINGS FROM TASK I.B, THE PROCESS OWNERS ARE TO OPTIMIZE THE X-RAY PROCESS AND MAKE IT NO FAIL. RESPONSIBILITY: W. MATTHEESSEN/3741 - D. WESTPHAL/3740 - RELIABILITY D. LOWE/4420 - P. HINKELDEY/4640 - ENGINEERING R. WHITE/3614 - R. WEAVER/3614 - MANUFACTURING ENGINEERING C. CLAUSS/3623 - J. STANLEY/3620 - X-RAY OPERATIONS S. MCEVOY/3742 - D. WESTPHAL/3740 - QUALITY NDE C. CULVER/3743 - D. WESTPHAL/3740 - QUALITY ENGINEERING G. CROMER/3743 - D. WESTPHAL/3740 - HAC ECD: 4/28/00 - ASSUMES PARTIAL IN PARALLEL ACTIVITY WITH TASK I.B. ECD: 6/30/00 - INITIAL SCOPE OF WORK WAS UNDER ESTIMATED. ECD: 12/22/00 - INCREASED SCOPE OF WORK. ECD: 7/31/01 - INCREASED SCOPE OF WORK COMPLETED: 1/24/01 CLOSURE STATEMENT BOTH CORRECTIVE ACTIONS AND A SERIES OF RECOMMENDED PROCESS ENHANCEMENTS WERE PRESENTED TO A MANAGEMENT TEAM CONSISTING OF THE COGNIZANT MANAGERS. ALL CORRECTIVE ACTIONS HAD BEEN IMPLEMENTED PRIOR TO THE NEQA AUDIT. CORRECTIVE ACTIONS (IMPLEMENTED): 1. DUAL INDEPENDENT REVIEW OF MANUAL HAC & EXCEL SPREAD SHEET DATA REPORT 2. REQUIREMENT MATRIX (REUSABLE & GENERATED BY ME & QE) 3. CONTROLS IMPLEMENTED ON X-RAY FILM AREA (PROD OPS X-RAY) 4. RE-INSTITUTED 35( ANGLE SHOTS EXCEPT FOR OBSTRUCTED AREAS PROCESS IMPROVEMENT RECOMMENDATIONS: 1. ENHANCE NCD SYSTEM TO IMPROVE INFORMATION RETRIEVABILITY & ALLOW FOR AUTOMATION OF HAC & REQUIREMENT MATRIX. 2. AUTOMATE THE HAC REPORT, SHOULD ALLOW FOR THE AUTOMATIC GENERATION OF REQUIREMENT MATRIX. 3. AUTOMATE THE GENERATION OF THE REQUIREMENT MATRIX. THIS SHOULD MIMIC THE PRESENT MATRIX. 4. ENHANCE ACCESS AND CONTROL OF FILM STORAGE AND TECHNIQUE SHEET. 5. EVALUATE 8090...069 TO IMPROVE CLARITY & EASE OF USE. 6. ENHANCED LONG TERM STORAGE CONTROLS INCLUDING DIGITIZATION OF RADIOGRAPHS & DIGITAL X-RAY. 7. EVALUATE THE ELIMINATION OF ARBITRATION IN PRE-PROOF X- RAYS. REF.: W. G. MATTHEESSEN PRESENTATION AND MEETING MINUTES OF 10/24/00 MEETING. * D. PERFORM A MANAGEMENT LEVEL REVIEW AND OVERSIGHT OF TASKS I.A THRU I.C WITH NASA. RESPONSIBILITY: E. HORAK/3000 ECD: 4/28/00 - EXTENSION OF I.C TASKS ECD: 7/15/00 ECD: 12/22/00 - INCREASED SCOPE OF WORK. ECD: 7/31/01 - INCREASED SCOPE OF WORK CANCELED 1/31/01 CANCELLATION RATIONALE BASED ON THE NASA NEQA AUDIT AND PROCESS OWNERS' REVIEW OF TASK I.C, THIS TASK IS NO LONGER REQUIRED. SUBJECT ITEMS HAVE BEEN REVIEWED WITH NASA PROJECT INCREMENTALLY AS IMPLEMENTATION WAS BEING ACCOMPLISHED. E. SEARCH FOR AND IDENTIFY NCDS WHICH HAD PREVIOUS INCIDENCES OF MISSED OR MISSING X-RAY FILM OR X-RAY REQUIREMENTS. RESPONSIBILITY: D. DONNELLY/3741- D. WESPHAL/3740 N. GILLIAM/3712 - G. WHEELER/3710 ECD: 3/29/00 COMPLETE: 4/4/00 CLOSURE STATEMENT: A REVIEW WAS CONDUCTED OF NCD HISTORY, NASA DISCREPANCY REPORTS, AND SPECIAL INVESTIGATIONS (SI). IN 1988 MAJOR CHANGES TOOK PLACE IN THE X-RAY PROCESS AS A RESULT OF TD- 808. SINCE THAT TIMES THE MAJOR ISSUE OF MISSING X-RAY FILM HAS BEEN WITH THE SUPPLIERS. OTHER AREAS HIGHLIGHTED ARE FROM PLANNING ERRORS AND WELD REPAIRS THAT ALLOWED MISSED FILM. THE SIS SHOWED AREAS OF CONCERN ON PLANNING AND REQUIREMENTS THAT WERE FIXED WITH SYSTEM TYPE CORRECTIVE ACTIONS. OF NOTE IS THE CHANGE FROM AN AUTOMATED HAC REPORT FROM THE LWT TANKS TO A MANUAL HAC ON SUPER LWT. A NASA DISCREPANCY REPORT DOCUMENTED A PLANNING ERROR. THESE ISSUES WILL BE INCORPORATED IN TO THE TASK I.C REVIEW. REF.: CAPS S-083 TASK I.E REPORT. F. REVIEW ALL LO2 AND LH2 TANKS FOR ADEQUATE POST PROOF FILM COVERAGE. STARTING WITH ET-102, THEN CONTINUING WITH ET-103 THRU 111, ET-93 AND ET-94. RESPONSIBILITY: D. LOWE/4420 - P. HINKELDEY/4640 - ENGINEERING C. CLAUSS/3623 - J. STANLEY/3620 - X-RAY OPERATIONS S. MCEVOY/3742 - D. WESTPHAL/3740 - QUALITY NDE G. CROMER/3743 - D. WESTPHAL/3740 - HAC COMPLETE: 5/16/00 CLOSURE STATEMENT: ATTACHMENT #1 LISTS THE NCDS GENERATED, STATUS, & DISPOSITION. G. REVIEW ET-102 & 103 ORIGINAL WELDS FOR ADEQUATE FILM COVERAGE. RESPONSIBILITY: C. CLAUSS/3623 - J. STANLEY/3620 - X-RAY OPERATIONS S. MCEVOY/3742 - D. WESTPHAL/3740 - QUALITY NDE W. MATTHEESSEN/3741-D. WESTPHAL/3740 - RELIABILITY ASSURANCE COMPLETE: 3/24/00 NO ISSUES PER DISCUSSION WITH PA-NDT SUPERVISION. * H. PROVIDE FLEET CLEARANCE RATIONALE AND PRODUCTION CLEARANCE FOR THE 35 DEGREE ANGLE ISSUE. RESPONSIBILITY: E. SWEET/4400 D. BOLSTAD/4600 ECD: 6/23/00 ECD: 12/22/00 -- INCREASED SCOPE OF WORK. ECD: 1/31/01 - INCREASED SCOPE OF WORK ECD: 5/11/01 - INCREASED SCOPE OF WORK TASK OPEN * I. IMPLEMENT THE PROCESS IMPROVEMENT RECOMMENDATION TASKS GENERATED IN TASK I.C. 1. ENHANCE NCD SYSTEM TO IMPROVE INFORMATION RETRIEVABLY. RESPONSIBILITY: D. O'NEAL/3744 - D. WESTPHAL/3740 - MRB ECD: 4/30/01 2. ENHANCE ACCESS AND CONTROL OF FILM STORAGE AND TECHNIQUE SHEET CONTROL. RESPONSIBILITY: C. CLAUSS/3623 - M. MCGEHEE/3620 - X-RAY OPERATIONS ECD: 6/29/01 3. EVALUATE 8090...069 TO IMPROVE CLARITY & EASE OF USE. RESPONSIBILITY: W. SIGUR/4010 - TECH OPS ECD: 6/29/01 4. ENHANCED LONG TERM STORAGE CONTROLS. RESPONSIBILITY: C. CLAUSS/3623 - M. MCGEHEE/3620 - X-RAY OPERATIONS R. BESIN/3711 - G. WHEELER/3710 - QUALITY OPERATIONS MANAGEMENT ECD: 6/29/01 TASK OPEN * J. CONDUCT AN EVALUATION OF THE TASKS GENERATED IN TASK I.C. 1. ENHANCE NCD SYSTEM TO ALLOW FOR AUTOMATION OF HAC & REQUIREMENT MATRIX. 2. AUTOMATE THE HAC REPORT, SHOULD ALLOW THE AUTOMATIC GENERATION OF REQUIREMENT MATRIX. 3. AUTOMATE THE GENERATION OF THE REQUIREMENT MATRIX. THIS SHOULD MIMIC THE PRESENT MATRIX. RESPONSIBILITY: C. CULVER/3743 - D. WESTPHAL/3740 - QUALITY ENGINEERING ECD: 3/07/01 COMPLETE: 3/7/01 CLOSURE STATEMENT: THERE IS NO BENEFIT TO GENERATE AN AUTOMATED HAC & REQUIREMENT MATRIX BEFORE THE IMPLEMENTATION OF PMES. REF. C. CULVER EMAIL DATED 3/7/01 4. ENHANCED LONG TERM STORAGE INCLUDING DIGITIZATION OF RADIOGRAPHS & DIGITAL X-RAY. RESPONSIBILITY: W. SIGUR/4010 - TECH OPS ECD: 6/29/01 5. EVALUATE THE ELIMINATION OF ARBITRATION IN PRE-PROOF X- RAYS. RESPONSIBILITY: D. WESTPHAL/3740 - QUALITY NDE ECD: 3/16/01 TASK OPEN * K. REVISE STPS & 8090...069 TO INCORPORATE CHANGES FOR 35 DEGREE ANGLE SHOTS ISSUES & PENTRAMETER ISSUES, WHICH INCLUDE PENTRAMETER COVERAGE, USE OF UNSHIMMED PENTRAMETERS FOR WELD BEAD AND RADIOGRAPHIC SIMILARITY OF PENTRAMETER TO WELD BEAD. RESPONSIBILITY: F. OGDEN/4630 - P. HINKELDEY/4640 - ENGINEERING ECD: 07/06/01 CAUSE POST PROOF RADIOGRAPHY PROCESS CONTROLS INADEQUATE FOR SYSTEM COMPLEXITY AND QUANTITY OF AREAS TO BE X-RAYED ROOT CAUSE 2195 ALLI ALLOY IMPLEMENTATION FAILED TO CONSIDER THE PROCESS CONTROL REQUIREMENTS NEEDED TO ADDRESS IMPACT OF SIGNIFICANT INCREASED INSPECTION REQUIREMENTS (REPAIRS & DESIGN) ON POST PROOF RADIOGRAPHIC INSPECTION SYSTEM * TASK II. CORRECTIVE ACTION 1. DUAL INDEPENDENT REVIEW OF MANUAL HAC & EXCEL SPREAD SHEET DATA REPORT. 2. REQUIREMENT MATRIX (REUSABLE & GENERATED BY ME & QE). 3. CONTROLS IMPLEMENTED ON X-RAY FILM AREA (PROD OPS X-RAY). 4. RE-INSTITUTED 35( ANGLE SHOTS EXCEPT FOR OBSTRUCTED AREAS. TASK CLOSED TASK III. CLEARANCE OF EFFECTIVITIES GENERAL ISSUES: ET-102 - CLEARED ON N037982 & N037997 AND IN PFA FRR'S ET-103 - CLEARED NCDS N037983, N051135, & N011518 ET-104 & UP - SEE ATTACHMENT 1 35 DEGREE ANGLE ISSUE: IN WORK, SEE TASK I.H & ATTACHMENT 1 * ET-113 LOX FILM DENSITY UAI, NCD N051237 TASK IV. CAPS CLOSURE SUMMARY TASK OPEN THIS CAPS IS OPEN. SEE TASKS I, III, & IV ATTACHMENT 1 GENERAL ISSUE: ET #REVIEW STATUS NCD# NCD STATUS 93 COMPLETE N037989 CLOSED, UAI 94 COMPLETE N037990 CLOSED, NO DEFECT 102 COMPLETE N037982 CLOSED & EITHER & N037994 UAI OR NO DEFECT 103 COMPLETE N037983 & N051135 CLOSED, UAI 104 COMPLETE N037986 CLOSED, UAI 105 COMPLETE N037987 & N049017 CLOSED, UAI 106 COMPLETE N037988 & N051152 CLOSED, UAI 107 COMPLETE N037984 & N051136 CLOSED, UAI 108 COMPLETE N044332 CLOSED, UAI 109 COMPLETE N037985 & N051104 CLOSED, UAI 110 COMPLETE N039728 CLOSED, UAI 111 COMPLETE N037976 & N039742 CLOSED, NO DEFECT * 35 DEGREE ANGLE ISSUE ET NCD # STATUS 103 N011518 CLOSED, UAI 104 N011519 CLOSED, UAI 105 N042453 CLOSED, UAI 106 N054925 CLOSED, UAI 107 N038134 CLOSED, UAI 108 N055082 CLOSED, UAI 109 N055083 IN WORK 110 N051236 CLOSED, UAI 111 N052454 CLOSED, UAI 112 N055452 (LOX) CLOSED, UAI 113 N034518 (LOX) IN WORK, 114 SEE TASK I, H & LC M270-1657, 1658, 1659 115 & UP SEE TASK I, H & LC M270-1657, 1658, 1659 07/26/2001 - CONTRACTOR SUBMITTED REVISED CLOSED PROBLEM REPORT AS FOLLOWS: GENERAL ------- DURING PREPARATIONS FOR INCORPORATING THE PRODUCTION OPERATIONS NDT WELD LOCATION GUIDE INTO THE 80900000069 ENGINEERING DRAWINGS, IT WAS DETERMINED THAT THE START LOCATION FOR PREVIOUS O-1 X-RAY MEASUREMENT POSITIONING TAPE HAD BEEN MISLOCATED 3.4 INCHES (LOCATION TOLERANCE IS 1 1.0 INCH). THIS POTENTIALLY IMPACTED ADEQUATE POST PROOF FILM COVERAGE OF THE INADEQUATELY PROOFED ZONES AND ROOT/COVER OVERLAP ZONES. REVIEW OF THE PRODUCTION OPERATIONS NDT WELD LOCATION GUIDE SHOWED THAT ALL KNOWN COPIES OF THIS GUIDE INCLUDING THOSE THAT ARE 15 PLUS YEARS OLD SHOWED THE SAME MISLOCATED O-1 START POINT. RESEARCH OF THE MISLOCATED O-1 START POINT ANOMALY IDENTIFIED AREAS OF INADEQUATE FILM COVERAGE ON MULTIPLE TANKS AND THAT THE POST PROOF O-1 WELD ROOT BEAD OVERLAP, +/- 7.5 DEGREE ANGLE X-RAY FILM WAS MISSING FOR ET-111. ADDITIONALLY, REVIEW OF THE OTHER ET-102 POST PROOF FILM REVEALED THE FOLLOWING MISSED REQUIREMENTS: 1. HFF-4 WELD: THE PENETRAMETERS WERE MISLOCATED AND THE PROPER ACCEPTANCE HAD NOT BEEN PERFORMED ON THE FILM. 2. ODG-9 AT 19 INCHES THRU 32-1/4 INCHES: THE "AT RISK" PERPENDICULAR X-RAY FILMS ARE MISSING. 3. ODG-5 AT 100 INCHES THRU 116 INCHES: THE "AT RISK" PERPENDICULAR X-RAY FILMS ARE MISSING. 4. OADC AT 315 INCHES THRU 334-1/2 INCHES: THE REQUIRED FILMS ARE MISSING. NCDS HAVE BEEN GENERATED FOR ET'S 92, 93, AND 102 THRU 111 ON EVERY X- RAY ISSUE FOUND TO DATE (3-17-2000). AS OTHER ITEMS HAVE BEEN FOUND APPROPRIATE NONCONFORMANCE DOCUMENTATION WAS GENERATED. AS THE RESULT OF A MEETING CHAIRED BY PRODUCT ASSURANCE AND ATTENDED BY TECHNICAL OPERATIONS, MANUFACTURING ENGINEERING, PRODUCTION OPERATIONS AND MISSION SUCCESS THE LISTED ACTION ITEMS WERE ESTABLISHED. ATTENDEES: --------- PRODUCT ASSURANCE P. POWELL, D. WESTPHAL, D. OWENS, T. MCKEOUGH, & W. MATTHEESSEN TECHNICAL OPERATIONS P. HINKELDEY & D. BOLSTAD MANUFACTURING ENGINEERING R. WHITE & R. WEAVER PRODUCTION OPERATIONS D. LINCOLN & P. THERRIEN MISSION SUCCESS E. HORAK GENERAL CONTINUED ----------------- DURING A POST PROOF LOX TANK X-RAY INSPECTION (ET-113) AN X-RAY TECHNICIAN DETERMINED THAT ON THE O-5 WELD, THE WELD REPAIR 35 DEGREE ANGLE SHOTS COULD NOT BE PERFORMED. ON THE FORWARD (+35) SHOT THERE EXISTS INTERFERENCE WITH SUPPORT TOOLING. A REVIEW SHOWED THAT OTHER WELDS HAVE INTERFERENCE PROBLEMS OF VARIOUS TYPES. THESE CAN BE BROKEN DOWN INTO SEVERAL BROAD CLASSES: 1. PHYSICAL INTERFERENCE DUE TO OTHER FLIGHT HARDWARE. 2. PHYSICAL INTERFERENCE DUE TO REQUIRED SUPPORT TOOLING. 3. METAL THICKNESS THAT DOES NOT ALLOW ALL REQUIRED FILM ELEMENTS (PENETRAMETERS, X-RAY TAPE, AND BOTH FACES OF THE WELD) TO BE RECORDED ON THE SAME PIECE OF 70MM FILM. 4. GEOMETRY & THICKNESSES THAT MAKE THE RADIOGRAPH DIFFICULT TO INTERPRET. DURING THE INSPECTION OF ET-113 LOX TANK AN AREA OF FILM DENSITY BEING INCORRECT WAS FOUND. THIS WAS DOCUMENTED & DISPOSITIONED UAI ON NCD N051237. TASK I. FAILURE INVESTIGATION --------------------- A. PERFORM AND DOCUMENT A DETAILED STEP BY STEP PROCESS FLOW OF THE X-RAY PROCESSES FROM ENGINEERING REQUIREMENTS TO ARCHIVAL STORAGE OF THE FILM. RESPONSIBILITY: W. MATTHEESSEN/3741 - D. WESTPHAL/3740 - RELIABILITY ASSURANCE D. LOWE/4420 - P. HINKELDEY/4640 - TECHNICAL OPERATIONS R. WHITE/3614 - R. WEAVER/36 - MANUFACTURING ENGINEERING C. CLAUSS/3623 - J. STANLEY/3620 - X-RAY OPERATIONS S. MCEVOY/3742 - D. WESTPHAL/3740 - QUALITY NDE C. CULVER/3743 - D. WESTPHAL/3740 - QUALITY ENGINEERING G. CROMER/3743 - D. WESTPHAL/3740 - HAC ECD: 3/31/00 COMPLETE: 3/29/00 CLOSURE STATEMENT: ----------------- PROCESS HAS BEEN REVIEWED AND FLOW CHARTS GENERATED. REF.: CAPS S-083_ATT2_ X-RAY PROCESS FLOW.PDF , ATTACHED. B. PERFORM AN ASSESSMENT OF THE X-RAY PROCESS DOCUMENTED IN TASK I.A. TO DETERMINE THE MATCH WITH COMMAND MEDIA. RESPONSIBILITY: J. RUSSELL/4210 - D. CALLAN/4210 - W. SIGUR/4010 - TECHNICAL OPERATIONS ECD: 4/14/00 COMPLETE: 4/5/00 CLOSURE STATEMENT: ------------------ FOUR FINDINGS WERE FOUND: #1: THE CURRENT PRACTICES RELATED TO SECURITY AND CONTROLLED ACCESS TO X-RAY FILMS DO NOT MEET THE REQUIREMENTS OF THE COMMAND MEDIA. #2: THE LEVEL OF INSTRUCTIONS AND DETAIL CONTAINED IN THE PRODUCTION PROCESS DATABASE (PPD) FOR IMPLEMENTATION OF STP-2503 IS INADEQUATE TO CONTROL THE WORK AND SURE "STAMP WARRANTY" IS MAINTAINED. #3: THE PROCESS OF GENERATING THE HARDWARE ACCEPTANCE COMMITTEE (HAC) SUMMARY FOR EACH ET IS SUBJECT TO A SINGLE POINT FAILURE THAT CAN RESULT IN A WELD HEAT REPAIR NCD NOT BEING INCLUDED IN THE FINAL REPORT. MISSING SUCH AN NCD WILL RESULT IN NEEDED POST-PROOF X-RAYS NOT BEING ACCOMPLISHED. #4: THE LOCATION AND IDENTIFICATION OF X-RAY FILM STRIPS IS SUBJECT TO A SINGLE POINT FAILURE. THE FILM POSITION ON A WELD CAN BE IN ERROR. REF.: CAPS_S-083_IB_ATTACHMENT.DOC C. EVALUATE THE COMPLETE PROCESS FROM TASK I.A, AND BY INCORPORATING ANY RESULTING AUDIT FINDINGS FROM TASK I.B, THE PROCESS OWNERS ARE TO OPTIMIZE THE X-RAY PROCESS AND MAKE IT NO FAIL. RESPONSIBILITY: W. MATTHEESSEN/3741 - D. WESTPHAL/3740 - RELIABILITY D. LOWE/4420 - P. HINKELDEY/4640 - ENGINEERING R. WHITE/3614 - R. WEAVER/3614 - MANUFACTURING ENGINEERING C. CLAUSS/3623 - J. STANLEY/3620 - X-RAY OPERATIONS S. MCEVOY/3742 - D. WESTPHAL/3740 - QUALITY NDE C. CULVER/3743 - D. WESTPHAL/3740 - QUALITY ENGINEERING G. CROMER/3743 - D. WESTPHAL/3740 - HAC ECD: 4/28/00 - ASSUMES PARTIAL IN PARALLEL ACTIVITY WITH TASK I.B. ECD: 6/30/00 - INITIAL SCOPE OF WORK WAS UNDER ESTIMATED. ECD: 12/22/00 - INCREASED SCOPE OF WORK. ECD: 7/31/01 - INCREASED SCOPE OF WORK COMPLETED: 1/24/01 CLOSURE STATEMENT ----------------- BOTH CORRECTIVE ACTIONS AND A SERIES OF RECOMMENDED PROCESS ENHANCEMENTS WERE PRESENTED TO A MANAGEMENT TEAM CONSISTING OF THE COGNIZANT MANAGERS. ALL CORRECTIVE ACTIONS HAD BEEN IMPLEMENTED PRIOR TO THE NEQA AUDIT. CORRECTIVE ACTIONS (IMPLEMENTED): 1. DUAL INDEPENDENT REVIEW OF MANUAL HAC & EXCEL SPREAD SHEET DATA REPORT 2. REQUIREMENT MATRIX (REUSABLE & GENERATED BY ME & QE) 3. CONTROLS IMPLEMENTED ON X-RAY FILM AREA (PROD OPS X-RAY) 4. RE-INSTITUTED 35 DEGREE ANGLE SHOTS EXCEPT FOR OBSTRUCTED AREAS *5. INSTITUTED A TRAINING CLASS FOR WELD LOCATION TAPE INSTALLATION & VERIFICATION (G-64) PROCESS IMPROVEMENT RECOMMENDATIONS: ------------------------------------ 1. ENHANCE NCD SYSTEM TO IMPROVE INFORMATION RETRIEVABILITY & ALLOW FOR AUTOMATION OF HAC & REQUIREMENT MATRIX. 2. AUTOMATE THE HAC REPORT, SHOULD ALLOW FOR THE AUTOMATIC GENERATION OF REQUIREMENT MATRIX. 3. AUTOMATE THE GENERATION OF THE REQUIREMENT MATRIX. THIS SHOULD MIMIC THE PRESENT MATRIX. 4. ENHANCE ACCESS AND CONTROL OF FILM STORAGE AND TECHNIQUE SHEET. 5. EVALUATE 8090...069 TO IMPROVE CLARITY & EASE OF USE. 6. ENHANCED LONG TERM STORAGE CONTROLS INCLUDING DIGITIZATION OF RADIOGRAPHS & DIGITAL X-RAY. 7. EVALUATE THE ELIMINATION OF ARBITRATION IN PRE-PROOF X-RAYS. REF.: W. G. MATTHEESSEN PRESENTATION AND MEETING MINUTES OF 10/24/00 MEETING. D. PERFORM A MANAGEMENT LEVEL REVIEW AND OVERSIGHT OF TASKS I.A THRU I.C WITH NASA. RESPONSIBILITY: E. HORAK/3000 ECD: 4/28/00 - EXTENSION OF I.C TASKS ECD: 7/15/00 ECD: 12/22/00 - INCREASED SCOPE OF WORK. ECD: 7/31/01 - INCREASED SCOPE OF WORK CANCELED 1/31/01 CANCELLATION RATIONALE ---------------------- BASED ON THE NASA NEQA AUDIT AND PROCESS OWNERS' REVIEW OF TASK I.C, THIS TASK IS NO LONGER REQUIRED. SUBJECT ITEMS HAVE BEEN REVIEWED WITH NASA PROJECT INCREMENTALLY AS IMPLEMENTATION WAS BEING ACCOMPLISHED. E. SEARCH FOR AND IDENTIFY NCDS WHICH HAD PREVIOUS INCIDENCES OF MISSED OR MISSING X-RAY FILM OR X-RAY REQUIREMENTS. RESPONSIBILITY: D. DONNELLY/3741- D. WESPHAL/3740 N. GILLIAM/3712 - G. WHEELER/3710 ECD: 3/29/00 COMPLETE: 4/4/00 CLOSURE STATEMENT: ------------------ A REVIEW WAS CONDUCTED OF NCD HISTORY, NASA DISCREPANCY REPORTS, AND SPECIAL INVESTIGATIONS (SI). IN 1988 MAJOR CHANGES TOOK PLACE IN THE X-RAY PROCESS AS A RESULT OF TD-808. SINCE THAT TIMES THE MAJOR ISSUE OF MISSING X-RAY FILM HAS BEEN WITH THE SUPPLIERS. OTHER AREAS HIGHLIGHTED ARE FROM PLANNING ERRORS AND WELD REPAIRS THAT ALLOWED MISSED FILM. THE SIS SHOWED AREAS OF CONCERN ON PLANNING AND REQUIREMENTS THAT WERE FIXED WITH SYSTEM TYPE CORRECTIVE ACTIONS. OF NOTE IS THE CHANGE FROM AN AUTOMATED HAC REPORT FROM THE LWT TANKS TO A MANUAL HAC ON SUPER LWT. A NASA DISCREPANCY REPORT DOCUMENTED A PLANNING ERROR. THESE ISSUES WILL BE INCORPORATED IN TO THE TASK I.C REVIEW. REF.: CAPS S-083 TASK I.E REPORT. F. REVIEW ALL LO2 AND LH2 TANKS FOR ADEQUATE POST PROOF FILM COVERAGE. STARTING WITH ET-102, THEN CONTINUING WITH ET-103 THRU 111, ET-93 AND ET-94. RESPONSIBILITY: D. LOWE/4420 - P. HINKELDEY/4640 - ENGINEERING C. CLAUSS/3623 - J. STANLEY/3620 - X-RAY OPERATIONS S. MCEVOY/3742 - D. WESTPHAL/3740 - QUALITY NDE G. CROMER/3743 - D. WESTPHAL/3740 - HAC COMPLETE: 5/16/00 CLOSURE STATEMENT: ------------------ ATTACHMENT #1 LISTS THE NCDS GENERATED, STATUS, & DISPOSITION. G. REVIEW ET-102 & 103 ORIGINAL WELDS FOR ADEQUATE FILM COVERAGE. RESPONSIBILITY: C. CLAUSS/3623 - J. STANLEY/3620 - X-RAY OPERATIONS S. MCEVOY/3742 - D. WESTPHAL/3740 - QUALITY NDE W. MATTHEESSEN/3741 - D. WESTPHAL/3740 - RELIABILITY ASSURANCE COMPLETE: 3/24/00 NO ISSUES PER DISCUSSION WITH PA-NDT SUPERVISION. H. PROVIDE FLEET CLEARANCE RATIONALE AND PRODUCTION CLEARANCE FOR THE 35 DEGREE ANGLE ISSUE. RESPONSIBILITY: E. SWEET/4400 D. BOLSTAD/4600 ECD: 6/23/00 ECD: 12/22/00 -- INCREASED SCOPE OF WORK. ECD: 1/31/01 - INCREASED SCOPE OF WORK ECD: 5/11/01 - INCREASED SCOPE OF WORK * COMPLETE: 5/11/01 * CLOSURE STATEMENT: ----------------- SEE ATTACHMENT #1, 35 DEGREE ISSUE ALL WERE UAI. * I. IMPLEMENT THE PROCESS IMPROVEMENT RECOMMENDATION TASKS GENERATED IN TASK I.C. 1. ENHANCE NCD SYSTEM TO IMPROVE INFORMATION RETRIEVABLY. RESPONSIBILITY: D. O'NEAL/3744 - D. WESTPHAL/3740 - MRB ECD: 4/30/01 TRANSFERRED: 7/23/01 TO SI-2001-S005 2. ENHANCE ACCESS AND CONTROL OF FILM STORAGE AND TECHNIQUE SHEET CONTROL. RESPONSIBILITY: C. CLAUSS/3623 - M. MCGEHEE/3620 - X-RAY OPERATIONS ECD: 6/29/01 TRANSFERRED: 7/23/01 TO SI-2001-S005 3. EVALUATE 8090069 TO IMPROVE CLARITY & EASE OF USE. RESPONSIBILITY: W. SIGUR/4010 - TECH OPS ECD: 6/29/01 TRANSFERRED: 7/23/01 TO SI-2001-S005 4. ENHANCED LONG TERM STORAGE CONTROLS. RESPONSIBILITY: C. CLAUSS/3623 - M. MCGEHEE/3620 - X-RAY OPERATIONS R. BESIN/3711 - G. WHEELER/3710 - QUALITY OPERATIONS MANAGEMENT ECD: 6/29/01 EXTENSION: 9/30/01 - MANAGERIAL REVIEW OF BUDGETS TRANSFERRED: 7/23/01 TO SI-2001-S005 TASK TRANSFERRED ---------------- THESE TASKS ARE ENHANCEMENTS ONLY TO IMPROVE THE CURRENT SYSTEM AND WILL BE TRACKED ON SI-2001-S005 * J. CONDUCT AN EVALUATION OF THE TASKS GENERATED IN TASK I.C. 1. ENHANCE NCD SYSTEM TO ALLOW FOR AUTOMATION OF HAC & REQUIREMENT MATRIX. 2. AUTOMATE THE HAC REPORT, SHOULD ALLOW THE AUTOMATIC GENERATION OF REQUIREMENT MATRIX. 3. AUTOMATE THE GENERATION OF THE REQUIREMENT MATRIX. THIS SHOULD MIMIC THE PRESENT MATRIX. RESPONSIBILITY: C. CULVER/3743 - D. WESTPHAL/3740 - QUALITY ENGINEERING ECD: 3/07/01 COMPLETE: 3/7/01 CLOSURE STATEMENT: ------------------ THERE IS NO BENEFIT TO GENERATE AN AUTOMATED HAC & REQUIREMENT MATRIX BEFORE THE IMPLEMENTATION OF PMES. REF. C. CULVER EMAIL DATED 3/7/01 4. ENHANCED LONG TERM STORAGE INCLUDING DIGITIZATION OF RADIOGRAPHS & DIGITAL X-RAY. RESPONSIBILITY: W. SIGUR/4010 - TECH OPS ECD: 6/29/01 TRANSFERRED: 7/23/01 TO SDS 3770 5. EVALUATE THE ELIMINATION OF ARBITRATION IN PRE-PROOF X-RAYS. RESPONSIBILITY: D. WESTPHAL/3740 - QUALITY NDE ECD: 3/16/01 ECD: 05/04/01 ECD: 06/04/01 TRANSFERRED: 7/23/01 TO SI-2001-S005 TRANSFERRED STATEMENT: ---------------------- BASIC PROCEDURE HAS BEEN ESTABLISHED AND STANDARD PROCEDURES ARE IN THE PROCESS OF BEING REVISED. * K. REVISE STPS & 8090...069 TO INCORPORATE CHANGES FOR 35 DEGREE ANGLE SHOTS ISSUES & PENTRAMETER ISSUES, WHICH INCLUDE PENTRAMETER COVERAGE, USE OF UNSHIMMED PENTRAMETERS FOR WELD BEAD AND RADIOGRAPHIC SIMILARITY OF PENTRAMETER TO WELD BEAD. RESPONSIBILITY: F. OGDEN/4630 - P. HINKELDEY/4640-ENGINEERING ECD: 07/06/01 TRANSFERRED 7/23/01 TO SI 2001-S005 TASK TRANSFERRED ---------------- THE STPS & 809069 HAVE BEEN REVISED TO INCORPORATE ALTERNATIVE ANGLE SHOTS, (H36809-534, 533, 240, & 463). THE OTHER X-RAY ISSUES UNTIL RESOLVED WILL BE WORKED ON A CASE BY CASE BASIS ON NCDS. THUS THESE TASKS ARE ENHANCEMENTS ONLY TO IMPROVE THE CURRENT SYSTEM AND WILL BE TRACKED ON SI-2001-S005 CAUSE ----- POST PROOF RADIOGRAPHY PROCESS CONTROLS INADEQUATE FOR SYSTEM COMPLEXITY AND QUANTITY OF AREAS TO BE X-RAYED ROOT CAUSE 2195 ALLI ALLOY IMPLEMENTATION FAILED TO CONSIDER THE PROCESS CONTROL REQUIREMENTS NEEDED TO ADDRESS IMPACT OF SIGNIFICANT INCREASED INSPECTION REQUIREMENTS (REPAIRS & DESIGN) ON POST PROOF RADIOGRAPHIC INSPECTION SYSTEM TASK II. CORRECTIVE ACTION ----------------- 1. DUAL INDEPENDENT REVIEW OF MANUAL HAC & EXCEL SPREAD SHEET DATA REPORT. 2. REQUIREMENT MATRIX (REUSABLE & GENERATED BY ME & QE). 3. CONTROLS IMPLEMENTED ON X-RAY FILM AREA (PROD OPS X-RAY). 4. RE-INSTITUTED 35 DEGREE ANGLE SHOTS EXCEPT FOR OBSTRUCTED AREAS. TASK CLOSED ----------- TASK III. CLEARANCE OF EFFECTIVITIES GENERAL ISSUES: ET-102 - CLEARED ON N037982 & N037997 AND IN PFA FRR'S ET-103 - CLEARED NCDS N037983, N051135, & N011518 ET-104 & UP - SEE ATTACHMENT 1 35 DEGREE ANGLE ISSUE: ET-103 & UP - SEE ATTACHMENT 1 ET-113 LOX FILM DENSITY UAI, NCD N051237 * TASK IV. CAPS CLOSURE SUMMARY -------------------- MULTIPLE CONCERNS WERE NOTED IN THE PRESSURE VESSEL POST PROOF X-RAY PROCESS. THESE CONCERNS INCLUDED AREAS OF MISSED REQUIREMENTS (AREAS OF COVERAGE), FILM DOCUMENTATION, FILM ACCEPTANCE, AND FILM STORAGE. AN EXTENSIVE REVIEW WAS PERFORMED BY A MULTI-DISCIPLINARY TEAM. A SECOND MULTI-DISCIPLINARY TEAM WAS FORMED TO REVIEW THE APPROPRIATE COMMAND MEDIA. THESE WERE COMBINED BY THE ORIGINAL MULTI-DISCIPLINARY TEAM AND SEVERAL AREAS OF CONCERN WERE NOTED AND DOCUMENTED. CORRECTIVE ACTIONS AND ENHANCEMENTS WERE PRESENTED TO MANAGEMENT (TASK C). IN ADDITION, ALL VEHICLES WERE CLEARED (SEE APPENDIX 1). ATTACHMENT 1 GENERAL ISSUE: ------------- ET #REVIEW STATUS NCD# NCD STATUS -------------------------------------- 93 COMPLETE N037989 CLOSED, UAI 94 COMPLETE N037990 CLOSED, NO DEFECT 102 COMPLETE N037982 CLOSED & EITHER & N037994 UAI OR NO DEFECT 103 COMPLETE N037983 & N051135 CLOSED, UAI 104 COMPLETE N037986 CLOSED, UAI 105 COMPLETE N037987 & N049017 CLOSED, UAI 106 COMPLETE N037988 & N051152 CLOSED, UAI 107 COMPLETE N037984 & N051136 CLOSED, UAI 108 COMPLETE N044332 CLOSED, UAI 109 COMPLETE N037985 & N051104 CLOSED, UAI 110 COMPLETE N039728 CLOSED, UAI 111 COMPLETE N037976 & N039742 CLOSED, NO DEFECT 35 DEGREE ANGLE ISSUE --------------------- ET NCD # STATUS ------------------------ 103 N011518 CLOSED, UAI 104 N011519 CLOSED, UAI 105 N042453 CLOSED, UAI 106 N054925 CLOSED, UAI 107 N038134 CLOSED, UAI 108 N055082 CLOSED, UAI 109 N055083 CLOSED, UAI 110 N051236 CLOSED, UAI 111 N052454 CLOSED, UAI 112 N055452 (LOX) CLOSED, UAI 113 N034518 (LOX) CLOSED, UAI 114 H36809-534, 533, 240, & 463 * 115 & UP H36809-534, 533, 240, & 463 * * LIAISON CALL VS BUILD ENGINEERING ----------------------------------- EFFECTIVITY LIAISON STATUS IMPLEMENTING COMMENTS (ET) CALL ENGINEERING ------------------------------------------------------------------- 108 M270-1659 CLOSED(12/19/00) H36809-534 (12/9/00) PRE PROOF (STP5509) N/A M270-1658 CLOSED(12/19/00) H36809-533 (12/19/00) PRE PRO0F (STP5508) N/A M270-1657 CLOSED (8/17/00) H36809-240 (8/17/00) PRE PROOF (STP5507) 114 M270-1663 CLOSED (8/17/00) H36809-464 (8/17/00) POST PROOF (80969) |
| MSFC Response/Concurrence 10/31/2000 - BOARD ACCEPTS POA UNTIL 12/22/2000 PER RATIONALE B: WORST CASE MANIFESTATION OF THE PROBLEM IS NOT A FMEA CRITICALITY 1 EFFECT. CRIT 3 NO SIGN-OFF SIGNATURES NEEDED. 01/30/2001 - BOARD ACCEPTS POA UNTIL 3/26/2001 PER RATIONALE (B): THE PROBLEM CONDITION IS CLEARLY SCREENED DURING PRELFIGHT CHECKOUT OR SPECIAL TESTS. 03/29/2001 - REOPENED PROBLEM REPORT DUE TO MSFC APPROVED DEFER UNTIL DATE HAS PASSED. 04/11/2001 - BOARD ACCEPTS POA UNTIL 6/30/2001 PER RATIONALE (B): THE PROBLEM CONDITION IS CLEARLY SCREENED DURING PREFLIGHT CHECKOUT OR SPECIAL TEST. 07/09/2001 - BOARD ACCEPTED PLAN OF ACTION UNTIL 8/30/2001 PER RATIONALE (B): THE PROBLEM CONDITION IS CLEARLY SCREENED DURING PREFLIGHT CHECKOUT OR SPECIAL TESTS. 08/30/2001 - PROBLEM REPORT REOPENED SINCE DEFERRAL DATE PASSED. 10/23/2001 - CAPS CLOSURE ACCEPTED. SIGNATURES ON FILE IN THE PAC. |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A17568 | IFA# -- | Contractor RPT# S-083 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# STP 2503 | Asmnt Part Name RADIOGRAPHIC INSPECT | Asmnt Serial/Lot# N/A |
| HCRIT CD 1 | FCRIT CD 3 | CAUSE CD MP - MFG-PRC | FAIL MODE UC - UNSAT |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |