Leading edge specimens are required for performance testing in a high heat flux test facility.  The leading edges (LE) will be fabricated as carbon-carbon (C-C) composites machined to final part dimensions.  Two different fiber architectures are required, but each leading edge involves the use of an unbalanced carbon fabric with different fibers in the warp and fill directions.  The supplier must 1) procure the fabric, 2) assemble the fabric layup, 3) fabricate the carbon-carbon composite using a pitch matrix (or equivalent) using a high graphitization temperature, and 4) machine the parts to final dimensions.  To insure highest possible thermal conductivity, carbon-carbon

composites shall be fabricated using a combination of pitch matrix densification and chemical vapor infiltration (CVI) process.  CVI shall also be formed on post-machined parts to enhance mechanical strength of leading edge components.  Coatings are not required.  The supplier will deliver a total of four (4) LE specimens, two (2) of each architecture, with each LE specimen eighteen (18) inches in width.  The supplier will also deliver a total of four (4) flat panels, two (2) of each architecture, for material property testing and subsequent laboratory environment coating evaluations.

Table 1 lists the specifications to be used by the supplier in procuring the fabric.

Table 1.  Preform construction for C-C leading edge specimens.

| Fabric No. 1 | 0/90 K321/T300 3:1 5HS |  |  |  |
| --- | --- | --- | --- | --- |
|  | Fiber Type | Tow Size | Ends/Inch | Direction |
|  | K321 (or P-30X) | 2k | 22.5 | Warp |
|  | T-300 | 3k | 10.5 | Fill |
|  | Fabric Style | 5 HS |  |  |
|  | Areal Weight | > 368 g/m2 |  |  |
| Fabric No. 2 | 0/90 T300 1:1 5HS |  |  |  |
|  | Fiber Type | Tow Size | Ends/Inch | Direction |
|  | T-300 | 3k | 16 | Warp |
|  | T-300 | 3k | 16 | Fill |
|  | Fabric Style | 5 HS |  |  |
|  | Areal Weight | > 252 g/m2 |  |  |
| Tape | 0° K321 |  |  |  |
|  | Fiber Type | Tow Size | Ends/Inch | Direction |
|  | K321 (or P-30X) | 2k | 22.5 | 0° |
|  | Areal Weight | > 285 g/m2 |  |  |

Details and totals for the fabric area requirements are provided in Table 2 below.  The details of the C-C parts and processing are provided in Table 3 below.

Table 2.  Fabric and tape area requirements for construction of C-C leading edge specimens and property panels.

| Fabric No. 1 | K321/T300 3:1 5HS |  |
| --- | --- | --- |
| Part | LE Specimen 1 | Material Property Panel 1 |
| Part Planar Dimensions (inches) | 18 x 5 | 10 x 10 |
| Warp Width (inch) | 18 | 10 |
| Part Thickness (inch) | 0.51 | 0.2 |
| Plies Req'd (#) | 35 | 14 |
| Fabric Planar Dimensions (inches) | 18 x 5 | 10 x 10 |
| Ply Area (in2) | 90 | 100 |
| Area/Part | 3,150 | 1,400 |
| Total Parts (#) | 2 | 2 |
| Total Ply Area (in2) | 6,300 | 2,800 |
| Total Req'd Fabric Area (in2) | 9,100 | K321/T300 4:1 5HS |
| Fabric No. 2 | T300 1:1 5HS |  |
| Part | LE Specimen 2 | Material Property Panel 2 |
| Part Planar Dimensions (inches) | 18 x 5 | 10 x 10 |
| Warp Width (inch) | 18 | 10 |
| Part Thickness (inch) | 0.51 | 0.2 |
| Fabric Planar Dimensions (inches) | (5+18)/(2^0.5) x (5+18)/(2^0.5) | 10*(2^0.5) x 10*(2^0.5) |
| Plies Req'd (#) | 26 | 10 |
| Ply Area (in2) | 265 | 200 |
| Area/Part | 6,877 | 2,000 |
| Total Parts (#) | 2 | 2 |
| Total Ply Area (in2) | 13,754 | 4,000 |
| Total Req'd Fabric Area (in2) | 17,754 | T300 1:1 5HS |
| Tape | 0° K321 |  |
| Part | LE Specimen 2 | Material Property Panel 2 |
| Part Planar Dimensions (inches) | 18 x 5 | 10 x 10 |
| Warp Width (inch) | 18 | 10 |
| Part Thickness (inch) | 0.51 | 0.2 |
| Plies Req'd (#) | 26 | 10 |
| Fabric Planar Dimensions (inches) | 18 x 5 | 10 x 10 |
| Ply Area (in2) | 90 | 100 |
| Area/Part | 2,340 | 1,000 |
| Total Parts (#) | 2 | 2 |
| Total Ply Area (in2) | 4,680 | 2,000 |
| Total Req'd Tape Area (in2) | 6,680 | K321/T300 4:1 5HS |

Table 3.  C-C leading edge and property panels part and processing requirements.

Figure 1 provides finished part dimensions for the leading edge specimens.  The cutting plan for the material property testing panel is included for reference as Figure 2.  The supplier should machine one of the two flat material property panels of each fiber architecture.  NASA LaRC will use the second flat material property panel for high temperature coating evaluations.

The list of contract deliverables is itemized in Table 4.

# Sharp Passive Leading Edge Geometry

# Tip Region Close-up

Figure 2.  	Cutting plan to be used to machine material property specimens from one of two flat C-C panels made for each fiber architecture.

Table 4.  List of contract deliverables.

| Layup Architecture | C-C Parts to be delivered |
| --- | --- |
| (0/90 K321/T300 3:1)35 | 2 LE specimens1 |
| (0/90 K321/T300 3:1)14 | 1-10”x10” flat panel plus 38 coupon specimens2 |
| [(±45 T300/0 K321/-,+45 T300/0 K321)6(±45 T300/0 K321)]S | 2 LE specimens1 |
| [(±45 T300/0 K321/-,+45 T300/0 K321)2(±45 T300/0 K321)]S | 1-10”x10” flat panel plus 38 coupon specimens2 |

1  Final part geometry is detailed in Figure 1.  Width of each LE specimen is 18 inches.

2  Coupons to be machined from second 10”x10” using cutting plan of Figure 2.  38 coupon specimens include 9 fill compression, 9 warp compression, 8 warp conductivity, 8 fill conductivity, 2 warp thermal expansion, and 2 fill thermal expansion.

# Text boxes

0.255”

L=2.5°

u=4°

4.001”

0.864”

Max thickness = 0.51”

0.028”

Figure 1.  Finished part geometry of C-C LE specimens.  Final width of each specimen is 18 inches.

Note: Detailed machine drawings for contractor compliance in machining leading edge specimens will be supplied by government prior to contractor machining.

0.06 “