MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A06911 | In-Flight Anomaly Number -- | Contractor Report Number S-061 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title PEAKING AND MISMATCH LH2 AND LO2 WELDS |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (5) B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE EXTERNAL TANK | PART# N/A | SER/LOT# N/A | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE LH2 & LO2 TANK | PART# 80904000000 | SER/LOT# N/A | MANUFACTURER MMC |
| Test/Operation M - MFG | Prevailing Condtion F - FUNCTIONAL | F / U UC | Fail Mode UC - UNSAT | Cause MAT - MFG-ASY-EQUP |
| System STRUCTURAL | Defect XN - NA | Material H - WELD | Work Contact C. VOGEL | Fail Date 03/25/1983 |
| Received at MSFC 07/22/1983 | Date Isolated -- | FMEA Reference 1.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text UNK |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 02/10/1995 | CN RSLV SBMT 06/11/1985 | Defer Date -- | Add Date -- | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design J. WHITE | Chief Engineer -- | S & MA D. NEWMAN | Project M. PESSIN | Project MGR -- |
| Approval |
| Design J. NICHOLS | Chief Engineer -- | S & MA D. NEWMAN | Project M. PESSIN | Project MGR -- |
| PAC Assignee G. MILLER | PAC Review Complete GM | MSFC Closure Date 07/29/1985 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: PREVIOUS CAPS S-039 PEAKING & MISMATCH VIOLATIONS ARE A GENERAL PROB ASSOCIATED WITH WELDING IN MANY AREAS, AS A RESULT, A CONSIDERABLE AMOUNT OF EFFORT IS EXPENDED IN MAG-HAMMERING THESE AREAS |
| Contractor Investigation/Resolution CAUSE - TOOLING, PROCEDURES & ENGR'G ARE UNDER INVESTIGATION. 3/5/84 PRB STATUS - THIS IS AN ODD CAPS WHICH WAS OPENED AS A CATCH ALL FOR PEAKING & MISMATCH VIOLATIONS. ALL BUT 5 OF THE NUMEROUS TASKS LISTED ON ADDENDUMS TO THE CAPS HAVE BEEN COMPLETED. MMC EXPECTS TO COMPLETE THESE & CLOSE THE CAPS BY 8-15-84. SINCE GOOD PROGRESS IS BEING MADE, D. NEWMAN/SA32 STATED HE WILL CLEAR THIS DATE WITH THE MSFC ET PROJ MGR WHO HAS BEEN CONCERNED WITH THIS CAPS BEING KEPT OPEN SO LONG 9/6/84 - PRB STATUS, CAPS IS FOR FOR TRACKING PURPOSES REQUESTED BY JOHN WHITE ACTION ITEM ET-34 TO DISCUSS ACTION NECESSARY TO CLOSE 1/15/85 - ALL TASKS IN THIS CAP ARE CLOSED EXCEPT B-III, PEAKING & MISMATCH. DATA-PLASMA; & BIV - CORRELATION OF BOSORS TO TEST COUPON NEW ESTIMATED COMPLETION DATE AT MMC IS OCT. 1985 PER TD-1012. 3/6/85 STATUSED AT PRB MTG 2-25-85 AS FOLLOWS - PRB QUESTIONS WHY THIS CAPS CANNOT BE CLOSED. PRB ACTION ITEM ET-36 WAS ACCEPTED BY D NEWMAN/MSFC/SA-32 TO INQUIRE INTO CLOSING THIS PROBLEM. 6/5/85 PRB STATUS - 4-16-85 MTG - NOT DISCUSSED IN DETAIL. CAPS IS IN MMC CLOSURE CYCLE. 6/5/85 PRB STATUS 5-16-85 MTG - NOT DISCUSSED IN DETAIL. CAPS IN MMC CLOSURE CYCLE. WILL BE SENT TO MSFC SHORTLY. 6/26/85 INVESTIGATION - TASK I - GENERAL INVESTIGATION INTO THE PEAKING & MISMATCH PROBLEM WAS DIVIDED INTO 2 MAJOR CATEGORIES: CATEGORY A - EFFORTS TO IMPROVE PEAKING & MISMATCH CONTROL. CATEGORY B - EFFORTS TO IMPROVE THE DEFINITION OF TOLERANCES OR TO IMPROVE THE PEAKING & MISMATCH DISCREPANCY REPORTING SYSTEM. CATEGORY A INCLUDED ALL EFFORTS WHICH WOULD BE EXPECTED TO ACTUALLY REDUCE PEAKING & MISMATCHING SEEN IN HARDWARE. CATEGORY B ANALYZED THE REQMNTS THAT THE HARDWARE HAS TO MEET. SUBJECT OF CATEGORY A EFFORTS ARE SET FORTH IN TASK A-I THROUGH TASK A-V, & TASK AX. RESULTS OF THESE INVESTIGATIONS ARE SHOWN BELOW TASK A-I - MSRMNTS WERE TAKEN BY QUALITY PERSONNEL, USING THE AIMS 65, ON THE LO2 TANK O-2 WELD MADE ON THE 5018 FIXTURE TO DETERMINE THE AMOUNT OF PEAKING THAT OCCURS DURING BUILD. RESULTS OF THESE MSRMNTS FOLLOW. THIS TASK COMPLETED 10-30-83. LO2 TANK, 0-2 WELD PEAKING & MISMATCH: BEFORE - TACKING AFFECT OF MANDREL PRESSURE CHANGE ON PEAKING & MISMATCH (AVG'D) BASED ON SAMPLING 20% OF AREA: MAN. PRESSURE 20 PSI 40 PSI PEAKING 2.2 DEG 3.1 MISMATCH .027 INCHES .014 TRENDING OF PEAKING & MISMATCH (AVG'D OVER 100% OF AREA) DURING WELDING OPERATION OPERATION MAN. PRESSURE PEAKING MISMATCH AFTER TACK 40 PSI 2.5 DEG .008 IN. AFTER SEAL 40 PSI 4.2 DEG .012 IN. AFTER PEN 40 PSI 6.7 DEG .015 IN. AFTER FILL 0 PSI 7.1 DEG .020 IN. RESULTS OF PEAKING VS. MANDREL PRESSURE 0-2 WELD: MANDREL PR LWT AVG PEAKING AVG MISMATCH (SEAL, PEN, FILL) 14 9.2 DEG .019 IN. 50,60,60 PSI 15 7.2 DEG .018 IN. 45,20,20 PSI 16 5.9 DEG .015 IN. 35,20,20 PSI TASK A-II - PEAKING & MISMATCH DATA BANK - TO BE ABLE TO MONITOR TRENDS A PROGRAM WAS GENERATED TO MONITOR PEAKING & MISMATCH ON THE 5018 & 5019 WELD FIXTURES. DATA WAS OBTAINED & STORED IN THE DATA BANK. THIS TASK WAS COMPLETED 8-1-84. TASK A-III - PEAKING & MISMATCH MSRMNTS - PEAKING & MISMATCH MSRMNTS, INCLUDING A COMPARISON OF COMBINATION GAUGE & COMPUTERIZED GAUGE (AIMS-65), WERE EVALUATED BY QUALITY ENGR'G. PRELIMINARY REPORT RESULTS WERE PUBLISHED IN REPORT 3743-83-140. ADDITIONALLY, A NEW OPERATING MANUAL FOR THE AIMS-65 WAS DEVELOPED & PUBLISHED. ALSO, AN AUTOMATIC PEAK- ING & MISMATCH INSTRUMENT THAT IS INTEGRATED WITH THE MSFC CIRCUMFERENTIAL WELD FIXTURE WAS DEVELOPED. THIS WAS A PORTION OF THE EFFORT UNDER TD-1054. TASK A-IV - CIRCUMFERENTIAL MSRMNTS - MSRMNTS WERE TAKEN ON THE 5018 & 5019 FIXTURES & CIRCUMFER- ENTIAL GROWTH WAS CONFIRMED. THE BARREL CIRCUMFERENCE GREW 0.230 IN. WITH A 20 PSI INCREASE IN MANDREL PRESSURE (INITIAL 20 PSI, FINAL 40 PSI). TASK A-V - PRESENT TOOLING & PROCEDURES - MFR'G ENGR'G DEVELOPED A PLAN FOR IDENTIFYING & EVALUAT- ING POSSIBLE MODS TO EXISTING TOOLING & PROCEDURES TO REDUCE PEAKING & MISMATCH AT THE 5018, 5019, & 5012 (0-1). THIS EFFORT WAS COORDINATED WITH TASKS A-I, A-II, & A-IV & WAS PUBLISHED ON AN INTEROFFICE MEMO 9-15-83. ENGR'G PERFORMED AN ANALYSIS TO ESTABLISH WORSE CAST CONTOUR DEVIATIONS WHICH WOULD RESULT IN A FACTOR-OF-SAFETY OF 1.0 & A MARGIN-OF-SAFETY OF 0.0 (FS = 1.0/MS = 0). THIS TASK WAS COMPLETED & CRITERIA ESTABLISHED PER MEMO 3521-84-108. QUALITY CONTROL PROVIDED STRESS ENGR'G WITH CONTOUR MSRMNTS, & PEAKING & MISMATCH READINGS ALONG THE 0-2 & 0-3 WELDS. THE PHASING OF THE READINGS WAS AFTER HEAT REPAIR & AFTER MAG-HAMMER REPAIR. READINGS WERE TAKEN ON LWT-18, -19, -20, & -21. TASK WAS COMPLETED 7-15-84. QUALITY ENGR'G ADDED STATEMENTS TO THE MPP'S FOR LWT-19, -20, & -21 DIRECTING INSPEC- TION TO MAKE MSRMNTS ON THE FWD & AFT OGIVES FOR CONTOUR ADJACENT TO THE 0-2 WELD, & ON THE AFT OGIVE ADJACENT TO THE 0-3 WELD. MSRMNTS WERE TAKEN USING THE 612.180-IN. RADIUS OSL TEMPLATE EVERY 12 IN. ALONG THE CIRCUMFERENCE & EVERY 2 IN. ALONG THE TEMPLATE. READINGS WERE MADE AFTER HEAT REPAIR & AFTER MAG HAMMERING TO WITHIN DWG PEAKING TOLERANCE OF 6.5 DEGS FOR 0-2 WELD, & 4.7 DEGS FOR 0-3 WELD. STRESS ENGR'G & RELIABILITY ASSURANCE REVIEWED LWT-6 THRU LWT-15 MARS (0-2 & 0-3 WELDS) WITH RESPECT TO PEAKING & MISMATCH CONDITIONS. IT WAS FOUND THAT IN THE ORIGINALLY WELDED CONDITION EXTENSIVE OUT PEAKING WAS FOUND ON THE 0-2 & 0-3 WELDS (EXCEPTION LWT-13, 0-2). NO PROBLEM EXISTS AFTER MAG-HAMMER REPAIRS THIS TASK WAS COMPLETED 8-31-84 & RESULTS WERE PUBLISHED ON MEMO'S 374-84-118 & 3521-84-063. MSFC QUALITY MEASURED CONTOUR, PEAKING, & MISMATCH AT THE 0-2 & 0-3 WELDS ON STATION. CONTOUR MSRMNTS WERE TAKEN USING A 612.180-IN. RADIUS OSL TEMPLATE EVERY 12 IN. ALONG THE CIRCUMFERENCE & EVERY 2 IN. ALONG THE TEMPLATE. PEAKING & MISMATCH READINGS WERE MADE EVERY 6 IN. ALONG THE CIRCUMFERENCE. ACCUMULATED DATA WAS PROVIDED TO MMC STRESS ENGR'G FOR INCLUSION IN THE DATA BASE THIS TASK WAS COMPLETED 7-30-84. MFR'G ENGR'G REVIEWED TOOLING CHANGES ON THE 5018 THAT MAY HAVE AFFECTED CONTOUR, PEAK- ING, & MISMATCH CONDITIONS ON LWT-6 THRU LWT-15 (0-2 & 0-3 WELDS). RESULTS OF THIS REVIEW WERE SUBMITTED TO RELIABILITY ASSURANCE FOR COMPARISON OF TOOLING CHANGES VS. TANK DEFECTS. THIS TASK WAS COMPLETED 9-15-84. TASK AX - ANALYSIS OF MISMATCH ON 0-1 - TOOLING ASSOCIATED WITH THE T03A5012 TOOL WAS INVESTI- GATED TO RESOLVE A SIGNIFICANT MISMATCH PROBLEM ON LWT-26 & LWT-28. THE T03A5012 TOOL WAS INSPECTED & REALIGNED (LOWER MANDREL ALIGNMENT & UPPER MANDREL HEIGHT ALIGNMENT). THE LWT-29 OGIVE MISMATCH WAS CHECKED & FOUND TO BE IN TOLERANCE COMING OFF THE FIXTURE SUBJECT OF CATEGORY "B" EFFORTS ARE SET FORTH IN TASKS B-I THRU B-V RESULTS OF THESE INVESTIGA- TIONS ARE SHOWN BELOW. TASK B-I - PEAKING & MISMATCH DATA & MAG-HAMMER EFFECTS - CURVES SHOWING THE EFFECTS OF PEAKING & MISMATCH ON TIG WELD MECHANICAL PROPERTIES WERE GENERATED UNDER TD 1012. THE EFFECT OF MAG-HAMMERING TO REMOVE PEAKING & MISMATCH WAS ALSO EVALUATED UNDER THE SAME TD. RESULTS OF THESE INVESTIGATIONS WERE DOCUMENTED ON MEMO 3516-83-279. ADDITIONALLY, THE PEAKING & MISMATCH DATA BASE WAS EXTENDED TO THAN 10 DEGS PEAKING & GREATER GREATER THAN 0.090-IN. MISMATCH. COMPLETED 9-15-83. TASK B-II - WELD ACCEPTANCE MANUAL-TIG - A BOSOR5 ANALYSIS FOR 5018 & 5019 WELDS WAS PERFORMED TO ESTABLISH PEAKING, MISMATCH, & STRESS INTERACTION CURVES THIS ANALYSIS WAS COM- PLETED IN MARCH 1983. ALSO, A TIG WELD ACCEPTANCE MANUAL BASED ON FLOW SIZE, STRESS, LOCATION, & PEAKING & MISMATCH VALUES FOR SELECTED WELDS WAS DEVELOPED. THIS WAS COMPLETED 11-30-83 & DOCUMENTED ON B01640. A FEASIBILITY STUDY FOR INCREASING PEAKING & MISMATCH TOLERANCES IN STABILITY CRITICAL AREAS ON 5018 & 5019 WELDS WAS PERFORMED. IT WAS DETERMINED THAT INCREASING TOLERANCES IS FEASIBLE & WAS DOCUMENTED ON MEMO'S 3512-83-070 & 3512-83-087. A WELD ACCEPTANCE MANUAL SHALL BE GENERATED ON REMAINING MAJOR WELDS NOTE: THIS TASK IS CLOSED BASED UPON AN AGREEMENT BETWEEN MSFC & MMC TO CLOSE THIS CAPS & CONTINUE TRACKING PROBLEM ON TD-1012. TASK B-III - PEAKING & MISMATCH DATA-PLASMA - VARIABLE POLARITY PLASMA ARC (VPPA) WELDING CURVES SHALL BE DEVELOPED UNDER TD-1012. CURVES SHALL SHOW THE EFFECTS OF PEAKING & MISMATCH ON WELD MECHANICAL PROPERTIES. NOTE: THIS TASK IS CLOSED BASED UPON AN AGREEMENT BETWEEN MSFC & MMC TO CLOSE THIS CAPS & CONTINUE TRACKING PROBLEM ON TD-1012. TASK B-IV - CORRELATION OF BOSOR5 TO TEST COUPON. NOTE: SAME AS TASK B-III NOTE. TASK B-V - MASS REPORTING SYSTEM - AN INVESTIGATION WAS CONDUCTED INTO THE FEASIBILITY OF MODI- FYING MARS (MARTIN ANOMALY REPORTING SYSTEM) WRITTEN ON PEAKING & MISMATCH PROCEDURES SO AS TO REDUCE OVERALL TIME. THIS RESULTED IN A REVISION TO THE STD REPAIR PROCEDURE (SRI) TO DEFINE WHEN A MARS WRITTEN ON PEAKING & MISMATCH MAY BE PROCESSED AS NON-MRB OR MRB. COMPLETED 7-18-83. RESOLUTION - INVESTIGATION HAS DETERMINED THAT THE PEAKING & MISMATCH VIOLATIONS OF WELD JOINTS WERECAUSED BY INADEQUATE TOOLING, INADEQUATE PROCEDURES, & EXCEEDINGLY TIGHT TOLERANCE. MUCH WORK HAS BEEN DONE TO REDUCE THE INCIDENCE OF PEAKING & MISMATCH WELD VIOLATIONS. INCLUDED ARE: DEVELOPMENTOF A PEAKING & MISMATCH COMPUTERIZED DATA BANK; DEVELOPMENT OF A NEW OPERATING INSTRUCTIONS MANUAL FOR THE USE OF THE AIMS-65 COMPUTERIZED PEAKING & MISMATCH MACHINE; THE 5012 TOOL MANDRELS WERE REALIGNED; & A WELD ACCEPTANCE MANUAL BASED ON FLOW SIZE, STRESS, LOCATION, ETC., WAS DEVELOPED. ALTHOUGH ALL TASKS ASSIGNED ON THIS CAPS HAVE NOT BEEN CLOSED MSFC & MMC AGREED TO CLOSE THIS CAPS & TRACK UNFINISHED TASKS ON TD-1012. RECOMMEND THIS PROBLEM REPORT BE CLOSED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A06911 | IFA# -- | Contractor RPT# S-061 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80904000000 | Asmnt Part Name L02 & LH2 TANKS | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MAT - MFG-ASY-EQUP | FAIL MODE MS - STRUCT |
| Asmnt FMEA 6.2.1.1 | Asmnt FM 1 | FMEA CSE D | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |