03M06/13/07

S725-03M.doc

Use on projects as appropriate.

Section 725. - MISCELLANEOUS MATERIAL

When fiber reinforced Shotcrete is required, include the following. When fiber reinforced concrete is required also include 501, 552, or 601 SCR as applicable.

725.29  Reinforcing Fibers.  Delete the text and substitute the following:

(a) Use with shotcrete.  Fibers will be deformed steel or fibrillated polypropylene conforming to ASTM C 1116, Type I or Type III.

(b) Use with concrete.  Fibers will be fully oriented, 100% virgin polypropylene, collated fibrillated, white in color, 38 mm long, dosed at 0.9 kilograms per cubic meter of concrete, conforming to ASTM C 1116, Type III.