MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A10077 | In-Flight Anomaly Number -- | Contractor Report Number P-053-1 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title GO2 PRESSLINE (S/N 1120) MOISTURE SEEPAGE FROM BELLOWS - ATP/HYDRO |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT 1 | Sys_Lvl N | Misc Codes A (4) B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE ET | PART# 80901000000 | SER/LOT# NOTED | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE GO2 PRESS LINE | PART# PD4800180-090 | SER/LOT# 1120 | MANUFACTURER ARROWHD PROD |
| Test/Operation A - ATP | Prevailing Condtion F - FUNCTIONAL | F / U F | Fail Mode UC - UNSAT | Cause MP - MFG-PRC |
| System PROPULSION | Defect DC - BROKEN | Material H - WELD | Work Contact C. CAMPBELL | Fail Date 03/11/1986 |
| Received at MSFC 06/09/1986 | Date Isolated -- | FMEA Reference 3.4.5 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom MV - EXT LEAK | Time Cycle -- |
| Effectivity Text LWTS 16, 20, 21, 22 AND 24 THRU 54 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 05/07/1992 | CN RSLV SBMT 05/23/1988 | Defer Date -- | Add Date -- | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design P. MULLER | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR P. BRIDWELL |
| Approval |
| Design P. MULLER | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR P. BRIDWELL |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete JE | MSFC Closure Date 06/15/1989 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: A10072 (P-053), A10078 (P-053-2), A10079 (P-053-3), AND A10080 (P-053-4). A GO2 PRESSLINE (PD4800180-090, S/N 1120) EXHIBITED MOISTURE SEEPAGE FROM THE BELLOWS SLIDE JOINT (INCONEL 718) DURING THE DEFLECTION TESTS OF PARAGRAPH 5.3.1P OF ET ATP-180-390. THE MOISTURE WAS OBSERVED AFTER ALL HYDROSTATIC PROOF PRESSURE TESTS WERE COMPLETE THE MOISTURE WAS PRESENT BETWEEN THE 14180-59 TUBE AND 14180-87 BELLOWS ASSEMBLY. THIS TUBE AND BELLOWS ASSEMBLY WERE REMOVED FOR SUBSEQUENT TESTING. LIGHT WEIGHT TANKS AFFECTED ARE 16, 20, 21, 22 AND 24 THROUGH 45 |
| Contractor Investigation/Resolution CAUSE: CRACK IN THE BELLOWS WELD AS A RESULT OF RESIZING OPERATIONS R/C: ADDITIONAL INSPECTION STEPS HAVE BEEN ADDED AFTER RE-ROLLING R/A - EXTERNAL AND INTERNAL LEAK TESTS WERE PERFORMED TO DETERMINE THE ORIGIN OF THE MOISTURE. NO LEAKAGE WAS DETECTED. SUBSEQUENTLY, THE BELLOWS WAS FIXTURED TO ALLOW IT TO BE PRESSURIZED TO 700 PSIG FOR 1 MINUTE AS WAS DONE DURING ACCEPTANCE TESTING. AGAIN NO LEAKAGE COULD BE FOUND. DURING A JOINT VISIT TO THE VENDOR'S FACILITY BY ENGINEERING AND RELIABILITY ASSURANCE, THE LEAKAGE WAS VERIFIED BY BAKING THE ASSEMBLY AND LEAK TESTING WITH HELIUM. SUBSEQUENT DOCUMENTATION AND HARDWARE REVIEW REVEALED THAT THE BELLOWS HAD BEEN RE-ROLLED, WHICH CAUSED CRACKS ALONG THE LONGITUDINAL WELD. THE VENDOR WILL SUBMIT A FAILURE ANALYSIS PLAN FOR APPROVAL BY MAF. THIS WILL OUTLINE A METHOD TO ISOLATE AND IDENTIFY CAUSE FOR THE LEAKAGE 7/15/86 PRB STATUS - FA COMPLETE. DETERMINED TO BE AN ISOLATED CASE DUE TO REROLLING OF THE BELLOWS 8/21/86 PRB STATUS - AFTER HEAT TREATED CONDITION, INSPECT BY VISUAL, PENETRANT AND HELIUM LEAK. DOCUMENT AND USE CLEANING AND HELIUM LEAK TEST PROCEDURE. ECD 10-1-86 9/18/86 PRB STATUS - NO CHANGE FROM ACTION STATED ABOVE EXCEPT A BAKEOUT AFTER CLEANING SHOULD BE INCLUDED. ECD 10-2-86. 10/16/86 PRB STATUS - NO CHANGE EXCEPT ECD IS PROJECTED TO 4-1-88 DUE TO X-RAY REVIEW 2/19/87 PRB STATUS - NO CHANGE 3/19/87 UPDATE - NO CHANGE 3/26/87 PRB STATUS - NO CHANGE 5/28/87 PRB STATUS - LWT 21 IS CLEARED. MCC TO SUBMIT A REVISED CAPS 7/3/87 PRB STATUS - CHANGED LAUNCH CONSTRAINTS ASSIGNMENT FROM 61M TO 61N (STS-39) DUE TO CONSTRAINTS ON LWT 24. THIS ASSIGNMENT HAS BEEN COORDINATED WITH: MR. BRIDWELL - ET PROJECT MANAGER ______________________________ MR. J. NICHOLS - CHIEF ENGINEER ________________________________ 9/15/87 UPDATE (REFERENCE CAPS P-053C): TASK I GENERAL: A G02 PRESSLINE (PD4800180-090), S/N 1120) EXHIBITED MOISTURE SEEPAGE FROM THE BELLOWS SLIDE JOINT (INCONEL 718) DURING THE DEFLECTION TESTS OF PARAGRAPH 5.3.1P OF ET ATP-180-390. THE MOISTURE WAS OBSERVED AFTER ALL HYDROSTATIC PROOF PRESSURE TESTS WERE COMPLETE. THE MOISTURE WAS PRESENT BETWEEN THE 14180-59 TUBE AND 14180-87 BELLOWS ASSEMBLY. THIS TUBE AND BELLOWS ASSEMBLY WERE REMOVED FOR SUBSEQUENT TESTING EXTERNAL AND INTERNAL LEAK TESTS WERE PERFORMED TO DETERMINE THE ORIGIN OF THE MOISTURE. NO LEAKAGE WAS DETECTED. SUBSEQUENTLY, THE BELLOWS WAS FIXTURED TO ALLOW IT TO BE PRESSURIZED TO 700 PSIG FOR 1 MINUTE AS WAS DONE DURING ACCEPTANCE TESTING. AGAIN NO LEAKAGE COULD BE FOUND. DURING A JOINT VISIT OF THE VENDOR'S FACILITY BY ENGINEERING AND RELIABILITY ASSURANCE, THE LEAKAGE WAS VERIFIED BY BAKING THE ASSEMBLY AND LEAK TESTING WITH HELIUM. SUBSEQUENT DOCUMENTATION AND HARDWARE REVIEW REVEALED THAT THE BELLOWS HAD BEEN REROLLED, WHICH CAUSED CRACKS ALONG THE LONGITUDINAL WELD TASK II FAILURE ANALYSIS THE VENDOR WILL SUBMIT A FAILURE ANALYSIS PLAN FOR APPROVAL BY MAF. THIS WILL OUTLINE A METHOD TO ISOLATE AND IDENTIFY CAUSE FOR THE LEAKAGE CLOSURE STATEMENT CONCLUSIONS OF THE FAILURE ANALYSIS ARE: A. THE LEAKAGE WAS CAUSED BY CRACKS IN THE CROWN OF THE WELD. THE CRACKS WERE CREATED BY A REROLLING OPERATION B. THE REROLLING OPERATION WAS DUE TO THE BELLOWS FAILING THE FUNCTIONAL MOTION TEST C. THE WELD WAS NORMAL COLD WORKED AGED INCONEL 718 WELD METAL TASK III CORRECTIVE ACTION A. PROCUREMENT QUALITY WILL, IN CONJUNCTION WITH THE VENDOR, REVIEW ALL DOCUMENTATION ON EXISTING BELLOWS TO DETERMINE IF ANY OTHER UNITS HAVE BEEN REROLLED SIMILAR TO ITEM 2 CANCELLED. REROLL ACTIVITY IS VERY COMMON. ATP WOULD REVEAL ANY DEFECTS RESULTING FROM REROLL ACTIVITY B. AFTER REROLLING OF BELLOWS IN THE FINAL HEAT TREATED CONDITION, INSPECT BY VISUAL, PENETRANT, AND HELIUM LEAK TESTING C. DOCUMENT AND USE A CLEANING AND HELIUM LEAK TEST PROCEDURE WHICH ASSURES PROPER TESTING OF THE BELLOWS. THIS SHOULD INCLUDE A BAKEOUT AFTER CLEANING CLOSURE STATEMENT THE ABOVE ACTIONS WERE ACCOMPLISHED. REFERENCE SCAD-030 ITEM CLOSED D. REVISE ARROWHEAD HELIUM LEAK TEST PROCEDURE (MPQ-109) FOR ENHANCE- MENT OF DWELL TIME OF HELIUM. A MINIMUM DWELL TIME OF 5 MINUTES IS RECOMMENDED CLOSURE STATEMENT MPQ-109, IS AN ARROWHEAD SUBASSEMBLY PROCESSING DOCUMENT AND IS NOT SUBMITTED FOR MAF APPROVAL. FINAL ACCEPTANCE LEAK TESTING, WHICH IS SUBMITTED FOR MAF APPROVAL, IS ACCOMPLSIHED BY ET-ATP-180-390 PARAGRAPH 5.4.1 REQUIRES A MINIMUM DWELL TIME OF 5 MINUTES ITEM CLOSED TASK IV CLEARANCE OF EFFECTIVITIES MAF ACCEPTS THESE FAILURES TO HAVE NO CONSTRAINTS BASED UPON RATIONALE THAT THE FAILURES OCCURRED DURING ATP, WHICH IS DESIGNED TO DETECT THESE TYPES OF DEFECTS. THESE ARE KNOWN AND UNDERSTOOD DEFECTS TASK V CLOSEOUT SUMMARY THE CAUSE OF THE MOISTURE SEEPAGE FROM THE BELLOWS SLIDE JOINT AFTER ATP HYDROSTATIC TEST WAS A CRACK IN THE CROWN OF THE WELD. THE CRACK WAS FORMED WHEN THE BELLOWS WAS REROLLED AFTER FAILING THE FUNCTIONAL MOTION TEST. THE CORRECTIVE ACTIONS TAKEN ARE AFTER REROLLING IN THE FINAL HEAT TREATED CONDITION INSPECT BY VISUAL, PENETRANT, AND HELIUM LEAK TESTING. THE HELIUM LEAK TEST PROCEDURE HAS PROPER CLEANING AND BAKEOUT TO ASSURE PROPER TESTING 5/3/88 - THIS REPORT HAS BEEN DEFERRED FOR STS-26, PER NSTS 07700, VOLUME XI AND NSTS 08126 PARAGRAPH 3.4.1, ITEM C WHICH STATES "PROBLEM CONDITION DOES NOT EXIST IN THE FLIGHT HARDWARE AND IS CLEARLY SCREENED BY ACCEPTANCE TEST, PREFLIGHT CHECKOUT, OR SPECIAL TEST." THE DEFERRAL STATUS HAS BEEN APPROVED BY THE ET PROJECT MANAGER, MR. G.P. BRIDWELL _______________________________ THIS PROBLEM IS CONSIDERED CLOSED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A10077 | IFA# -- | Contractor RPT# P-053-1 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# PD4800180-090 | Asmnt Part Name G02 PRESS LINE | Asmnt Serial/Lot# 1120 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MP - MFG-PRC | FAIL MODE UC - UNSAT |
| Asmnt FMEA 2.2.4.1 | Asmnt FM 1 | FMEA CSE C | FMEA SCSE 2 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |