03M03/29/06

S705-03M.doc

Use on projects as appropriate.

Section 705. - ROCK

705.01  Gabion and Revet Mattress Rock.  Add the following:

(d) Los Angeles abrasion, AASHTO T 96	50% max.

When riprap is specified, include the following:

705.02  Riprap Rock.  Delete lines (a), (b), (c), (d), and substitute the following:

(a) Apparent specific gravity, AASHTO T 85	2.40 min.

(b) Absorption, AASHTO T 85	4.0% max.

(c) Los Angeles abrasion, AASHTO T 96	50% max.

(d) Gradation for the class specified	Table 705-1

When class 7 riprap is specified, include the following:

Table 705-1.  Add the following to Table 705-1:

Table 705-1

Gradation Requirements for Riprap

| Class | Percent of Rock by Mass | Mass (Kg) | Approximate Cubic Dimension (1) (2) (mm) |
| --- | --- | --- | --- |
| 7 | 20 | 4000 to 6500 | 1150 to 1400 |
|  | 30 | 1500 to 4000 | 800 to 1150 |
|  | 40 | 150 to 1500 | 350 to 800 |
|  | 10 (1) | 0 to 150 | 0 to 350 |

(1) Furnish spalls and rock fragments graded to provide a stable dense mass.

(2) The volume of the rock with these cubic dimensions will have a mass approximately equal to the specified rock mass.

(3) Furnish rock with breadth and thickness at least one-third its length.