Package Characteristics:  1206 capacitor

| Feature | Value |
| --- | --- |
| Package Length | 3.33 mm |
| Package Width | 1.65 mm |
| Package Thickness | 0.74 mm |
| End of cap Length | 1.553 mm |
| End of cap Width | 0.631 mm |
| Weight | 0.0202 g |
| CTE | 8.885 ppm/C |
| Layer 1 Metallization | Tin |
| Layer 1 Plating Thickness | 0.007 mm |
| Layer 2 Metallization | Nickel |
| Layer 2 Plating Thickness | 0.012 mm |
| End Cap Base Metal Alloy | Silver |
|  | 0.013 mm |

Top View

End View

End cap cross-section

X-ray					SEM of end cap cross section