Quarterly Report - Public Page

Date of Report: March 15, 2007

Project Title: Dissecting Coating Disbondments

Prepared by:  CC Technologies – A DNV Company

Contact Information:   Mariano Iannuzzi, Thomas Bubenik, Sean Brossia (614-761-1214)

CC Technologies

5777 Frantz Road

Dublin, OH 43017

Email: mariano.iannuzzi@dnv.com

For quarterly period ending:  March 15, 2007

Progress To date:

The main objective of the project is to investigate what causes a given coating to disbond during in-service exposure. A set of variables including, coating chemistry, steel surface chemistry, steel surface roughness and anchor pattern, coating underside chemistry and optical analysis of blister geometries is being investigated to define the critical parameters leading to disbonding. It is expected that the better understanding of the system gained during the project will serve as a stepping stone for developing a field-based methodology aimed to help in the prediction of long-term coating failure.

In this quarter efforts were mainly directed at demonstrating the standardized procedure for characterizing disbonded areas that was presented in the previous report. An intense laboratory investigation was initiated in order to get a detailed understanding of the onset of coating disbondment. The laboratory investigation includes cathodic disbondment tests on aged coal tar and FBE pipe samples and long term exposure of pipe steel coupons in soil electrolytes. On site investigations were also initiated.