SNAP Telescope Metering Structure Analysis

# Executive Summary

A baseline design has been developed for the SuperNova/Acceleration Probe (SNAP) telescope structure, which, combined with the optical elements, forms the optical telescope assembly (OTA).  Finite element modal and stress analyses have been performed to evaluate and refine the design.  These analyses validate the baseline design as a viable configuration.

On-orbit performance goals include the ability to maintain precise and well-controlled spatial relations between all the optical components, subject to thermal variations and the influence of attitude control and other spacecraft accelerations.  This goal is to be met with a minimum of mass and with a minimum of obscuration of the field of view.  Additionally, the support structure must survive the launch acceleration and vibration environment.

The dynamic influences on optics positioning and alignment are minimized and launch loads are tolerated by making the structure stiff.  Thermal distortion effects are minimized by employing materials with near-zero coefficients of thermal expansion, in combination with active thermal control of the structure.  Mass may be traded for stiffness to some extent, with the optimal balance to be determined subject to refined spacecraft requirements.

Figure 1 shows a schematic view illustrating the light paths of the SNAP Telescope.  As currently envisioned, the SNAP telescope employs a three-mirror anastigmat (TMA) configuration1,2,3.  The concave primary mirror and convex secondary mirror are on a common axis, and the folding flat mirror folds the image 90 degrees toward the concave tertiary mirror, which projects the image through a hole in the folding flat mirror onto the flat focal plane.

The current mechanical design configuration is illustrated in Figures 2 and 3 and is summarized in Table 1.  The predominant structural material used throughout is a quasi-isotropic layup of M55J carbon fiber/cyanate ester, with very low in-plane coefficients of thermal expansion.  The primary, secondary, and tertiary mirrors are assumed to be lightweighted ULE glass, while the folding flat mirror is silicon carbide.  The design has a fundamental natural frequency of 39 hertz.  Its total mass is around 497kg, consisting of 147kg of structure supporting 350kg of dead load. Launch load strength safety factors for the telescope structure itself are nearly 40.

Information on the SNAP mission and science are available at the SNAP home page, http://snap.lbl.gov.

## Figure 1-Schematic of SNAP Optics

Figure 2-Telescope design configuration

Figure 3-Telescope design configuration

Table 1-Summary of FEA Model

# Description of the model

Figures 2 and 3 illustrate the complete OTA model.  Table 1 lists particulars of the model.  The entire OTA is supported on six carbon fiber struts mounted to a perfectly rigid base.  These struts will actually mount to the spacecraft assembly, but for this study, the OTA is analyzed independently.

The OTA support struts mount to the triangular bench, 200mm thick, approximately 2m long each side, comprised of face sheets, perimeter and eggcrating made from 2mm thick sheets of carbon fiber.  Figures 4 and 5 show the internal structure of the bench.  Moisture absorption in cyanate ester matrix materials raises concerns for both optical surface contamination and dimensional stability.  Published water diffusion data suggest a maximum lamina thickness of approximately 2mm for a one-month post launch dry-out period, which is consistent with SNAP commissioning plans.

The secondary mirror assembly (SMA) support structure mounts to the corners of the bench.  It is comprised of three legs and a shroud, all constructed of 2mm thick carbon fiber.  The base of each leg includes a larger base section, outside the field of view of the telescope.  The thinner portions of the legs obscure part of the field of view and are therefore as narrow as practical.  To minimize the effects of stray light from the side faces of the legs, they taper from a width of 38mm on the side facing the primary mirror to 19mm on the opposite side.  Figure 6 illustrates this taper and shows bulkheads within the leg sections that raise the frequency of drumhead modes of the sides of the legs.  The legs are 250mm deep.  The SMA itself is represented by a mass dummy supported on six struts (not shown here).

Because of geometric constraints, the SMA support structure must attach to the bench after the primary mirror is installed.  Therefore, it may be a bolt-on assembly.

The inner baffle mounts to the center of the bench.  It is modeled as a simple carbon fiber tube, with the mass of the baffle blades rolled into the mass of the tube.

Below the bench is the lower optics bay, which consists of 2mm thick carbon fiber outer walls and bulkheads, to which are mounted the lower optical elements—tertiary mirror, folding flat mirror, and instrument (focal plane/focal plane shield/spectrograph).

Three startracker mass representations are mounted to the anti-sunward side of the bench.  The startrackers are baselined in this model as Ball Aerospace CT-602’s with light shades.

The SIRU (inertial reference unit) mass dummy is mounted to the lower side of the bench.  It has the mass and size of a Northrop Grumman SIRU-Dual String model.

The focal plane is a hexagonal mass dummy, mounted on six struts to the lower optics bay.  The 10mm thick focal plane shield is in turn kinematically mounted to the focal plane using another six struts.  The spectrograph is integrally installed on the focal plane.

The primary, folding flat, and tertiary mirrors are each modeled using plate elements, with material properties set to simulate thick, lightweighted parts.  These components are intended primarily to be mass representations in the telescope model.  More detailed baseline designs for each of the telescope’s four mirrors have been developed and studied independently.  The mirror studies are discussed separately in the tech note, SNAP-TECH-05007.doc.

Figure 4-Telescope cutaway view

Figure 5-Bench eggcrating

Figure 6-Slice through SMA support leg showing taper

# Performance goals and results

For a Delta IV Medium launch vehicle, minimum natural frequencies for primary structures are 27 Hz axial and 10 Hz lateral, and the minimum natural frequency for secondary structures is 35 Hz, regardless of orientation.  Maximum quasi-static accelerations are 6.5g axial and 2g lateral4.

Figures 7 through 10 illustrate the first four vibration modes of the design.  Natural frequencies are all 39 Hz and higher.  The first, second, and fourth modes are dominated by compliance of the SMA support structure, while the third exhibits some bench deformations.  The fourth mode is a fundamentally rotational mode, which should not be strongly excited under launch conditions.  The first predominantly axial mode has a frequency of 68 Hz.

Due to compliance of the spacecraft, natural frequencies of the OTA installed on the spacecraft will be lower than when it is mounted rigidly, as in this study.  A sufficiently stiff spacecraft and high OTA natural frequencies will ensure that the structure meets launch vehicle frequency requirements.  Preliminary studies with provisional spacecraft designs have shown that the frequency requirements described above can be met with ample margins.

The intent of this study is to analyze the telescope structure itself.  The mirrors, instrument, and other payload items, along with their respective support struts are not modeled in detail, and stresses in these elements are not examined in this model.  Under quasi-static accelerations of 6.5 g axial or 2 g lateral, worst-case principal stresses in the carbon fiber telescope structure show a factor of safety of 37 against material failure.  This indicates that designing for high natural frequencies results in an extremely strong structure.

Figure 7-First Mode, 39 Hz

Figure 8-Second Mode, 40 Hz

Figure 9-Third Mode, 44 Hz

Figure 10-Fourth Mode, 44 Hz

# Conclusion

A baseline design for the SNAP telescope structure has been developed and shown to meet basic launch requirements.  Input from industry is warranted to further examine many issues, including manufacturability, integration, and spacecraft interactions.

## REFERENCES

- M. Lampton, et al, “SNAP Telescope” SPIE 4849 pp.215-226, 2002.

- M. Lampton, et al, “SNAP Telescope: an Update”  SPIE 5166 pp. 113-123, 2004.

- M. Sholl, et al, “SNAP Telescope” SPIE 5487-73, in press 2004.

- Boeing Delta IV Payload Planners Guide, October 2000.