96E09/22/06

S706-96E.doc

Include subsections below as appropriate.

Section 706. - CONCRETE AND PLASTIC PIPE

Include the following when precast concrete box culverts are allowed:

706.07  Precast Reinforced Concrete Box Sections.  Delete this subsection and substitute the following:

Conform to ASTM C 1433.  Provide concrete box culvert sections meeting the design requirements for HS20 loading.

The following information shall be clearly marked on the inner surface of each box section by indentation, waterproof paint or other approved means.

- Box span and rise

- Date of manufacture

- Name of manufacturer

Include when plastic pipe is specified or an option:

706.08  Plastic Pipe.  Delete the text and substitute the following:

Furnish perforated and nonperforated plastic pipe conforming to the following for the size and types specified.  For watertight joints, conform to ASTM D 3212.  For pipe culvert, furnish pipe conforming to types (a), (b), or (c) for the size specified.

(b) Corrugated polyethylene pipe.  Delete the text and substitute the following:

Furnish 12 to 48 inch diameter pipe conforming to AASHTO M 294.  For sanitary sewer applications, furnish AASHTO M 294, type S pipe with watertight joints.

Include when Section 255 or 605 is specified:

(d) Corrugated polyethylene drainage tubing.  Delete the title and text and substitute the following:

(d) Drainage pipe.  Furnish polyethylene perforated or non-perforated corrugated plastic pipe conforming to AASHTO M 252.  Furnish perforated or non-perforated polyvinyl chloride pipe with smooth interior, smooth or ribbed exterior conforming to AASHTO M 278, ASTM F 758, or ASTM F 949.