WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A12525 | In-Flight Anomaly Number -- | Contractor Report Number P-065 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title LH2 PROPELLANT FEEDLINE LEAKS IN THE OUTER ARGON JACKET |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT 1 | Sys_Lvl N | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| Test/Operation A - ATP | Prevailing Condtion E - ENVIRONMENT | F / U F | Fail Mode MS - STRUCT | Cause MA - MFG-ASY |
| System PROPULSION | Defect CR - CORROD | Material S - STRUCT | Work Contact -- | Fail Date 10/03/1989 |
| Received at MSFC 10/11/1989 | Date Isolated -- | FMEA Reference 2.5.8.2 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location ARROWHEAD | Symptom MV - EXT LEAK | Time Cycle -- |
| Effectivity Text -- |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 02/10/1995 | CN RSLV SBMT -- | Defer Date -- | Add Date 10/12/1989 | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design W. PATTERSON | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR G. LADNER |
| Approval |
| Design W. PATTERSON | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR G. LADNER |
| PAC Assignee T. HESTER | PAC Review Complete TH | MSFC Closure Date 05/07/1990 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description DURING A PRE-ATP LEAK TEST ON A LH2 PROPELLANT FEEDLINE (PD4800184), A LEAK WAS DETECTED IN THE OUTER ARGON JACKET. THIS LEAK TEST IS THE LAST ONE PERFORMED PRIOR TO ARGON FILLING AND PRIOR TO ATP. REPLACEMENT PARTS WERE TESTED AT SUB-ASSEMBLY LEVELS AND LEAKAGE OCCURRED. THIS PROMPTED AN INVESTIGATION BY ARROWHEAD TO PERFORM A FAILURE ANALYSIS ON THESE PARTS TO DETERMINE THE CAUSE FOR THE LEAKING CONDITION. IT WAS DETERMINED THAT THE LEAK OCCURRED FROM CORROSION THROUGH THE THREE PLIES OF THE 21-6-9 STAINLESS STEEL PART. FURTHER ANALYSES WERE PERFORMED BY MAF PERSONNEL AND CONFIRMED THE CONDITION OF STRESS CORROSION CRACKING THE CORROSIVE CONDITION WAS SUSPECTED TO BE CAUSED BY THE INTRUSION OF CHLORIDE BEARING WATER INTO THE PLIES DURING A SEAM WELD PROCESS AND OTHER CONTRIBUTING FACTORS OTHER BELLOWS LINES CONSTRUCTED BY ARROWHEAD OF 21-6-9 STAINLESS STEEL ARE: PD4800178 LH2 RECIRCULATION LINE (1) PD4800175 L02 PROPELLANT FEEDLINE (3) PD4800180 G02 PRESSURIZATION LINES (3) PD4800205 GH2 PRESSURIZATION LINES (3) THE ABOVE LINES ARE PROCESSED SIMILARLY TO THE LH2 FEEDLINE. HOWEVER, THE ABOVE LINES DO NOT HAVE INCONEL 718 AS PRESSURE CARRIERS. THE ONLY LINE (OTHER THAN THE LH2 FEEDLINE) THAT HAS AN ARGON-FILLED ANNULUS IS THE RECIRCULATION LINE |
| Contractor Investigation/Resolution TASK I. FAILURE/PROBLEM INVESTIGATION: 1. PROCUREMENT QUALITY (3760) REVIEW ALL VENDOR PROCESS PLANS TO DETERMINE WHICH LINES WERE SUBJECTED TO A PROCESS WHICH PRODUCES A POTENTIAL FOR WATER INTRUSION INTO THE INNER PLIES OF BELLOWS CONSTRUCTED OF 21-6-9 STAINLESS STEEL RESPONSIBILITY: M. TAYLOR/3761 - C. COYAN/3760 COMPLETED 11/10/89 CLOSURE STATEMENT: A REVIEW OF PROCESSES RELATING TO BELLOWS FABRICATION HAVE BEEN COMPLETED FOR FLOWN AND UNFLOWN ETS THROUGH ET-62. FIVE PLANNING LEVELS WERE UTILIZED. ADDITIONALLY, 96 TYPE TWO BELLOWS ARE IN PROCESS AT ARROWHEAD 2. RELIABILITY ASSURANCE (3741) AND MATERIALS ENGINEERING (3573) PUBLISH FAILURE ANALYSIS RESULTS ON ALL MATERIALS AND SOLUTIONS ANALYZED DURING THE INVESTIGATION OF THE PROPULSION HARDWARE IN QUESTION RESPONSIBILITY: B. MATTHEESSEN/3741 - E. HARTLEY/3740 P. HINKELDEY/3573 - C. GRAY/3570 COMPLETED 11/16/89 CLOSURE STATEMENT: IT WAS DETERMINED THAT STRESS CORROSION CRACKING RESULTED IN LEAKAGE OF THE BELLOWS. METALLURGICAL ANALYSIS DETERMINED THAT THE 21-6-9 MATERIALS MET ALL SPECIFICATION REQUIREMENTS. THE MOST PROBABLE CAUSE FOR STRESS CORROSION CRACKING WAS THE INDUCEMENT OF CHLORIDE LADEN WATER USED FOR COOLANT DURING THE SEAM WELDING PROCESS 3. SYSTEMS ENGINEERING (3530) ANALYZE LINE CONFIGURATIONS AND DETERMINE ALLOWABLE LEAKAGE ON LH2 FEEDLINE OUTER JACKET, LH2 RECIRCULATION LINE INNER AND OUTER JACKET, GH2 PRESSURIZATION LINE FLEXIBLE BELLOW AND G02 PRESSURIZATION SYSTEM FLEXIBLE BELLOWS. PROVIDE TECHNICAL ASSESSMENT RELATIVE TO POTENTIAL CRACK GROWTH, MISSION LIFE CAPABILITY, STRUCTURAL ANALYSIS, ICE POTENTIAL AND EFFECTS, AND FRACTURE MECHANICS ANALYSIS RESPONSIBILITY: E. ZISK/3531 - J. JOHNSON/3530 COMPLETED: 10/26/89 - INITIAL TECHNICAL ASSESSMENT (SEE TASK III FLEET CLEARANCE) 03/23/90 - FINAL ENGINEERING REPORT (DATED 1/30/90) CLOSURE STATEMENT: A TECHNICAL ASSESSMENT WAS MADE RELATIVE TO LEAKAGE POTENTIAL, CRACK GROWTH POTENTIAL, MISSION LIFE CAPABILITY, BELLOWS FABRICATION HISTORY ICE POTENTIAL AND EFFECTS, STRUCTURAL ANALYSIS AND A FRACTURE MECHANICS ANALYSIS, ETC. THIS TECHNICAL ASSESSMENT WAS PRESENTED OCTOBER 26, 1989 IN THE STS-33R FLIGHT READINESS REVIEW AND FLEET CLEARANCE RATIONALE WAS DEVELOPED (SEE TASK III) TASK II CORRECTIVE ACTIONS: 1. PROCUREMENT QUALITY (3760) OBTAIN CORRECTIVE ACTIONS FROM THE VENDOR (ARROWHEAD) RELATIVE TO PROCESSES AND PROCEDURES WHICH WILL PRECLUDE A RECURRENCE OF MOISTURE INTRUSION INTO INNER PLIES OF BELLOWS ASSEMBLIES RESPONSIBILITY: M. TAYLOR/3761 - C. COYAN/3760 COMPLETED 2/12/90 CLOSURE STATEMENT: ALL ARROWHEAD PLANNING HAS BEEN REVISED TO PERVENT WATER INTRUSION INTO FAYING SURFACES. FURTHER PRECAUTIONS ARE TAKEN BY CONTROLLING THE WATER USED DURING RESISTANCE WELDING OF BELLOWS. THIS IS ACCOMPLISHED BY TESTING THE DI. WATER TWICE DAILY, MAINTAINING RECORDS OF CHLORINE CONTENT, AND CHANGING WATER SAMPLES IF CHLORINE CONTENT EXCEEDS 20 PARTS PER MILLION. THE PRACTICE OF "COURTESY CLEANING" IS NOW PROHIBITED ONLY CLEANING OPERATIONS AUTHORIZED ON SHOP TRAVELERS SHALL BE ACCOMPLISHED 2. PROCUREMENT QUALITY (3760) PROVIDE PLAN FOR REVALIDATING PROCESSES TO PRECLUDE MOISTURE INTRUSION INTO THE INNER PLIES OF BELLOWS RESPONSIBILITY: M. TAYLOR/3761 - C. COYAN/3760 COMPLETED 11/09/89 CLOSURE STATEMENT: A PLAN WAS FORMULATED TO PREVENT MOISTURE INTRUSION INTO THE BELLOWS ASSEMBLIES. IMPLEMENTATION OF THIS PLAN WAS ACCOMPLISHED ON ITEM 1, TASK II 3. RELIABILITY ASSURANCE (3741) GENERATE A GENERIC ALERT ADDRESSING THE FABRICATION OF 21-6-9 BELLOWS WITH MOISTURE INTRUSION RESPONSIBILITY: J. FINCHER/3741 - E. HARTLEY/3740 CANCELLED CLOSURE STATEMENT: LEAKAGE OF THE INITIAL GROUP OF BELLOWS (LOT F) WAS NOT DEFINITELY AND SOLELY ATTRIBUTABLE TO WATER INTRUSION INTO THE INNER PLIES. IT WAS SUSPECTED BY ALL COGNIZANT PARTIES THAT THIS GROUP OF BELLOWS WAS UNIQUE IN THEIR CONSTRUCTION AND PROCESSING. THEREFORE, BY MANAGEMENT DIRECTION, THE ALERT WAS NOT ISSUED 4. RELIABILITY ASSURANCE, PROCUREMENT QUALITY AND ENGINEERING DEVELOP RATIONALE FOR CLEARANCE OF ET-38 AND SUBSEQUENT LAUNCHES (SEE ATTACHED PLAN) RESPONSIBILITY: J. FINCHER/3741 - E. HARTLEY/3740 A. LISTEMA/3515 - R. ROGERS/3510 M. TAYLOR/3761 - C. COYAN/3760 COMPLETED 10/26/89 CLOSURE STATEMENT: SEE TASK III FOR CLEARANCE OF FLEET TASK III CLEARANCE OF EFFECTIVITIES: IT HAS BEEN DETERMINED THE THREE OF FIVE BELLOWS FABRICATION SEQUENCES USED BY THE VENDOR PREVENTS WATER INTRUSION INTO THE INNER PLIES WHICH DOES NOT CREATE A SUSPECT CONDITION OF STRESS CORROSION CRACKING HOWEVER, TWO OF THE SEQUENCES ARE SUSPECTED OF HAVING HAD WATER INTRUSION INTO THE BELLOWS PLIES WHICH MAY RESULT IN STRESS CORROSION CRACKING. CRACKING IS SUSPECTED TO BE A RESULT OF CHLORIDE BEARING WATER OR OTHER CHLORIDE SOLUTION BEING PRESENT ALONG WITH RESIDUAL STRESSES IN THE MATERIAL DURING THE PROCESS RESISTANCE WELDING AND BAKING OF THE BELLOWS ASSEMBLIES A TECHNICAL ASSESSMENT WAS MADE OF THE SUSPECT CONDITION AND THE FOLLOWING ASSESSMENTS WERE DOCUMENTED: 1. PARTS THAT PASS ACCEPTANCE PROOF LEAK TESTS ARE ACCEPTABLE A. SIZING OPENS UP AND BLUNTS ANY CRACKS B. STRESS CORROSION CRACKS DO NOT GROW AFTER ACCEPTANCE TESTING C. BELLOWS HAVE HIGH STRENGTH FACTORS OF SAFETY D. FRACTURE ANALYSIS SHOWS LARGE CRITICAL FLAW SIZE AND MISSION LIFE CAPABILITY E. SYSTEM IS TOLERANT TO LEAKAGE ALL ENGINEERING ANALYSES HAVE DETERMINED THAT IF LEAKAGES DID OCCUR, IT WOULD BE LESS THAN THE ALLOWABLES PER THE TM04 REQUIREMENTS. NO SIGNIFICANT CRACK GROWTH IS EXPECTED AFTER THE LINES HAVE BEEN SIZED, PASSED LEAK AND PROOF TEST. ALL AS-BUILT HARDWARE IS ACCEPTABLE TASK IV CAPS CLOSURE SUMMARY A THOROUGH ANALYSIS OF ALL ASPECTS OF BELLOWS FABRICATION INDICATED THAT THE MOST PROBABLE CAUSE FOR THE STRESS CORROSION CRACKING WAS THE MIGRATION OF CHLORINE LADEN WATER INTO THE BELLOWS PLIES. ALL BELLOWS PROCESSING PAPER HAS BEEN REVISED AT ARROWHEAD TO PROTECT THE BELLOWS FROM SOLUTION INTRUSION INTO THE PLIES. ADDITIONALLY, DE-IONIZED WATER IS NOW PUMPED ONTO THE SEAM WELDS AND THE WATER IS MONITORED TWICE DAILY FOR CHLORINE CONTENT IT WAS DETERMINED BY ENGINEERING ANALYSIS THAT ALL LINES THAT PASS PROOF TEST ARE FLIGHT WORTHY DUE TO THE FACT THAT NO MECHANISM IS PRESENT TO PROPAGATE THE CRACK |
| MSFC Response/Concurrence |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A12525 | IFA# -- | Contractor RPT# P-065 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# PD-4800184 | Asmnt Part Name LH2 PROP. FEEDLINE | Asmnt Serial/Lot# N/A |
| HCRIT CD 1 | FCRIT CD 1 | CAUSE CD MA - MFG-ASY | FAIL MODE MS - STRUCT |
| Asmnt FMEA 2.5.8.2 | Asmnt FM 2 | FMEA CSE A | FMEA SCSE N/A |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |