MSFC PRACA : 2003-02-12 07:54

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A01623 | In-Flight Anomaly Number -- | Contractor Report Number T-012 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title PI 1508/1509 ABLATOR MATERIAL FAILS TENSILE STRENGTH |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (1) B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE PI-1508/1509 | PART# NONE | SER/LOT# SLA 561 | MANUFACTURER N/A |
| Test/Operation M - MFG | Prevailing Condtion -- | F / U UC | Fail Mode -- | Cause -- |
| System THERMAL | Defect -- | Material -- | Work Contact F. RAMSEY | Fail Date 04/01/1980 |
| Received at MSFC 06/20/1980 | Date Isolated -- | FMEA Reference 1.2.5 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom -- | Time Cycle -- |
| Effectivity Text NONE |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 10/07/1987 | CN RSLV SBMT 01/04/1982 | Defer Date -- | Add Date -- | R/C Codes 3 - F/TE -- -- |
| Assignee |
| Design B. DAVIS | Chief Engineer -- | S & MA D. NEWMAN | Project G. CAVALARIS | Project MGR -- |
| Approval |
| Design R. ZAGRODSKY | Chief Engineer -- | S & MA D. NEWMAN | Project J. ODOM | Project MGR -- |
| PAC Assignee M. GLASS | PAC Review Complete MG | MSFC Closure Date 01/22/1982 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: NONE A. CONTINUING FAILURES IN FLAT WISE TENSILE STRENGTH VALUES FOR PI 1508/1509 ABLATOR MTRL TENSILE STRENGTH VALUE SHOULD BE 30 PSI B. SLA 561 MOLD MIX PER PI 1508, 1509, & 1510 FAILED TO CURE |
| Contractor Investigation/Resolution 12/15/81 CAUSE - 1. 655 RESIN NOT COMPATIBLE WITH 652 RESIN. 2 IMPROPER TEST SAMPLE PREPARATION. 3. AIR BORNE CONTAMINATION AFFECTING RESIN CURE. 4. STORAGE & HANDLING CAPABILITIES NOT PER SPEC. 5 CONTAMINATION INDUCED BY ELE. OF MIX. 1/6/82 RESOLUTION - INVESTIGATION OF POSSIBLE CAUSES REVEALED THE FOLLOWING: 1. 655/652 COMPATIBILITY TEST (LOT JH073 PER QLT-T020) CURED WITHIN 12 HRS OF BLENDING MAX REQ IS 16 HRS. 2. REVIEW OF SAMPLE PREPARATION PROCEDURE PI 1508 SHOWED NO ADVERSE CRITERIA OR READINGS. 3. AIR BORNE CONTAMINATION WHICH COULD INHIBIT CURE WAS MOSTLY SULFUR. AIR SAMPLING & PARTICULATE FALL OUT FOR A 3 MO. PERIOD WERE INCONCLUSIVE. 4. STORAGE & HANDLING ENVIRONMENTAL CONDITIONS WERE NOT PER SPEC. THE MAX STORAGE TEMP (80 DEGS F) WAS EXCEEDED (85 DEGS F+). AIR CONDITIONING WAS INSTALLED. 5. INVESTIGATION OF CONTAMINANTS INDUCED BY ELEMENTS OF MIX. IS ALSO BEING INVESTIGATED BY T-011 T-018, T-015. NEW TREND DATA SHEETS FOR BETTER MIX ROOM TRACING HAS BEEN IMPLEMENTED. RECURRENCE CONTROL - STORAGE AREA ENVIRONMENT DID NOT MEET PI REQMNTS THEREFORE AREA WAS AIR TIONED. NEW TREND DATA SHEETS WERE INITIATED TO OBTAIN BETTER DATA FOR REC'G INSPECTION, MIX ROOM DATA OF PI 1508/1509 BASE MIXES. SINCE THE INITIATION OF THIS CAPS IN APRIL 1980 SUBSTANTIAL DECREASE IN THE FAILURE RATE HAS BEEN OBSERVED. 1/6/82 - CLOUSRE DISTRIBUTED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A01623 | IFA# -- | Contractor RPT# T-012 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# -- | Asmnt Part Name -- | Asmnt Serial/Lot# -- |
| HCRIT CD -- | FCRIT CD -- | CAUSE CD -- | FAIL MODE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |