|  | MSFC PRACA : 2003-02-12 08:41 |
| --- | --- |
| WHOLE RECORD REPORT( + ADDENDUM) |
| MSFC Record # A10482 | In-Flight Anomaly Number -- | Contractor Report Number T-056 | JSC# -- | KSC# -- |
| Problem Title LWT-30 HAD BLISTER-LIKE CONDITION IN THE BX-250 FOAM |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl N | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE BX-250 FOAM | PART# 80973018414 | SER/LOT# N/A | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE INTERTANK | PART# 80903000000 | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE BX-520 FOAM | PART# 80973018414 | SER/LOT# N/A | MANUFACTURER MMC |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U F | Fail Mode MSI - INSULATION | Cause MAP - MFG-ASY-INST |
| System TPS | Defect CX - VOID | Material F - INSUL | Work Contact W. JOHNSON | Fail Date 07/22/1985 |
| Received at MSFC 01/09/1987 | Date Isolated -- | FMEA Reference 5.6.1.2 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text NONE |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 01/15/1992 | CN RSLV SBMT 11/06/1987 | Defer Date -- | Add Date -- | R/C Codes 5 - TRNG -- -- |
| Assignee |
| Design F. HUNEIDI | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project J. CAVALARIS | Project MGR -- |
| Approval |
| Design F. HUNEIDI | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project J. CAVALARIS | Project MGR -- |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete JE | MSFC Closure Date 12/03/1987 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF DOC: MMC MARS T-76521 ON JULY 22, 1985, DURING AN INSPECTION OF THE LWT-30 INTERTANK (POST CPR FOAM PAPER SPRAY), A "BLISTER-LIKE" CONDITION WAS OBSERVED IN THE BX-250 FOAM. THIS CONDITION WAS REPEATED ON LWT'S 31 AND 32 INTERTANKS |
| Contractor Investigation/Resolution R/A - LWT-30, -31, AND -32 WERE REPAIRED PER MARS T-76521, T-85078, AND T-85070, RESPECTIVELY. 1/9/87 - DISCREPANT BX-250 CONDITION WAS A RESULT OF AN IMPROPER MIXTURE (OFF-RATIO) OF "A" AND "B" FOAM SPRAY COMPONENTS. 1/9/87 BACKGROUND - A. ON JULY 22, 1985, DURING AN INSPECTION OF THE LWT-30 INTERTANK (POST CPR FOAM PAPER SPRAY) A "BLISTER/SWOLLEN" CONDITION WAS OBSERVED IN THE BX-250 FOAM (REF. MARS T-75621). B. AFTER THE INTERTANK BX-250 FOAM APPLICATION WAS COMPLETED PER ENGINEERING DRAWING 80973018414 AND ASSOCIATED PROCESS DOCUMENTS, IT WAS PLACED IN CELL "H" FOR CPR APPLICATION. A CPR-488 FOAM PAPER SPRAY WAS THEN CONDUCTED OVER THE BX-250 MATERIAL. APPLICATION TEMPERATURES RANGED FROM 184 TO 226 DEGREES F. AFTER THE REMOVAL OF THE CPR PAPER SPRAY, THE ABNORMAL BX-250 CONDITION WAS SITED. THIS CONDITION WAS ALSO SIMILAR ON LWT-31, AND 32. FAILURE ANALYSIS T-75621 INDICATES THAT THIS ANOMALY RESULTED FROM AN IMPROPER MIXTURE ("OFF-RATIO") OF FOAM SPRAY COMPONENTS. THE "A" COMPONENT OF THE TWO COMPONENTS (A AND B) SYSTEM WAS "BLED- OFF" TO COMPENSATE FOR AN IMBALANCE OF PROPORTIONER SPRAY PRESSURE. 5/28/87 - STATUS UPDATE - NO CHANGE ECD 6/30/87. 11/10/87 - CLOSURE UPDATE - REFERENCE MMC CAPS T-056 TASK I FOAM PROCESSES/EQUIPMENT INVESTIGATION THIS TASK REQUIRES THE SUBMITTAL TO RELIABILITY ASSURANCE, COPIES OF PROCESS DOCUMENTS (AND ASSO- CIATED EQUIPMENT REQUIREMENTS) FOR THE SPRAY APPLICATION OF NCFI, CPR, PDL, AND BX-250 FOAMS. IN ADDITION, PROBLEM HISTORIES (WHICH INDIVIDUAL DEPARTMENTS ARE COGNIZANT OF) SHALL BE SUBMITTED. THIS INFORMATION SHALL BE REVIEWED AND CATEGORIZED PRIOR TO DETERMINING THE ADDITIONAL TASKS FOR THE RESOLUTION OF THIS CAPS. A. ENGINEERING SPECIFICATION - 1512, 1513, 1518, 1523 B. PROCESS INSTRUCTIONS - 1512, 1513, 1518, 1523 C. MANUFACTURING PROCESS PLANS D. MANUFACTURING OPERATION PROCEDURES E. TOOLING INSTRUCTION/DESIGN F. PRODUCTION OPERATIONS - OPERATION/MAINTENANCE PROCEDURES CLOSURE STATEMENT ALL NECESSARY DOCUMENTS AND PROBLEM HISTORIES HAVE BEEN SUBMITTED TO RELIABILITY ASSURANCE. AN IN DEPTH REVIEW OF THESE ITEMS REVEALED THAT SYSTEM AMELIORATION IS NEEDED IN THE FORM OF UPGRADING FOAM OPERATOR SKILLS AND OVERALL EQUIPMENT EVALUATION. TASK II OF THIS CAPS WILL ADDRESS CORREC- TIVE ACTION. TASK CLOSED *TASK II CORRECTIVE ACTION A UPGRADE OPERATOR SKILL LEVELS INVESTIGATIONS HAVE SHOWN THAT WHEN A SPRAY FOAM APPLICATOR IS KNOWLEDGEABLE OF THE OPERATING EQUIPMENT, MATERIALS, AND APPLICATION PRINCIPLES, LATENT DEFECTS CAN BE PREVENTED 1. DEVELOPMENT OF A VIABLE FOAM APPLICATOR TRAINING (CERTIFICATION) COURSE IN CONJUNCTION WITH THE PRIME EQUIPMENT VENDOR (GUSMER CORPORATION). 2. TAILOR/ENHANCE THE TRAINING COURSE TO ALLOW FOR GUSMER EQUIPMENT MODIFICATIONS PECULIARIZED BY MMMSS DESIGN. *CLOSURE STATEMENT A FOUR DAY TRAINING COURSE WAS GIVEN TO MMMSS PRODUCTION FOAM OPERATORS AND SUPERVISORS BY A GUSMER CORPORATION REPRESENTATIVE. THE SYLLABUS CONSISTED OF EQUIPMENT COMPONENT ANALYSIS, PRAC- TICAL APPLICATIONS AND TROUBLESHOOTING, BASIC FIELD KNOWLEDGE OF RELATED CHEMISTRY, AND KNOWLEDGE OF PROPER SPRAY TECHNIQUES AND PROCEDURES EIGHT INDIVIDUALS (A TOTAL OF 25 INDIVIDUALS PARTICI- PATED) FAILED THE EXAMINATION GIVEN AT THE COURSE COMPLETION (CORRECTIVE ACTION WILL BE ADDED AS A TASK, HEREIN). THE MMMSS TRAINING DEPARTMENT HAS DEVELOPED A CERTIFICATION COURSE BASED ON MMMSS PROCEDURES AND OBSERVATION OF GUSMER'S CURRICULUM (REFERENCE INTEROFFICE MEMORANDUM 3084-87-026, AND GUSMER CORPORATION CORRESPONDENCE TO WM. JOHNSON; DATED MAY 7, 1987) ITEM CLOSED B. PROCEDURE A REVIEW/REVISION OF ALL STP/PI FOAM DOCUMENTS FOR CONSISTENCY AND CONTROL. CLOSURE STATEMENT STP/PI CONTROLS WERE FOUND TO BE ADEQUATE FOR THESE DOCUMENTS WHICH ARE NOT PART PECULIAR DETAILEDSPRAY INSTRUCTIONS ARE FURNISHED IN THE MPP SPRAY SCHEDULES FOR EACH PARTICULAR APPLICATION. IT WAS AGREED THAT A STATEMENT COULD BE ADDED TO THE ABOVE PROCESS INSTRUCTIONS DIRECTING THAT PROPORTIONER NEEDLE VALVES NOT BE ADJUSTED AFTER PRODUCTION SPRAY HAS BEEN STARTED THIS WILL BE DONE AT THE NEXT SCHEDULED REVISIONS TO PIS 1503, 1512, 1513, AND 1523. A PRODUCTION TIP WAS ISSUED IN DECEMBER, 1986 TO CALL ATTENTION TO THIS ITEM (REFERENCE INTEROFFICE MEMORANDUM 3693-87- 177) ITEM CLOSED C. EQUIPMENT EVALUATION 1. OFF-RATIO FOAM DETERMINATION/MEASUREMENT EVALUATE THE DETERMINATION OF IMPROPER SPRAY RATIOS THROUGH THE USE OF FLOW METERS, MANI- FOLDS, ETC. EVALUATE THE USAGE OF WARNING ALARMS; GO/NO-GO GAUGES, ETC. METHOD ACCURACY SHALL BE A FOCAL POINT. CLOSURE STATEMENT MEMOS 3572-87-123 AND 3614-87-192 SUMMARIZE THE RESULTS OF THE EVALUATION; WHICH CONCLUDED THAT THE ACCURACY OF THE EXISTING PISTON TYPE PROPORTIONERS COULD NOT BE GREATLY IMPROVED. A NEW TECHNICAL DIRECTIVE, ENTITLED "SOFI PROCESS IMPROVEMENTS" (TD-675), WILL BEGIN IN FY 88. IT WILL DEVELOP A LONG TERM EQUIPMENT UPGRADE PROGRAM FOR SOFI PROCESSES. ONE SPECIFIC ELEMENT OF THIS PROGRAM, CON- DUCTED AT MSFC, (RADIAL PUMPS AND FLOW METERS) DEMONSTRATED NOTABLY IMPROVED FOAM RATIO CONTROL (REF. IOM 3691-87-MJ-118). ITEM CLOSED 2. EVALUATION OF SPRAY GUN INITIAL INVESTIGATIONS INDICATE INDISCRIMINATE PROBLEMS WITH SPRAY GUN EQUIPMENT, SPRAY PATTERN ESTABLISHMENT, MIXING MODULE, CONTROL, ETC EVALUATE THE GUSMER MODEL GX7 FOAM APPLICATION GUN AGAINST THE EXISTING EQUIPMENT. PROVIDE A PROS VERSUS CONS LIST IN CONJUNCTION WITH EX- PECTED FAILURES, OPERATOR COMPREHENSION, AND FINISHED PRODUCT RESULTS CLOSURE STATEMENT A SPRAY GUN COMPARISON STUDY WAS CONDUCTED ON THE GUSMER MODEL GX7 SPRAY UNIT VERSUS THE GUSMER AR (CURRENTLY UTILIZED) COMPARISON PARAMETERS WERE MATERIAL OUTPUT, MATERIAL QUALITY, PATTERN STABILITY, PRESSURE FLUCTUATION, MULTIPLE FIRING CAPABILITY, EASE OF OPERATION/MAINTENANCE, AND OPERATOR TRAINING REQUIREMENTS. PRELIMINARY DATA INDICATES THAT THE GX7 GUN HAS THE POTENTIAL TO OUTPERFORM THE PRESENT 1:1 RATIO SPRAY GUNS USED IN PRODUCTION FOR OVERALL RELIABILITY IN MEETING PRODUCTION NEEDS AND THE END ITEM (SOFI) ENGINEERING SPECIFICATIONS (REFERENCE TPS MATE- RIALS JOB #2645 AND TEST RESULTS) A MORE DETAILED EVALUATION OF A UNIVERSAL SPRAY GUN SYSTEM WILL BE ADDRESSED AS A TASK, HEREIN (REF. SECT. F., ITEM #2). ITEM CLOSED 3 PERIODIC MAINTENANCE EVALUATE PRESENT SYSTEM OF EQUIPMENT OVERHAUL AND PERIODIC MAINTENANCE. DEVELOP A REALISTIC PREVENTIVE MAINTENANCE PLAN WHICH WILL ENCOMPASS: A. REDUCTION OF EQUIPMENT MAINTENANCE FROM ANNUALLY TO QUARTERLY, SEMI-ANNUALLY, OR TRI- ANNUALLY. B. MAINTENANCE OF BACKUP SYSTEMS C. IMPLEMENTATION PLAN CLOSURE STATEMENT REVIEW OF THE EXISTING PERIODIC MAINTENANCE SCHEDULE RESULTED IN A CHANGE FROM AN ANNUAL/VISUAL CHECK TO A QUARTERLY SPECIFIC FUNCTION INSPECTION (REF MEMOS 3614-87-287 AND 3614-87-288). ITEM CLOSED D. FOAM OPERATOR SKILLS CORRECTIVE ACTION SEVERAL PRODUCTION FOAM OPERATORS FAILED TO ACHIEVE AN ACCEPTABLE GRADE AS A RESULT OF A FOAM OPERATOR TRAINING COURSE GIVEN AT MAF. PRODUCTION OPERATIONS MANAGEMENT HAS COMMITTED TO ADDITIONAL TRAINING FOR THESE INDIVIDUALS. AT THE COMPLETION OF THIS ADDITIONAL INSTRUCTION, THE INDIVIDUALS WILL BE RE-EXAMINED. CLOSURE STATEMENT PRODUCTION FOAM OPERATORS WERE TRAINED, RE-EXAMINED BY GUSMER CORPORATION AND ACHIEVED ACCEPTABLE GRADES. ALL OPERATORS HAVE NOW ACHIEVED ACCEPTABLES SCORES (REFERENCE GUSMER CORPORATION 0023 DENCE TO B. JOHNSON, DATED JULY 21, 1987). ITEM CLOSED E. FACILITY - EQUIPMENT/SURPLUS/INVENTORY THIS TASK SHALL EVALUATE THE FOAM EQUIPMENT STORAGE AND REPAIR AREA, EQUIPMENT SURPLUS, AND THE INVENTORY OF ALL EQUIPMENT AND SPARE PARTS. 1. IDENTIFY (AND PLAN) STORAGE SPACE FOR FOAM EQUIPMENT AND SPARE PARTS. MAINTAIN ADEQUATE SEPARATION BETWEEN USED AND NEW MATERIALS (I.E., SOLUTION/SOLVENT CLEANING AREAS FOR SPRAY GUNS/PARTS - STORAGE OF SYSTEM READY EQUIPMENT - STORAGE OF SURPLUS). CLOSURE STATEMENT A STUDY WAS MADE FOR THE FOAM EQUIPMENT STORAGE AND REPAIR AREAS. BASED ON THIS STUDY, RFF NO. C09-0093 WAS SUBMITTED TO PURCHASE AND INSTALL THE DECKING, SHELVING, LIGHTS, ETC.; THAT WERE IDENTIFIED AS NECESSARY TO CORRECT AND IMPROVE THE PRESENT OPERATION (REF. MEMO 3100-87-1486). ITEM CLOSED 2. COMPUTER/MECHANIZED SYSTEM FOR INVENTORY CONTROL CLOSURE STATEMENT AN IBM-PC COMPUTER HAS BEEN PROCURED (ON-LINE 9/1/87) FOR THE COMPILATION OF INVENTORY PERSONNEL SHALL BE TRAINED AND THE SOFTWARE REQUIREMENTS IDENTIFIED (INVENTORY INPUT/ ASSESSEMENT SPECIFICATIONS). THIS SYSTEM WILL GIVE ADEQUATE EQUIPMENT AND SPARE PARTS CONTROL FOR THE FOAM PROPORTIONER/SPRAY GUN STORAGE AREA (REFERENCE INTEROFFICE MEMORANDUM 3652/EH/87-182 AND INFORMATION SYSTEMS SERVICE REQUEST CONTROL #53237, USER REFERENCE #IE-768). ITEM CLOSED F. UNIVERSAL SPRAY GUN EVALUATION PRELIMINARY TEST DATA (USING GUSMER GX7 SPRAY GUN) INDICATES THAT ONE SPRAY GUN MAY BE USED TO REPLACE ALL EXISTING UNITS. THIS TASK WILL DEVELOP A PLAN TO FURTHER EVALUATE/VERIFY THE INITIAL ENGINEERING DATA IT IS EXPECTED THAT A MORE RELIABLE, SINGLE SPRAY UNIT WILL GREATLY REDUCE FOAM FAILURES AND AUTOMATIC FOAM SPRAY ABORTIONS. 1 PROCUREMENT/EVALUATION OF SIMILAR GUNS. CLOSURE STATEMENT FEASIBILITY OF A UNIVERSAL SPRAY GUN WILL BE BASED ON THE GUSMER GX7 MODEL AS A PATHFINDER FOR THE PURPOSES OF THIS CAPS; SIMILAR UNITS MAY BE EVALUATED (OUTSIDE THE SCOPE OF THIS CAPS) SHOULD THE UNIVERSAL GUN CONCEPT BE DEEMED VIABLE. GUSMER CORPORATION HAS EXTENDED THE CON- SIGNMENT OF THE GX7 UNIT FOR 90 DAYS (REF. GUSMER CORPORATION CORRESPONDENCE TO R. WADSWORTH DATED 6/22/87). ITEM CLOSED 2. TEST PLAN FOR SPRAY GUN EVALUATION CLOSURE STATEMENT A TEST PLAN TO EVALUATE "UNIVERSAL" SPRAY GUN CANDIDATES, HAS BEEN APPROVED AND INITIATED (REF IOM 3691-87-DAC-025 AND ADVANCED MANUFACTURING TECHNOLOGY TEST PLAN 3691-87-DAC-002). IN ADDITION, A PRODUCTION OPERATIONS DIRECTIVE (ET-3600-1968) WILL DIRECT THE EFFORT TO IMPROVE THE INCUMBENT SPRAY GUNS IN CONJUNCTION WITH THE AMT PARALLEL EFFORT. ITEM CLOSED TASK CLOSED TASK III CLEARANCE OF EFFECTIVITIES NO CONSTRAINTS - THIS IS A PRODUCTION CONCERN ONLY LWTS 30, 31, AND 32 WERE REPAIRED PER MARS T-76521, T-85078, AND T-85070, RESPECTIVELY. THE "BLISTER/SWOLLEN" FOAM ANOMALY IS VISUALLY DETECTABLE DURING THE INTERTANK FOAM APPLICATION PROCESSING. THIS DISCREPANCY HAS ALSO BEEN OBSERVED ON THE LWT-40 INTERTANK (REFERENCE MARS T-84749). TASK IV CAUSE/CORRECTIVE ACTION SUMMARY CAPS T-056 WAS INITIATED TO DETERMINE AN EFFECTIVE RECURRENCE CONTROL MODE TO PRECLUDE THE APPLICATION OF OFF-RATIO FOAM ON THE EXTERNAL TANK SUBSTRATES. FOLLOWING A FOAM PROCESS (AND ASSOCIATED EQUIPMENT) INVESTIGATION, CORRECTIVE ACTION/SYSTEM AMELIORATION WAS FOCUSED ON THE OPERATOR/TECHNICIAN SKILL LEVELS, FOAM PROCESS PROCEDURES, FOAM APPLICATION SUPPORT EQUIPMENT, AND THE CARE AND CONTROL OF FOAM EQUIPMENT. OPERATOR/TECHNICIAN SKILLS IN ORDER TO FACILITATE AN OVERALL FOAM PROCESSING AWARENESS, A FOAM APPLICATION COURSE WAS CON- DUCTED BY GUSMER CORPORATION AT THE MICHOUD ASSEMBLY FACILITY FOR THE PRODUCTION TPS TECHNICIANS AND SUPERVISION. THE COURSE CURRICULUM CONSISTED OF EQUIPMENT COMPONENT ANALYSIS, PRACTICAL APPLICATIONS AND TROUBLESHOOTING, BASIC FIELD KNOWLEDGE OF RELATED CHEMISTRY, AND PROPER SPRAY TECHNIQUES AND PROCEDURES. ALL OF THE PRODUCTION TPS TECHNICIANS (WHO COMPLETED THE COURSE RE- QUIREMENTS) WERE CERTIFIED BY THE GUSMER CORPORATION AND THE MANNED SPACE SYSTEMS' TRAINING DEPARTMENT. THE GUSMER CORPORATION CURRICULUM, WAS WITNESSED BY THE MANNED SPACE SYSTEMS' TRAINING DEPARTMENT; AND ADOPTED AS AN ANNUAL CERTIFICATION COURSE. FOAM PROCESS PROCEDURES THE APPLICABLE STP/PI FOAM DOCUMENTS WERE REVIEWED FOR PROCESS ADEQUACY. IT WAS DETERMINED THAT THE PROCEDURAL SYSTEM WAS SUFFICIENT TO CONTROL THE APPLICATION OF FOAM PRODUCTS TO THE EXTERNAL TANKS (AS SPECIFIED PER THE ENGINEERING AND QUALITY REQUIREMENTS). IN ADDITION, HOWEVER, A (WARNING) STATEMENT TO ADDRESS THE ADJUSTMENT OF VALVES DURING THE SPRAY APPLICATION WILL BE ADDED TO THE APPLICABLE PROCESS INSTRUCTIONS AT THE NEXT SCHEDULED UPDATE (IN THE INTERIM, A PRODUCTION TIP WAS INITIATED FOR DIRECTION). THE ADJUSTMENT OF THE PROPORTIONER VALVES, DURING THE AUTOMATIC SPRAY OPERATIONS, RESULTED IN AN OFF-RATIO CONDITION ON THE LWT-31 INTERTANK. FOAM APPLICATION SUPPORT EQUIPMENT AN EVALUATION OF THE EXISTING SOFI PROCESS EQUIPMENT CONCLUDED THAT THE PRESENT SYSTEM COULD NOT BE IMPROVED WITH "BAND-AID" TYPE RESOLUTIONS HOWEVER, THROUGH THE USE OF PAST FAILURES, AND PRESENT TECHNOLOGY, THE ENTIRE SYSTEM CAN BE ENHANCED TO PRODUCE, CONSISTENTLY, CONFORMING FOAM APPLICATIONS. CONSEQUENTLY, A TECHNICAL DIRECTIVE WAS INITIATED TO DEVELOP/DESIGN EQUIPMENT UPGRADES FOR THE SOFI PROCESSES. THE INTERIM IMPROVEMENTS WERE THE OPTIMIZATION OF THE SOFI SPRAY GUN SYSTEMS AND THE UPGRADE OF THE FOAM PROCESS EQUIPMENT MAINTENANCE AND CONTROL EQUIPMENT CARE AND CONTROL THE ON-SET OF "RATE-PRODUCTION" RESULTED IN ADDITIONAL FOAM EQUIPMENT (THE STOCKPILING OF FORMU- LATORS/PROPORTIONERS, SPRAY GUNS, SPARE PARTS, ETC. TO SUPPORT THE "RATE PRODUCTION" MATERIAL/ EQUIPMENT DEMAND) FOR THE MAF PRODUCTION SOFI EQUIPMENT AREA. A REDUCTION IN PRODUCTION ACTIVITY HOWEVER, CREATED A SURPLUS IN EQUIPMENT AND PARTS. TO PRECLUDE THE POSSIBILITY OF ANOMALIES RESULTING FROM HOUSEKEEPING (SURPLUS MATERIAL IN DISARRAY), A SYSTEM WAS INITIATED TO PROVIDE IN- VENTORY CONTROL, AND ARRANGE/TIDY THE EQUIPMENT STORAGE/REPAIR AREA. CONCLUSION THE APPLICATION OF OFF-RATIO FOAM ONTO AN EXTERNAL TANK SUBSTRATE CAN ONLY BE PRECLUDED BY EQUIPMENTDESIGN. ADVANCED MANUFACTURING TECHNOLOGY IS PRESENTLY WORKING A LONG TERM PLAN TO DEVISE SUCH A SYSTEM. IN THE INTERIM, SYSTEM AMEILORATION WILL BE AFFECTED THROUGH THE EDUCATION OF PRODUCTION WORKERS, MAINTAINING ADEQUATE CONTROL OF EQUIPMENT AND ASSOCIATED SYSTEM PROCEDURES, AND THE IM- PROVEMENT OF RELATED SOFI TOOLING (SPRAY GUNS). UNTIL A NEW SYSTEM (DESIGNED TO PRECLUDE THE APPLICATION OF OFF-RATIO FOAM ONTO THE TANK SUBSTRATES) IS BROUGHT ON-LINE, THE INTERIM CORRECTIVE ACTION SHOULD PRECLUDE THE APPLICATION OF ANOMALOUS MATERIAL ONTO THE EXTERNAL TANK. TASK CLOSED |
| MSFC Response/Concurrence |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A10482 | IFA# -- | Contractor RPT# T-056 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80973018414 | Asmnt Part Name BX-520 FOAM | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 3 | CAUSE CD MAP - MFG-ASY-INST | FAIL MODE MI - INSULATION |
| Asmnt FMEA 5.6.1.2 | Asmnt FM 2 | FMEA CSE A | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |