| CABLE No. | . L7O-B0940R |
| --- | --- |
| MFG. | 3/20/2006 Rev. 3/24/06 DRD |
| OPERATOR: | H.Higley & N.Liggins |

CABLE LOG SHEET

LBNL-SUPERCON-AFRD

SUPERCONDUCTING MAGNET CABLES

BLD 52

Objective :  Mfg. LARP TQ-Production Cable

- STRAND INFORMATION -

| MANUFACTURER : | Oxford |
| --- | --- |
| BILLET #: | 8647 |
| SPOOL #: | 8647-1 ,2 & 3 see “Strand Map Log” |
| COMPOSITION : | Nb3Sn -RRP |
| STRAND Dia.. NOMINAL : | 0.7mm | INSP. DIA..: | 0.704mm avg. |
| Cu/SC RATIO NOMINAL : |  | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : |  | DIRECTION : | Right |
| SHARP BEND TEST : |  |
| LENGTH PER SPOOL : | 139m x 27 spools |

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | LARP TQ-Production Cable |
| --- | --- |
| No. of STRANDS: | 27 |
| PITCH DIRECTION: | LEFT | PITCH Set | 77.5mm | Pitch Check | 80.5mm |
| PLANETARY RATIO: | -0.57 : 1 |
| ROLLER ID #: | P69 & P70 | WIDTH: | 9.999 | ANGLE:: | 1.050 deg. |
| MANDREL ID #: | 7 | WIDTH: | 9.21mm | THICKNESS:: | 0.61mm |
| LUBRICATION : | 4BR 1d/pitch |
| STRAND TENSION: | 2.0 kg. | TURKS HEAD LOAD "SGM": | -105 lb. +/- 5 lb. |
| Nom. THICKNESS: | 1.260 +/-0.010mm |
| Nom. WIDTH: | 10.077mm +0.000 -0.100mm or ( 10.027 +/-0.050mm) |
| Nom. ANGLE: | 1.00 +/-0.10 deg. |

- Pre-Annealed CABLE -

|  | 940 |
| --- | --- |
| FINISHED LENGTH: | 131.5m |
| Avg. THICKNESS: | 1.3149 mm |
| Avg. WIDTH: | 10.036 mm |
| Avg. ANGLE: | 0.983 deg. |

- Annealed & Rerolled FINISHED CABLE -

|  | L70-B0940R |
| --- | --- |
| FINISHED LENGTH: | 128.8m + 2.7m LBNL sample |
| Avg. THICKNESS: | 1.264 mm |
| Avg. WIDTH: | 10.026 mm |
| Avg. ANGLE: | 0.977 deg. |

NOTES:  Cabling went very well.  First-pass cabling tension 105+/- 5 lbs.

A 2.7m cable sample was cut from the point end of the cable for LBNL archives. All but 6m of the cable were insulated at LBNL giving an insulated length of 122.8m for a total cable length of 128.8 m. There is 6 m of un-insulated cable on the top layer of the spool.  Two samples each 5 cm long were cut from the point and tail ends of the cable for metallography.

| 03-23-2006 Cable RunLRP-7-O-B0940R Unit 0 07:49:20 |  |
| --- | --- |
| LARP TQ 27st-.7mm-1deg CME #2 |  |  |
| Annealed and Rerolled Cable Measurements. |  |  |  |  |
| Notes | POINT | METERS | kPa | ANGLE | WIDTH | THICK |
| Gaqge Start | 1 | 0 | 16,969 | 0.001 | 9.9953 | 1.5054 |
| Gaqge Start | 2 | 0 | 16,969 | 0.002 | 9.9955 | 1.5055 |
| Gaqge Start | 3 | 0 | 16,969 | 0 | 9.9949 | 1.5052 |
| Gaqge Start | 4 | 0 | 16,969 | 0 | 9.9947 | 1.5054 |
| Gaqge Start | 5 | 0 | 16,977 | 0 | 9.995 | 1.5053 |
| Notes | POINT | METERS | kPa | ANGLE | WIDTH | THICK |
| L7O-B0940R Tail End | 6 | 0 | 16,969 | 1.027 | 10.0464 | 1.2812 |
| L7O-B0940R | 6 | 0 | 16,969 | 1.027 | 10.0464 | 1.2812 |
| L7O-B0940R | 8 | 0 | 16,969 | 1.019 | 10.0346 | 1.2618 |
| L7O-B0940R | 9 | 0.33 | 16,969 | 1.003 | 10.0339 | 1.2619 |
| L7O-B0940R | 10 | 1 | 16,969 | 0.999 | 10.0272 | 1.2673 |
| L7O-B0940R | 11 | 1.33 | 16,969 | 0.995 | 10.0275 | 1.2682 |
| L7O-B0940R | 12 | 2.33 | 16,969 | 0.996 | 10.0286 | 1.268 |
| L7O-B0940R | 13 | 3 | 16,969 | 0.989 | 10.0287 | 1.2632 |
| L7O-B0940R | 14 | 5.67 | 16,969 | 0.993 | 10.0299 | 1.2639 |
| L7O-B0940R | 15 | 7 | 16,969 | 0.986 | 10.031 | 1.2627 |
| L7O-B0940R | 16 | 8.33 | 16,969 | 0.977 | 10.0243 | 1.2625 |
| L7O-B0940R | 17 | 8.67 | 16,969 | 0.986 | 10.0268 | 1.263 |
| L7O-B0940R | 18 | 8.67 | 16,969 | 0.981 | 10.0266 | 1.2625 |
| L7O-B0940R | 19 | 9 | 16,991 | 0.98 | 10.0264 | 1.2624 |
| L7O-B0940R | 20 | 11 | 16,969 | 0.969 | 10.0246 | 1.2616 |
| L7O-B0940R | 21 | 13 | 16,977 | 0.978 | 10.0241 | 1.2627 |
| L7O-B0940R | 22 | 15 | 16,969 | 0.991 | 10.0243 | 1.2629 |
| L7O-B0940R | 23 | 17 | 16,969 | 0.984 | 10.0251 | 1.2627 |
| L7O-B0940R | 24 | 19 | 16,969 | 0.971 | 10.0245 | 1.2625 |
| L7O-B0940R | 25 | 21 | 16,969 | 0.976 | 10.0231 | 1.2626 |
| L7O-B0940R | 26 | 23 | 16,969 | 0.976 | 10.0267 | 1.263 |
| L7O-B0940R | 27 | 25 | 16,969 | 0.962 | 10.0258 | 1.2621 |
| L7O-B0940R | 28 | 27 | 16,969 | 0.968 | 10.0235 | 1.2624 |
| L7O-B0940R | 29 | 29 | 16,969 | 0.991 | 10.0237 | 1.2634 |
| L7O-B0940R | 30 | 31 | 16,969 | 0.975 | 10.0244 | 1.2625 |
| L7O-B0940R | 31 | 33 | 16,969 | 0.98 | 10.0245 | 1.2623 |
| L7O-B0940R | 32 | 35 | 16,969 | 0.978 | 10.0228 | 1.2626 |
| L7O-B0940R | 33 | 37 | 16,977 | 0.968 | 10.0225 | 1.2623 |
| L7O-B0940R | 34 | 39 | 16,969 | 0.972 | 10.0246 | 1.263 |
| L7O-B0940R | 35 | 41 | 16,969 | 0.973 | 10.0244 | 1.2631 |
| L7O-B0940R | 36 | 43 | 16,969 | 0.964 | 10.0244 | 1.2625 |
| L7O-B0940R | 37 | 45 | 16,969 | 0.965 | 10.0241 | 1.2629 |
| L7O-B0940R | 38 | 47 | 16,969 | 0.973 | 10.0242 | 1.2621 |
| L7O-B0940R | 39 | 49 | 16,969 | 0.986 | 10.0267 | 1.2631 |
| L7O-B0940R | 40 | 51 | 16,969 | 0.974 | 10.0234 | 1.2623 |
| L7O-B0940R | 41 | 53 | 16,969 | 0.978 | 10.0237 | 1.2628 |
| L7O-B0940R | 42 | 55 | 16,969 | 0.974 | 10.0243 | 1.2626 |
| L7O-B0940R | 43 | 57 | 16,977 | 0.979 | 10.0241 | 1.263 |
| L7O-B0940R | 44 | 59 | 16,969 | 0.968 | 10.0248 | 1.2623 |
| L7O-B0940R | 45 | 61 | 16,969 | 0.956 | 10.0253 | 1.2629 |
| L7O-B0940R | 46 | 63 | 16,969 | 0.965 | 10.0239 | 1.2624 |
| L7O-B0940R | 47 | 65 | 16,977 | 0.973 | 10.0239 | 1.2629 |
| L7O-B0940R | 48 | 67 | 16,969 | 0.973 | 10.0241 | 1.2626 |
| L7O-B0940R | 49 | 69 | 16,969 | 0.978 | 10.0237 | 1.2634 |
| L7O-B0940R | 50 | 71 | 16,969 | 0.986 | 10.0224 | 1.2628 |
| L7O-B0940R | 51 | 73 | 16,977 | 0.971 | 10.0254 | 1.2628 |
| L7O-B0940R | 52 | 75 | 16,969 | 0.974 | 10.0233 | 1.2624 |
| L7O-B0940R | 53 | 77 | 16,969 | 0.973 | 10.0241 | 1.2626 |
| L7O-B0940R | 54 | 79 | 16,969 | 0.966 | 10.0248 | 1.2626 |
| L7O-B0940R | 55 | 81 | 16,977 | 0.977 | 10.0244 | 1.2633 |
| L7O-B0940R | 56 | 83 | 16,969 | 0.979 | 10.0252 | 1.2625 |
| L7O-B0940R | 57 | 85 | 16,969 | 0.982 | 10.0258 | 1.2627 |
| L7O-B0940R | 58 | 87 | 16,969 | 0.975 | 10.025 | 1.2632 |
| L7O-B0940R | 59 | 89 | 16,969 | 0.98 | 10.0246 | 1.263 |
| L7O-B0940R | 60 | 91 | 16,969 | 0.977 | 10.0238 | 1.2634 |
| L7O-B0940R | 61 | 93 | 16,969 | 0.965 | 10.0237 | 1.2626 |
| L7O-B0940R | 62 | 95 | 16,969 | 0.967 | 10.0233 | 1.2631 |
| L7O-B0940R | 63 | 97 | 16,969 | 0.959 | 10.0241 | 1.2634 |
| L7O-B0940R | 64 | 99 | 16,969 | 0.964 | 10.0243 | 1.2626 |
| L7O-B0940R | 65 | 101 | 16,977 | 0.97 | 10.0225 | 1.2628 |
| L7O-B0940R | 66 | 103 | 16,977 | 0.971 | 10.0217 | 1.2634 |
| L7O-B0940R | 67 | 105 | 16,984 | 0.969 | 10.023 | 1.263 |
| L7O-B0940R | 68 | 107 | 16,969 | 0.966 | 10.0231 | 1.2625 |
| L7O-B0940R | 69 | 109 | 16,977 | 0.967 | 10.0245 | 1.2636 |
| L7O-B0940R | 70 | 111 | 16,984 | 0.96 | 10.0227 | 1.2631 |
| L7O-B0940R | 71 | 113 | 16,969 | 0.971 | 10.0239 | 1.2631 |
| L7O-B0940R | 72 | 115 | 16,977 | 0.981 | 10.0255 | 1.2629 |
| L7O-B0940R | 73 | 117 | 16,969 | 0.975 | 10.0251 | 1.2637 |
| L7O-B0940R | 74 | 119 | 16,991 | 0.981 | 10.0233 | 1.2627 |
| L7O-B0940R | 75 | 121 | 16,977 | 0.981 | 10.0242 | 1.263 |
| L7O-B0940R | 76 | 123 | 16,977 | 0.969 | 10.0245 | 1.2629 |
| L7O-B0940R | 77 | 125 | 16,969 | 0.958 | 10.0243 | 1.2656 |
| L7O-B0940R | 78 | 127 | 16,969 | 0.958 | 10.0244 | 1.2656 |
| L7O-B0940R | 79 | 129 | 16,969 | 0.969 | 10.0256 | 1.2669 |
| L7O-B0940R | 80 | 131 | 16,977 | 0.969 | 10.0274 | 1.2667 |
| L7O-B0940R Point End | 81 | 131 | 16,977 | 0.984 | 10.0289 | 1.2707 |
| L7O-B0940R |  |  | AVG | 0.977 | 10.0256 | 1.2637 |
| L7O-B0940R |  |  | MAX | 1.027 | 10.0464 | 1.2812 |
| L7O-B0940R |  |  | MIN | 0.956 | 10.0217 | 1.2616 |
| L7O-B0940R |  |  | STDEV | 0.014 | 0.0041 | 0.0033 |
| Gage End | 82 | 131 | 16,969 | 0 | 9.9958 | 1.5058 |
| Gage End | 83 | 131 | 16,969 | 0.002 | 9.9957 | 1.5058 |
| Gage End | 84 | 131 | 16,969 | 0.002 | 9.9956 | 1.5059 |
| Gage End | 85 | 131 | 16,969 | 0.002 | 9.9956 | 1.5057 |
| Gage End | 86 | 131 | 16,969 | 0.002 | 9.9957 | 1.506 |

Respool Log  / Strand Map