| CABLE No. | . L7O-B00982R |
| --- | --- |
| MFG. | 6/3/2008 |
| OPERATOR: | H.Higley, N.Liggins |
| Rev: | 6/27/2008 HH |

CABLE LOG SHEET

LBNL-SUPERCON-AFRD

SUPERCONDUCTING MAGNET CABLES

BLD 52

Objective : Mfg. 5UL Production  LARP-TQ Cable.  First to use 108/127 stack billet.

- STRAND INFORMATION -

| MANUFACTURER : | Oxford |
| --- | --- |
| BILLET #: | 10400 |
| SPOOL #: | 10400-3= 1ul, 10400-4= 10ul, 10400-5=14ul, 10400-7 = 2ul |
| COMPOSITION : | RRP Nb3Sn |
| STRAND Dia.. NOMINAL : | 0.700 | INSP. DIA..: | 0.703 w/ hand micrometer |
| Cu/SC RATIO NOMINAL : |  | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : |  | DIRECTION : | Right |
| SHARP BEND TEST : |  |
| LENGTH PER SPOOL : | 357m |

NOTES:  Laser micrometer for strand diameter inspection was not operational.

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | LARP-TQ-Production cable |
| --- | --- |
| No. of STRANDS: | 27 |
| PITCH DIRECTION: | Left | PITCH LENGTH: | Nom = 80mm +-5mm ( measured 76.5mm) |
| PLANETARY RATIO: | -.57:1 |
| 1st. pass ROLLER ID #: | P69 & P70 | WIDTH: | 9.999 | ANGLE:: | 1.000 |
| 2nd. pass ROLLER ID #: | P71 & P72 | WIDTH: | 10.047 | ANGLE:: | 1.000 |
| MANDREL ID #: | 7 | WIDTH: | 9.23mm | THICKNESS:: | 0.63mm |
| LUBRICATION : | 4BR 1d/p |
| STRAND TENSION: | 2.5kg | TURKS HEAD LOAD "SGM": | -110 lbs |
| Nom. THICKNESS: | 1.26 +/-0.010mm 1st. pass = 1.310 +/- 0.010mm |
| Nom. WIDTH: | 10.027 +/- 0.050mm 1st pass 10.00 +/- 0.050 |
| Nom. ANGLE: | 1.00 +/- 0.10 |

- CABLE -

|  | 1st pass 982 | 982R |
| --- | --- | --- |
| FINISHED LENGTH: | 338m (-5m) | 333m (-5m) |
| Avg. THICKNESS: | 1.3079mm | 1.2607mm |
| Avg. WIDTH: | 10.0227mm | 10.0538mm |
| Avg. ANGLE: | 0.986 deg. | 0.982 |
| Facet:Pitch Maj/Min: | @5m 0.68/0.78 | @5m 0.72/0.83 |

NOTES:

.

982R tail end metallographic samples were taken. Length = 328m

- Insulation 6/26/2008  FII-282-1358-01-003 cleaned and Palmitic acid treated at LBNL.

This spool of insulation had several damaged spots that were not apparent until applied to the cable

The remaining short lengths of FII-282 insulation were not long enough to insulate 328m in one piece.

The 5UL of cable was cut at 3UL.  The remaining 2UL section was then cut to 1UL pieces.

L7O-B0982R spool 1/3 total length 198m  needs decision about weather splices would be acceptable in the insulation.

L7O-B0982R spool 2/3 65m no splices. Insulated

L7O-B0982R spool 3/3 65m no splices  Insulated