MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A17356 | In-Flight Anomaly Number -- | Contractor Report Number S-081 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title STRUCTURAL - INCORRECT WEAVE SCRIM CLOTH UTILIZED DURING BONDING |
| EICN# -- | ELEMENT ET | Contractor LMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE GUIDE RAIL | PART# 21037-019 | SER/LOT# N/A | MANUFACTURER SCHMIEDE |
| Test/Operation MI - MFI | Prevailing Condtion N - INSPECTION | F / U F | Fail Mode MS - STRUCT | Cause MA - MFG-ASY |
| System STRUCTURAL | Defect -- | Material -- | Work Contact D. DONNELLY | Fail Date 11/10/1998 |
| Received at MSFC 01/06/1999 | Date Isolated -- | FMEA Reference NONE | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom MS - STRUCT | Time Cycle -- |
| Effectivity Text ET 92 - 95, 97, 99 AND SUBSEQUENT |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date 01/27/1999 | LVL 3 Close -- | Remark / Action 01/27/1999 |
| Investigation / Resolution Summary |
| Last MSFC Update 09/03/1999 | CN RSLV SBMT -- | Defer Date -- | Add Date 01/06/1999 | R/C Codes -- -- -- |
| Assignee |
| Design S. SPARKS | Chief Engineer J. LUSK | S & MA S. GORUM | Project -- | Project MGR P. COUNTS |
| Approval |
| Design S. SPARKS | Chief Engineer J. LUSK | S & MA A. ADAMS | Project -- | Project MGR P. COUNTS |
| PAC Assignee R. TUCKER | PAC Review Complete -- | MSFC Closure Date 08/31/1999 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID N034083 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description PROBLEM ITEM 1: VESPEL GUIDE RAIL STRIP SLICKED OFF DURING MAF SLA CURING PROCESSING ITEM 2: UNAUTHORIZED USE OF GLASS FABRIC SCRIM CLOTH BY THE SUPPLIER CRITICALITY: THE FAILURE OF A GUIDE RAIL ASSEMBLY IS A CRITICALITY 1, BUT THE LOSS OF THE RUB-STRIP DOES NOT CAUSE FAILURE OF THE ENTIRE GUIDE RAIL AND THEREFORE IS A CRITICALITY 3. REF. FMEA PARAGRAPHS 4.4.20, 4.4.23, AND 4.4.29. THIS CAPS IS GENERATED AT THE REQUEST OF MANAGEMENT TO TRACK RECURRENCE CONTROL *REVISION A Dated 2-2-99 - UPDATES AND CLOSES ALL TASKS SEE ASTERISKS |
| Contractor Investigation/Resolution GENERAL: THIS CAPS WAS INITIATED AT MANAGEMENT'S REQUEST. TRACKING WAS PREVIOUSLY ACCOMPLISHED IN SPECIAL INVESTIGATION SI-98-S009 THE FOLLOWING IS A SUMMARY OF ALL ACTIONS COMPLETED IN THE SI AS OF THE INITIATION OF THIS CAPS. FOR COMPLETE HISTORY SEE THE SPECIAL INVESTIGATION ITEM 1: DURING PROCESSING OF THE 80921021037-019 GUIDE RAIL UP TO THE 80971028480-050 ASSEMBLY LEVEL, THE VESPEL STRIP WAS DISCOVERED SEPARATED FROM THE METAL SUBSTRATE. THE GUIDE RAIL PROGRESSED THROUGH THE NORMAL SLA APPLICATION PROCESS THROUGH THE INITIAL ELEVATED CURE CYCLE AND THE FINAL HAND PACK (PLUG PULL) CURE CYCLE. UPON REMOVAL OF THE GUIDE RAIL MOLD, THE TECHNICIAN FOUND THE VESPEL STRIP LAYING IN THE MOLD, NO LONGER ADHERED TO THE AL SUBSTRATE OF THE RAIL ASSEMBLY THE VESPEL STRIP IS BONDED TO THE AL SUBSTRATE PER STPS 6001 AND 5013 USING HYSOL EA934NA ADHESIVE. THERE ARE SIX (6) DIFFERENT MAF PART NUMBERS SUPPLIED BY SCHMIEDE WITH THIS ADHESIVE BONDING PROCESS. THREE (3) OF THESE PARTS HAVE SLA APPLIED PRIOR TO ASSEMBLY AT THE ET LEVEL. THE SIX (6) PART CONFIGURATIONS ARE LOCATED ALONG THE AFT CROSSBEAM STRUCTURE AND ARE USED TO LIMIT MOVEMENT TO THE GO2 AND GH2 PRESS LINES ITEM 2: REVIEW OF THE MATERIAL DATA SHEETS FOR THE MATERIALS USED BY THE SUPPLIER IN THE MANUFACTURING OF THESE GUIDE RAILS REVEALED THAT THE GLASS FABRIC SCRIM CLOTH USED WAS STYLE 1659, FINISH 271. STP 6001 REQUIRES H226A, GLASS STYLE 1675, WITH I-399 SILANE * BACKGROUND: REVIEW AND TESTING TO DETERMINE FLIGHT IMPACT OF POSSIBLE GUIDE RAIL VESPEL STRIP DEBRIS DURING FLIGHT, THE STRUCTURAL IMPLICATIONS OF MISSING GUIDE RAIL VESPEL STRIPS, AND STRESS ANALYSIS OF PRESS LINES USING INCREASED DYNAMIC LOADS WERE COMPLETED. FROM THIS REVIEW, RETROFITS WERE DONE ON THE GO2 GUIDE RAILS FOR ET-97 AND ET-99 WITH SECONDARY MECHANICAL FASTENERS. THE OTHER TWO (2) COMPLETE GUIDE RAIL ASSEMBLIES, UNDER THE AFT CENTER CROSSBEAM AND ON THE GH2 SIDE OF THE CROSSBEAM, WERE ACCEPTED FOR FLIGHT BASED ON A RISK ANALYSIS AND ACCEPTABLE FACTOR OF SAFETY. FOR COMPLETE CLOSURE RATIONALE INFORMATION SEE THE FIELD ENGINEERING CHANGES FOR ET-99 (FEC KET-0045) AND ET-97 (FEC KET-0044R1), AND STS- 88/ET-97 FRR SPECIAL TOPIC PRESENTATION A FULL ENGINEERING CHANGE, B02050 WAS INITIATED, REQUIRING SECONDARY MECHANICAL FASTENERS ON THE SIX (6) DIFFERENT GUIDE RAIL CONFIGURATIONS USED ON ET-104 AND UP. ET-103 HARDWARE WAS NOT COMPLETELY STAGED AND WAS DOCUMENTED ON PIECE PART NCDS. ALL OTHER PARTS BUILT PER STP 6001, TYPE II DIRECT BONDING TO A METAL SUBSTRATE WERE REVIEWED FOR THE PRESENCE OF REDUNDANT SECONDARY FASTENERS. ALL THE PARTS HAD A REDUNDANT FASTENER DESIGN. (REF. CCMAIL FROM B. HANSLICK DATED 2-1-99) A REVIEW OF THE SUPPLIER BUILD PAPER DID NOT REVEAL ANY PROCESS ITEMS THAT COULD BE IDENTIFIED AS DEFINITELY CONTRIBUTING TO THIS PROBLEM. FURTHER REVIEW OF THE PASA- JELL ETCHANT, MMSY912A100 SUPPLIED BY MAF TO THE SUPPLIER FOR THE 1997 MANUFACTURING LOT REVEALED THE ETCHANT TO BE OVER THIRTY-FOUR (34) MONTHS OLD. THE LMMSS PASA-JELL SPECIFICATIONS REQUIRE A 12 MONTH SHELF LIFE AFTER REMOVAL FROM STORAGE, REGARDLESS OF THE AGE OF THE STORED MATERIAL ALSO, FURTHER LAB ANALYSIS LED TO THE REQUEST FOR THE SUPPLIER'S DATA SHEET ON THE FIBER GLASS SCRIM CLOTH USED IN THE PROCESS. THIS LED TO THE DISCOVERY THAT SCHMIEDE USED SCRIM CLOTH GLASS STYLE 1659, FINISH 271. STP 6001 REQUIRES H226A, GLASS STYLE 1675, WITH I-399 SILANE ALL SIX (6) PART CONFIGURATIONS SUPPLIED AND ASSEMBLED WITH ADHESIVE PER STP 6001 BY SCHMIEDE HAD NCDS INITIATED FOR SUSPECT DEBONDING OF GUIDE RAIL RUB-STRIPS AND FOR UNAUTHORIZED USE OF SCRIM CLOTH GLASS STYLE 1659, FINISH 271 (SEE ATTACHMENT 1.1 OF SI-98-S009) RELIABILITY ASSURANCE INITIATED SCAR(S) 98-073 AND 98-081, WHICH WERE ISSUED TO SCHMIEDE A REVIEW WAS CONDUCTED OF THE SLA PROCESSING ON THE 80971028480-050 ASSEMBLY, WHICH IS MADE FROM THE DISCREPANT 80921021037-019 GUIDE RAIL. NO ITEMS COULD BE IDENTIFIED AS DEFINITELY CONTRIBUTING TO THIS PROBLEM TASK I FAILURE/PROBLEM INVESTIGATION *A. COMPLETE MATERIAL ANALYSIS FROM SI-98-S009 ACTION ITEMS, INCLUDING THE CHEMFILM TESTING AND ANALYSIS, AND PRODUCE WRITTEN LAB REPORT RESPONSIBILITY: E. PRATZ /4643 L. RANDO /4643 R. MEYER /4640 ECD: 1-12-99 COMPLETE: 1-27-99 CLOSURE STATEMENT: THE ORIGINAL RAIL FAILURE, 80921021037-019, THAT DEBONDED WAS ANALYZED ON LAB 98A311 WITH OTHER GUIDE RAILS, TESTED AND ANALYZED ON LABS 98A314, 98A315, 98A316, 98A317, 98A318, AND 98A319. ALL INVESTIGATION WAS COMPLETED IN THESE JOBS WITH NO ANALYTICAL RESULT REVEALING AN OBVIOUS CAUSE FOR THE DEBOND. (REF. CCMAIL FROM E. PRATZ DATED 1-26-99) B. OBTAIN A SAMPLE OF CHEMFILM FROM THE SUPPLIER FOR TESTING IN TASK A RESPONSIBILITY: D. BALES /3840 W. SCHRIEFFIER /3810 ECD: 12-22-98 COMPLETE: 12-27-98 CLOSURE STATEMENT: CHEMFILM SAMPLE OBTAINED AND SUPPLIED TO THE TECHNICAL LAB FOR ANALYSIS REQUIRED IN TASK A *C. REVIEW AND IDENTIFY OTHER USAGE'S OF HYSOL EA934NA, VESPEL, PASA-JELL ETCHANT, AND GLASS FABRIC SCRIM CLOTH DELIVERED BY SUPPLIERS ON THE ETS RESPONSIBILITY: G. DAUGHDRILL / 4610 P. HINKELDEY / 4430 B. HANSLICK / 4420 R. PONTIFF /4400 S. PARIKH /3760 ECD: 1-8-99 COMPLETE: 1-26-99 CLOSURE STATEMENT: ALL PART USAGE IS IDENTIFIED IN THE ENGINEERING PART MANAGER (PM) SYSTEM *D. PERFORM COMPARISON STRENGTH TESTING ON PREPARED HYSOL STRIPS WITH CHEMFILM, CHEMFILM AND EPOXY PRIMER, PLAIN BARE ALUMINUM AND VESPEL STRIPS RESPONSIBILITY: G. DAUGHDRILL / 4610 P. HINKELDEY / 4430 ECD: 1-12-99 COMPLETE: 1-26-99 CLOSURE STATEMENT: VESPEL STRIPS WERE BONDED WITH THE UNAPPROVED SCRIM CLOTH, (GLASS STYLE 1659, FINISH 271) USED BY SCHMIEDE AND WERE CYCLED THREE (3) TIMES TO +350F WITH NO DEBONDS. (REF CCMAIL FROM G. DAUGHDRILL DATED 1-26-99) *E. PERFORM COMPARISON STRENGTH TESTING, (COMBINED WITH TASK D), USING STP 6001 REQUIRED SCRIM CLOTH H226A, GLASS STYLE 1675, WITH I-399 SILANE AGAINST GLASS STYLE 1659, FINISH 271 USED BY THE SUPPLIER RESPONSIBILITY: G. DAUGHDRILL / 4610 P. HINKELDEY / 4430 ECD: 1-12-99 COMPLETE: 1-26-99 CLOSURE STATEMENT: THE LAP SHEAR DATA SUMMARY RESULTS IDENTIFY THE SCRIM CLOTH GLASS STYLE 1659, FINISH 271 USED BY SCHMIEDE AS WEAKER AT BOTH ROOM TEMPERATURE, (APPROXIMATELY 15%) AND AT +350F, (APPROXIMATELY 5%), BUT NOTHING POINTS TO THE CLOTH CAUSING THE ORIGINAL SLICK OFF TYPE DEBOND. (REF. CCMAIL FROM G DAUGHDRILL DATED 1-26-99) *F. INVESTIGATE MAF SUPPLIER FIRST ARTICLE APPROVAL PROCESS AGAINST SCHMIEDE'S UNAUTHORIZED USE OF SCRIM CLOTH FOR POSSIBLE ENHANCEMENTS RESPONSIBILITY: C. PEMBO / 3761 S. PARIKH / 3760 ECD: 1-12-99 COMPLETE: 1-6-99 CLOSURE STATEMENT: PROCUREMENT QUALITY CONTROL HAS ENHANCED THE FIRST ARTICLE VERIFICATION AND VALIDATION PROCESSES IN SEVERAL WAYS, INCLUDING THE PQC FIELD REPRESENTATIVE OBTAINING THE APPLICABLE MATERIAL SPECIFICATION CODE CONTROL SHEET, ETC FOR REVIEW OF REQUIREMENTS. REF. CCMAIL FROM S. PARIKH DATED 1-6-99 *G. INVESTIGATE FLOW DOWN OF MATERIAL REQUIREMENTS FROM ENGINEERING PROCESS SPECIFICATIONS (STPS, ETC.) THAT REQUIRE COMMERCIAL PRODUCTS WITH SPECIFIC ENGINEERING REQUIREMENTS EXAMPLES STP 6001 REQUIRES: GLASS FABRIC (SCRIM CLOTH); SPEC: COMMERCIAL; CODE: H226A ADHESION PROMOTER (DOW CORNING Z-6040); SPEC: COMMERCIAL; CODE: K329A SOLVENT METHYL ETHYL KETONE (MEK); SPEC: ASTM D740; CODE: K527A RESPONSIBILITY: P. HINKELDEY / 4430 ECD: 1-12-99 COMPLETE: 1-26-99 CLOSURE STATEMENT: FLOW DOWN OF MATERIAL REQUIREMENTS TO SUPPLIERS IS ACCOMPLISHED WHEN THE STP IS INCLUDED IN THE SUPPLIER'S CONTRACT. THE SUPPLIER THEN REVIEWS THE STP TO IDENTIFY ALL THE REQUIRED MATERIALS IN THE APPROVED MATERIALS LIST (CODE SHEETS) THEY WILL NEED TO PRODUCE THE SPECIFIC HARDWARE SUPPLIERS THEN CONTACT LOCKHEED MARTIN FOR THE CODE SHEETS REQUIRED TO DETERMINE THE MATERIAL, WHERE TO BUY IT, AND OTHER INFORMATION (SUCH AS SHELF LIFE REQUIREMENTS) THAT ARE NOT SPECIFIED IN THE STP. (REF. CCMAIL FROM M. GERKEN DATED 1-26-99) THE PROCUREMENT QUALITY FIELD REPRESENTATIVES WERE TRAINED IN A LESSONS LEARNED CONFERENCE ON 1-6-99 TO REVIEW SUPPLIER DOCUMENTATION AT THE TIME OF DAS SUBMITTAL, MANUFACTURING PLAN REVIEW, FIRST ARTICLE PRODUCTION AND PRIOR TO FINAL BUYOFF TO ENSURE COMPLIANCE TO REQUIREMENTS. (REF. CCMAIL FROM C. PEMBO DATED 1-26-99) *H. SUBMIT MATERIAL USAGE AGREEMENT (MUA) FOR THE USE OF SCRIM CLOTH GLASS STYLE 1659, FINISH 271 RESPONSIBILITY: G. DAUGHDRILL / 4610 P. HINKELDEY / 4430 COMPLETE: 1-7-99 CLOSURE STATEMENT: LIMITED USAGE MUA ET-0413 WAS SUBMITTED AND APPROVED BY MSFC TO ALLOW USAGE OF SCRIM CLOTH GLASS STYLE 1659, FINISH 271 *CAUSE INVESTIGATION IDENTIFIED THAT NO ONE PARTICULAR ITEM CAUSED THE DEBOND FAILURE OF THE RUB-STRIP FROM THE GUIDE RAIL. A COMBINATION OF DIFFERENT PROCESS FACTORS, PROCESS VARIABILITY, INCORRECT SCRIM CLOTH, AGED ETCHANT, ETC. MAY HAVE PRODUCED THE ONE DEBOND FAILURE SEEN TO DATE *TASK II CORRECTIVE ACTION THE DESIGN HAS BEEN REVISED WITH THE ADDITION OF MECHANICAL FASTENERS, RIVETS, AS A REDUNDANT METHOD OF FASTENING THE RUB-STRIPS. ADHESIVE FASTENING IS STILL NECESSARY FOR MACHINING THE RADIUS ON THE RUB-STRIPS. ENGINEERING CHANGE B02050, PRESS LINE GUIDE RAIL RUB-STRIP MODIFICATION HAS BEEN APPROVED TO REVISE THE DESIGN FOR ET-92 THRU ET-95 AND ET-104 & UP. REWORK DCN'S WERE RELEASED TO REWORK EXISTING PARTS (REF. CCMAIL FROM A. LISTEMAA DATED 1-27-99) ENGINEERING RELEASED A LIMITED USAGE MATERIAL USAGE AGREEMENT (MUA), ET-0413, ON THE SCRIM CLOTH, GLASS STYLE 1659, FINISH 271 ALLOWING USE OF THIS SCRIM CLOTH THROUGH ET-120 THE PASA-JELL ETCHANT SHELF LIFE WAS REVISED PER SI-98-S009 ACTION #16, CHANGE H36809-146 *TASK III CLEARANCE OF EFFECTIVITIES ET CLEARANCE DOC. (DEBONDING) ET-97 FEC KET-0044R1 & FRR SPECIAL PRESENTATION ET-99 FEC KET-0045 & FRR SPECIAL PRESENTATION ET-100 NCD N037752 ET-101 NCD N037751 ET-102 NCD N037721 ET-103 NCDS N033793, N039757, N039775, N039776, N038801 ET- 92 THRU 95 & ET-104 & UP ENGINEERING CHANGE B02050 *TASK IV CAPS CLOSURE SUMMARY AN 80921021037-019 GUIDE RAIL RUB-STRIP DEBONDED DURING THE SLA CURING PROCESS AT MAF. DURING THE FAILURE INVESTIGATION IT WAS ALSO DETERMINED THE SUPPLIER USED THE INCORRECT SCRIM CLOTH GLASS STYLE 1659, FINISH 271 INSTEAD OF THE REQUIRED H226A, GLASS STYLE 1675, WITH I-399 SILANE LABORATORY FAILURE INVESTIGATION AND TESTING PROVIDED NO ANALYTICAL RESULT REVEALING AN OBVIOUS ROUTE TO FAILURE CORRECTIVE ACTION INCLUDED: ENGINEERING CHANGE B02050 ADDED SECONDARY MECHANICAL FASTENERS, RIVETS, TO SECURE THE RUB-STRIPS TO THE GUIDE RAILS, REMOVING THE POSSIBILITY OF THE RUB-STRIP SEPARATION FROM THE GUIDE RAIL ENGINEERING RELEASED MATERIAL USAGE AGREEMENT ET-0413 ALLOWING USE OF SCRIM CLOTH, GLASS STYLE 1659, FINISH 271 AND THE PASA-JELL ETCHANT SHELF LIFE WAS REVISED TO 12 MONTHS PER H36809-146 THIS CAPS IS CLOSED. NO FURTHER ACTION IS REQUIRED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A17356 | IFA# -- | Contractor RPT# S-081 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80921021037 | Asmnt Part Name GUIDE RAIL | Asmnt Serial/Lot# -- |
| HCRIT CD -- | FCRIT CD 3 | CAUSE CD MA - MFG-ASY | FAIL MODE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |