Poster Presentation 1B-52

Enzymatic Activities of Ceriporiopsis subvermispora

Acting on Sugarcane Bagasse

Adilson R. Gonçalves1, Sirlene M. Costa1 and Elisa Esposito2

1Depto. Biotecnologia - FAENQUIL, CP 116, CEP 12.600-970 Lorena, SP-Brazil

2Núcleo Integrado de Biotecnologia, Universidade de Mogi das Cruzes, Brazil

Phone: 55-12-31595033; Fax: 55-12-5533165; E-mail: adilson@debiq.faenquil.br

URL: http://www.debiq.faenquil.br/adilson

Sugarcane bagasse was pre-treated with the white-rot fungus Ceriporiopsis subvermispora from 7 to 60 days. The aim of the work was the production of pulps or modified fibers from the pre-treated bagasse. Enzymatic activities for lignin peroxidase (LiP), manganese peroxidase (MnP), laccase (Lac) and xylanase (Xyl) were determined. The table shows the preliminar results for Xyl and MnP production in experiments in which the inoculum charge was varied. Xyl increased during the fermentation and also by the increasing of inoculum charge. On the other hand, MnP has a maximum of production until 30 days and seems to be not influenced by the inoculum charge. These parameters are useful to determine the better fermentation conditions. Additional results on Lac and LiP production  will be presented.

| Inoculum charge (mL) | 7 days | 15 days | 30 days | 45 days | 60 days |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Xylanase |  |  |
| 100 | 51 ( 1 | 118 ( 5 | 4787 ( 269 | 3542 ( 195 | 4847 ( 446 |
| 250 | 1065 ( 30 | 1209 ( 90 | 4384 ( 189 | 4161 ( 480 | 6678 ( 479 |
| 500 | 526 ( 25 | 1661 ( 93 | 4691( 190 | 5504 ( 316 | 6709 ( 447 |
| 750 | 1094 ( 20 | 5273 ( 94 | 4931( 295 | 2314 (196 | 5960 ( 514 |
|  |  |  | MnP |  |  |
| 100 | - | - | 310 ( 29 | 82 ( 3 | 19 ( 2 |
| 250 | 294 ( 12 | 6 ( 1 | 215 ( 20 | 23 ( 2 | 28 ( 1 |
| 500 | 339 ( 13 | 101 ( 5 | 30 ( 3 | 97 ( 3 | 6 ( 1 |
| 750 | 294 ( 12 | 112 ( 9 | 118 ( 12 | 30 ( 2 | 27 ( 2 |

[Financial support from FAPESP and CNPq]