MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A10051 | In-Flight Anomaly Number -- | Contractor Report Number S-069 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title LH2 TANK CLIP PARTIALLY SEPARATED FROM AFT DOME - LWT-35/MFG |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT 1 | Sys_Lvl Y | Misc Codes A (6) B C D E (X) F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE LH2 TANK CLIP | PART# 80914900992-002 | SER/LOT# N/A | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE LH2 TANK WELD ASSY | PART# 80914000000 | SER/LOT# N/A | MANUFACTURER MMC |
| HARDWARE NCA | NOMENCLATURE LH2 TANK CLIP | PART# 80914900992-002 | SER/LOT# N/A | MANUFACTURER MMC |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U F | Fail Mode UC - UNSAT | Cause MN - MFG-ISP |
| System ELECTRICAL | Defect DD - DETACH | Material L - FASTNR | Work Contact C. VOGEL | Fail Date 01/03/1986 |
| Received at MSFC 05/21/1986 | Date Isolated -- | FMEA Reference 1.2.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text LWTS 16, 20, 21, 22, 24 AND UP |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 02/22/1995 | CN RSLV SBMT 09/28/1987 | Defer Date -- | Add Date -- | R/C Codes 1 - DES -- -- |
| Assignee |
| Design J. WHITE | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| Approval |
| Design -- | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete JE | MSFC Closure Date 11/04/1987 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF: MARS T-81209 A CLIP ON LWT-35 LH2 TANK PARTIALLY SEPARATED FROM THE AFT DOME. ONE OF ITS TWO TIG SPOT WELDS WAS ONLY PARTIALLY FORMED; THE AREA OF PENETRATION WAS SIGNIFICANTLY LESS THAN NORMAL. A SIMILAR PROBLEM WAS SEEN ON LWT'S 39 AND 41 AS WELL. DURING ANALYSIS OF INVENTORY STOCK, ANOTHER PROBLEM WAS DISCOVERED. TWO CLIPS HAD CONDUCTIVITY AND HARDNESS READINGS SIGNIFICANTLY DIFFERENT FROM 2219 T-62 TYPICALS |
| Contractor Investigation/Resolution R/C - A COMPLETE RETROFIT HAS BEEN INITIATED FOR THE FLEET. ALL LH2 AFT DOME CLIPS SHALL BE BONDED WITH SCRIM CLOTH, LAID OVER THE EXISTING CLIP. A REDESIGNED FILLET WELDED CLIPS WITH "T" CONFI- GURATION HAVE BEEN IMPLEMENTED FOR PRODUCTION. 5/21/86 LAUNCH CONSTRAINTS - LWT'S 16, 20, 21, 22, 24 AND UP HAVE CONSTRAINTS TO LAUNCH BASED UPON FMEA ANALYSIS OF THE LH2 DEPLETION SENSOR SYSTEM. A FAILURE OF THE BRACKETS MAY LEAD TO LOSS OF SIGNAL FROM THIS SYSTEM. SUSPECT CAUSE OF POOR AREA OF PENETRATION TO BE RANDOM PRODUCTION VARIATION DUE TO DIFFICULTY OF OERATION. MMC MANAGEMENT HAS ASSIGNED TASKS FOR INVESTIGATION OF THIS PROBLEM AS FOLLOWS: GENERAL - ONE CLIP (80914900992-002) ON LWT-35, LH2 AFT DOME, WAS SEVERED AT ONE OF ITS TWO TACK WELDS. THE BREAK OCCURRED AFTER ACCEPTANCE OF THE CLIP INSTALLATION (AT 5083 TOOL, BUILDING 103) AND WAS DISCOVERED DURING ELECTRICAL CABLE INSTALLATION (AT CELL "E" IN VAB BUILDING). THIS HALF OF THE CLIP WAS REMOVED FOR ANALYSIS; HARDNESS AND CONDUCTIVITY READINGS WERE SLIGHTLY OUT. THE FRACTURE, HOWEVER, WAS ATTRIBUTED TO THE ACCIDENTAL IMPACT OF ITS PARTIALLY FORMED SPOT WELD THAT HAD APPROXIMATELY 20 PERCENT OF THE AREA OF PENETRATION COMPARED TO A NORMAL WELD. (RESULTS WERE SIMILAR ON LWT'S 39 AND 41.) THE SLIGHT DISCREPANCIES THAT WERE FOUND IN HARDNESS AND CONDUCTIVITY PRECIPITATED FURTHER INVESTIGATION. CHEMISTRY WAS VERIFIED TO BE GOOD, BUT A RANDOM CHECK OF INVENTORY SHOWED RESULTS IN HARDNESS AND CONDUCTIVITY SIMILAR TO WHAT WAS FOUND ABOVE. A SHEET SAMPLE WAS SENT TO BATSON HEAT TREAT TO CONFIRM THE STRENGTH PROPERTIES OF THE CURRENT HEAT TREATMENT OF PRODUCTION HARDWARE (REFERENCE TASK II). TYPICAL CLIP TENSILE SAMPLE 2219-62 (BRITTAIN (BATSON HEAT REQUIREMENTS MACHINE) TREAT) YIELD STRENGTH 36 KSI MIN --- 39 KSI ULTIMATE STRENGTH 54 KSI MIN --- 56 KSI HARDNESS (ROCKWELL) B-67 TYPICAL B-53 - 63 B-63 CONDUCTIVITY 30.5 - 33.5% TYPICAL 35 - 37% 34.5% DURING INVESTIGATION OF THE CLIPS, TWO CLIPS WERE FOUND THAT HAD HARDNESS AND CONDUCTIVITY READINGS SIGNIFICANTLY DIFFERENT FROM THE OTHERS. THE READINGS WERE SIMILAR TO WHAT MIGHT BE TYPICAL FOR 2219-0. THE CHEMISTRY WAS VERIFIED TO BE CORRECT FOR 2219. THE CLIPS WERE DRAWN FROM STOCK TO BE USED FOR TEST SERIALIZATION IS NOT REQUIRED AND IDENTIFICATION ON THE SUPPLIER COULD NOT BE DETERMINED. 2219-0 SUSPECT TYPICALS CLIP HARDNESS RH-70 RH-68 CONDUCTIVITY 48% 49% INVESTIGATION INTO THE PRODUCTION PROCESSES REVEALED THAT DIFFICULTIES EXIST IN CONSISTENTLY PRODUCING AN ACCEPTABLE SPOT WELD. VIOLATIONS EXIST FOR UNDERFILL, BURN THROUGH, CRACKS, UNDERCUT AND LACK OF FUSION. THESE VIOLATIONS, HOWEVER, ARE SEEN AND CORRECTED AT THE TIME THE WELD IS MADE.REVIEW OF RECORDS SHOWS THAT THE CLIP IS CURRENTLY BEING MADE BY BRITTAIN MACHINE (HEAT TREAT BY BATSON) WITH PREVIOUS CONTRACTS WITH NEIL AIRCRAFT, VOUGHT AND MACHINE CRAFT. THIS IS A NON- SERIALIZED PART. TASK I A. CLIP HEAT TREAT - HEAT TREAT A SAMPLE OF 2219-0 SHEET TO T-62 PER MIL-H-6088, USING PRODUCTION FURNACES AND METHODS AT BATSON HEAT TREATING. AFTER HEAT TREATING, TEST TO DETERMINE HARDNESS, CONDUCTIVITY AND TENSILE STRENGTH. PRIOR TO HEAT TREATING, VERIFY CONDUCTIVITY AND HARDNESS TASK CLOSURE STATEMENT A SAMPLE WAS HEAT TREATED AND ANALYZED. HARDNESS AND CONDUCTIVITY READINGS WERE WITHIN THE RANGE FOUND IN PRODUCTION CLIPS AND THE TENSILE SPECIMENS PULLED WITH STRENGTHS MEETING 2219-T62 REQUIRE- MENTS. REFERENCE MATERIALS TEST REPORT NO. 86A049-B. B. CLIP ANALYSIS (80914900992-002) - ENGINEERING PERFORM ANALYSIS TO DETERMINE THE ADEQUACY OF A CLIP IF ITS PROPERTIES SHOULD HAVE THE FOLLOWING STRENGTHS (AT ROOM TEMPERATURE). CASE 1: 36.0 KSI YIELD STRENGTH (2219 T-62) 54.0 KSI ULTIMATE STRENGTH CASE 2: 16.0 KSI YIELD STRENGTH (2219 - 0) 32.0 KSI ULTIMATE STRENGTH DETERMINE THE EFFECTS OF LOSS OF ONE CLIP ON THE SYSTEM (INTEGRITY OF WIRES AND REMAINING CLIPS). CLOSURE STATEMENT ENGINEERING DETERMINED THE ADEQUACY OF THE CLIPS AS FOLLOWS: CASE 1: + .02 MS (YIELD) AND + 1.08 MS (PLASTIC) CASE 2: - .56 MS (YIELD) AND + .22 MS (PLASTIC) ENGINEERING PERFORMED VIBRATIONAL TESTING. THE TIG SPOT WELD CLIP PASSED THE QUALIFICATION REQUIRE-MENTS (180 SECONDS) BUT FAILED AT 240 SECONDS. THE "T" STYLE CLIP WITH FILLET WELDS PASSED 540 SECONDS AND SHOWED NO SIGN OF FAILURE. REFERENCE INTEROFFICE MEMORANDUM 3524-86-240. RESULTS FROM LIMITED TESTING INDICATE THAT THE LOSS OF ONE CLIP IN A SEQUENTIAL WIRE/CLIP ROUTING SYSTEM WOULD NOT DEGRADE ITS INTEGRITY (REFERENCE INTEROFFICE MEMORANDUM 3524-86-256). C. NONDESTRUCTIVE TESTING FOR INSTALLED CLIPS - DETERMINE A METHOD(S) BY WHICH SPOT WELDED CLIPS CAN BE VERIFIED FOR INTEGRITY OF WELD. THE PROPOSED NDE METHOD(S) SHALL BE VERIFIED BY COMPARING NDE RESULTS AGAINST THE MEASURED PENETRATION AREA OBSERVED AFTER FRACTION. CLIPS FROM TASKS VI, VIII AND IX SHALL BE USED. CLOSURE STATEMENT ULTRASONIC NONDESTRUCTIVE TESTING UTILIZING A MODIFIED IMMERSION TECHNIQUE WAS UNSUCCESSFUL IN DISCRIMINATING TIG SPOT WELDS WITH INADEQUATE FUSION AREAS. RESULTS UTILIZING RESISTIVITY MEA- SUREMENT (AT&T MICROHMETER - 100) ARE GOOD BASED UPON A SAMPLE OF EIGHT WELDS MEASURED THEN LAP/ SHEAR TESTED TO DESTRUCTION. A LARGER SAMPLE BASE WOULD BE NECESSARY FOR CONCLUSIVE EVALUATION (REFERENCE INTEROFFICE MEMORANDUM 3773-86-157. D. IMPROVEMENTS TO PRODUCTION SPOT WELD PROCESS - INVESTIGATE AND PROVIDE SUGGESTIONS FOR IMPROVEMENTS TO THE SPOT WELDING OPERATION TO REDUCE THE NUMBER OF DEFECTS (UNDERFILL, BURN THROUGH,CRACKS, UNDERCUT AND LACK OF FUSION). CLOSURE STATEMENT IT WAS DETERMINED THAT TIG SPOT WELDING TECHNIQUES COULD NOT BE IMPROVED UPON TO GUARANTEE CON- SISTENTLY GOOD SPOT WELDS. IT WAS SUGGESTED THAT FILLET WELDING BE SUBSTITUTED; REFERENCE MEMORAN- DUM 3614-86-274. E TIG SPOT WELDING HARDWARE VERIFICATION - INSPECT THE WELD GUN AND ASSOCIATED EQUIPMENT TO DETERMINE IF THERE ARE ANY DEFECTIVE OR INADEQUATE COMPONENTS. DETERMINE IF REPEATED USAGE, AS MIGHT BE SEEN IN PRODUCTION, CAN CAUSE A MALFUNCTION. CLOSURE STATEMENT TESTING WAS PERFORMED MAKING 100 TEST WELDS. OF THESE WELDS, THE MACHINE FUNCTIONED PROPERLY FOR ALL EXCEPT ONE. THE ONE MALFUNCTION COULD NOT BE DUPLICATED OR ANALYZED, BUT THE RESULTING WELD WAS VISUALLY UNACCEPTABLE AND WOULD NOT HAVE RESULTED IN A LATENT DEFECT. REFERENCE MEMORANDUM 3100-86-0953. F. PROOF LOAD TEST - DEVELOP PROOF LOAD NECESSARY TO LOAD THE CLIPS TO 100 PERCENT LOAD. A MINIMUM OF 10 CLIPS SHALL BE WELDED TO PANELS. THESE SHALL BE WELDED IN ATTITUDES SIMILAR TO THOSE USED IN STANDARD PRODUCTION PRACTICE. AFTER FABRICATION THEY SHALL BE USED FOR TASK IV INSPECTION. THE CLIPS SHALL THEN BE PULLED USING A 100 PERCENT PROOF LOAD TO DETERMINE ACCEPTABLE DEFORMATON CLOSURE STATEMENT TESTS WERE PERFORMED AND IT WAS DETERMINED THAT THE CLIPS START TO YIELD AT APPROXIMATELY 30 POUNDS.ANALYTICAL RESULTS INDICATE THAT A 30 POUND PULL TEST WOULD PROVIDE A PROOF FACTOR OF APPROXIMATELY 1.0. THIS STATIC PROOF LOAD, HOWEVER, DOES NOT GUARANTEE SPECIFIC CYCLE LIFE. A PROOF LOAD BASED ON CYCLE LIFE CANNOT BE DETERMINED AT THIS TIME. REFERENCE INTEROFFICE MEMORANDUM 3521-86-074 G. ANALYSIS OF TEST CLIPS - PERFORM METALLURGICAL TESTING TO DETERMINE WELD GEOMETRY AND FAILURE MODE OF PULLED TIG SPOT WELD. CLOSURE STATEMENT CLIPS WITH BOTH NORMAL TIG SPOT WELDS AND WELDS WITH POOR FUSION WERE ANALYZED. SECTIONING THROUGH THE CENTER OF THE WELD, GOOD FUSION SHOWED NORMAL WELD SOLIDIFICATION STRUCTURE, WHEREAS POOR SHOWED ONLY HEAT ALTERED MICROSTRUCTURE IN THE BASE METAL. REFERENCE LAB REPORT #86A195. H. CRYOGENIC TESTS - A MINIMUM OF 10 CLIPS SHALL BE WELDED TO PANELS. THESE SHALL BE WELDED IN ATTITUDES SIMILAR TO THOSE USED IN STANDARD PRODUCTION PRACTICE. AFTER FABRICATION, THEY SHALL BE USED FOR TASK IV INSPECTION. THE CLIPS SHALL THEN BE PULLED AT CRYOGENIC TEMPERATURES TO DETER- MINE THE STRENGTH OF THE WELDS CANCELLED I. NDE TEST SPECIMENS - MANUFACTURING SHALL PRODUCE 100 TENSILE SHEAR TEST SPECIMENS FOR USE IN DEVELOPMENT OF NDE TECHNIQUE FOR SPOT WELDS. THE SPECIMENS SHALL BE WELDED IN A WAY TO SIMULATE PRODUCTION CONDITIONS. EVERY EFFORT SHALL BE MADE TO PRODUCE 25 WELDS WITH ONLY PARTIAL FUSION (INCOMPLETE METAL TO METAL CONTACT). CLOSURE STATEMENT THE CLIPS WERE FABRICATED AND DELIVERED TO RELIABILITY ASSURANCE. REFERENCE RTM 1275. CLOSURE STATEMENT CLIPS WERE WELDED AND PULL TESTED. CURRENT PRODUCTION CLIPS THAT WERE FILLET WELDED PULLED FROM 120 TO 172 LBS. THE FILLET WELDED "T" CLIPS PULLED FROM 1,300 LBS TO 1,700 LBS. AND READINGS WERE FROM 450 TO 490 LBS. WHEN STRESSED IN BENDING (REFERENCE MECHANICAL PROPERTIES REPORT TEST NO. 86A255 AND 86A273). 6/19/86 PRB STATUS - PROBLEM RESULTED FROM A DEFECTIVE SPOTWELD. MMC IS INVESTIGATING A NON- DESTRUCTIVE INSPECTION METHOD (ULTRASONIC) FOR DETECTING DEFECTIVE SPOTWELDS. ECD IS UNDETERMINED 7/15/86 PRB STATUS - PRELIMINARY ANALYSIS INDICATES THAT THE CLIPS MAY EXPERIENCE SOME YIELDING BUT NOT AN ACTUAL FRACTURE. LOSS OF ONE OR TWO WELDS ON ONE CLIP HAS NOT BEEN TESTED. PULL TESTS WERE PROPOSED TO BE CONDUCTED. MMC MANAGEMENT DOES NOT AGREE ON THIS TYPE TESTING CONSIDERATION IS BEING GIVEN TO CHANGING THE WELD TO A FILLET TYPE WELD. 8/21/86 PRB STATUS - PERFORMING VIBRATION/TENSILE TESTING. SHOULD BE FINISHED BY MID-SEPTEMBER. 9/18/86 PRB STATUS - CLIPS TO BE FILLET (FUSION) WELDED INSTEAD OF SPOT WELDED. 10/16/86 PRB STATUS - NO CHANGE. ECD IS 1-30-87 AT MMC. 11/24/86 PRB STATUS - NEW FILLET WELDED T-CLIP ENGINEERING DETAIL DRAWINGS ARE COMPLETE AND ARE IN THE APPROVAL CYCLE. INSTALLATION DRAWING IS IN WORK. ECD REMAINS 1-30-87. 4/31/87 - UPDATE - TASK REOPENED TO REDESIGN AND TEST NEW NARROW "T" CLIP (A RESULT OF UNDERCUT CONDITION DISCOVERED ON VALIDATION ARTICLES). ECD 6/5/87 5/28/87 - PRB STATUS - NO CHANGE 9/28/87 CLOSURE UPDATE (REF CAPS S-069C) TASK II CORRECTIVE ACTION A. NEW CLIP - ENGINEERING 1 ENGINEERING SHALL INCORPORATE A NEW CLIP DESIGN, "T" CROSS-SECTION, WITH FILLET WELD. MAKE ALL DRAWING CHANGES NECESSARY AT THE DETAIL AND INSTALLATION LEVELS. NOTE: THIS CHANGE WILL INCLUD THE CLIPS ON THE LH2 FORWARD DOME (2 CLIPS) AND L02 DOME (2 CLIPS), AS WELL AS THE LH2 AFT DOME (24 CLIPS). CLOSURE STATEMENT NEW CLIPS WERE DESIGNED HAVING A "T" CONFIGURATION WITH A NARROW BASE TO MINIMIZE THE AFFECTS OF HEAT INPUT DURING FILLET WELDING (REFERENCE INTEROFFICE MEMORANDUM FROM D. KIRK TO C. VOLGEL, DATED 6/16/87. 2. PREPRODUCTION EFFORTS ON THE NARROW BASE "T" CLIP WITH FILLET WELD SHOWED A PROBLEM WHERE THE HEAT AFFECTED ZONE APPROACHED THE EDGE OF THE PRIMARY WELD LAND AS THE CLIP WAS REPOSITIONED FOR BETTER CLEARANCE TO THE PRIMARY WELD BEAD. MODIFY THE DIMENSIONS ON THE CLIP AND REDEFINE POSITIONING OF THE CLIP FOR PROPER CLEARANCES. CONDUCT TESTS TO DETERMINE THE ADEQUACY OF CON- TROL OVER THE HEAT AFFECTED ZONE ON THE PRIMARY WELD LAND. CLOSURE STATEMENT CLIPS WITH 0.4" X 1.0" BASE WERE USED. A 0.45" OFFSET IN RELATION TO THE GORE WELD WAS ESTA- BLISHED AS OPTIMUM; AND AN INCREASE OF WELD LAND WIDTH TO 1.8" WAS RECOMMENDED. REFERENCE REPORT NO. 3690-87-117 3. INITIATE A CHANGE SUMMARY (J31024, SUP. "A") TO IMPLEMENT FOR PRODUCTION THE NEW "T" CLIP DESIGN AND INSTALLATION, AND TO IMPLEMENT AN INCREASE IN GORE PANEL WELD LAND WIDTH ON WELD LANDS WHERE CLIPS ARE INSTALLED. PRODUCTION IMPLEMENTATION TO BE SCHEDULED FOR LWT-54 CLOSURE STATEMENT CHANGE SUMMARY WAS INITIATED AND APPROVED. REFERENCE J31024, SUPP. A. B. EVALUATION OF AS BUILT CONFIGURAITON FOR POSSIBLE RETROFIT 1. ENGINEERING SHALL EVALUATE THE CURRENT CONFIGURATION (SPOT WELDED CLIPS) TO DETERMINE THE NEED FOR RETROFIT AND PROVIDE POSSIBLE RETROFIT PLAN. CLOSURE STATEMENT A FLEET RETROFIT HAS BEEN DEFINED FOR LWTS 16, 20, 21, 22, AND 24 THROUGH 46. THE EXIST- ING CLIPS SHALL RECEIVE REINFORCEMENT FROM SCRIM CLOTH BONDED OVER THE FEET OF EACH CLIP (REFERENCE CHANGE SUMMARY B0 1783). 2. INITIATE A REVISION TO B0 1783 TO CHANGE THE EFFECTIVITIES COVERED BY THE RETROFIT TO BE LWT'S 16, 20, 21, 22, AND 24 THROUGH 53. CLOSURE STATEMENT REVISION WAS MADE TO B0 1783 TO EXTEND THE RETROFIT OUT TO LWT-53 (REFERENCE B0 1783, SUP. "A"). TASK III CLEARANCE OF EFFECTIVITIES LWTS 16, 20, 21, 22, AND 24 THROUGH 53 NO CONSTRAINTS. CHANGE SUMMARY B0 1783, SUP. "A", SHALL RETROFIT THE TANKS WITH SCRIM CLOTH REIN- FORCEMENT BONDED TO THE BASE OF EACH CLIP. MOD KITS SHALL COVER LWTS 16, 20, 21, 22, AND 24 3 40. IN-LINE PLANNING (OUT OF POSITION LOGS) SHAL COVER LWTS 41 THROUGH 53. LWT-54/SUBSEQUENT A NEW "T" SECTION CLIP WITH FILLET WELD SHALL BE INCORPORATED INTO PRODUCTION. PRODUCTION SHALL NO LONGER USE A TIG SPOT WELD IN ANY APPLICATION (REFERENCE CHANGE SUMMARY J31024, SUP "A"). TASK IV CAUSE/CORRECTIVE ACTION SUMMARY FOUR CLIPS WERE FOUND PARTIALLY SEVERED FROM THEIR SUBSTRATE; IN EACH CASE, THE TIG SPOT WELD WAS FRACTURED ON ONE LEG OF THE CLIP, LEAVING THE OTHER LEG TO HOLD THE CLIP. IN EACH CASE, THE BROKEN WELD HAD INSUFFICIENT AREA OF PENETRATION, APPROXIMATELY 20% OF NORMAL AREA. THE REDUCED AREA WAS CAUSED BY RANDOM PRODUCTION VARIATION DUE TO THE DIFFICULTY OF THE OPERATION. INSPECTION (NDE) OF THE COMPLETED WELD FOR AREA OF PENETRATION IS NOT POSSIBLE. THE OUTER WELD NUGGET HAD ALL THE APPEARANCES OF A NORMAL WELD FOR ALL FOUR CLIPS MENTIONED ABOVE CORRECTIVE ACTION WAS TAKEN BY INITIATING A COMPLETE RETROFIT FOR THE FLEET. ALL LH2 AFT DOME CLIPS SHALL BE BONDED WITH SCRIM CLOTH LAID OVER THE EXISTING CLIP. THE BONDED CLIP WAS TESTED BOTH STATICALLY AND DYNAMICALLY AND VERIFIED TO BE ADEQUATE EVEN WITHOUT THE SUPPORT OF A WELD. CLIPS SHALL RECEIVE BONDING REINFORCEMENT UP THROUGH LWT-53, LWT-54 AND UP SHALL HAVE A REDESIGNED CLIP. THE NEW CLIP SHALL BE A FILLET WELDED "T" CONFIGURED CLIP. THE FUSION OF THE FILLET WELD IS VERIFIABLE BY SIGHT. STATIC AND DYNAMIC TESTS WERE PERFORMED, AND THE "T" CLIP FAR EXCEEDED ITS REQUIREMENTS. THE 24 CLIPS, ON THE LH2 AFT DOME, SUPPORT WIRING FOR THE FOUR LH2 DEPLETION SENSORS. BECAUSE OF THE POTENTIAL FOR CATASTROPHIC FAILURE, THIS SYSTEM IS CLASSED AS CRITICALITY 1. THE CORRECTIVE ACTION TAKEN TO ASSURE THE INTEGRITY OF THIS SYTEM WAS CONSISTENT WITH ITS CRITICALITY 1 CLASSI- FICATION. THIS PROBLEM IS SUBMITTED TO MSFC FOR CLOSURE REVIEW AND APPROVAL |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A10051 | IFA# -- | Contractor RPT# S-069 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80914900992-002 | Asmnt Part Name LH2 TANK CLIP | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD DHV - DES-HDW-VIBR | FAIL MODE MS - STRUCT |
| Asmnt FMEA 3.6.2.1 | Asmnt FM 1 | FMEA CSE D | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |