# Text boxes

Combustion           S*

Percent moisture-(D-3302)

volatile matter,

fixed carbon, and

ash

Proximate analysis

(D-3172 through

D3175)

Ultimate

analysis

(D-3176

through

D-3179)

Moisture-(D-3302)

C

H

O

N

S (total)-(D-4239c)

Calorific value

(D-1989)

Reserved for subsequent analysis

Sample pulverized to -60 mesh (100-150 g)

Crushed to -8 mesh--

1000g split out for analysis

Remainder

split out for

storage

Equilibrium moisture (D-1412)

Hardgrove

Grindability Index

(D-409)

Raw coal as-received

Lump coal as received (1/4 to 1 inch)

Apparent Specific Gravity

(D-167)

Se

Btu per pound

(Kcal per kg)

About 100g of

crushed coal

(-20 mesh) split

out for petrologic

analysis

About 100g of coal split

out for standard coal analysis

crushed to -60 mesh

Residual Moisture

(D-3302)

Ultimate and proximate analyses

(following ASTM

designations, D-___ shown at

each procedure)

Sulfur form

(D-2492)

S (sulfate)

S (pyritic)

S (organic)

Crushed to -4 mesh

Air dried (D-2013, D-3302)

*Optional analysis must be requested

Also available INAA

ICP-AES Inductively Coupled Plasma—Atomic Emission Spectroscopy

ICP-MS Inductively Coupled Plasma—Mass Spectroscopy

AAS-Atomic Absorption Spectroscopy

MAS-Molecular Absorption Spectroscopy

IC-Ion Chromotography

Hg

Hg

Hg

Figure 1.  Flow diagram of procedures used after December 1994, for the analysis of coal samples collected.

(Current ASTM procedures effective July, 1991)

(ASTM-American Society for Testing and Materials, USGS-United States Geological Survey.)

Ce

Dy

Er

Eu

Gd

Hf

Ho

La

Nd

Pr

Sm

Ta

Tb

Tm

W

Yb

Nb

Pb

Rb

Sb

Sn

Te

Tl

U

Ag

As

Au

Bi

Cd

Cs

Ga

Ge

Mo

K2O

Fe2O3

TiO2

P2O5

SO3

Zr

SiO2

Al2O3

CaO

MgO

B

Ba

Ni

Sc

Sr

Th

V

Y

Zn

Na2O

Be

Co

Cr

Cu

Li

Mn

Acid Digest

Sinter*

ICP--MS

Acid Digest

Sinter

ICP--AES

Moisture D3173

AAS

Cold Vapor

Pulverized coal

Fusibility of ash

(D-1857)

Free swelling

index

(D-720)

Cl

AAS

Hydride

Ion

Chromo-tography

Coal ash

Pulverized coal (25 to 50 g) ashed at

525(C and percent ash calculated