the university of north carolina

at

chapel hill

Department of		The University of North Carolina at Chapel Hill

Physics and Astronomy	CB# 3255, Phillips Hall

College of Arts and Sciences	Chapel Hill, N.C. 27599-3255

Tel: (919) 962-5002

Email: daxing@physics.unc.edu	Fax: (919) 962-0480

July 12, 2004

Dr. Bolko von Roedern

NREL

1617 Cole Blvd.

Golden, CO  80401

Dear Bolko,

Here is the Quarterly Technical Status Report for the period of April/01/04-June/30/04 on the NREL Subcontract No. ADJ-1-30630-09 with the University of North Carolina at Chapel Hill. We are reporting the micro-Raman studies of thickness dependence of µc-Si:H solar cells in cooperation with United Solar Ovonic Corporation.

Sincerely,

Daxing Han

cc:	Carolyn Lopez (NREL)

Donna Braxton (UNC)

Quarterly Technical Status Report			April/01/04-June/30/04

NREL Subcontract ADJ-1-30630-09 with the University of North Carolina at Chapel Hill

Bolko von Roedern, NREL Technical Monitor;

Carolyn Lopez, NREL Subcontract Associate;

Daxing Han, principal investigator; Brittany Huie, student; Fengzheng Liu, visiting scholar; and Keda Wang, co-P.I.

Submitted: July 7, 2004

Micro-Raman Studies of  µc-Si:H solar cells with Varied Thickness

# Two series of µc-Si:H single-junction solar cells with thickness from 0.3-µm to 2.0-µm were studied using Micro-Raman spectroscopy. The deposition condition of the intrinsic layers was the same for all of the samples except the deposition time of the intrinsic layer. As listed in Table I, one set of the samples was deposited on the textured Ag/ZnO back reflectors (BR), and the other on specular stainless steel (SS). X-ray diffraction (XRD) results have shown that the crystallinity increases with the µc-Si:H film thickness. We used Micro-Raman spectroscopy to study the effects of thickness on i-layer structures and the electronic density of states of the solar cells.

Table I.  Solar cell conditions

| Sample | i-layer thickness (nm) | Bottom layer/substrate |
| --- | --- | --- |
| RF-12116 | 290 | Ag/ZnO BR |
| RF-12120 | 490 | Ag/ZnO BR |
| RF-12121 | 940 | Ag/ZnO BR |
| RF-12119 | 990 | Ag/ZnO BR |
| RF-12122 | 1340 | Ag/ZnO BR |
| RF-12124 | 1930 | Ag/ZnO BR |
| RF-12129 | 335 | SS |
| RF-12125 | 470 | SS |
| RF-12127 | 720 | SS |
| RF-12123 | 1040 | SS |
| RF-12128 | 1300 | SS |
| RF-12126 | 1970 | SS |

Micro-Raman measurements were made directly on solar cells using 514.5-nm line from an argon-ion laser under ambient conditions. The diameter of the laser  spot was 3 µm. The laser power density was one order of magnitude lower than that of the laser-crystallization power density. The penetration depth of the 514.5-nm light is ~60 nm for a-Si:H and is larger for µc-Si:H. fc was deduced using [1]

fc =(Ic + Igb)/[Ic + Igb +y(L)Ia], 	(1)

where Ic + Igb and Ia are integrated intensities of the peaks associated with c-Si, g.b., and a-Si:H components, respectively. y(L) decreases from 1 to 0.8 when the grain size (L) grows from 3-nm to 10-nm. Raman spectra were taken at four locations that are dispersed on four quadrants for each dot.

Figure 1 shows the Raman TO modes for the cells on the textured Ag/ZnO back reflectors with i-layer thickness from 290-nm to 1930-nm. Each spectrum is the average of four spectra from four locations on each solar cell. The c-Si volume fraction dispersion is ± 2-3% for the four locations. The spectra are normalized at 520 cm-1 of the c-Si peak frequency. One can see clearly that the a-Si component decreases in the top layers of ~60 nm as the i-layer thickness increases from 290-nm to 1930-nm. The scattering signal between 530 cm-1 - 600 cm-1 is related to the BR

Fig. 1 Raman TO modes for the cells on Ag/ZnO BR with a i-layer thickness from 290-nm to 1930-nm. The arrows indicate the direction of the increase of the thickness.

Figure 2 shows the Raman TO modes for the cells on SS. The results also show that the a-Si component decreases in the top layers of ~60 nm as the i-layer thickness increases from 335-nm to 1970-nm. Notice, the lowest a-Si component is at 1300-nm and not at 1970-nm.

Fig. 2  Raman TO modes for the cells on ss with a i-layer thickness from 290-nm to 1930-nm. The arrows indicate the direction of the increase of the thickness.

The Raman TO mode was deconvoluted into two Gaussian functions for a-Si:H and intermediate components and one Lorenzian function for the c-Si component. According to Eq. (1), the c-Si and g.b. volume fractions, fc and fgb were calculated and plotted in Fig. 3 and Fig. 4 as a function of i-layer thickness for the cells on textured Ag/ZnO BR and SS, respectively. One can see that in Fig. 3 when the thickness of the i-layer increases, the fc of the top layer increases; at above 1 µm the fc gradually saturates. Meanwhile, the g.b. component decreases slightly when i-layer thickness increases. However, as shown in Fig. 4 for the solar cells on SS substrate, when the thickness of the i-layer increases, the fc of the top layer does not increase as simply as that shown in Fig. 3 for the solar cells on BR.  The fc of the top layer reaches a maximum at above 1.3 µm and then decreases. It indicates the effect of the substrate surface on the i-layer structures.

Fig. 3  fc and fgb as a function of i-layer thickness for the cells on textured Ag/ZnO BR.

Fig. 4  fc and fgb as a function of i-layer thickness for the cells on SS.

# SUMMARY

The XRD results on µc-Si films and early Raman results on µc-Si cells on Ag/ZnO BR [2] showed that the fc increases with the film thickness. We have double checked the Raman data and found that although the spectra were reproducible the values of the fc were too high (60%-80% needs to be 40%-60%) due to improper data analysis. For these two groups of samples, two persons did the data analysis respectively. The results were consistent for each. We found that the value of fc in the top ~60-nm layer reaches a saturation and/or decreases when the i-layer thickness > 1µm.

It has been found [2] that Jsc reaches a maximum with a thickness in the range between 1 and 2 µm. Figs 3 and 4 imply a possible link between Jsc and fc which is that an increase of the thickness leads to an increase of the resistance after the fc value was saturated. Hence, increasing the thickness further leads to a decrease in Jsc.

# Reference

# Daxing Han, J. D. Lorentzen, J. Weinberg-Wolf, L. E. McNeil, and Qi Wang, J. Appl. Phys., 94, 5 (2003) 2930-2936.

# Baojie Yan, Guozhen Yue, Jeffrey Yang, Subhendu Guha, Keda Wang and Daxing Han, MRS symp. Proc. 808, A8.5 (2004), in press.